Supporting Information

Probing the Reaction Mechanisms Involved in the Decomposition of Solid 1,3,5-Trinitro-1,3,5-Triazinane (RDX) by Energetic Electrons

*Santosh K. Singha, Cheng Zhua, Vasant Vuppulurib, Steven F. Sonb,*

*Ralf I. Kaisera\**

*aDepartment of Chemistry, University of Hawaii, 2545 McCarthy Mall, 96822 HI, USA*

*W. M. Keck Research Laboratory in Astrochemistry, University of Hawaii, 96822 HI, USA*

*bMechanical Engineering, Purdue Energetics Research Center, Purdue University, 500 Allison Road,*

*West Lafayette, IN 47907-2088*

\*Corresponding authors. E-mail: [ralfk@hawaii.edu](mailto:ralfk@hawaii.edu),



**Figure S1.** 13C NMR spectra of (a) recrystallized RDX (b) crude RDX. Peak at 63.47 ppm in the NMR spectra of crude RDX corresponds to HMX impurity which is absent is the NMR spectra measured after recrystallization of RDX.



**Figure S2.** Infrared spectra of (a) amorphous phase of RDX film measured in the current work and (b) crystalline phase of RDX film measured by Botcher, T. R. *et al*. Fig (b) is adapted with permission from Botcher, T. R.; Wight, C. A. *J. Phys. Chem.* **1993,** *97*, 9149-9153. Copyright (1993) *American Chemical Society.*