Supplementary Information

A Combined Spectroscopic and Computational Investigation on the Oxidation of exo-Tetrahydrodicyclopentadiene (JP-10; C10H16) Doped with Titanium-Aluminum-Boron Reactive Metal Nanopowder

SUPPLEMENTARY INFORMATION

Stephen J. Brotton, Sahan D. Perera, Anupam Misra, N. Fabian Kleimeier, Andrew M. Turner, Ralf I. Kaiser*

Department of Chemistry, University of Hawaii at Manoa, Honolulu, HI 96822, USA

Mark Palenik, Matthew T. Finn, Albert Epshteyn*

U.S. Naval Research Laboratory, Washington, DC 20375, USA

Bing-Jian Sun, Li-Jie Zhang, Agnes H. H. Chang*

Department of Chemistry, National Dong Hwa University, Shoufeng, Hualien 974, Taiwan

Figure S1: Calibration curves used to calibrate the (a) low energy region of Raman data (100 cm−1 – 2400 cm−1) and (b) high energy region of Raman data (2200 cm−1 – 4000 cm−1). Each region was calibrated with cyclohexane (red), toluene (blue) and acetonitrile (green) respectively. The graphs were fit with the following second order polynomials: (a) y= -0.001x2+3.5711x-134.65 and (b) y= -0.001x2+3.236x+2154.1.

Figure S2: Comparison between the calculated vibrational wavenumber and (a) the experimental Raman wavenumber and (b) the experimental FTIR wavenumber of the normal modes of exo-tetrahydrodicyclopentadiene. Both the lower energy (red; 100 – 1100 cm-1) and high energy region (blue; 1120 – 3100 cm-1) of each plot were linearly fit to obtain a scaling factor for each region of 0.99 and 0.94 for Raman and 0.98 and 0.94 for FTIR, respectively.

Figure S3: Overview Raman spectra of (a) JP-10, (b) JP-10-Al, and (c) JP-10-Ti-Al-B NPs (RMNPs) in the 100 – 4,000 cm-1 region.

Figure S4: Raman spectra of (a) pure JP-10, (b) JP-10-Al, (c) JP-10-Ti-Al-B NPs (RMNPs), and (d) Ti-Al-BNPs (RMNPs) in the 100 – 350 cm-1 region. The total fit and individual peak fits are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S5: Raman spectra of (a) pure JP-10, (b) JP-10-Al, and (c) JP-10-Ti-Al-B NPs (RMNPs)  in the 350 – 600 cm-1 region. The total fit and individual peak fits are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S6: Raman spectra of (a) pure JP-10, (b) JP-10-Al, and (c) JP-10-Ti-Al-B NPs (RMNPs) in the 600 – 1,100 cm-1 region. The total fit and individual peak fits are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S7: Raman spectra of (a) pure JP-10, (b) JP-10-Al, and (c) JP-10-Ti-Al-B NPs (RMNPs)  in the 1,100 – 1,800 cm-1 region. The total fit and individual peak fits are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S8: Raman spectra of (a) pure JP-10, (b) JP-10-Al, and (c) JP-10-Ti-Al-B NPs (RMNPs)  in the 2,500 – 4,000 cm-1 region. The total fit and individual peak fits are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S9:  FTIR spectra of pure JP-10 in the 500 – 4,000 cm-1 region

Figure S10:  FTIR spectra of JP-10 in the (a) 500 –1,100 cm-1 (b) 1,100 – 1,800 cm-1, and (c) 2,000 –4,000 cm-1 region. The overall fit and individual peak fits in each region are shown in red and green, respectively. Peak assignments are compiled in Table S1.

Figure S11:  Raman spectra of new peaks resulting from photochemically activated JP-10-Ti-Al-B NPs (RMNPs) by a tightly focused 532 nm laser beam (45 – 50 µm) at 1 kHz

Table S1: Vibrational Mode Assignments for the Observed Peaks in the Raman Spectra of JP-10, JP-10-Al, and JP-10-Ti-Al-B NPs (RMNPs), Ti-Al-B NPs (RMNPs), and the FTIR Spectra of JP-10.

| Normal Mode | Raman Wavenumber (cm-1) JP-10 | Raman Wavenumber (cm-1) JP-10 Al | Raman Wavenumber (cm-1) JP-10 Ti-Al-B NPs | Raman Wavenumber (cm-1) Ti-Al-B NPs | FTIR Wavenumber (cm-1) JP-10 | Calculated Wavenumber(cm-1) JP-10 | Calculated FTIR Intensity JP-10 | Vibrational Mode Assignment* |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ν1 | - | - | - | - | - | 140 | 0.009 | Ring twist |
| ν2 | 188 | 188 | 192 |  | - | 177 | 0.003 | CCC bend |
| νA | - | - | 227 | 231 | - | - | - | Al-B stretch |
| νB | - | - | 267 | 267 | - | - | - | Ti-B stretch |
| ν3 | 271 | 270 | 297 | - | - | 270 | 0.068 | CCC bend |
| ν4 | - | - | - | - | - | 317 | 0.028 | CH2 rock |
| ν5 | - | - | - | - | - | 319 | 0.046 | Ring twist |
| ν6 | 401 | 401 | 401 | - | - | 398 | 0.043 | CCC bend |
| ν7 | 490 | 490 | 482 | - | 513 | 495 | 0.237 | CCC bend |
| ν8 | 532 | 531 | 525 | - | 528 | 534 | 0.180 | Ring twist |
| ν9 | 551 | 551 | 544 | - | 554 | 554 | 0.661 | CCC bend |
| ν10 | - | - | 660* | - | 659 | 671 | 0.678 | Ring rock |
| ν11 | 732 | 732 | 740 | - | 733 | 739 | 0.369 | Ring rock |
| ν12 | 744 | 743 |  | - | 745 | 753 | 0.356 | CC stretch |
| ν13 | 783 | 783 | 782 | - | 783 | 792 | 1.292 | CC stretch |
| ν14 | 814 | 813 | 813 | - | 816 | 828 | 0.643 | CH2 rock |
| ν15 | 853 | 852 | 845 | - | - | 864 | 0.067 | CCC bend |
| ν16 |  |  |  | - | 855 | 865 | 1.181 | CCC bend |
| ν17 | 879 | 879 | 879 | - | 883 | 889 | 0.626 | CCC rock |
| ν18 | 903 | 903 | 910 | - | - | 894 | 0.116 | CC stretch |
| ν19 | 914 | 914 |  | - | 907 | 913 | 0.882 | Ring stretch |
| ν20 | - | - | - | - | - | 918 | 0.041 | CH2bend/rock |
| ν21 | - | - | - | - | 918 | 926 | 1.102 | CCC rock |
| ν22 | 945 | 944 | 941 | - | 945 | 955 | 2.044 | Ring breathing |
| ν23 | - | - | - | - | - | 963 | 0.045 | CC stretch |
| ν24 | 980 | 980 | 976 | - | 980 | 992 | 1.882 | CC stretch |
| ν25 | - | - | - | - | 988 | 999 | 0.806 | CH2 bend |
| ν26 | 1030 | 1030 | 1040 | - | 1032 | 1041 | 0.206 | CH2 twist |
| ν27 | 1050 | 1049 |  | - | - | 1050 | 0.488 | CH2 bend |
| ν28 |  |  |  | - | 1057 | 1052 | 0.083 | CH2 rock |
| ν29 |  |  |  | - | - | 1054 | 0.001 | CH2 bend |
| ν30 | 1107 | 1106 | 1157 | - | 1113 | 1073 | 0.780 | CH2 twist/rock |
| ν31 | 1126 | 1124 |  | - | 1129 | 1138 | 0.097 | CH2 wag |
| ν32 | 1138 | 1138 |  | - | - | 1153 | 0.026 | CH2 twist |
| ν33 | 1161 | 1160 |  | - | 1144 | 1169 | 1.210 | CH2 twist |
| ν34 | 1196 | 1196 |  | - | 1179 | 1193 | 0.188 | CH2 wag |
| ν35 | - | - |  | - | - | 1204 | 0.068 | CH2 rock |
| ν36 | - | - |  | - | 1186 | 1209 | 1.777 | CH2 bend |
| ν37 | 1219 | 1219 |  | - | 1201 | 1227 | 1.564 | CH2 bend |
| ν38 | - | - | - | - | - | 1251 | 0.018 | CH2 twist |
| ν39 | - | - | - | - | 1233 | 1261 | 0.807 | CH2 twist |
| ν40 | 1276 | 1275 | 1315 | - | 1254 | 1289 | 1.3410 | CH2 wag |
| ν41 | - | - |  | - | - | 1301 | 0.0411 | CH wag |
| ν42 | 1304 | 1303 |  | - | 1270 | 1306 | 0.1915 | CH2 wag |
| ν43 | - | - |  | - | - | 1312 | 0.372 | CH2 wag |
| ν44 | - | - |  | - | - | 1317 | 0.002 | CH2 wag |
| ν45 | 1327 | 1328 |  | - | 1277 | 1327 | 0.051 | CH2 wag |
| ν46 |  |  |  | - | 1297 | 1331 | 1.908 | CH2 wag |
| ν47 | - | - | - | - | 1310 | 1343 | 0.680 | CH wag |
| ν48 | - | - | - | - | 1318 | 1349 | 0.982 | CH2 wag |
| ν49 | - | - | - | - | 1330 | 1367 | 1.003 | CH2 wag |
| ν50 | - | - | - | - | - | 1372 | 0.514 | CH2 twist |
| ν51 | 1420 | 1420 | 1431 | - | - | 1492 | 0.776 | CH wag |
| ν52 |  |  |  | - | - | 1494 | 2.166 | CH2 rock |
| ν53 |  |  |  | - | - | 1496 | 1.794 | CH2 rock |
| ν54 | 1444 | 1442 |  | - | 1456 | 1503 | 6.403 | CH2 scissor |
| ν55 | 1465 | 1463 |  | - | 1468 | 1514 | 11.009 | CH2 scissor |
| ν56 | - | - | - | - | 1475 | 1526 | 4.457 | CH2 rock |
| 2ν13 | - | - | 1560 | - | - | - | - | overtone |
| 2ν17 | - | - | 1728 | - | - | - | - | overtone |
| ν57 | 2870 | 2869 | 2866 | - | 2865 | 3016 | 20.073 | CH stretch |
| ν58 |  |  |  | - | - | 3021 | 30.463 | CH stretch |
| ν59 |  |  |  | - | - | 3024 | 22.102 | CH stretch |
| ν60 |  |  |  | - | - | 3030 | 1.097 | CH2 stretch |
| ν61 |  |  |  | - | - | 3034 | 25.961 | CH2 stretch |
| ν62 | 2910 | 2910 | 2915 | - | 2913 | 3042 | 58.93 | CH2 stretch |
| ν63 |  |  |  | - | - | 3044 | 12.198 | CH2 stretch |
| ν64 |  |  |  | - | - | 3046 | 66.233 | CH2 stretch |
| ν65 | 2954 | 2953 | 2951 | - | - | 3065 | 6.172 | CH2 stretch |
| ν66 |  |  |  | - | - | 3068 | 46.085 | CH stretch |
| ν67 |  |  |  | - | - | 3071 | 38.453 | CH stretch |
| ν68 |  |  |  | - | 2942 | 3073 | 104.144 | CH stretch |
| ν69 |  |  |  | - | - | 3077 | 49.579 | CH stretch |
| ν70 |  |  |  | - | - | 3080 | 9.511 | CH stretch |
| ν71 | - | - | - | - | - | 3087 | 85.784 | CH2 stretch |
| ν72 | - | - | - | - | - | 3088 | 61.510 | CH2 stretch |

Table S2: Total reaction energies (E) and zero point energy corrected reaction energies (E+ZPE) for the hydrogen abstraction channels of aluminum, boron, and titanium leading to the mono hydrides plus the corresponding JP-10 radical R1 to R6 refer (Figure 2). The Cartesian coordinates and vibrational modes are compiled in Table S6

| reactants | E B3LYP/def2-TZVP | E +ZPE B3LYP/ def2-TZVP | E MP2/6-311g* | E +ZPE MP2/6-311g* |
| --- | --- | --- | --- | --- |
|  | products |  |  |  |
| JP-10 + Al | R1 + AlH 129 | R1 + AlH 91 | R1 + AlH 159 | R1 + AlH 131 |
|  | R2 + AlH 162 | R2 + AlH 129 | R2 + AlH 192 | R2 + AlH 169 |
|  | R3 + AlH 151 | R3 + AlH 113 | R3 + AlH 180 | R3 + AlH 153 |
|  | R4 + AlH 131 | R4 + AlH 93 | R4 + AlH 164 | R4 + AlH 138 |
|  | R5 + AlH 124 | R5 + AlH 84 | R5 + AlH 156 | R5 + AlH 127 |
|  | R6 + AlH 126 | R6 + AlH 85 | R6 + AlH 159 | R6 + AlH 130 |
| JP-10 + B | R1 + BH 160 | R1 + BH 135 | R1 + BH 111 | R1 + BH 88 |
|  | R2 + BH 193 | R2 + BH 173 | R2 + BH 145 | R2 + BH 125 |
|  | R3 + BH 182 | R3 + BH 158 | R3 + BH 132 | R3 + BH 109 |
|  | R4 + BH 162 | R4 + BH 139 | R4 + BH 116 | R4 + BH 94 |
|  | R5 + BH 155 | R5 + BH 129 | R5 + BH 108 | R5 + BH 84 |
|  | R6 + BH 157 | R6 + BH 131 | R6 + BH 111 | R6 + BH 86 |
| JP-10 + Ti | R1 + TiH 253 | R1 + TiH 223 | R1 + TiH 272 | R1 + TiH 243 |
|  | R2 + TiH 287 | R2 + TiH 262 | R2 + TiH 305 | R2 + TiH 281 |
|  | R3 + TiH 274 | R3 + TiH 245 | R3 + TiH 293 | R3 + TiH 265 |
|  | R4 + TiH 255 | R4 + TiH 228 | R4 + TiH 277 | R4 + TiH 251 |
|  | R5 + TiH 247 | R5 + TiH 217 | R5 + TiH 269 | R5 + TiH 240 |
|  | R6 + TiH 250 | R6 + TiH 220 | R6 + TiH 272 | R6 + TiH 242 |

Table S3: Total energies (E) and zero point energy corrected total energies (E+ZPE) computed with MP2/6-311g* for the initial van-der-Waals (vdW) complexes (vdW I), transition states (TS), final van-der-Waals (vdW II) complexes, and products during the reaction of aluminum monoxide (AlO) and boron monoxide (BO) with JP-10. R1 to R6 refer to distinct JP-10 radicals whose structures are shown in Figure 2. The Cartesian coordinates and vibrational modes of the stationary points are compiled in Table S6.

| reactants | E | E+ZPE |  | E+ ZPE |  | E+ ZPE |  | E+ ZPE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | vdW I |  | TS |  | vdW II |  | products |  |
| JP-10 + BO | -9 | -8 | 23 | 8 | -37 | -46 | -29 | R1 + HBO -41 |
|  | -7 | -6 | 35 | 21 | -5 | -11 | 4 | R2 + HBO -3 |
|  | -11 | -10 | 42 | 28 | -15 | -24 | -8 | R3 + HBO -19 |
|  | -10 | -9 | 15 | 1 | -33 | -42 | -24 | R4 + HBO -34 |
|  | -9 | -7 | 28 | 14 | -38 | -49 | -322 | R5 + HBO -45 |
|  | -11 | -10 | 23 | 8 | -43 | -54 | -29 | R6 + HBO -42 |
| JP-10 + AlO | 42 | 3 | 58 | 6 | -60 | -106 | -36 | R1 + AlOH -90 |
|  | 42 | 3 | 55 | 8 | -28 | -71 | -3 | R2 + AlOH -52 |
|  | -33 | -48 | 53 | 4 | -40 | -85 | -15 | R3 + AlOH -68 |
|  | -33 | -8 | 45 | 8 | -59 | -104 | -39 | R4 + AlOH -82 |
|  | -33 | -8 | 61 | 8 | -58 | -106 | -39 | R5 + AlOH -93 |
|  | -33 | -8 | 65 | 20 | -61 | -109 | -39 | R6 + AlOH -91 |

Table S4: Total energies (E) and zero point energy corrected total energies (E+ZPE) for the transition states, final van-der-Waals (vdW) complexes (vdW II), and products during the reaction of boron dioxide (BO2) with JP-10. R1 to R6 refer to distinct JP-10 radicals whose structures are shown in Figure 2. The Cartesian coordinates and vibrational modes of the stationary points are compiled in Table S6.

| reactants | E | E+ ZPE | E | E+ ZPE | E | E+ ZPE |
| --- | --- | --- | --- | --- | --- | --- |
|  | TS |  | vdW II |  | products |  |
| JP-10 + BO2 | 10 | 17 | -97 | -85 | -62 | R1 + BO2H -56 |
|  | 9 | 19 | -69 | -56 | -29 | R2 + BO2H -35 |
|  | 14 | 13 | -73 | -62 | -41 | R3 + BO2H -35 |
|  | 5 | 5 | -99 | -87 | -57 | R4 + BO2H -49 |
|  | 15 | 23 | -100 | -89 | -65 | R5 + BO2H -60 |
|  | 30 | 29 | -93 | -83 | -62 | R6 + BO2H -58 |

Table S5: Total energies (E) and zero point energy corrected total energies (E+ZPE) for van-der-Waals (vdW) complexes in the exit channel (vdW II), transition state to insertion (TS), the intermediates, and products accessed during the reaction of atomic and molecular oxygen with JP-10. R1 to R6 refer to distinct JP-10 radicals whose structures are shown in Figure 2. The Cartesian coordinates and vibrational modes of the stationary points are compiled in Table S7.

| reactants | E | E+ZPE | E | E+ZPE |  | E | E +ZPE |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | TS |  | vdW II complex |  |  | products |  |
| JP-10 + O | 49 | 34 | -4 |  | -13 | R1 + OH 14 | R1 + OH -2 |
|  | 60 | 43 | 26 |  | 20 | R2 + OH 46 | R2 + OH 34 |
|  | 59 | 43 | 18 |  | 8 | R3 + OH 35 | R3 + OH 19 |
|  | 42 | 28 | -4 |  | -12 | R4 + OH 18 | R4 + OH 3 |
|  | 49 | 33 | -6 |  | -17 | R5 + OH 11 | R5 + OH -6 |
|  | 50 | 34 | -4 |  | -15 | R6 + OH 14 | R6 + OH -4 |
| reactants | E | E+ ZPE | E |  | E+ ZPE | E | E +ZPE |
|  | TS |  | VdW complex |  |  | products |  |
| JP-10 + O2 | 210 | 196 | 197 |  | 191 | R1 + O2H 217 | R1 + O2H 206 |
|  | 230 | 224* | 222 |  | 227 | R2 + O2H 249 | R2 + O2H 242 |
|  | 218 | 209 | 215 |  | 208 | R3 + O2H 237 | R3 + O2H 227 |
|  | 205 | 199 | 193 |  | 197 | R4 + O2H 220 | R4 + O2H 211 |
|  | 205 | 190 | 190 |  | 183 | R5 + O2H 213 | R5 + O2H 202 |
|  | 202 | 188 | 192 |  | 184 | R6 + O2H 217 | R6 + O2H 204 |

* This transition state could not be located at the B3LYP/cc-pVTZ level of theory. MP2/cc-pVDZ does locate the transition state; however, with zero-point energy correction (either with harmonic or anharmonic frequencies), the energy is found lower than the corresponding R2-OOH van-der-Waals complex and likewise for CCSD/cc-pVTZ energy.

Table S6: Cartesian coordinates and vibrational frequencies of  van-der-Waals complexes, transition states and products of the reactions of BO, AlO, and BO2 with JP-10. Calculations are performed at the MP2/6-311g* level unless otherwise indicated.

| Atom | X | Y | Z |  |
| --- | --- | --- | --- | --- |
| JP-10 |  |  |  |  |
| C; -0.362754; -0.785814; -0.514719. C; -0.362754; 0.785811; -0.514726. C; 0.879767; -1.131868; 0.324589. C; 0.879774; 1.131874; 0.32457. C; 0.888333; 0.000014; 1.367226. C; 2.128868; -0.779704; -0.505758. C; 2.128874; 0.779688; -0.505769. C; -1.718206; -1.199374; 0.088531. C; -1.7182; 1.199373; 0.088531. C; -2.63457; 0.000002; -0.18068. H; -0.269974; -1.189074; -1.531257. H; -0.269983; 1.189061; -1.531269. H; 0.877652; -2.154287; 0.718985. H; 0.877666; 2.154302; 0.718943. H; 0.017186; 0.000022; 2.028639. H; 1.793214; 0.000017; 1.985804. H; 2.080761; -1.204432; -1.513657. H; 3.03321; -1.171596; -0.028391. H; 3.033218; 1.171577; -0.028402. H; 2.080776; 1.204402; -1.513674. H; -1.619754; -1.353279; 1.170221. H; -2.091151; -2.135852; -0.33893. H; -2.091143; 2.135854; -0.338926. H; -1.619744; 1.353272; 1.170222. H; -2.945458; 0; -1.232529. H; -3.541266; 0.000002; 0.433452. |  |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R1 |  |  |  | R2 |  |  |  |
| C; 0.354; 0.792227; -0.528413. C; 0.302153; -0.778172; -0.515397. C; -0.89737; 1.179636; 0.306674. C; -0.948358; -1.087524; 0.331605. C; -0.919575; 0.055; 1.363006. C; -2.093616; 0.799885; -0.519299. C; -2.193808; -0.70807; -0.499451. C; 1.716735; 1.171174; 0.082399. C; 1.644532; -1.229103; 0.090346. C; 2.597116; -0.057416; -0.178149. H; 0.276556; 1.189579; -1.5475. H; 0.195433; -1.184508; -1.529229. H; -0.884381; 2.209211; 0.678687. H; -0.969804; -2.104778; 0.737439. H; -0.038942; 0.04115; 2.011143. H; -1.817305; 0.086288; 1.989169. H; -2.515721; 1.42909; -1.296802. H; -3.114517; -1.050831; -0.00374. H; -2.18461; -1.160241; -1.499772. H; 1.617999; 1.334378; 1.162481. H; 2.119161; 2.093162; -0.349509. H; 1.991754; -2.17615; -0.335407. H; 1.540128; -1.379575; 1.171964. H; 2.91244; -0.069828; -1.228573. H; 3.500956; -0.082762; 0.439729. | C; -0.368548; -0.850808; -0.463545. C; -0.33928; 0.734012; -0.552709. C; 0.8699; -1.101186; 0.369201. C; 0.908734; 1.108559; 0.276113. C; 0.88935; 0.028682; 1.387578. C; 2.136753; -0.880453; -0.434369. C; 2.166287; 0.689611; -0.518723. C; -1.72899; -1.198294; 0.167924. C; -1.690504; 1.19882; 0.019876. C; -2.623542; -0.001658; -0.17772. H; -0.282434; -1.307976; -1.456254. H; -0.23396; 1.07083; -1.591798. H; 0.918882; 2.152385; 0.610805. H; 0.010929; 0.075407; 2.034986. H; 1.791889; 0.041717; 2.00679. H; 2.097222; -1.35714; -1.41764. H; 3.018605; -1.260235; 0.090984. H; 3.071978; 1.088375; -0.050091. H; 2.139277; 1.053781; -1.550665. H; -1.629882; -1.289217; 1.255495. H; -2.117367; -2.15221; -0.201788. H; -2.049267; 2.111606; -0.467007. H; -1.59262; 1.41917; 1.089928. H; -2.933159; -0.061076; -1.228294. H; -3.531043; 0.050878; 0.432792. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R3 |  |  |  | R4 |  |  |  |
| C; -0.356909; -0.786935; -0.498841. C; -0.356909; 0.786936; -0.498842. C; 0.876342; -1.136847; 0.35768. C; 0.876343; 1.136848; 0.357677. C; 0.876694; 0.000002; 1.352077. C; 2.13995; -0.780727; -0.469251. C; 2.139951; 0.780725; -0.469253. C; -1.709529; -1.195627; 0.111241. C; -1.709529; 1.195626; 0.111242. C; -2.627118; 0; -0.165467. H; -0.258293; -1.19347; -1.513472. H; -0.258294; 1.19347; -1.513473. H; 0.872829; -2.154934; 0.75836. H; 0.872831; 2.154936; 0.758356. H; 1.434973; 0.000003; 2.285304. H; 2.095146; -1.207038; -1.477212. H; 3.040009; -1.171933; 0.015217. H; 3.040011; 1.171933; 0.015212. H; 2.095144; 1.207033; -1.477215. H; -1.597351; -1.325376; 1.194786. H; -2.08258; -2.139695; -0.29953. H; -2.082581; 2.139695; -0.299529. H; -1.59735; 1.325375; 1.194787. H; -2.935434; 0; -1.218295. H; -3.534778; 0; 0.447119. | C; 0.381883; 0.748353; -0.387131. C; 0.369798; -0.777621; -0.467491. C; -0.880694; 1.149551; 0.328404. C; -0.918476; -1.124633; 0.308762. C; -0.97415; -0.001501; 1.363299. C; -2.082728; 0.817626; -0.585587. C; -2.113107; -0.74153; -0.588011. C; 1.76383; 1.237324; -0.037018. C; 1.72343; -1.174362; 0.150477. C; 2.648676; -0.008845; -0.234208. H; 0.316545; -1.152851; -1.501128. H; -0.88407; 2.166961; 0.731442. H; -0.954319; -2.150872; 0.690278. H; -0.138431; -0.013533; 2.070142. H; -1.914155; 0.006032; 1.92833. H; -1.954054; 1.24021; -1.585569. H; -3.005986; 1.229976; -0.164757. H; -3.0493; -1.115851; -0.160616. H; -2.01955; -1.163956; -1.593385. H; 1.791759; 1.566204; 1.01458. H; 2.085287; 2.094544; -0.640614. H; 2.081115; -2.146893; -0.203274. H; 1.633563; -1.230963; 1.242334. H; 2.929194; -0.097293; -1.28999. H; 3.571625; 0.022113; 0.353247. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R5 |  |  |  | R6 |  |  |  |
| C; -0.350357; -0.825491; -0.525469. C; -0.398433; 0.743945; -0.566562. C; 0.872848; -1.1191; 0.375624. C; 0.822013; 1.141064; 0.282966. C; 0.81772; 0.050663; 1.36992. C; 2.139627; -0.775111; -0.428686. C; 2.098416; 0.781631; -0.502048. C; -1.684982; -1.228276; 0.015957. C; -1.758062; 1.153083; 0.042654. C; -2.65761; -0.09339; -0.054774. H; -0.186253; -1.261127; -1.525257. H; -0.308853; 1.125432; -1.59119. H; 0.869925; -2.125335; 0.807725. H; 0.792444; 2.178; 0.636177. H; -0.082924; 0.043228; 1.990933. H; 1.697528; 0.098727; 2.021859. H; 2.1393; -1.247328; -1.416463. H; 3.03548; -1.119696; 0.098488. H; 2.980972; 1.220757; -0.025225. H; 2.061376; 1.157243; -1.529822. H; -1.979126; -2.266367; 0.143577. H; -2.183917; 2.02365; -0.466065. H; -1.625182; 1.428331; 1.094529. H; -3.19027; -0.100958; -1.020897. H; -3.427575; -0.128666; 0.724137. | C; -0.379506; -0.786675; -0.582736. C; -0.379505; 0.786675; -0.582735. C; 0.81636; -1.130205; 0.32341. C; 0.816357; 1.130202; 0.323417. C; 0.75241; -0.000005; 1.365748. C; 2.113179; -0.779169; -0.428733. C; 2.113178; 0.779175; -0.428727. C; -1.752008; -1.235208; -0.03154. C; -1.752008; 1.23521; -0.031542. C; -2.595004; 0.000001; -0.015902. H; -0.231031; -1.186871; -1.592632. H; -0.231026; 1.186872; -1.59263. H; 0.790243; -2.153346; 0.714703. H; 0.790237; 2.153341; 0.714714. H; -0.169064; -0.000008; 1.957326. H; 1.608153; -0.000006; 2.050599. H; 2.126341; -1.204578; -1.437405. H; 2.986138; -1.171974; 0.103155. H; 2.986133; 1.171975; 0.103172. H; 2.126348; 1.204593; -1.437394. H; -1.635935; -1.651408; 0.983883. H; -2.192206; -2.039101; -0.634444. H; -2.192205; 2.039101; -0.634449. H; -1.635937; 1.651412; 0.98388. H; -3.646908; 0.000001; 0.253554. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| JP-10 B3LYP/def2-TZVP |  |  |  |  |  |  |  |
| C; -0.36439; -0.787455; -0.51267. C; -0.36439; 0.787456; -0.512666. C; 0.883784; -1.131549; 0.325555. C; 0.88378; 1.131545; 0.325568. C; 0.894691; -0.000008; 1.370829. C; 2.135266; -0.781168; -0.507259. C; 2.135262; 0.781178; -0.507253. C; -1.724307; -1.203612; 0.081085. C; -1.724308; 1.203613; 0.081085. C; -2.641653; 0; -0.171254. H; -0.268338; -1.185699; -1.524931. H; -0.268335; 1.185705; -1.524925. H; 0.882773; -2.149132; 0.717323. H; 0.882766; 2.149124; 0.717344. H; 0.025842; -0.000015; 2.029763. H; 1.793692; -0.000011; 1.990989. H; 2.087322; -1.20194; -1.513055. H; 3.037011; -1.172474; -0.032878. H; 3.037006; 1.172487; -0.032873. H; 2.087309; 1.201957; -1.513046. H; -1.631147; -1.372976; 1.158043. H; -2.103167; -2.129512; -0.354984. H; -2.103167; 2.129513; -0.354984. H; -1.631152; 1.372975; 1.158043. H; -2.975415; -0.000001; -1.213824. H; -3.535404; 0; 0.455864. |  |  |  |  |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R1 B3LYP/def2-TZVP |  |  |  | R2 B3LYP/def2-TZVP |  |  |  |
| C; 0.355894; 0.792306; -0.53033. C; 0.306604; -0.780814; -0.513364. C; -0.907096; 1.178281; 0.301743. C; -0.949187; -1.088092; 0.333403. C; -0.92523; 0.055858; 1.365895. C; -2.097596; 0.792575; -0.522272. C; -2.197766; -0.708812; -0.501063. C; 1.721116; 1.177706; 0.073957. C; 1.653931; -1.231267; 0.084292. C; 2.605284; -0.053424; -0.166787. H; 0.276334; 1.184366; -1.545156. H; 0.196708; -1.185292; -1.521567. H; -0.89429; 2.205176; 0.666205. H; -0.973161; -2.100444; 0.736414. H; -0.045505; 0.046901; 2.00987. H; -1.815755; 0.084477; 1.99575. H; -2.587128; 1.435708; -1.240225. H; -3.116732; -1.054329; -0.007842. H; -2.192411; -1.161513; -1.498986. H; 1.624834; 1.356524; 1.148774. H; 2.127653; 2.089546; -0.366432. H; 2.009667; -2.167152; -0.349756. H; 1.553791; -1.397251; 1.161095. H; 2.945529; -0.066824; -1.207068. H; 3.494744; -0.075796; 0.466089. | C; -0.368517; -0.854347; -0.460858. C; -0.341361; 0.738596; -0.550968. C; 0.872674; -1.095538; 0.366195. C; 0.913538; 1.110369; 0.276599. C; 0.895574; 0.026729; 1.390655. C; 2.140003; -0.885496; -0.433762. C; 2.173488; 0.691194; -0.520366. C; -1.734572; -1.202953; 0.161449. C; -1.696414; 1.202312; 0.013522. C; -2.629862; -0.001454; -0.16922. H; -0.279869; -1.305579; -1.450371. H; -0.233917; 1.069099; -1.585907. H; 0.92566; 2.149076; 0.61005. H; 0.019796; 0.076304; 2.036094. H; 1.793027; 0.041003; 2.010753. H; 2.10369; -1.358247; -1.4156. H; 3.020351; -1.262102; 0.089867. H; 3.077083; 1.087424; -0.054309. H; 2.146395; 1.049679; -1.55054. H; -1.640726; -1.306851; 1.245394. H; -2.128498; -2.147549; -0.216089. H; -2.061705; 2.105201; -0.479058. H; -1.602869; 1.434633; 1.078381. H; -2.960412; -0.059782; -1.211171. H; -3.525309; 0.051214; 0.453034. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R3 B3LYP/def2-TZVP |  |  |  | R4 B3LYP/def2-TZVP |  |  |  |
| C; -0.358103; -0.788763; -0.494995. C; -0.358103; 0.788764; -0.494995. C; 0.882363; -1.135664; 0.362626. C; 0.882365; 1.135667; 0.362621. C; 0.887008; 0.000004; 1.350522. C; 2.148681; -0.782213; -0.471695. C; 2.148682; 0.782208; -0.471699. C; -1.716346; -1.199953; 0.102585. C; -1.716345; 1.199953; 0.102587. C; -2.633868; 0; -0.161136. H; -0.254746; -1.189646; -1.505502. H; -0.254749; 1.189645; -1.505503. H; 0.881376; -2.148915; 0.761614. H; 0.88138; 2.14892; 0.761605. H; 1.35877; 0.000005; 2.323897. H; 2.101446; -1.205294; -1.477385. H; 3.046368; -1.17361; 0.008706. H; 3.046371; 1.173607; 0.008696. H; 2.101444; 1.205284; -1.477392. H; -1.612759; -1.344406; 1.182348. H; -2.094332; -2.133664; -0.3176. H; -2.094332; 2.133664; -0.317596. H; -1.612757; 1.344403; 1.18235. H; -2.959549; 0; -1.206498. H; -3.531949; 0; 0.459732. | C; 0.385824; 0.745625; -0.365345. C; 0.372843; -0.773608; -0.464913. C; -0.880309; 1.146474; 0.336827. C; -0.926054; -1.128023; 0.300251. C; -0.987893; -0.014985; 1.368513. C; -2.085515; 0.825678; -0.583361. C; -2.117932; -0.735877; -0.600806. C; 1.76521; 1.242531; -0.049022. C; 1.73113; -1.180532; 0.141465. C; 2.657751; -0.006354; -0.221753. H; 0.319488; -1.135781; -1.498856. H; -0.883555; 2.156134; 0.745546. H; -0.964676; -2.153518; 0.667466. H; -0.159321; -0.035145; 2.077982. H; -1.926855; -0.008136; 1.927694. H; -1.958705; 1.255107; -1.576961. H; -3.005279; 1.23368; -0.15967. H; -3.054104; -1.112089; -0.184484. H; -2.020476; -1.145441; -1.607364. H; 1.805892; 1.603381; 0.989833. H; 2.087032; 2.082398; -0.672779. H; 2.092798; -2.14166; -0.228297. H; 1.64549; -1.259663; 1.229452. H; 2.968664; -0.094355; -1.266524. H; 3.563279; 0.029505; 0.385822. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| R5 B3LYP/def2-TZVP |  |  |  | R6 B3LYP/def2-TZVP |  |  |  |
| C; -0.355427; -0.823585; -0.529747. C; -0.39841; 0.748529; -0.567637. C; 0.8734; -1.119914; 0.373906. C; 0.825336; 1.139828; 0.287563. C; 0.820626; 0.047198; 1.374375. C; 2.144451; -0.776252; -0.428893. C; 2.106506; 0.783674; -0.496387. C; -1.689329; -1.230022; -0.013332. C; -1.767002; 1.158835; 0.025443. C; -2.658486; -0.099741; -0.030847. H; -0.178314; -1.25631; -1.524508. H; -0.298134; 1.128373; -1.585926. H; 0.868701; -2.123212; 0.798886. H; 0.79613; 2.170965; 0.640977. H; -0.077847; 0.041974; 1.992873. H; 1.694091; 0.091691; 2.028377. H; 2.144442; -1.241662; -1.416099. H; 3.036369; -1.124216; 0.095287. H; 2.985476; 1.218378; -0.017236. H; 2.074651; 1.159298; -1.520637. H; -1.968701; -2.260775; 0.163574. H; -2.205462; 2.004017; -0.507062. H; -1.643534; 1.469367; 1.065365. H; -3.248335; -0.107939; -0.962671. H; -3.389528; -0.141246; 0.782137. | C; -0.380728; -0.78775; -0.583878. C; -0.380728; 0.787747; -0.583882. C; 0.818025; -1.129842; 0.325012. C; 0.818027; 1.129846; 0.325005. C; 0.756104; 0.000006; 1.370958. C; 2.118718; -0.780583; -0.426884. C; 2.118725; 0.780575; -0.426879. C; -1.761282; -1.23654; -0.049169. C; -1.761282; 1.23654; -0.049176. C; -2.585004; 0; 0.032446. H; -0.225482; -1.186497; -1.587341. H; -0.225483; 1.186489; -1.587347. H; 0.792548; -2.148399; 0.713103. H; 0.792553; 2.148405; 0.713089. H; -0.162351; 0.000011; 1.960684. H; 1.606275; 0.000008; 2.056361. H; 2.13352; -1.202238; -1.433342. H; 2.988333; -1.172829; 0.103429. H; 2.988342; 1.172811; 0.10344. H; 2.133537; 1.202233; -1.433335. H; -1.654937; -1.711308; 0.93963. H; -2.218658; -2.002384; -0.685553. H; -2.218658; 2.00238; -0.685565. H; -1.654937; 1.711313; 0.93962. H; -3.638055; 0; 0.281804. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 sites 1-2 JP-10/AlO |  |  |  | vdW1 site 3 JP-10/AlO |  |  |  |
| C; -1.845897; -0.620373; 0.222476. C; -1.155568; 0.139051; -0.966474. C; -0.657847; -1.261778; 0.958818. C; 0.336887; -0.164876; -0.752322. C; 0.441198; -0.195486; 0.785574. C; -0.102931; -2.400434; 0.081327. C; 0.591991; -1.644321; -1.091889. C; -2.621317; 0.455373; 1.005694. C; -1.568272; 1.614827; -0.811679. C; -2.883426; 1.55969; -0.025263. H; -2.539274; -1.390332; -0.139299. H; -1.490872; -0.242427; -1.939263. H; -0.879792; -1.556137; 1.990638. H; 0.997202; 0.529158; -1.287133. H; 0.208346; 0.756472; 1.274112. H; 1.411559; -0.558918; 1.145346. H; -0.897247; -3.073353; -0.257415. H; 0.621199; -3.001337; 0.640958. H; 1.666924; -1.847015; -1.108146. H; 0.183701; -1.911525; -2.071848. H; -2.002528; 0.850581; 1.820965. H; -3.535386; 0.057114; 1.457996. H; -1.660507; 2.121025; -1.778144. H; -0.813483; 2.160882; -0.231675. H; -3.700804; 1.258237; -0.691517. H; -3.159462; 2.518372; 0.426088. Al; 3.328476; 1.550786; 0.265866. O; 3.638917; -0.215132; 0.106815. | C; 1.094905; 0.865603; -0.785911. C; 1.094954; 0.86567; 0.785849. C; 1.418394; -0.598591; -1.129651. C; 1.418461; -0.598445; 1.129697. C; 0.697759; -1.35731; 0.000094. C; 2.897022; -0.854888; -0.779781. C; 2.897088; -0.854783; 0.779727. C; -0.307657; 1.352815; -1.193689. C; -0.30763; 1.352927; 1.193644. C; -0.772774; 2.194939; -0.000063. H; 1.86182; 1.541789; -1.188571. H; 1.861837; 1.541958; 1.188402. H; 1.145022; -0.881994; -2.153021. H; 1.145236; -0.881835; 2.153111. H; -0.388584; -1.236181; 0.00013. H; 0.94209; -2.428048; 0.000166. H; 3.558086; -0.09098; -1.203832. H; 3.22442; -1.824595; -1.171292. H; 3.224488; -1.824443; 1.171351. H; 3.558166; -0.090816; 1.203637. H; -0.987552; 0.501466; -1.293879. H; -0.291579; 1.904081; -2.141517. H; -0.291498; 1.904308; 2.141399. H; -0.987503; 0.501595; 1.29398. H; -0.271678; 3.172442; -0.000097. H; -1.854736; 2.369116; -0.00003. Al; -4.219396; -0.900399; -0.000009. O; -2.672378; -0.835037; 0.000085. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 site 4 JP-10/AlO |  |  |  | vdW1 sites 5-6 JP-10/AlO |  |  |  |
| C; 0.665171; 0.357543; 0.784778. C; 0.665205; 0.357554; -0.784777. C; 0.912678; -1.121426; 1.130932. C; 0.912668; -1.121412; -1.130933. C; 1.857914; -1.565132; -0.00001. C; -0.365245; -1.908466; 0.778975. C; -0.365315; -1.908384; -0.778949. C; 1.777072; 1.338172; 1.199812. C; 1.777167; 1.338165; -1.199739. C; 1.911507; 2.284429; 0.000037. H; -0.307568; 0.691771; 1.158514. H; -0.307488; 0.691877; -1.158554. H; 1.273122; -1.285785; 2.15384. H; 1.273076; -1.285804; -2.153848. H; 2.822474; -1.047768; -0.000016. H; 2.043222; -2.646375; -0.000018. H; -1.259169; -1.424885; 1.179056. H; -0.3114; -2.928887; 1.177378. H; -0.311632; -2.928762; -1.177467. H; -1.259203; -1.42461; -1.178874. H; 2.723101; 0.802899; 1.35425. H; 1.542938; 1.857442; 2.135851. H; 1.543087; 1.85743; -2.135794. H; 2.72321; 0.802897; -1.354106. H; 1.078668; 2.998295; 0. H; 2.844591; 2.859499; 0.000071. Al; -4.166579; 0.716618; 0.000167. O; -2.554806; 0.59856; -0.000402. | C; 0.374399; 0.225682; 0.784799. C; 0.374378; 0.22567; -0.784776. C; 1.763555; -0.336618; 1.131767. C; 1.763558; -0.336612; -1.131748. C; 2.636416; 0.235031; 0.000013. C; 1.76887; -1.836983; 0.779783. C; 1.768903; -1.836966; -0.779809. C; 0.114403; 1.685441; 1.198245. C; 0.114387; 1.68541; -1.198241. C; -0.631229; 2.284209; 0.000004. H; -0.430733; -0.409704; 1.166424. H; -0.430734; -0.40974; -1.166379. H; 2.093661; -0.117393; 2.154157. H; 2.093646; -0.117339; -2.154134. H; 2.696645; 1.327245; 0.00002. H; 3.655761; -0.170354; 0.000015. H; 0.901744; -2.354158; 1.20369. H; 2.667964; -2.325892; 1.171656. H; 2.66805; -2.325818; -1.171635. H; 0.901837; -2.354197; -1.203768. H; 1.064672; 2.214131; 1.354065. H; -0.452031; 1.750104; 2.133644. H; -0.452064; 1.750079; -2.133623. H; 1.064656; 2.214088; -1.354078. H; -1.65978; 1.912552; -0.000001. H; -0.644884; 3.380763; -0.000023. Al; -4.12735; -1.111835; 0.000055. O; -2.796088; -0.184513; -0.00012. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS1 JP-10/AlO |  |  |  | TS2 JP-10/AlO |  |  |  |
| C; 1.116564; -0.655207; 0.663072. C; 1.802351; 0.729226; 0.378115. C; -0.259943; -0.506549; -0.014586. C; 0.720156; 1.495932; -0.401738. C; 0.06467; 0.377051; -1.23166. C; -1.085295; 0.469326; 0.826796. C; -0.413142; 1.843793; 0.584734. C; 2.047301; -1.715498; 0.043943. C; 3.090234; 0.399492; -0.398814. C; 3.42312; -1.039077; 0.014456. H; 1.005074; -0.838427; 1.73951. H; 2.055022; 1.251551; 1.309739. H; -0.754045; -1.46255; -0.223745. H; 1.099307; 2.356105; -0.964233. H; 0.741049; -0.093553; -1.950479. H; -0.838832; 0.706018; -1.754623. H; -1.206764; 0.18254; 1.876206. H; -2.156302; 0.543751; 0.375681. H; -1.123485; 2.545609; 0.136274. H; -0.034412; 2.294727; 1.507817. H; 1.727484; -1.946646; -0.979579. H; 2.035656; -2.654143; 0.607232. H; 3.894173; 1.110474; -0.182791. H; 2.902877; 0.440044; -1.478769. H; 3.860329; -1.044114; 1.020287. H; 4.132985; -1.530992; -0.658618. Al; -4.100233; -1.089066; -0.030696. O; -3.384149; 0.488316; -0.345846. | Al; 4.359131; -0.373861; 0.151823. C; -0.548599; -0.404625; -0.785763. C; -2.005954; -0.145166; -0.243774. C; 0.24915; 0.717371; -0.11765. C; -1.826592; 1.093828; 0.653966. C; -0.425805; 0.85305; 1.252053. C; -0.104063; 2.053387; -0.779919. C; -1.554762; 2.31116; -0.254639. C; -0.191037; -1.836072; -0.348234. C; -2.412091; -1.444405; 0.476954. C; -1.547769; -2.529467; -0.177181. H; -0.500966; -0.320255; -1.87866. H; -2.707421; 0.063726; -1.06194. H; 1.392976; 0.487391; -0.084981. H; -2.642549; 1.244229; 1.370641. H; -0.353345; -0.04366; 1.872937. H; -0.052647; 1.708771; 1.825371. H; -0.048411; 1.997422; -1.871404. H; 0.580359; 2.842184; -0.451711. H; -1.601872; 3.241279; 0.321697. H; -2.289207; 2.387657; -1.063189. H; 0.346214; -1.811443; 0.606663. H; 0.466141; -2.329638; -1.07088. H; -3.48696; -1.639164; 0.399101. H; -2.171833; -1.374885; 1.54499. H; -1.95988; -2.787048; -1.16069. H; -1.493293; -3.451866; 0.410987. O; 2.757389; 0.078891; 0.032811. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS3 JP-10/AlO |  |  |  | TS4 JP-10/AlO |  |  |  |
| C; 1.049354; 0.881022; -0.785793. C; 1.049191; 0.880943; 0.785963. C; 1.181733; -0.611337; -1.135446. C; 1.181587; -0.611449; 1.135446. C; 0.409667; -1.289585; -0.000086. C; 2.619517; -1.053605; -0.78053. C; 2.619473; -1.05352; 0.780627. C; -0.273364; 1.552272; -1.198781. C; -0.273623; 1.552117; 1.198756. C; -0.635485; 2.43752; 0.000006. H; 1.899487; 1.448272; -1.186898. H; 1.899214; 1.448198; 1.187295. H; 0.871641; -0.865458; -2.154516. H; 0.871414; -0.865735; 2.15445. H; -0.750295; -1.067259; -0.000128. H; 0.468856; -2.38491; -0.000149. H; 3.36656; -0.375137; -1.205997. H; 2.823256; -2.055487; -1.172413. H; 2.823464; -2.055287; 1.172671. H; 3.366319; -0.374793; 1.206025. H; -1.047711; 0.791467; -1.332078. H; -0.177111; 2.107535; -2.138111. H; -0.177571; 2.107256; 2.13818. H; -1.047992; 0.791291; 1.331785. H; -0.015482; 3.342995; 0.000132. H; -1.684557; 2.75434; -0.000091. Al; -3.82982; -0.95691; 0.000036. O; -2.158767; -1.051718; -0.000199. | C; 0.155667; 0.3486; 0.505311. C; 0.853518; 0.378237; -0.891863. C; 0.764756; -0.876448; 1.193412. C; 1.804295; -0.830742; -0.82097. C; 2.212993; -0.832689; 0.663428. C; 0.22272; -2.135075; 0.48736. C; 0.947268; -2.109532; -0.892939. C; 0.397304; 1.721078; 1.143645. C; 1.509325; 1.768156; -0.983183. C; 0.657211; 2.642763; -0.054213. H; -0.97904; 0.206681; 0.369911. H; 0.123228; 0.256281; -1.701825. H; 0.644528; -0.882989; 2.282302. H; 2.623218; -0.798137; -1.548967. H; 2.767446; 0.058809; 0.972009. H; 2.793657; -1.719728; 0.943942. H; -0.865033; -2.092346; 0.394745. H; 0.482922; -3.037276; 1.051776. H; 1.583646; -2.99221; -1.020101. H; 0.248535; -2.083338; -1.735341. H; 1.286007; 1.685953; 1.789457. H; -0.446707; 2.038104; 1.764581. H; 1.55156; 2.139276; -2.012765. H; 2.540071; 1.726268; -0.608853. H; -0.294981; 2.880901; -0.542901. H; 1.140844; 3.586861; 0.21901. Al; -4.063433; -0.134438; -0.253408. O; -2.440701; 0.041061; 0.072175. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS5 JP-10/AlO |  |  |  | TS6 JP-10/AlO |  |  |  |
| C; 0.020121; 0.050079; -0.349404. C; 1.340017; 0.872062; -0.588349. C; 0.50375; -1.149724; 0.483128. C; 2.403076; 0.032033; 0.140718. C; 1.611775; -0.515369; 1.341925. C; 1.325824; -2.06745; -0.441635. C; 2.636201; -1.254735; -0.673887. C; -0.927217; 1.018915; 0.362575. C; 1.071672; 2.270156; 0.001992. C; -0.457408; 2.417176; -0.029266. H; -0.431221; -0.274711; -1.294879. H; 1.571388; 0.955695; -1.65749. H; -0.292114; -1.66834; 1.031526. H; 3.318878; 0.585523; 0.376283. H; 1.252078; 0.259308; 2.025864. H; 2.175899; -1.255509; 1.920506. H; 0.792889; -2.289723; -1.371566. H; 1.537519; -3.021861; 0.051266. H; 3.506946; -1.799027; -0.293883. H; 2.820444; -1.039474; -1.731179. H; -0.946449; 0.87409; 1.449022. H; -2.027036; 0.855289; -0.005625. H; 1.588158; 3.058554; -0.555025. H; 1.427016; 2.317903; 1.038364. H; -0.791287; 2.640835; -1.048698. H; -0.837812; 3.20276; 0.630031. Al; -3.526499; -1.257558; 0.137845. O; -3.24846; 0.363509; -0.480411. | Al; 5.233121; -0.000056; -0.236816. C; -0.904529; 0.78603; -0.620168. C; -0.904495; -0.78603; -0.620033. C; -2.108321; 1.128406; 0.279118. C; -2.108135; -1.128326; 0.279502. C; -2.083838; 0.000218; 1.324306. C; -3.39188; 0.779333; -0.498987. C; -3.391819; -0.77976; -0.498609. C; 0.473292; 1.21582; -0.068559. C; 0.47347; -1.215654; -0.068697. C; 1.055739; 0.000082; 0.652848. H; -1.058132; 1.19858; -1.625128. H; -1.058302; -1.198748; -1.624893. H; -2.089052; 2.152894; 0.667544. H; -2.088637; -2.152678; 0.668273. H; -1.197566; 0.0004; 1.96182. H; -2.974603; 0.000245; 1.964035. H; -3.385766; 1.203874; -1.508078. H; -4.274245; 1.173206; 0.016606. H; -4.274072; -1.173437; 0.017329. H; -3.385839; -1.204805; -1.507488. H; 0.401857; 2.099578; 0.575449. H; 1.132124; 1.477666; -0.904439. H; 1.132238; -1.477162; -0.904735. H; 0.402355; -2.099573; 0.575125. H; 2.213322; 0.00013; 0.545813. H; 0.871088; 0.000024; 1.731274. O; 3.618218; -0.000023; 0.183222. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 JP-10/R1 |  |  |  | vdW2 JP-10/R2 |  |  |  |
| C; 1.63335; -0.51238; 0.808329. C; 1.862562; 0.875495; 0.108984. C; 0.132283; -0.795691; 0.519682. C; 0.481968; 1.20241; -0.49301. C; -0.030362; -0.193318; -0.891683. C; -0.637124; 0.203396; 1.338856. C; -0.474411; 1.550599; 0.668824. C; 2.633737; -1.483462; 0.152321. C; 2.994568; 0.640793; -0.908536. C; 3.756118; -0.571905; -0.359314. H; 1.81814; -0.457129; 1.887961. H; 2.164553; 1.643809; 0.832121. H; -0.156394; -1.843527; 0.651866. H; 0.508821; 1.952717; -1.290318. H; 0.583784; -0.68679; -1.649704. H; -1.071172; -0.186587; -1.226731. H; -0.816588; 0.081283; 2.404653. H; -2.665978; -0.126502; 0.538375. H; -1.432064; 1.928718; 0.283161. H; -0.069012; 2.32003; 1.337799. H; 2.163178; -2.002129; -0.691572. H; 2.981397; -2.250161; 0.852086. H; 3.624802; 1.526949; -1.035111. H; 2.574628; 0.398878; -1.892552. H; 4.391779; -0.261909; 0.478938. H; 4.399594; -1.053192; -1.103238. Al; -5.044944; -0.439893; -0.448413. O; -3.441417; -0.095185; -0.026884. | Al; 4.51426; 0.017514; 0.151504. C; -0.765515; -0.382176; -0.960334. C; -1.997021; -0.457327; 0.04067. C; -0.132211; 0.911417; -0.498812. C; -1.823516; 0.806745; 0.910961. C; -0.281742; 0.910097; 1.016267. C; -0.925196; 2.122866; -0.943274. C; -2.146213; 2.046433; 0.045553. C; 0.025654; -1.684586; -0.734965. C; -1.840484; -1.80197; 0.773014. C; -1.015603; -2.667495; -0.186336. H; -1.100482; -0.311698; -2.001755. H; -2.949547; -0.431001; -0.503528. H; -2.373238; 0.768289; 1.858431. H; 0.193528; 0.065584; 1.517824. H; 0.054431; 1.839641; 1.48598. H; -1.223759; 2.065169; -1.993417. H; -0.363069; 3.050633; -0.798927. H; -2.201516; 2.947873; 0.664223. H; -3.101353; 1.943999; -0.47896. H; 0.822374; -1.525147; -0.001692. H; 0.504181; -2.030238; -1.656688. H; -2.809624; -2.241565; 1.03076. H; -1.288075; -1.660176; 1.70973. H; -1.653954; -3.028678; -1.001914. H; -0.568712; -3.541937; 0.297648. O; 2.8453; 0.302666; 0.16759. H; 2.022119; 0.616211; -0.214443. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 JP-10/R3 |  |  |  | vdW2 JP-10/R4 |  |  |  |
| Al; 4.095524; -0.69772; -0.000129. C; -1.088607; 0.887382; 0.786423. C; -1.087972; 0.886736; -0.787095. C; -1.379; -0.584568; 1.138781. C; -1.377783; -0.585652; -1.138361. C; -0.699266; -1.310212; 0.000885. C; -2.861715; -0.871703; 0.780555. C; -2.860897; -0.872419; -0.781416. C; 0.305547; 1.395537; 1.195541. C; 0.306204; 1.395255; -1.195751. C; 0.768171; 2.235265; -0.000031. H; -1.867297; 1.545808; 1.191469. H; -1.86677; 1.544285; -1.193337. H; -1.097301; -0.872298; 2.155848. H; -1.094942; -0.874355; -2.154832. H; -0.514711; -2.384328; 0.001415. H; -3.529249; -0.115547; 1.206827. H; -3.171417; -1.84535; 1.172437. H; -3.170353; -1.846368; -1.172744. H; -3.527907; -0.116581; -1.209065. H; 0.984735; 0.545272; 1.321992. H; 0.286597; 1.947269; 2.140998. H; 0.287188; 1.947224; -2.141062. H; 0.985684; 0.545213; -1.322272. H; 0.255492; 3.205005; -0.000355. H; 1.846117; 2.429943; 0.000291. O; 2.5291; -1.342602; 0.000644. H; 1.57142; -1.297743; 0.001731. | C; 0.430832; 0.376646; 0.635545. C; 0.786479; 0.379587; -0.852382. C; 1.030918; -0.872995; 1.223273. C; 1.657814; -0.888466; -0.964546. C; 2.35191; -0.928228; 0.411189. C; 0.285709; -2.09836; 0.644126. C; 0.71297; -2.103384; -0.85505. C; 0.580955; 1.763759; 1.207038. C; 1.45139; 1.754653; -1.048029. C; 0.712478; 2.65329; -0.043653. H; -1.633192; 0.132118; 0.231936. H; -0.0972; 0.307527; -1.502862. H; 1.129034; -0.872016; 2.313182. H; 2.315742; -0.907387; -1.839944. H; 3.012134; -0.076078; 0.601445. H; 2.913338; -1.854801; 0.580693. H; -0.79604; -2.016299; 0.769966. H; 0.614111; -3.010637; 1.153174. H; 1.242461; -3.027258; -1.10989. H; -0.143269; -2.014138; -1.530201. H; 1.497296; 1.814299; 1.817067. H; -0.247031; 2.056055; 1.864232. H; 1.380745; 2.110769; -2.080704. H; 2.51522; 1.700133; -0.786139. H; -0.285066; 2.889969; -0.430898. H; 1.227481; 3.598333; 0.154087. Al; -4.199599; -0.066018; -0.095101. O; -2.507463; -0.023921; -0.139237. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 JP-10/R5 |  |  |  | vdW2 JP-10/R6 |  |  |  |
| Al; -4.290743; -1.127192; -0.247615. C; 0.270918; -0.031515; 0.617712. C; 0.601366; 0.346557; -0.868319. C; 1.63325; -0.513924; 1.177344. C; 2.083795; -0.047785; -0.989595. C; 2.627245; 0.355712; 0.393559. C; 1.907787; -1.903365; 0.575169. C; 2.189179; -1.584323; -0.924588. C; -0.283501; 1.222935; 1.213093. C; 0.348189; 1.865342; -1.007505. C; -0.538079; 2.282102; 0.184549. H; -0.452621; -0.859384; 0.674577. H; -0.026535; -0.212149; -1.57203. H; 1.702099; -0.47122; 2.269488. H; 2.585746; 0.397193; -1.856026. H; 2.534836; 1.423371; 0.614731. H; 3.669562; 0.052976; 0.545816. H; 1.063239; -2.586025; 0.714076. H; 2.781716; -2.361704; 1.049936. H; 3.191057; -1.915956; -1.216206. H; 1.475511; -2.065552; -1.60109. H; -0.494285; 1.340434; 2.272854. H; -2.340756; 0.309184; 0.671533. H; 1.30062; 2.404305; -0.967878. H; -1.596105; 2.296382; -0.118857. H; -0.30956; 3.290211; 0.549702. O; -3.02891; -0.055467; 0.116179. H; -0.114484; 2.104754; -1.969581. | Al; -4.292772; -1.099693; -0.000807. C; 0.397964; 0.082639; 0.786753. C; 0.396683; 0.080381; -0.785972. C; 1.877341; -0.164207; 1.129895. C; 1.875496; -0.167448; -1.130826. C; 2.59365; 0.593325; -0.002137. C; 2.214909; -1.625428; 0.780591. C; 2.213631; -1.627662; -0.777889. C; -0.143666; 1.45926; 1.232616. C; -0.145662; 1.455722; -1.234909. C; -0.727353; 2.074559; -0.00156. H; -0.242706; -0.713057; 1.180435. H; -0.244608; -0.71646; -1.176319. H; 2.145919; 0.123632; 2.152527. H; 2.142402; 0.117459; -2.154716. H; 2.396382; 1.670702; -0.003517. H; 3.678528; 0.437421; -0.002801. H; 1.487169; -2.322999; 1.207143. H; 3.200119; -1.89846; 1.173063. H; 3.198194; -1.901824; -1.171197. H; 1.485192; -2.326451; -1.201246. H; 0.674319; 2.086163; 1.626705. H; -0.871891; 1.369643; 2.048088. H; -0.875183; 1.363794; -2.04897. H; 0.671696; 2.081475; -1.632113. H; -1.21408; 3.047061; -0.00256. O; -2.852151; -0.210196; 0.004287. H; -2.32617; 0.592633; 0.002295. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 Site 1 JP-10/BO |  |  |  | vdW1 Site 2 JP-10/BO |  |  |  |
| C; -1.286342; -0.786229; -0.500869. C; -1.286011; 0.785302; -0.502464. C; 0.148561; -1.131535; -0.06581. C; 0.149023; 1.130911; -0.068073. C; 0.468168; 0.000617; 0.92678. C; 1.098476; -0.781059; -1.227126. C; 1.098865; 0.777729; -1.228635. C; -2.40296; -1.198466; 0.476515. C; -2.402473; 1.199985; 0.47406. C; -3.358119; 0.000968; 0.489536. H; -1.498827; -1.190246; -1.499225. H; -1.498315; 1.187373; -1.501643. H; 0.263197; -2.153772; 0.312784. H; 0.264065; 2.153855; 0.308485. H; -0.168294; 0.001641; 1.816957. H; 1.517319; 0.000729; 1.238689. H; 0.756809; -1.208964; -2.175669. H; 2.104136; -1.163338; -1.02867. H; 2.104705; 1.1599; -1.030842. H; 0.757475; 1.203941; -2.178032. H; -1.988366; -1.350936; 1.480711. H; -2.886069; -2.135383; 0.179918. H; -2.885201; 2.136491; 0.175553. H; -1.987816; 1.354335; 1.477941. H; -3.966171; 0.000156; -0.42348. H; -4.042879; 0.00198; 1.344385. B; 5.330651; 0.001592; 0.823605. O; 4.142231; 0.000618; 0.592579. | C; -0.088229; -0.301962; -0.772602. C; -1.537642; -0.633887; -0.264029. C; 0.229213; 1.034954; -0.079758. C; -1.862899; 0.559166; 0.651504. C; -0.48917; 0.870544; 1.271403. C; -0.63346; 2.127191; -0.740032. C; -2.073633; 1.798961; -0.239057. C; 0.784279; -1.497705; -0.347518. C; -1.428503; -2.004235; 0.430589. C; -0.205062; -2.661997; -0.219328. H; -0.059714; -0.190731; -1.864328. H; -2.2538; -0.694355; -1.093826. H; 1.298561; 1.260411; -0.035613. H; -2.68191; 0.368736; 1.354639. H; -0.087696; 0.062241; 1.889512. H; -0.490971; 1.792087; 1.865269. H; -0.549549; 2.108336; -1.83161. H; -0.319238; 3.12161; -0.40535. H; -2.484583; 2.628792; 0.345929. H; -2.773151; 1.597961; -1.057153. H; 1.253237; -1.295036; 0.622632. H; 1.594264; -1.687357; -1.059009. H; -2.345631; -2.593702; 0.32729. H; -1.248385; -1.870349; 1.50446. H; -0.471591; -3.03429; -1.216281. H; 0.189167; -3.506935; 0.355611. B; 4.975952; 0.313481; 0.215318. O; 3.797735; 0.577375; 0.134276. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 Site 3 JP-10/BO |  |  |  | vdW1 Site 4 JP-10/BO |  |  |  |
| C; 0.637902; 0.879564; -0.785759. C; 0.637879; 0.879491; 0.785824. C; 1.139565; -0.533352; -1.131277. C; 1.139535; -0.533457; 1.13124. C; 0.524033; -1.37646; -0.000063. C; 2.637861; -0.607415; -0.779689. C; 2.637834; -0.607533; 0.779686. C; -0.811963; 1.194611; -1.198703. C; -0.812002; 1.194486; 1.198747. C; -1.392189; 1.954425; 0.000052. H; 1.315887; 1.643402; -1.188582. H; 1.315853; 1.64329; 1.188739. H; 0.903344; -0.849141; -2.153881. H; 0.903274; -0.849327; 2.15381. H; -0.56872; -1.389443; -0.000073. H; 0.888036; -2.410971; -0.000101. H; 3.198463; 0.231959; -1.204142. H; 3.081582; -1.528928; -1.171678. H; 3.081484; -1.529141; 1.171537. H; 3.198484; 0.231732; 1.204288. H; -1.375131; 0.265998; -1.342899. H; -0.858888; 1.759385; -2.136038. H; -0.858971; 1.759157; 2.136141. H; -1.375164; 0.265849; 1.34282. H; -1.02755; 2.989375; 0.00011. H; -2.486873; 1.984457; 0.000034. B; -4.336747; -1.726171; -0.00014. O; -3.210262; -1.281621; 0.000034. | C; 0.379974; 0.333007; 0.785312. C; 0.379837; 0.333122; -0.785227. C; 0.331391; -1.165736; 1.131349. C; 0.331193; -1.16558; -1.131472. C; 1.171149; -1.784644; -0.000182. C; -1.074783; -1.689172; 0.779331. C; -1.074915; -1.689074; -0.779284. C; 1.663274; 1.076766; 1.199455. C; 1.663058; 1.076937; -1.199488. C; 1.981561; 1.977751; 0.000021. H; -0.501502; 0.853022; 1.178088. H; -0.501717; 0.853179; -1.177772. H; 0.652307; -1.396038; 2.153884. H; 0.651931; -1.395722; -2.154099. H; 2.21806; -1.46682; -0.000252. H; 1.141007; -2.880617; -0.000252. H; -1.861519; -1.052786; 1.19445. H; -1.219019; -2.701138; 1.173573. H; -1.219204; -2.700995; -1.173623. H; -1.861729; -1.052647; -1.194191. H; 2.483241; 0.363983; 1.35301. H; 1.535833; 1.629902; 2.136026. H; 1.535454; 1.630212; -2.135954. H; 2.482999; 0.364178; -1.353294. H; 1.308788; 2.844185; 0.000143. H; 3.009896; 2.355101; -0.000045. B; -4.04504; 1.927611; -0.000238. O; -3.017507; 1.286835; 0.000325. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 Site 5 JP-10/BO |  |  |  | vdW1 Site 6 JP-10/BO |  |  |  |
| C; 0.162527; 0.205488; 0.426204. C; -0.368143; -0.523045; -0.860937. C; -1.13012; 0.68876; 1.106199. C; -1.894106; -0.359941; -0.748451. C; -2.11461; -0.445938; 0.772322. C; -1.708318; 1.841577; 0.263033. C; -2.235827; 1.118831; -1.014159. C; 0.974317; -0.851769; 1.196573. C; 0.162958; -1.965522; -0.768713. C; 1.407845; -1.852431; 0.119306. H; 0.815736; 1.046829; 0.169896. H; 0.008773; -0.04685; -1.775208. H; -1.010077; 0.928408; 2.168908. H; -2.46356; -1.067913; -1.361481. H; -1.838356; -1.411742; 1.205264. H; -3.145644; -0.21559; 1.065486. H; -0.950372; 2.599159; 0.039176. H; -2.524614; 2.34076; 0.796245. H; -3.317676; 1.252281; -1.121702. H; -1.767558; 1.485479; -1.933409. H; 0.340824; -1.353571; 1.939326. H; 1.81882; -0.40456; 1.729633. H; 0.370123; -2.392356; -1.755838. H; -0.58025; -2.612251; -0.285461. H; 2.237088; -1.424372; -0.454464. H; 1.73815; -2.814426; 0.526364. B; 4.557266; 1.646835; -0.392524. O; 3.492891; 1.09006; -0.242297. | C; 0.637852; 0.879442; -0.78586. C; 0.637917; 0.87957; 0.785708. C; 1.139585; -0.533504; -1.13123. C; 1.139677; -0.533324; 1.131267. C; 0.524162; -1.376503; 0.000113. C; 2.637908; -0.60743; -0.779722. C; 2.63797; -0.607316; 0.779648. C; -0.812056; 1.194328; -1.198756. C; -0.811956; 1.194523; 1.198678. C; -1.392267; 1.954273; -0.000074. H; 1.315775; 1.643256; -1.188833. H; 1.315882; 1.643444; 1.188495. H; 0.90332; -0.849413; -2.153785. H; 0.90349; -0.849062; 2.153892. H; -0.568595; -1.389536; 0.000163. H; 0.888195; -2.411005; 0.000181. H; 3.198459; 0.231897; -1.204337. H; 3.081648; -1.52899; -1.171585. H; 3.081734; -1.528824; 1.171607. H; 3.198565; 0.232066; 1.204094. H; -1.375171; 0.265653; -1.342777. H; -0.859089; 1.758955; -2.136174. H; -0.858909; 1.759304; 2.136007. H; -1.375067; 0.265878; 1.342897. H; -1.027715; 2.989254; -0.000177. H; -2.486951; 1.984195; -0.000031. B; -4.336727; -1.72652; -0.000581. O; -3.210586; -1.281103; 0.00058. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS1 JP-10/BO |  |  |  | TS2 JP-10/BO |  |  |  |
| C; 1.014145; -0.652867; 0.684473. C; 1.412093; 0.825558; 0.331264. C; -0.397908; -0.788092; 0.069935. C; 0.177615; 1.347016; -0.42613. C; -0.285182; 0.092351; -1.187829. C; -1.32501; 0.059418; 0.9287. C; -0.967; 1.516019; 0.595009. C; 2.099818; -1.541239; 0.046702. C; 2.709671; 0.717782; -0.490835. C; 3.321461; -0.620345; -0.058791. H; 0.986729; -0.818203; 1.76875. H; 1.59341; 1.419609; 1.235961. H; -0.724379; -1.823657; -0.075957. H; 0.367808; 2.238616; -1.033146. H; 0.443807; -0.276043; -1.914298. H; -1.242477; 0.232569; -1.702623. H; -1.404032; -0.214336; 1.984575. H; -2.517852; -0.158877; 0.496746. H; -1.818766; 2.041493; 0.143712. H; -0.663231; 2.088068; 1.477839. H; 1.789051; -1.860625; -0.955434. H; 2.286088; -2.446937; 0.632428. H; 3.373575; 1.572145; -0.325028. H; 2.479133; 0.690212; -1.562858. H; 3.790896; -0.512868; 0.926467. H; 4.084101; -0.991898; -0.750866. B; -3.871099; -0.402171; -0.015786. O; -5.003323; -0.612752; -0.402791. | C; 0.272786; 0.43704; -0.773867. C; 1.657749; -0.134243; -0.264942. C; -0.693408; -0.527298; -0.104895. C; 1.2437; -1.321391; 0.629803. C; -0.06892; -0.804004; 1.260335. C; -0.662033; -1.890188; -0.785316. C; 0.709879; -2.45188; -0.276863. C; 0.231941; 1.90266; -0.303205. C; 2.342391; 1.042589; 0.454247. C; 1.708923; 2.292448; -0.167823. H; 0.190162; 0.385513; -1.866026. H; 2.276986; -0.475944; -1.103781. H; -1.953494; -0.0197; -0.031817. H; 2.023053; -1.640091; 1.33136. H; 0.056591; 0.082014; 1.887152. H; -0.600989; -1.573018; 1.830007. H; -0.714841; -1.810656; -1.874767. H; -1.493793; -2.520139; -0.452655. H; 0.563981; -3.372628; 0.296965. H; 1.398352; -2.677988; -1.096942. H; -0.261933; 1.977905; 0.672902. H; -0.324796; 2.540656; -0.996547. H; 3.431321; 1.008911; 0.347088. H; 2.121365; 1.010836; 1.528122. H; 2.137468; 2.470948; -1.161349. H; 1.8629; 3.19803; 0.427544. B; -3.248166; 0.498339; 0.093944. O; -4.366196; 0.956156; 0.223522. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS3 JP-10/BO |  |  |  | TS4 JP-10/BO |  |  |  |
| C; 0.607771; 0.923543; -0.785755. C; 0.607835; 0.923685; 0.785556. C; 0.960913; -0.531952; -1.139281. C; 0.960789; -0.531802; 1.139312. C; 0.327335; -1.322277; 0.000038. C; 2.451824; -0.753161; -0.781217. C; 2.45174; -0.753098; 0.781417. C; -0.793095; 1.408137; -1.201704. C; -0.792854; 1.408697; 1.201659. C; -1.283753; 2.22551; -0.000164. H; 1.368206; 1.605911; -1.185579. H; 1.368468; 1.605956; 1.185159. H; 0.694378; -0.832984; -2.157382. H; 0.694161; -0.832682; 2.157432. H; -1.033643; -1.319837; -0.000488. H; 0.502984; -2.403813; 0.000131. H; 3.084718; 0.031883; -1.207289. H; 2.805394; -1.711781; -1.173338. H; 2.805291; -1.711671; 1.17367. H; 3.084573; 0.032002; 1.207475. H; -1.461472; 0.555638; -1.368372. H; -0.76841; 1.980828; -2.134342. H; -0.767684; 1.982027; 2.133898. H; -1.461329; 0.556454; 1.369348. H; -0.801824; 3.210716; -0.000412. H; -2.366632; 2.385119; -0.000092. B; -2.4122; -1.581556; -0.000581. O; -3.584652; -1.90121; 0.00049. | C; -0.213747; 0.326327; 0.446942. C; 0.580804; 0.435358; -0.878368. C; 0.388763; -0.863395; 1.18003. C; 1.615488; -0.696317; -0.7262. C; 1.876298; -0.689633; 0.792031. C; 0.041769; -2.157509; 0.415164. C; 0.875465; -2.037511; -0.896373. C; -0.231158; 1.702107; 1.100175. C; 1.110893; 1.880914; -0.888424. C; 0.081733; 2.660094; -0.058036. H; -1.443723; 0.078661; 0.157731. H; -0.058388; 0.268589; -1.757413. H; 0.16448; -0.894361; 2.251059. H; 2.494635; -0.58278; -1.369499. H; 2.321424; 0.237993; 1.164174. H; 2.493891; -1.532413; 1.123634. H; -1.031683; -2.259664; 0.231199. H; 0.352543; -3.02936; 0.999574. H; 1.588585; -2.863416; -0.983993. H; 0.251941; -2.047171; -1.795831. H; 0.556355; 1.754419; 1.86466. H; -1.181778; 1.914116; 1.603746. H; 1.231577; 2.268912; -1.904728. H; 2.092244; 1.9255; -0.400604. H; -0.823645; 2.82898; -0.653066. H; 0.44466; 3.636396; 0.277851. O; -3.997019; -0.515425; -0.371026. B; -2.846961; -0.188723; -0.152387. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS5 JP-10/BO |  |  |  | TS6 JP-10/BO |  |  |  |
| C; -0.152024; -0.259404; -0.170492. C; 0.812778; 0.85797; -0.716938. C; 0.771813; -1.135205; 0.692661. C; 2.165082; 0.465655; -0.095756. C; 1.739701; -0.090964; 1.275111. C; 1.702745; -1.91494; -0.255038. C; 2.663101; -0.812678; -0.796707. C; -1.23555; 0.499338; 0.583969. C; 0.227604; 2.197526; -0.225448. C; -1.262852; 1.911628; 0.025405. H; -0.599986; -0.843706; -0.986697. H; 0.8627; 0.847086; -1.81272. H; 0.238709; -1.762772; 1.415296. H; 2.895027; 1.282631; -0.08107. H; 1.255548; 0.646406; 1.923056. H; 2.571818; -0.543889; 1.825561. H; 1.144948; -2.421675; -1.048866. H; 2.256088; -2.682014; 0.296202. H; 3.70039; -1.024896; -0.518109. H; 2.630303; -0.71854; -1.886752. H; -1.190312; 0.42443; 1.674835. H; -2.364228; -0.073817; 0.30207. H; 0.386736; 3.006316; -0.945966. H; 0.7092; 2.498045; 0.712201. H; -1.804703; 1.919939; -0.929448. H; -1.744205; 2.63561; 0.689125. O; -4.680504; -1.251177; -0.275972. B; -3.619678; -0.698657; -0.06431. | O; 4.426367; -1.442731; 0.000026. C; -0.127232; -0.092518; -0.786394. C; -0.127238; -0.092561; 0.786382. C; -1.619648; 0.053471; -1.131741. C; -1.619654; 0.053449; 1.131734. C; -2.119705; 0.968621; 0.000005. C; -2.322109; -1.271409; -0.779523. C; -2.32216; -1.2714; 0.779494. C; 0.767042; 1.087868; -1.214427. C; 0.767054; 1.087789; 1.214479. C; 1.628388; 1.368854; 0.00003. H; 0.278234; -1.029132; -1.188688. H; 0.278203; -1.029204; 1.18863. H; -1.804179; 0.400179; -2.154554. H; -1.804175; 0.400144; 2.154554. H; -1.663917; 1.963818; 0.000015. H; -3.209013; 1.087544; 0.000006. H; -1.800546; -2.134681; -1.204705. H; -3.34413; -1.280895; -1.172019. H; -3.344215; -1.280803; 1.171914. H; -1.800692; -2.134704; 1.204731. H; 0.158079; 1.974289; -1.442602. H; 1.351638; 0.864823; -2.113895. H; 1.351648; 0.864692; 2.113936. H; 0.158095; 1.9742; 1.442706. H; 2.236527; 2.277895; 0.000061. B; 3.522055; -0.631545; -0.000096. H; 2.508793; 0.428426; -0.000059. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 HBO/R1 |  |  |  | vdW2 HBO/R2 |  |  |  |
| C; 1.06015; -0.422629; 0.874749. C; 1.683835; 0.746792; 0.030983. C; -0.447076; -0.34187; 0.505197. C; 0.47096; 1.331998; -0.719007. C; -0.375063; 0.072691; -0.979292. C; -0.961317; 0.928626; 1.122785. C; -0.411005; 2.076819; 0.307074. C; 1.794445; -1.701016; 0.426944. C; 2.758687; 0.087681; -0.853518. C; 3.142105; -1.191146; -0.098638. H; 1.203123; -0.265511; 1.950526. H; 2.14507; 1.50528; 0.676069. H; -1.008942; -1.251622; 0.74221. H; 0.736193; 1.925971; -1.600145. H; 0.117556; -0.665117; -1.618125. H; -1.357337; 0.302588; -1.405502. H; -1.238685; 1.012076; 2.170177. H; -3.460249; 0.091031; 0.410367. H; -1.20955; 2.639341; -0.199864. H; 0.156621; 2.801451; 0.904573. H; 1.242945; -2.194333; -0.382556. H; 1.891883; -2.425714; 1.24156. H; 3.607766; 0.754251; -1.035732. H; 2.336615; -0.173242; -1.83184. H; 3.797298; -0.941438; 0.744653. H; 3.668159; -1.921403; -0.722332. O; -5.36655; -1.047284; -0.458145. B; -4.398078; -0.468602; -0.016509. | O; 5.123371; 0.217198; 0.069428. C; -0.064226; -0.294278; -0.661145. C; -1.607255; -0.560083; -0.393209. C; 0.120752; 1.001773; 0.098204. C; -2.01886; 0.628464; 0.502696. C; -0.736988; 0.852064; 1.345055. C; -0.504482; 2.174161; -0.632254. C; -2.030907; 1.910148; -0.360746. C; 0.662111; -1.543373; -0.127899. C; -1.672044; -1.950518; 0.263717. C; -0.392275; -2.654465; -0.201505. H; 0.137807; -0.164145; -1.730847. H; -2.176664; -0.558352; -1.331137. H; -2.945215; 0.458197; 1.063345. H; -0.473669; 0.00559; 1.983041. H; -0.783447; 1.760263; 1.954103. H; -0.258675; 2.183856; -1.69766. H; -0.19172; 3.131172; -0.203107. H; -2.478231; 2.744478; 0.189121. H; -2.602531; 1.777103; -1.284574. H; 0.968324; -1.390562; 0.913524. H; 1.565789; -1.768771; -0.702901. H; -2.585908; -2.488655; -0.008163. H; -1.665447; -1.854239; 1.356303. H; -0.508084; -2.986775; -1.2402. H; -0.137093; -3.532153; 0.401065. B; 3.957036; 0.541682; 0.122606. H; 2.827653; 0.853644; 0.172148. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 HBO/R3 |  |  |  | vdW2 HBO/R4 |  |  |  |
| O; 4.86964; -1.191161; 0.000139. C; -0.916675; 0.832268; 0.786703. C; -0.916611; 0.83217; -0.786787. C; -1.132834; -0.653066; 1.137569. C; -1.132695; -0.653216; -1.137485. C; -0.410766; -1.33718; 0.000132. C; -2.59959; -1.013041; 0.780758. C; -2.59949; -1.013165; -0.780807. C; 0.450905; 1.407005; 1.19697. C; 0.450982; 1.406901; -1.197024. C; 0.879488; 2.262628; -0.00005. H; -1.726187; 1.451752; 1.192834. H; -1.726112; 1.451575; -1.193061. H; -0.838361; -0.924515; 2.155738. H; -0.838096; -0.924792; -2.155583. H; -0.146682; -2.393335; 0.00022. H; -3.304847; -0.291973; 1.207396. H; -2.859906; -2.00122; 1.172397. H; -2.859732; -2.001413; -1.172321. H; -3.304709; -0.292181; -1.207651. H; 1.165834; 0.586874; 1.336487. H; 0.402615; 1.963669; 2.138547. H; 0.402733; 1.963488; -2.138649. H; 1.165933; 0.586773; -1.336439. H; 0.324739; 3.208829; -0.000109. H; 1.947456; 2.504643; -0.000027. B; 3.661678; -1.282694; -0.00009. H; 2.493526; -1.373227; -0.000319. | C; 0.055228; 0.229493; 0.623954. C; 0.392086; 0.438239; -0.851985. C; 1.159863; -0.613511; 1.202806. C; 1.756555; -0.273995; -0.966436. C; 2.368497; -0.027724; 0.426916. C; 1.073264; -2.026124; 0.579827. C; 1.48999; -1.791639; -0.904436. C; -0.458308; 1.51323; 1.224355. C; 0.349647; 1.969673; -1.00975. C; -0.726992; 2.405464; -0.003088. H; -2.359343; -0.675068; 0.235686. H; -0.342831; -0.017667; -1.534108. H; 1.230797; -0.601632; 2.294703. H; 2.359935; 0.041573; -1.824303. H; 2.5543; 1.027321; 0.651442. H; 3.294455; -0.591683; 0.591728. H; 0.070275; -2.450357; 0.677825. H; 1.76995; -2.704924; 1.082837. H; 2.398757; -2.351273; -1.148827. H; 0.716051; -2.098886; -1.614862. H; 0.318075; 1.962923; 1.864127. H; -1.340777; 1.375557; 1.861634. H; 0.13442; 2.282177; -2.036644. H; 1.317503; 2.401432; -0.727178. H; -1.720778; 2.187241; -0.411151. H; -0.694247; 3.474361; 0.228918. O; -4.634075; -1.193439; -0.260676. B; -3.478583; -0.930444; -0.007882. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 HBO/R5 |  |  |  | vdW2 HBO/R6 |  |  |  |
| O; -5.066482; -1.266714; -0.438997. C; -0.034586; -0.172982; 0.443366. C; 0.509464; 0.483381; -0.875785. C; 1.244805; -0.717143; 1.124697. C; 2.017515; 0.184796; -0.801045. C; 2.291679; 0.326607; 0.707343. C; 1.708459; -1.948575; 0.325934. C; 2.225711; -1.328174; -1.007438. C; -0.740083; 0.938098; 1.15163. C; 0.158132; 1.986007; -0.793714. C; -0.971499; 2.10785; 0.247828. H; -0.718435; -1.01278; 0.233852. H; 0.059486; 0.032983; -1.769112. H; 1.131223; -0.890707; 2.199964. H; 2.621625; 0.81316; -1.464983. H; 2.087644; 1.324569; 1.106742. H; 3.312916; 0.03832; 0.981279. H; 0.898477; -2.669341; 0.173873. H; 2.513533; -2.468514; 0.855524. H; 3.286041; -1.554008; -1.160518. H; 1.683695; -1.695621; -1.884826. H; -1.177651; 0.83472; 2.140656. H; -3.150043; -0.200397; 0.492309. H; 1.031857; 2.552422; -0.454529. H; -1.952938; 2.035556; -0.251179. H; -0.966122; 3.0691; 0.773844. B; -4.092356; -0.72466; 0.034675. H; -0.125254; 2.388358; -1.771188. | O; 3.113165; 1.684621; -0.057578. C; 0.065817; 0.388285; 0.594482. C; -0.062709; -0.295893; -0.816015. C; -1.384372; 0.384472; 1.109777. C; -1.570006; -0.588815; -0.921993. C; -1.922005; -0.937643; 0.535148. C; -2.186724; 1.418037; 0.298252. C; -2.311302; 0.748678; -1.103608. C; 1.047508; -0.471802; 1.420263. C; 0.832324; -1.555289; -0.784347. C; 1.683813; -1.401938; 0.436901. H; 0.453939; 1.408295; 0.509897. H; 0.260856; 0.377793; -1.61905. H; -1.464272; 0.510115; 2.195273. H; -1.819224; -1.343749; -1.676288. H; -1.402322; -1.824194; 0.913634. H; -2.998368; -1.069053; 0.694926. H; -1.680481; 2.387816; 0.262962. H; -3.173399; 1.57874; 0.745387. H; -3.360503; 0.575163; -1.364915. H; -1.870699; 1.352566; -1.903462. H; 0.504657; -1.038368; 2.196117. H; 1.780423; 0.148164; 1.949135. H; 1.416517; -1.672533; -1.706469. H; 0.209439; -2.463398; -0.713237. H; 2.447486; -2.124095; 0.716566. B; 3.387029; 0.741116; -0.769686. H; 3.701412; -0.114369; -1.50458. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW1 JP-10/BO2 |  |  |  | vdW2 JP-10/BO2 |  |  |  |
| C; -1.733966; -0.657576; -0.622443. C; -1.572927; 0.888352; -0.38956. C; -0.356978; -1.214031; -0.220451. C; -0.121189; 1.013045; 0.10502. C; 0.049713; -0.275864; 0.929334. C; 0.662361; -0.80827; -1.301609. C; 0.807975; 0.730204; -1.092168. C; -2.915717; -1.088308; 0.266403. C; -2.665862; 1.270216; 0.625946. C; -3.740746; 0.191289; 0.447992. H; -1.955502; -0.886144; -1.672926. H; -1.717476; 1.453584; -1.319335. H; -0.359232; -2.285425; 0.008786. H; 0.090196; 1.954859; 0.624349. H; -0.608634; -0.332159; 1.801124. H; 1.080443; -0.4452; 1.257632. H; 0.318897; -1.068645; -2.308095. H; 1.61446; -1.320514; -1.13157. H; 1.841191; 1.006651; -0.85549. H; 0.516654; 1.307739; -1.975694. H; -2.548847; -1.432592; 1.241258. H; -3.484595; -1.913231; -0.174819. H; -3.039899; 2.286842; 0.466268. H; -2.266129; 1.228213; 1.646627. H; -4.319547; 0.391585; -0.461991. H; -4.445422; 0.13849; 1.284627. O; 3.763701; -1.111134; 0.865873. B; 4.21371; -0.058002; 0.447736. O; 4.703664; 1.100087; -0.0109. | C; 0.16166; 0.488401; -0.225288. C; 1.61713; 0.09062; -0.665799. C; -0.287904; -0.727438; 0.605263. C; 1.805067; -1.299511; -0.033957. C; 1.024377; -1.159991; 1.283854. C; -0.527164; -1.904632; -0.360868. C; 0.916766; -2.298162; -0.800377. C; 0.305033; 1.81454; 0.543347. C; 2.529535; 1.206896; -0.124616. C; 1.604452; 2.423289; 0.002806. H; -0.491735; 0.637905; -1.093349. H; 1.704589; 0.036342; -1.758443. H; -1.118391; -0.526642; 1.29461. H; 2.852316; -1.609528; 0.055029. H; 1.434645; -0.410192; 1.966064. H; 0.92807; -2.108407; 1.824637. H; -1.158864; -1.6201; -1.209037. H; -1.023697; -2.734528; 0.152676. H; 1.148209; -3.326944; -0.5052. H; 1.063894; -2.226617; -1.882719. H; 0.407146; 1.621636; 1.618858. H; -0.568769; 2.458919; 0.406117. H; 3.393284; 1.383558; -0.773895. H; 2.91791; 0.932764; 0.864127. H; 1.424185; 2.857821; -0.987865. H; 2.012192; 3.212981; 0.642482. O; -3.517514; -0.662742; 0.521782. B; -3.30461; 0.494362; -0.113511. O; -3.144441; 1.555885; -0.695874. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW3 JP-10/BO2 |  |  |  | vdW4 JP-10/BO2 |  |  |  |
| C; -1.848; -0.062721; -0.280286. C; -0.950366; -0.22457; 0.999284. C; -1.119511; 1.031777; -1.079208. C; 0.176726; 0.795086; 0.761763. C; 0.356206; 0.722168; -0.767665. C; -1.306264; 2.371276; -0.342078. C; -0.409167; 2.210726; 0.9226. C; -1.890031; -1.456714; -0.933685. C; -0.523211; -1.704702; 1.022775. C; -1.614743; -2.425451; 0.222509. H; -2.865102; 0.258149; -0.021267. H; -1.505228; 0.018856; 1.914346. H; -1.389488; 1.061417; -2.140692. H; 1.065389; 0.617618; 1.378821. H; 0.676365; -0.257269; -1.135205. H; 1.034818; 1.490442; -1.158953. H; -2.356818; 2.55661; -0.096523. H; -0.962861; 3.205303; -0.963089. H; 0.389595; 2.959844; 0.934849. H; -0.969154; 2.313094; 1.857577. H; -1.09728; -1.547386; -1.686561. H; -2.841563; -1.644706; -1.441659. H; -0.413402; -2.084165; 2.043971. H; 0.445349; -1.833515; 0.525064. H; -2.516435; -2.534639; 0.837519. H; -1.316364; -3.424513; -0.111398. O; 3.156471; -1.643754; -0.445984. B; 3.285811; -0.455079; -0.195834. O; 3.46394; 0.84113; 0.081774. | C; 0.15811; 0.268219; 0.783547. C; 0.165566; 0.382358; -0.785028. C; 1.571567; -0.250323; 1.101434. C; 1.581782; -0.089987; -1.156651. C; 2.41678; 0.444834; 0.019701. C; 1.65339; -1.7195; 0.645209. C; 1.655182; -1.609471; -0.910213. C; -0.180507; 1.679169; 1.300142. C; -0.161088; 1.855534; -1.09302. C; -0.934201; 2.339986; 0.139337. H; -0.590145; -0.448811; 1.151319. H; -0.58526; -0.265417; -1.255247. H; 1.87911; -0.084191; 2.139839. H; 1.901164; 0.218486; -2.158299. H; 2.425625; 1.535854; 0.097041. H; 3.453483; 0.089661; 0.000418. H; 0.816974; -2.313907; 1.026711. H; 2.576765; -2.183949; 1.006883. H; 2.57572; -2.025727; -1.332605. H; 0.814828; -2.138035; -1.371825. H; 0.743523; 2.233067; 1.507398. H; -0.75556; 1.649868; 2.231423. H; -0.724208; 1.963283; -2.025526. H; 0.765522; 2.43249; -1.202677. H; -1.963399; 1.966205; 0.099447. H; -0.978196; 3.431094; 0.220026. O; -3.608864; -0.278832; -0.369134. B; -2.87082; -1.190403; -0.029947. O; -2.086302; -2.210278; 0.337718. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW5 JP-10/BO2 |  |  |  | vdW6 JP-10/BO2 |  |  |  |
| C; 0.403328; 0.446756; 0.709745. C; 0.521435; 0.320123; -0.851471. C; 0.628772; -1.000127; 1.193848. C; 0.775776; -1.187054; -1.050657. C; 1.634975; -1.555126; 0.17028. C; -0.626421; -1.815944; 0.829046. C; -0.534373; -1.931596; -0.724021. C; 1.465413; 1.479047; 1.139874. C; 1.678953; 1.253968; -1.267317. C; 2.493992; 1.557888; 0.000803. H; -0.590268; 0.78773; 1.035101. H; -0.40059; 0.609864; -1.368139. H; 0.914753; -1.071191; 2.249182. H; 1.192741; -1.434454; -2.033104. H; 2.61406; -1.074466; 0.193819. H; 1.777241; -2.637579; 0.272452. H; -1.545006; -1.329964; 1.175753. H; -0.592346; -2.80425; 1.299583. H; -0.469013; -2.979685; -1.034255. H; -1.39195; -1.490182; -1.240336. H; 1.915997; 1.224827; 2.105971. H; 0.98355; 2.456655; 1.258657. H; 1.259603; 2.18722; -1.660522. H; 2.287329; 0.816406; -2.066956. H; 2.974819; 2.540358; -0.047577. H; 3.29245; 0.825396; 0.141918. O; -3.063842; 0.977132; 1.230449. B; -3.080373; 0.84876; -0.099884. O; -3.120234; 0.738106; -1.315814. | C; -0.977908; -0.877496; -0.785649. C; -0.977702; -0.87734; 0.785796. C; -1.606552; 0.483743; -1.131251. C; -1.606257; 0.483964; 1.131272. C; -1.071808; 1.38053; -0.000147. C; -3.105186; 0.418825; -0.779469. C; -3.104983; 0.418927; 0.779897. C; 0.494623; -1.056724; -1.199686. C; 0.49493; -1.056482; 1.19949. C; 1.14034; -1.761253; -0.000111. H; -1.581585; -1.700803; -1.189035. H; -1.581271; -1.700569; 1.189506. H; -1.40071; 0.819608; -2.153928. H; -1.40018; 0.820038; 2.153832. H; 0.01465; 1.501226; -0.000314. H; -1.531306; 2.375952; -0.000191. H; -3.586269; -0.468416; -1.204047. H; -3.631519; 1.295575; -1.171439. H; -3.631241; 1.295708; 1.171895. H; -3.585915; -0.468278; 1.204724. H; 0.961262; -0.075996; -1.346622. H; 0.594282; -1.614165; -2.137056. H; 0.594819; -1.613738; 2.136944. H; 0.961606; -0.075725; 1.346123. H; 0.86373; -2.822782; 0.000032. H; 2.235396; -1.711873; -0.000259. O; 2.706157; 1.68228; -0.00058. B; 3.6617; 0.923826; -0.000087. O; 4.708689; 0.090837; 0.000506. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS1 JP-10/BO2 |  |  |  | TS2 JP-10/BO2 |  |  |  |
| C; 1.461748; -0.733085; 0.563655. C; 1.555716; 0.832737; 0.479819. C; 0.098788; -1.036427; -0.092018. C; 0.228045; 1.222832; -0.192899. C; 0.008014; 0.055638; -1.17138. C; -0.983926; -0.565673; 0.886173. C; -0.906085; 0.98041; 0.824477. C; 2.691874; -1.265256; -0.196379. C; 2.833431; 1.126826; -0.327854. C; 3.705664; -0.117218; -0.121321. H; 1.484092; -1.086159; 1.602393. H; 1.634354; 1.285308; 1.476397. H; -0.016876; -2.072452; -0.42654. H; 0.224305; 2.227651; -0.628425. H; 0.77758; -0.025058; -1.943699. H; -0.971197; 0.08674; -1.662039. H; -0.896129; -0.990443; 1.891441. H; -1.981254; -0.952422; 0.50525. H; -1.843886; 1.425754; 0.474011. H; -0.688094; 1.421461; 1.802388. H; 2.433546; -1.462564; -1.243937. H; 3.063523; -2.203324; 0.227974. H; 3.317527; 2.054874; -0.007511. H; 2.593016; 1.23759; -1.392298. H; 4.161169; -0.089399; 0.875909. H; 4.514842; -0.20632; -0.853454. O; -3.405046; -1.363598; -0.178396. B; -3.91876; -0.137198; -0.216502. O; -4.391497; 0.992354; -0.262727. | C; 0.093937; 0.463436; -0.416197. C; 1.637901; 0.196117; -0.587296. C; -0.34347; -0.772204; 0.37499. C; 1.846976; -1.148913; 0.133745. C; 0.848113; -1.044085; 1.30439. C; -0.333849; -1.999313; -0.543368. C; 1.197012; -2.259471; -0.716601. C; -0.018912; 1.816779; 0.30928. C; 2.334867; 1.413904; 0.047065. C; 1.292152; 2.534703; -0.033508. H; -0.42108; 0.512641; -1.382413. H; 1.91195; 0.116686; -1.646604. H; -1.328697; -0.641096; 0.944487. H; 2.888452; -1.347819; 0.409848. H; 1.061077; -0.231058; 2.002122. H; 0.744556; -1.978725; 1.864942. H; -0.845391; -1.804541; -1.490463. H; -0.828408; -2.849203; -0.063256. H; 1.467796; -3.248704; -0.334118. H; 1.515624; -2.211219; -1.762296. H; -0.089074; 1.665696; 1.393678. H; -0.909247; 2.370339; -0.003625. H; 3.274313; 1.656983; -0.459686. H; 2.576923; 1.207752; 1.096903. H; 1.242573; 2.922926; -1.057762. H; 1.509437; 3.377218; 0.630821. O; -2.849437; -0.34976; 1.145073. B; -3.10113; 0.267469; -0.00844. O; -3.349753; 0.842143; -1.061996. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS3 JP-10/BO2 |  |  |  | TS4 JP-10/BO2 |  |  |  |
| C; 1.473689; 0.172466; -0.778193. C; 1.457155; 0.171799; 0.79412. C; 0.473715; -0.937825; -1.14212. C; 0.449386; -0.938525; 1.135946. C; -0.557811; -0.832391; -0.013905. C; 1.110152; -2.297323; -0.777012. C; 1.093347; -2.297867; 0.783749. C; 1.076681; 1.60135; -1.195021. C; 1.051985; 1.60047; 1.203803. C; 1.469445; 2.466121; 0.008875. H; 2.470235; -0.067359; -1.169414. H; 2.44517; -0.068761; 1.205979. H; 0.084412; -0.88238; -2.163557. H; 0.038501; -0.883692; 2.148941. H; -1.097534; 0.184839; -0.020238. H; -1.335245; -1.604329; -0.022433. H; 2.118605; -2.387753; -1.192168. H; 0.51353; -3.123611; -1.176067. H; 0.48813; -3.124326; 1.169276. H; 2.092612; -2.38877; 1.220449. H; -0.005082; 1.666778; -1.35561. H; 1.563873; 1.905712; -2.126946. H; 1.520056; 1.904021; 2.145738. H; -0.032795; 1.66596; 1.342189. H; 2.555698; 2.618377; 0.020085. H; 0.994522; 3.452237; 0.004353. O; -2.249682; 1.193759; -0.026215. B; -3.313376; 0.391132; -0.006537. O; -4.304602; -0.327792; 0.011297. | C; -0.444979; 0.324198; -0.691828. C; -0.423126; 0.276705; 0.843049. C; -0.807513; -1.062977; -1.174787. C; -0.888796; -1.169455; 1.103095. C; -1.85288; -1.408409; -0.07393. C; 0.325257; -2.047677; -0.814709. C; 0.282278; -2.105768; 0.742359. C; -1.15478; 1.589083; -1.14743. C; -1.352682; 1.438944; 1.245858. C; -1.170699; 2.461615; 0.115002. H; 0.824718; 0.52662; -1.135105. H; 0.57703; 0.44793; 1.264183. H; -1.148107; -1.104823; -2.212929. H; -1.2994; -1.32494; 2.105511. H; -2.729179; -0.752984; -0.077701. H; -2.189747; -2.447031; -0.160914. H; 1.288063; -1.716321; -1.208457. H; 0.105127; -3.024928; -1.254782. H; 0.079486; -3.123646; 1.08929. H; 1.218519; -1.776324; 1.199953. H; -2.176208; 1.298894; -1.437058. H; -0.691871; 2.054015; -2.022654. H; -1.096634; 1.834191; 2.232388. H; -2.395012; 1.099058; 1.280766. H; -0.205829; 2.968082; 0.22338. H; -1.951887; 3.226575; 0.090591. O; 2.366794; 0.724818; -1.26286. B; 2.706408; 0.570636; -0.020667. O; 3.031508; 0.423293; 1.168709. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TS5 JP-10/BO2 |  |  |  | TS6 JP-10/BO2 |  |  |  |
| C; 0.071036; -0.107928; 0.655572. C; 0.261834; 0.019994; -0.896666. C; 1.513979; 0.022421; 1.198059. C; 1.792314; 0.100544; -1.04137. C; 2.197153; 0.948066; 0.175925. C; 2.225348; -1.309672; 0.892464. C; 2.378046; -1.274084; -0.658891. C; -0.884744; 1.019391; 1.052585. C; -0.504735; 1.295287; -1.321317. C; -0.825955; 2.085851; -0.039957. H; -0.335412; -1.086188; 0.939478. H; -0.129378; -0.856396; -1.425102. H; 1.567087; 0.32727; 2.2491. H; 2.12024; 0.466932; -2.02035. H; 1.813721; 1.969845; 0.157613. H; 3.283362; 0.989451; 0.318598. H; 1.653634; -2.173771; 1.244574. H; 3.20367; -1.339798; 1.383573. H; 3.430288; -1.341325; -0.953525. H; 1.84535; -2.092073; -1.153734. H; -0.745007; 1.390622; 2.074571. H; -1.949186; 0.614591; 1.05655. H; -1.439347; 1.011728; -1.81748. H; 0.068411; 1.888561; -2.042428. H; -1.764468; 2.642756; -0.118957. H; -0.042865; 2.814593; 0.188559. O; -3.374455; 0.075284; 0.461825. B; -2.931365; -1.08289; -0.021543. O; -2.534162; -2.151732; -0.470794. | C; -0.6221; 0.242391; 1.145214. C; -1.25705; 1.230288; 0.103144. C; -0.687303; -1.120015; 0.416646. C; -1.758148; 0.281997; -0.998177. C; -0.609625; -0.735331; -1.073157. C; -2.149219; -1.594084; 0.502559. C; -2.898026; -0.576003; -0.41127. C; 0.784274; 0.777413; 1.46071. C; -0.122676; 2.179396; -0.350183. C; 1.14675; 1.711751; 0.335072. H; -1.210665; 0.194428; 2.068531. H; -2.082584; 1.810211; 0.532439. H; 0.052474; -1.845506; 0.767664. H; -2.019477; 0.794391; -1.930776. H; 0.344775; -0.31488; -1.392966. H; -0.838284; -1.58361; -1.727985. H; -2.525305; -1.602268; 1.530477. H; -2.241004; -2.612413; 0.111697. H; -3.445207; -1.086609; -1.209635. H; -3.620937; 0.035073; 0.139524. H; 1.521281; -0.015226; 1.634808. H; 0.763467; 1.384754; 2.379045. H; -0.313603; 3.210254; -0.019625. H; -0.023479; 2.223581; -1.440695. H; 1.945434; 2.439927; 0.504286. H; 1.8313; 0.984422; -0.587957. O; 2.848651; 0.031577; -1.288445. B; 2.90094; -0.895152; -0.369275. O; 2.95083; -1.772526; 0.501469. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 BO2/R1 |  |  |  | vdW2 BO2/R2 |  |  |  |
| C; -1.145326; -0.498976; -0.822161. C; -1.910508; 0.708415; -0.172209. C; 0.312293; -0.294249; -0.318987. C; -0.808716; 1.443633; 0.614952. C; 0.072618; 0.276784; 1.094174. C; 0.810904; 0.930558; -1.03766. C; 0.128733; 2.12542; -0.405965. C; -1.848343; -1.77; -0.307723. C; -3.028493; 0.076062; 0.677497. C; -3.266313; -1.295353; 0.033339. H; -1.186787; -0.464961; -1.917362. H; -2.347663; 1.364228; -0.935655. H; 0.934914; -1.191428; -0.400543. H; -1.185965; 2.115398; 1.392873. H; -0.440962; -0.419185; 1.761751. H; 0.994247; 0.609259; 1.582448. H; 1.12013; 0.908097; -2.081592. H; 2.666387; 0.866524; -0.243965. H; 0.845959; 2.784929; 0.105531. H; -0.407131; 2.745804; -1.134512. H; -1.35236; -2.141163; 0.596925. H; -1.824641; -2.578269; -1.045094. H; -3.925784; 0.702188; 0.707892. H; -2.690223; -0.055176; 1.712581. H; -3.848863; -1.176514; -0.888106. H; -3.809671; -1.990034; 0.681948. O; 3.49541; 0.65503; 0.227456. B; 3.834296; -0.626647; 0.179462. O; 4.177821; -1.800058; 0.157047. | C; 0.065223; 0.365085; -0.467204. C; 1.640829; 0.569357; -0.542133. C; 0.021697; -0.955831; 0.269699. C; 2.198373; -0.665873; 0.199181. C; 1.131769; -0.883022; 1.303993. C; 0.410667; -2.121412; -0.617461. C; 1.968788; -1.913939; -0.683122. C; -0.477271; 1.613032; 0.255581. C; 1.902739; 1.929127; 0.129131. C; 0.580385; 2.690098; -0.014491. H; -0.378273; 0.281381; -1.465938. H; 1.982679; 0.587437; -1.584285. H; -1.878316; -1.120725; 0.86894. H; 3.231623; -0.545001; 0.543495. H; 1.047619; -0.052722; 2.007636. H; 1.277298; -1.81586; 1.856936. H; -0.068066; -2.078157; -1.599034. H; 0.163848; -3.083545; -0.158218. H; 2.491572; -2.783002; -0.271724. H; 2.324172; -1.764345; -1.707027. H; -0.555024; 1.428744; 1.333838. H; -1.472768; 1.886663; -0.10483. H; 2.753885; 2.447837; -0.323666. H; 2.136453; 1.788506; 1.191489. H; 0.473639; 3.06144; -1.040555. H; 0.500106; 3.549174; 0.658941. O; -2.851599; -1.038372; 0.927254. B; -3.369869; -0.240397; 0.004668. O; -3.878438; 0.495175; -0.830801. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 BO2/R3 |  |  |  | vdW2 BO2/R4 |  |  |  |
| C; -0.881412; 0.968179; 0.764356. C; -0.896361; 0.922574; -0.807796. C; -1.378623; -0.434644; 1.163495. C; -1.399997; -0.501022; -1.115107. C; -0.830794; -1.288451; 0.043029. C; -2.890684; -0.517608; 0.821181. C; -2.905293; -0.563273; -0.740169. C; 0.573829; 1.281861; 1.15609. C; 0.5513; 1.212325; -1.244838. C; 1.167502; 1.982667; -0.071123. H; -1.554321; 1.741944; 1.153641. H; -1.577253; 1.672583; -1.228412. H; -1.132528; -0.73177; 2.186977. H; -1.172822; -0.857705; -2.123825. H; 1.256786; -1.634737; -0.037477. H; -0.843801; -2.379492; 0.074897. H; -3.436281; 0.33925; 1.229193. H; -3.333587; -1.42433; 1.244112. H; -3.355263; -1.493033; -1.101054. H; -3.459089; 0.268454; -1.187277. H; 1.115938; 0.348997; 1.354467. H; 0.637563; 1.880118; 2.070486. H; 0.596381; 1.756955; -2.193232. H; 1.087736; 0.268545; -1.399336. H; 0.832793; 3.026549; -0.098272. H; 2.261023; 1.977146; -0.079142. O; 2.169193; -1.963546; -0.115308. B; 3.131357; -1.061962; 0.022654. O; 4.051199; -0.264618; 0.141092. | C; 0.497429; 0.364124; 0.675806. C; 0.463726; 0.276913; -0.853881. C; 0.963232; -0.977249; 1.179198. C; 1.006145; -1.147444; -1.091224. C; 2.001088; -1.311445; 0.073897. C; -0.121955; -2.036009; 0.875596. C; -0.105877; -2.1356; -0.680839. C; 1.076568; 1.691355; 1.104385. C; 1.324443; 1.478538; -1.28872. C; 1.065846; 2.522353; -0.191369. H; -1.384343; 0.638854; 1.160588. H; -0.542131; 0.381243; -1.287327. H; 1.330383; -0.981686; 2.209871. H; 1.404814; -1.311955; -2.097553. H; 2.842538; -0.612269; 0.044206. H; 2.392969; -2.331209; 0.164186. H; -1.098758; -1.75822; 1.279716. H; 0.156261; -2.990406; 1.334099. H; 0.143871; -3.15125; -1.003456. H; -1.068208; -1.875865; -1.132033. H; 2.108165; 1.536443; 1.458533. H; 0.533385; 2.1632; 1.932326. H; 1.067155; 1.831576; -2.291924. H; 2.384993; 1.199269; -1.29467. H; 0.075246; 2.968844; -0.334616. H; 1.798527; 3.33469; -0.184171. O; -2.359706; 0.754129; 1.168158. B; -2.923656; 0.396657; 0.022903. O; -3.459101; 0.073651; -1.029332. |

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| vdW2 BO2/R5 |  |  |  | vdW2 BO2/R6 |  |  |  |
| C; 0.232005; 0.155898; 0.78197. C; 0.202568; -0.254542; -0.733478. C; 1.750149; 0.322439; 1.073321. C; 1.698054; -0.303682; -1.096. C; 2.274444; 0.857216; -0.268737. C; 2.369102; -1.08688; 1.104465. C; 2.324952; -1.521811; -0.391131. C; -0.538874; 1.436646; 0.859617. C; -0.604844; 0.837576; -1.477996. C; -0.839172; 2.006011; -0.493418. H; -0.181415; -0.615794; 1.447974. H; -0.265108; -1.23365; -0.883806. H; 1.960842; 0.928707; 1.960608. H; 1.883768; -0.271486; -2.174903. H; 1.876965; 1.839051; -0.541918. H; 3.368972; 0.901391; -0.303676. H; 1.815275; -1.764008; 1.762361. H; 3.39912; -1.042386; 1.473128. H; 3.332333; -1.712353; -0.77507. H; 1.735612; -2.429816; -0.551926. H; -0.545075; 2.046932; 1.762337. H; -2.30947; 0.510945; 1.238023. H; -1.558864; 0.420108; -1.811805. H; -0.075149; 1.170319; -2.37664. H; -1.855205; 2.415788; -0.563377. H; -0.168247; 2.85227; -0.705922. O; -3.086456; -0.080058; 1.231324. B; -3.115787; -0.911733; 0.199414. O; -3.16926; -1.688765; -0.744341. | C; -0.720762; 0.305292; 1.143938. C; -1.463548; 1.138442; 0.036263. C; -0.573614; -1.086552; 0.4893. C; -1.77114; 0.077428; -1.03408. C; -0.480936; -0.756511; -1.011676. C; -1.954413; -1.76346; 0.544475. C; -2.797547; -0.917374; -0.456967. C; 0.601998; 1.039164; 1.436649. C; -0.469398; 2.225049; -0.440966. C; 0.822746; 1.959497; 0.273584. H; -1.316676; 0.223728; 2.06019. H; -2.384805; 1.59775; 0.413078. H; 0.241552; -1.689119; 0.902631. H; -2.058876; 0.504165; -2.001374. H; 0.407959; -0.188832; -1.295989. H; -0.533609; -1.6511; -1.642239. H; -2.371867; -1.769434; 1.556298. H; -1.881144; -2.804645; 0.213929. H; -3.216973; -1.543895; -1.250482. H; -3.633053; -0.39904; 0.025061. H; 1.429366; 0.343775; 1.628503. H; 0.504391; 1.640313; 2.355908. H; -0.838547; 3.230815; -0.188167. H; -0.35494; 2.217422; -1.533775. H; 1.630908; 2.691556; 0.269907. H; 2.313547; 0.880688; -0.790405. O; 3.028747; 0.270043; -1.041284. B; 3.083416; -0.820381; -0.286511. O; 3.156925; -1.833555; 0.394579. |

|  | R1 |  | R2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 150.80. ν2; 178.27. ν3; 276.22. ν4; 305.30. ν5; 329.67. ν6; 385.28. ν7; 468.04. ν8; 496.17. ν9; 550.62. ν10; 575.95. ν11; 668.40. ν12; 758.68. ν13; 780.21. ν14; 814.91. ν15; 880.23. ν16; 884.44. ν17; 914.54. ν18; 924.55. ν19; 930.29. ν20; 941.29. ν21; 956.05. ν22; 960.59. ν23; 984.53. ν24; 1007.97. ν25; 1022.76. ν26; 1037.13. ν27; 1057.54. ν28; 1064.38. ν29; 1075.16. ν30; 1095.46. ν31; 1141.55. ν32; 1163.39. ν33; 1170.34. ν34; 1202.49. ν35; 1215.52. ν36; 1230.44. ν37; 1255.23. ν38; 1271.95. ν39; 1286.16. ν40; 1292.83. ν41; 1306.80. ν42; 1318.04. ν43; 1331.49. ν44; 1341.74. ν45; 1353.46. ν46; 1357.65. ν47; 1362.39. ν48; 1376.53. ν49; 1385.20. ν50; 1511.62. ν51; 1525.26. ν52; 1527.82. ν53; 1537.29. ν54; 1553.92. ν55; 3034.07. ν56; 3074.04. ν57; 3075.12. ν58; 3075.90. ν59; 3076.77. ν60; 3089.05. ν61; 3094.07. ν62; 3096.64. ν63; 3118.32. ν64; 3125.42. ν65; 3130.04. ν66; 3135.61. ν67; 3144.49. ν68; 3159.25. ν69; 3230.98. | 0.0565. 0.1355. 3.2021. 3.5611. 0.0812. 3.6049. 17.5334. 2.2611. 0.174. 5.5816. 0.8415. 0.6212. 0.5466. 1.5443. 0.2929. 1.6787. 0.1984. 0.6254. 1.8682. 1.2883. 0.3219. 0.1298. 2.9519. 0.7206. 1.445. 3.1683. 0.121. 0.1548. 0.1396. 0.7303. 0.592. 0.3808. 0.6483. 1.5431. 0.2356. 0.3789. 1.6136. 1.1613. 1.7483. 1.9139. 0.6116. 0.5003. 1.3477. 1.6207. 2.4893. 1.1672. 0.7739. 1.8215. 0.4517. 4.9085. 3.0828. 3.857. 7.5991. 13.0791. 39.922. 23.7347. 34.0002. 21.3529. 1.0908. 11.0864. 52.4341. 17.4993. 52.9796. 17.7962. 31.4355. 29.4332. 58.0494. 27.6229. 22.287. | 135.47. 178.27. 263.61. 316.98. 330.64. 402.51. 494.82. 522.67. 554.93. 662.09. 732.11. 763.99. 802.62. 838.60. 855.72. 878.64. 899.11. 913.86. 934.44. 939.16. 956.91. 976.43. 995.74. 1022.11. 1026.22. 1063.26. 1071.96. 1079.74. 1107.09. 1127.42. 1158.68. 1181.18. 1212.36. 1214.67. 1225.81. 1236.31. 1251.59. 1275.49. 1282.90. 1302.39. 1317.08. 1321.47. 1327.16. 1333.56. 1348.27. 1362.89. 1376.43. 1390.23. 1521.19. 1523.26. 1528.21. 1532.92. 1545.21. 1556.85. 3075.11. 3075.39. 3078.72. 3082.96. 3085.10. 3094.57. 3097.32. 3101.15. 3111.94. 3131.21. 3137.53. 3138.78. 3148.65. 3158.39. 3170.19. | 0.0973. 0.0472. 0.2159. 0.4626. 0.0729. 0.0998. 0.6943. 0.6841. 0.553. 1.3754. 0.1221. 0.3684. 0.6862. 0.6325. 5.2264. 0.491. 0.0932. 0.3485. 0.0652. 2.055. 1.9992. 1.666. 0.7941. 0.8302. 2.4999. 0.2115. 0.0572. 0.2131. 0.2356. 0.2747. 1.0416. 0.396. 0.2153. 0.5124. 4.9354. 1.7613. 3.2631. 0.718. 1.1925. 2.6855. 1.2727. 2.0023. 1.8236. 2.3021. 1.207. 0.3059. 0.5065. 0.9305. 2.1516. 0.3473. 3.9478. 11.1111. 13.0778. 8.698. 21.2737. 33.6201. 4.8542. 28.5711. 17.5351. 31.8993. 52.7881. 24.5497. 35.3399. 27.5236. 4.3181. 29.9643. 44.6576. 49.6916. 26.1427. |

|  | R3 |  | R4 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 104.16. ν2; 185.23. ν3; 242.11. ν4; 316.87. ν5; 318.54. ν6; 357.53. ν7; 448.13. ν8; 531.13. ν9; 545.67. ν10; 667.53. ν11; 721.19. ν12; 748.05. ν13; 784.07. ν14; 809.50. ν15; 847.58. ν16; 876.58. ν17; 887.72. ν18; 906.08. ν19; 932.43. ν20; 944.46. ν21; 946.02. ν22; 975.61. ν23; 976.18. ν24; 1018.18. ν25; 1023.41. ν26; 1038.80. ν27; 1064.70. ν28; 1071.56. ν29; 1074.56. ν30; 1096.18. ν31; 1172.68. ν32; 1182.00. ν33; 1208.44. ν34; 1214.91. ν35; 1223.76. ν36; 1225.05. ν37; 1249.99. ν38; 1263.31. ν39; 1284.20. ν40; 1285.33. ν41; 1309.40. ν42; 1319.45. ν43; 1323.88. ν44; 1344.33. ν45; 1346.61. ν46; 1362.80. ν47; 1363.35. ν48; 1380.09. ν49; 1381.68. ν50; 1519.61. ν51; 1522.90. ν52; 1525.93. ν53; 1541.13. ν54; 1544.65. ν55; 3071.89. ν56; 3073.20. ν57; 3073.57. ν58; 3073.72. ν59; 3078.72. ν60; 3086.95. ν61; 3089.82. ν62; 3128.11. ν63; 3130.08. ν64; 3132.46. ν65; 3132.82. ν66; 3134.74. ν67; 3144.21. ν68; 3149.73. ν69; 3214.44. | 0.0054. 0.1348. 0.0313. 0.078. 0.7193. 5.1519. 5.6907. 0.7104. 1.1932. 0.3373. 17.1714. 1.2071. 1.1605. 0.9972. 1.9684. 0.9678. 1.0122. 0.7601. 0.0221. 2.5387. 0.2079. 0.6065. 1.8518. 2.246. 1.485. 0.0837. 0.0626. 0.0748. 0.4156. 1.2723. 0.5595. 1.5394. 1.5999. 0.4279. 0.5893. 1.104. 0.9515. 0.7418. 2.4545. 0.0332. 0.0009. 0.0107. 0.2876. 2.2807. 0.1505. 0.8032. 0.4823. 3.6908. 0.5039. 4.8805. 1.0547. 8.2565. 2.9249. 8.6682. 33.7046. 15.9668. 0.2394. 29.398. 32.361. 13.7399. 76.3336. 25.7678. 27.7661. 0.7636. 38.8501. 27.0655. 44.897. 57.6503. 21.4684. | 116.76. 163.75. 236.22. 298.48. 315.66. 389.96. 485.76. 540.63. 557.48. 627.20. 730.84. 752.93. 812.34. 838.90. 865.35. 895.37. 902.41. 915.23. 919.73. 934.21. 946.63. 981.35. 982.70. 1020.37. 1034.85. 1059.75. 1068.51. 1077.45. 1114.04. 1141.99. 1147.14. 1169.76. 1176.75. 1208.19. 1230.04. 1243.23. 1250.17. 1267.13. 1276.32. 1289.14. 1321.32. 1323.00. 1330.06. 1333.94. 1355.97. 1357.53. 1368.98. 1385.34. 1508.81. 1521.84. 1524.58. 1531.77. 1541.39. 1554.17. 3022.95. 3040.00. 3074.05. 3080.31. 3081.79. 3081.97. 3092.26. 3100.07. 3118.08. 3130.69. 3134.21. 3135.49. 3144.10. 3148.39. 3156.58. | 0.118. 0.1894. 0.2715. 0.4033. 0.1367. 0.0329. 0.6848. 0.2203. 0.8622. 3.2183. 0.1909. 0.3897. 1.5299. 1.329. 0.4765. 1.9823. 0.509. 0.764. 0.5235. 0.3669. 1.4536. 0.232. 4.5103. 1.6645. 1.3566. 0.2177. 0.1557. 0.054. 2.0984. 0.6795. 0.077. 0.1267. 0.628. 1.6476. 1.535. 1.9789. 0.797. 0.2072. 1.1544. 1.0156. 0.2401. 0.2904. 1.8542. 4.3596. 2.0529. 0.2455. 0.5108. 0.7641. 4.882. 0.8681. 1.8937. 10.3184. 12.7643. 3.6726. 27.8484. 22.3692. 12.9793. 40.2035. 21.9296. 21.5085. 55.7636. 34.0208. 50.8464. 29.5244. 32.1031. 8.0411. 9.9717. 51.6051. 42.9328. |

|  | R5 |  | R6 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 119.67. ν2; 137.09. ν3; 255.60. ν4; 296.94. ν5; 317.78. ν6; 400.86. ν7; 416.92. ν8; 500.82. ν9; 535.19. ν10; 622.92. ν11; 747.00. ν12; 764.39. ν13; 774.02. ν14; 813.54. ν15; 846.25. ν16; 865.37. ν17; 888.39. ν18; 918.60. ν19; 935.38. ν20; 952.31. ν21; 955.23. ν22; 977.79. ν23; 986.25. ν24; 1006.20. ν25; 1028.10. ν26; 1046.51. ν27; 1064.92. ν28; 1072.04. ν29; 1085.22. ν30; 1097.94. ν31; 1139.79. ν32; 1154.09. ν33; 1177.00. ν34; 1205.45. ν35; 1226.58. ν36; 1235.12. ν37; 1251.63. ν38; 1263.89. ν39; 1291.28. ν40; 1297.64. ν41; 1308.16. ν42; 1316.66. ν43; 1331.37. ν44; 1332.77. ν45; 1337.56. ν46; 1346.72. ν47; 1364.62. ν48; 1377.67. ν49; 1387.79. ν50; 1511.01. ν51; 1525.03. ν52; 1526.88. ν53; 1542.70. ν54; 1554.72. ν55; 3004.31. ν56; 3014.09. ν57; 3079.07. ν58; 3083.14. ν59; 3086.14. ν60; 3088.00. ν61; 3088.98. ν62; 3108.42. ν63; 3113.96. ν64; 3123.04. ν65; 3128.97. ν66; 3141.40. ν67; 3148.40. ν68; 3152.21. ν69; 3222.35. | 0.0683. 0.2673. 0.3586. 0.6589. 0.4154. 0.4797. 22.4569. 0.597. 0.2082. 0.7574. 0.2122. 1.9491. 1.0861. 0.674. 0.5372. 0.5833. 1.7869. 0.6405. 0.2748. 0.1458. 1.5834. 2.7445. 0.4756. 1.9206. 1.5785. 0.1983. 0.1531. 0.0441. 0.3259. 1.0807. 0.0094. 0.3539. 1.0117. 0.4123. 3.9673. 0.5261. 0.6497. 0.1499. 1.5752. 0.3781. 0.4089. 0.5451. 0.0591. 1.933. 1.7659. 5.3194. 0.9899. 1.9113. 0.7712. 2.9537. 2.4332. 5.0538. 14.9919. 4.037. 39.6552. 29.3286. 21.9037. 13.082. 37.6354. 14.8897. 58.1459. 29.3292. 65.594. 17.8516. 1.0162. 30.185. 58.2285. 26.7011. 22.3624. | 96.11. 116.86. 252.25. 278.61. 325.99. 394.14. 402.77. 499.95. 531.09. 690.87. 703.96. 746.09. 785.70. 810.63. 841.15. 861.12. 914.88. 920.74. 933.15. 952.28. 953.68. 973.02. 987.74. 990.58. 1040.77. 1052.08. 1067.31. 1074.32. 1086.33. 1098.08. 1150.21. 1163.97. 1164.17. 1203.35. 1220.26. 1231.93. 1255.07. 1267.83. 1288.24. 1297.61. 1311.85. 1322.68. 1326.88. 1334.64. 1335.25. 1365.77. 1368.84. 1378.67. 1391.91. 1510.27. 1512.70. 1525.31. 1535.43. 1555.06. 3000.43. 3001.66. 3078.22. 3079.60. 3082.85. 3084.31. 3088.78. 3095.19. 3105.14. 3112.49. 3118.55. 3129.12. 3144.45. 3148.97. 3228.34. | 0.6883. 0.0028. 0.0102. 0.9791. 0.0043. 25.9986. 2.3727. 0.238. 0.0243. 1.0594. 0.5126. 0.3311. 0.0258. 0.8901. 1.0587. 0.9222. 1.7527. 0.3797. 1.2003. 1.303. 0.138. 1.4825. 0.4554. 2.1979. 2.2594. 0.0364. 0.6004. 0.2662. 0.0803. 0.0279. 0.7594. 0. 1.2014. 0.7623. 0.0001. 2.394. 2.0392. 0.0303. 0.8217. 0.3828. 0.1835. 0.0186. 0.2238. 0.2796. 5.7763. 0.3518. 4.6962. 0.4934. 0.6535. 6.8327. 1.9299. 1.5708. 16.2584. 4.6516. 30.893. 22.8575. 12.7894. 7.5315. 19.3657. 18.1288. 53.0711. 33.6013. 61.5819. 77.948. 2.9792. 0.0418. 23.2414. 61.8299. 30.3967. |

|  | JP-10 B3LYP/def2-TZVP |  |  |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 144.86. ν2; 183.19. ν3; 278.68. ν4; 323.98. ν5; 331.23. ν6; 406.96. ν7; 505.76. ν8; 538.22. ν9; 562.37. ν10; 677.86. ν11; 742.45. ν12; 759.89. ν13; 794.65. ν14; 835.78. ν15; 869.43. ν16; 870.56. ν17; 891.40. ν18; 899.24. ν19; 916.88. ν20; 924.82. ν21; 927.57. ν22; 961.72. ν23; 965.13. ν24; 994.87. ν25; 1004.67. ν26; 1047.38. ν27; 1055.60. ν28; 1057.47. ν29; 1058.01. ν30; 1080.23. ν31; 1140.77. ν32; 1157.37. ν33; 1173.26. ν34; 1193.87. ν35; 1207.72. ν36; 1214.09. ν37; 1232.45. ν38; 1254.23. ν39; 1264.61. ν40; 1293.87. ν41; 1303.64. ν42; 1309.67. ν43; 1316.68. ν44; 1321.65. ν45; 1331.83. ν46; 1334.48. ν47; 1348.14. ν48; 1353.50. ν49; 1373.56. ν50; 1377.82. ν51; 1494.18. ν52; 1497.05. ν53; 1499.72. ν54; 1505.95. ν55; 1516.87. ν56; 1531.63. ν57; 3018.20. ν58; 3024.48. ν59; 3027.22. ν60; 3033.56. ν61; 3038.18. ν62; 3046.39. ν63; 3047.55. ν64; 3049.67. ν65; 3067.56. ν66; 3070.81. ν67; 3074.56. ν68; 3077.32. ν69; 3080.47. ν70; 3083.92. ν71; 3091.25. ν72; 3092.16. | 0.009. 0.0031. 0.0817. 0.0513. 0.0421. 0.0462. 0.2251. 0.1734. 0.5638. 0.524. 0.3066. 0.3185. 1.3279. 0.5303. 1.0147. 0.0155. 0.6079. 0.0652. 0.9298. 0.077. 1.1053. 1.7838. 0.0305. 1.6714. 0.489. 0.2149. 0.6282. 0.0282. 0.0489. 0.5847. 0.1199. 0.0264. 1.0062. 0.2069. 0.0662. 1.3373. 1.2409. 0.0055. 0.7579. 1.2094. 0.0343. 0.2175. 0.412. 0.0001. 0.0798. 1.6902. 0.5566. 0.9748. 0.7613. 0.4264. 1.123. 1.8945. 1.9952. 4.2672. 10.7064. 4.8919. 20.496. 29.4339. 19.6381. 1.1218. 24.6142. 55.0985. 8.1301. 72.3811. 6.2772. 44.6458. 41.3424. 97.7589. 45.9135. 10.4729. 82.9497. 50.3735. |  |  |

|  | R1 B3LYP/def2-TZVP |  | R2 B3LYP/def2-TZVP |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 154.52. ν2; 179.74. ν3; 269.30. ν4; 304.29. ν5; 328.29. ν6; 377.36. ν7; 444.94. ν8; 506.69. ν9; 553.10. ν10; 573.17. ν11; 677.19. ν12; 747.23. ν13; 768.85. ν14; 795.54. ν15; 866.58. ν16; 869.54. ν17; 891.38. ν18; 904.31. ν19; 913.76. ν20; 916.62. ν21; 934.59. ν22; 936.76. ν23; 960.23. ν24; 981.98. ν25; 998.40. ν26; 1011.99. ν27; 1035.93. ν28; 1045.81. ν29; 1053.22. ν30; 1074.12. ν31; 1122.61. ν32; 1145.38. ν33; 1159.77. ν34; 1188.11. ν35; 1193.46. ν36; 1212.58. ν37; 1234.56. ν38; 1252.49. ν39; 1272.05. ν40; 1283.11. ν41; 1300.32. ν42; 1307.81. ν43; 1319.44. ν44; 1327.68. ν45; 1337.67. ν46; 1346.14. ν47; 1347.44. ν48; 1361.57. ν49; 1372.57. ν50; 1473.41. ν51; 1494.66. ν52; 1499.43. ν53; 1508.59. ν54; 1525.09. ν55; 2967.58. ν56; 3010.11. ν57; 3019.34. ν58; 3026.04. ν59; 3029.27. ν60; 3039.33. ν61; 3054.03. ν62; 3055.90. ν63; 3071.17. ν64; 3076.30. ν65; 3083.17. ν66; 3084.22. ν67; 3087.96. ν68; 3097.24. ν69; 3196.12. | 0.0815. 0.1742. 7.1892. 2.3774. 0.0587. 5.8178. 14.5213. 0.503. 0.0862. 3.5614. 0.4164. 0.6745. 0.2578. 1.5931. 0.5031. 0.2943. 0.5595. 1.3591. 0.6825. 0.5315. 0.1724. 0.2314. 2.2927. 0.7657. 1.0491. 1.1601. 0.0162. 0.87. 0.014. 0.716. 0.4333. 0.2268. 0.6362. 0.597. 0.3524. 0.1555. 1.1736. 0.8133. 0.4255. 1.9975. 0.1951. 0.1164. 0.5644. 0.4021. 1.5205. 0.5283. 0.6114. 1.1002. 0.3848. 4.1523. 2.2168. 2.8636. 4.6117. 8.8149. 46.9071. 25.6347. 21.4738. 29.8635. 22.6579. 7.4462. 42.901. 18.2456. 38.4271. 43.1507. 77.8015. 93.2132. 4.722. 32.9053. 21.3324. | 144.65. 181.25. 277.96. 321.93. 329.63. 404.89. 502.13. 526.28. 559.77. 668.25. 716.25. 755.95. 773.22. 830.80. 837.16. 858.47. 875.94. 886.36. 913.01. 921.73. 931.59. 950.69. 971.47. 995.61. 1007.00. 1042.38. 1052.47. 1065.04. 1087.08. 1100.16. 1143.07. 1166.20. 1190.35. 1199.66. 1212.04. 1219.35. 1236.52. 1255.45. 1264.39. 1290.15. 1303.74. 1311.10. 1315.93. 1322.15. 1336.45. 1347.68. 1364.89. 1375.72. 1492.06. 1493.09. 1497.95. 1502.77. 1514.00. 1526.60. 3019.50. 3028.39. 3036.56. 3040.21. 3042.05. 3050.66. 3055.79. 3058.66. 3071.46. 3074.56. 3077.44. 3078.55. 3087.58. 3098.93. 3109.20. | 0.0886. 0.0512. 0.3358. 0.3858. 0.0731. 0.0916. 0.6129. 0.7013. 0.5547. 1.0893. 0.1597. 0.2605. 0.646. 0.453. 3.4844. 0.4177. 0.2142. 0.3154. 1.7382. 0.254. 1.1531. 1.4763. 0.5595. 0.8167. 1.632. 0.5466. 0.1851. 0.1349. 0.1698. 0.1386. 1.0528. 0.149. 0.1553. 0.5433. 4.2047. 1.5739. 1.5887. 0.9149. 0.6344. 1.6759. 0.7396. 0.3102. 0.8326. 1.2636. 0.4335. 0.2288. 0.4053. 0.6912. 1.5808. 0.3995. 2.5398. 6.6318. 8.3847. 5.8937. 25.6647. 25.7544. 16.9318. 14.0374. 14.3771. 47.6343. 51.4164. 24.7223. 44.1276. 32.5003. 56.9166. 9.3664. 51.0083. 72.6197. 32.3534. |

|  | R3 B3LYP/def2-TZVP |  | R4 B3LYP/def2-TZVP |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 111.86. ν2; 187.42. ν3; 261.45. ν4; 308.49. ν5; 321.25. ν6; 337.24. ν7; 429.89. ν8; 535.22. ν9; 548.59. ν10; 674.72. ν11; 675.02. ν12; 739.90. ν13; 768.83. ν14; 794.66. ν15; 836.73. ν16; 855.58. ν17; 872.73. ν18; 878.33. ν19; 914.40. ν20; 919.24. ν21; 928.82. ν22; 948.99. ν23; 950.47. ν24; 991.11. ν25; 994.38. ν26; 998.52. ν27; 1041.85. ν28; 1052.21. ν29; 1058.98. ν30; 1078.17. ν31; 1156.48. ν32; 1167.36. ν33; 1191.32. ν34; 1192.74. ν35; 1208.06. ν36; 1208.95. ν37; 1239.71. ν38; 1244.86. ν39; 1263.13. ν40; 1277.97. ν41; 1299.40. ν42; 1309.49. ν43; 1316.00. ν44; 1333.44. ν45; 1333.73. ν46; 1348.42. ν47; 1348.92. ν48; 1369.20. ν49; 1372.65. ν50; 1489.88. ν51; 1493.07. ν52; 1493.30. ν53; 1508.94. ν54; 1513.37. ν55; 3015.69. ν56; 3020.86. ν57; 3024.86. ν58; 3033.21. ν59; 3036.58. ν60; 3045.15. ν61; 3050.22. ν62; 3069.62. ν63; 3071.10. ν64; 3074.48. ν65; 3082.09. ν66; 3090.87. ν67; 3094.27. ν68; 3097.54. ν69; 3190.92. | 0.0013. 0.1451. 0.0526. 2.5297. 0.0591. 8.1255. 4.7033. 0.5368. 0.9172. 13.1661. 0.1795. 1.2947. 0.5191. 0.812. 1.476. 0.3368. 0.1344. 1.0743. 0.0633. 1.9664. 0.0444. 0.1656. 1.5318. 1.5685. 0.151. 0.991. 0.154. 0.1074. 0.1418. 0.6567. 0.407. 1.1113. 0.2743. 0.9488. 0.3175. 0.2456. 1.0744. 0.1264. 1.5503. 0.0017. 0.0179. 0.2732. 0.0038. 0.8227. 0.0987. 0.549. 0.3872. 1.9851. 0.3784. 3.4971. 0.5015. 5.8954. 2.6721. 5.2584. 19.1536. 30.4691. 25.7237. 7.9221. 26.3054. 22.3585. 80.6865. 0.05. 39.3357. 51.8496. 58.3304. 53.6016. 73.0037. 20.462. 17.6983. | 116.60. 161.82. 239.56. 291.98. 316.28. 390.16. 494.61. 542.14. 561.15. 628.85. 723.59. 740.35. 795.26. 831.53. 849.30. 876.57. 882.40. 890.91. 896.22. 907.04. 917.41. 957.27. 964.24. 990.06. 1019.21. 1040.19. 1047.23. 1062.80. 1095.04. 1124.00. 1133.89. 1152.89. 1166.31. 1190.56. 1208.27. 1224.14. 1234.37. 1249.11. 1252.67. 1285.78. 1305.34. 1311.16. 1315.06. 1326.56. 1339.45. 1342.06. 1353.64. 1366.69. 1470.83. 1492.19. 1493.11. 1502.73. 1509.56. 1526.23. 2953.46. 2983.86. 3018.23. 3025.50. 3036.07. 3038.69. 3038.99. 3050.10. 3073.37. 3074.21. 3083.28. 3084.07. 3088.13. 3093.95. 3097.42. | 0.1225. 0.1459. 0.4748. 0.3404. 0.0869. 0.0281. 0.5806. 0.1624. 1.0262. 3.203. 0.1385. 0.2311. 2.1631. 0.7287. 0.1588. 0.8024. 0.6114. 0.2136. 0.7737. 0.2267. 0.915. 0.018. 2.8843. 1.1328. 0.2754. 0.0326. 1.0466. 0.2034. 1.1335. 0.3732. 0.2313. 0.2065. 0.6413. 1.7135. 1.4261. 0.9616. 0.3267. 0.2375. 0.6844. 1.0408. 0.4388. 0.2227. 0.4198. 1.5901. 0.3495. 1.0895. 0.0348. 0.2754. 3.8874. 1.2989. 1.6532. 3.198. 9.2603. 3.2276. 34.79. 26.3467. 19.0731. 11.6416. 55.6529. 26.2375. 42.3396. 64.2788. 2.7039. 64.1029. 23.1515. 70.1505. 45.8074. 20.2313. 60.2549. |

|  | R5 B3LYP/def2-TZVP |  | R6 B3LYP/def2-TZVP |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 120.90. ν2; 133.95. ν3; 267.23. ν4; 290.21. ν5; 319.78. ν6; 401.50. ν7; 418.33. ν8; 507.86. ν9; 538.59. ν10; 629.92. ν11; 740.16. ν12; 755.04. ν13; 767.56. ν14; 799.35. ν15; 836.68. ν16; 850.60. ν17; 873.21. ν18; 889.38. ν19; 909.53. ν20; 925.48. ν21; 927.62. ν22; 951.88. ν23; 963.46. ν24; 980.57. ν25; 1004.68. ν26; 1021.03. ν27; 1051.39. ν28; 1053.92. ν29; 1066.83. ν30; 1077.31. ν31; 1124.62. ν32; 1145.43. ν33; 1163.19. ν34; 1187.08. ν35; 1210.78. ν36; 1220.17. ν37; 1231.70. ν38; 1247.32. ν39; 1281.70. ν40; 1287.27. ν41; 1295.52. ν42; 1301.97. ν43; 1314.32. ν44; 1320.90. ν45; 1324.06. ν46; 1335.12. ν47; 1349.92. ν48; 1364.35. ν49; 1372.84. ν50; 1471.01. ν51; 1496.30. ν52; 1497.93. ν53; 1510.55. ν54; 1524.97. ν55; 2916.75. ν56; 2951.25. ν57; 3027.39. ν58; 3037.95. ν59; 3043.45. ν60; 3046.67. ν61; 3047.88. ν62; 3049.81. ν63; 3067.07. ν64; 3079.13. ν65; 3081.46. ν66; 3087.65. ν67; 3091.66. ν68; 3092.51. ν69; 3180.15. | 0.1143. 0.2081. 0.6456. 0.6426. 0.4363. 3.0735. 18.4598. 0.6899. 0.1126. 0.6461. 0.0986. 1.5252. 0.7481. 0.7287. 0.3308. 0.4925. 0.8881. 0.6722. 0.3198. 0.1109. 1.3552. 1.373. 0.1667. 1.6358. 0.8729. 0.3603. 0.3015. 0.2798. 0.3804. 0.9804. 0.0424. 0.2195. 0.7098. 0.2985. 2.7293. 0.3924. 0.8385. 0.0552. 0.4092. 1.3514. 0.0518. 0.4031. 0.291. 0.5354. 1.4645. 2.6536. 0.6291. 0.9604. 1.054. 2.2939. 1.0639. 2.9445. 11.4606. 3.0114. 47.5025. 36.524. 26.0106. 26.8405. 24.5827. 61.0348. 31.953. 32.8158. 4.955. 54.3734. 63.1313. 20.263. 65.3797. 39.0635. 22.9516. | 83.3286. 127.021. 265.134. 278.9338. 329.4545. 393.905. 405.1738. 511.1193. 536.0017. 687.9005. 711.3315. 733.6506. 772.9638. 799.0063. 833.6046. 843.2213. 890.3232. 895.0157. 913.112. 926.8657. 937.1678. 952.9848. 965.6014. 967.5085. 1016.724. 1025.347. 1048.893. 1057.725. 1064.171. 1080.183. 1134.295. 1147.262. 1151.437. 1180.725. 1201.713. 1217.232. 1236.958. 1252.339. 1269.27. 1294.831. 1306.422. 1308.093. 1311.509. 1322.565. 1329.05. 1348.758. 1355.671. 1366.202. 1379.298. 1471.471. 1473.821. 1494.006. 1509.049. 1529.677. 2924.335. 2926.529. 3003.138. 3003.252. 3037.463. 3045.19. 3048.151. 3048.603. 3064.499. 3067.151. 3077.834. 3084.06. 3086.597. 3091.189. 3183.43. | 0.7531. 0.0001. 0.0173. 0.8025. 0.0017. 26.4158. 0.3165. 0.1762. 0.0074. 0.6149. 0.3173. 0.269. 0.07. 0.9518. 0.7728. 0.3718. 0.5409. 0.8602. 1.087. 1.072. 0.6358. 0.6736. 0.0583. 1.422. 1.7597. 0.0102. 0.5321. 0.6523. 0.5682. 0.0102. 0.48. 0.7383. 0.1079. 0.5952. 0.0212. 1.1894. 1.3549. 0.0015. 0.0068. 0.9459. 0.3764. 0.1973. 0.2552. 0.264. 2.4189. 0.0892. 2.4239. 0.0777. 0.9583. 6.1364. 2.0765. 1.0736. 8.826. 4.1653. 33.6158. 30.7142. 35.8921. 20.2755. 19.2909. 39.8441. 50.7679. 20.2586. 52.0511. 10.2821. 83.6528. 2.7467. 27.5414. 86.8256. 30.2786. |

|  | vdW1 Site 1-2 JP-10/AlO |  | vdW1 Site 3 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 17.00. ν2; 35.15. ν3; 49.13. ν4; 55.59. ν5; 87.80. ν6; 134.82. ν7; 180.82. ν8; 264.48. ν9; 318.16. ν10; 332.61. ν11; 403.97. ν12; 494.40. ν13; 535.14. ν14; 556.78. ν15; 667.99. ν16; 739.50. ν17; 750.36. ν18; 767.11. ν19; 813.37. ν20; 846.27. ν21; 881.30. ν22; 882.73. ν23; 911.22. ν24; 917.71. ν25; 938.81. ν26; 941.44. ν27; 947.30. ν28; 982.98. ν29; 992.96. ν30; 1020.81. ν31; 1029.20. ν32; 1066.78. ν33; 1069.90. ν34; 1076.44. ν35; 1078.65. ν36; 1096.24. ν37; 1157.96. ν38; 1164.44. ν39; 1186.39. ν40; 1216.15. ν41; 1219.50. ν42; 1228.48. ν43; 1243.29. ν44; 1268.65. ν45; 1284.31. ν46; 1288.98. ν47; 1307.00. ν48; 1321.88. ν49; 1327.59. ν50; 1330.50. ν51; 1340.76. ν52; 1344.29. ν53; 1362.50. ν54; 1364.98. ν55; 1381.74. ν56; 1386.63. ν57; 1522.53. ν58; 1525.60. ν59; 1527.57. ν60; 1533.16. ν61; 1547.12. ν62; 1557.41. ν63; 3066.81. ν64; 3070.91. ν65; 3073.99. ν66; 3074.45. ν67; 3076.02. ν68; 3083.44. ν69; 3087.14. ν70; 3089.62. ν71; 3097.27. ν72; 3116.84. ν73; 3130.13. ν74; 3134.06. ν75; 3135.58. ν76; 3138.22. ν77; 3145.96. ν78; 3156.11. | 0.4753. 1.1885. 0.0313. 8.5907. 11.4418. 0.1075. 0.1409. 0.1635. 0.1256. 0.5765. 0.3471. 1.2699. 0.687. 0.1874. 1.0001. 189.6392. 0.4272. 1.3633. 1.2643. 1.0181. 1.2427. 3.5929. 0.3099. 0.5921. 0.3408. 1.8559. 3.4493. 4.0438. 1.1196. 2.166. 2.1967. 0.8177. 0.5057. 0.2632. 0.3722. 0.4668. 0.4134. 1.4713. 2.2199. 0.281. 2.4034. 3.9328. 1.8996. 0.222. 1.4462. 3.4556. 0.066. 0.2783. 0.5068. 2.3581. 4.2183. 4.6308. 0.6689. 2.0614. 1.4265. 0.5141. 1.3694. 1.285. 2.7122. 13.3134. 16.0041. 5.2029. 12.7887. 20.8058. 12.2776. 14.9103. 36.9065. 15.6569. 130.3601. 32.5941. 81.3895. 29.8883. 43.7406. 29.6455. 4.2558. 12.7946. 53.4531. 45.7328. | 22.26. 23.90. 64.50. 76.93. 89.36. 137.31. 187.66. 261.39. 318.91. 337.33. 407.11. 506.61. 532.81. 556.83. 670.24. 754.67. 767.97. 811.64. 844.24. 885.61. 886.59. 918.26. 922.32. 943.71. 944.17. 951.38. 984.48. 997.62. 1019.01. 1031.76. 1068.78. 1069.18. 1074.08. 1075.27. 1095.05. 1163.26. 1180.14. 1181.75. 1210.22. 1225.19. 1226.55. 1245.04. 1270.61. 1292.52. 1297.17. 1309.35. 1317.40. 1325.13. 1338.42. 1351.03. 1360.10. 1364.78. 1366.21. 1390.27. 1391.94. 1520.36. 1523.42. 1529.71. 1536.86. 1547.15. 1576.79. 3053.91. 3056.53. 3064.41. 3069.02. 3069.14. 3077.52. 3078.68. 3079.65. 3102.67. 3106.70. 3117.71. 3118.16. 3138.34. 3148.64. 3149.64. 3163.34. 4661.83. | 40.7366. 43.2182. 21.057. 17.9013. 20.229. 0.0738. 0.5789. 0.0542. 0.069. 0.8012. 0.3409. 2.5179. 0.1998. 0.3803. 1.8832. 0.2978. 0.4537. 1.9791. 1.4032. 0.2994. 3.4096. 1.0571. 0.2979. 2.2284. 0.6643. 0.7174. 1.0347. 5.9699. 3.1737. 2.1451. 1.5294. 0.2915. 0.3362. 0.503. 1.8937. 0.0997. 1.8224. 2.1879. 0.4979. 0.0252. 1.7454. 3.1783. 0.358. 3.5423. 0.5519. 0.2272. 0.4321. 1.8959. 0.147. 0.8046. 18.9673. 1.739. 3.0975. 15.9302. 0.0243. 3.1699. 1.3134. 0.2951. 18.1104. 0.4491. 34.3308. 2.336. 468.1902. 1254.6599. 22.5979. 143.156. 105.2997. 1396.5983. 85.9813. 128.511. 741.8283. 0.5857. 50.9124. 82.4097. 2513.5143. 5.9911. 52.8704. 2192532.61. |

|  | vdW1 Site 4 JP-10/AlO |  | vdW1 Site 5-6 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 11.82. ν2; 20.20. ν3; 32.24. ν4; 52.90. ν5; 73.20. ν6; 130.81. ν7; 182.22. ν8; 261.41. ν9; 319.49. ν10; 331.98. ν11; 403.48. ν12; 491.99. ν13; 534.03. ν14; 549.35. ν15; 555.16. ν16; 664.43. ν17; 750.26. ν18; 767.90. ν19; 812.32. ν20; 846.11. ν21; 880.04. ν22; 881.38. ν23; 913.06. ν24; 923.50. ν25; 939.24. ν26; 941.42. ν27; 953.82. ν28; 980.84. ν29; 983.76. ν30; 1019.63. ν31; 1030.86. ν32; 1066.86. ν33; 1068.73. ν34; 1076.84. ν35; 1086.14. ν36; 1093.51. ν37; 1147.93. ν38; 1165.40. ν39; 1191.20. ν40; 1212.34. ν41; 1218.95. ν42; 1226.42. ν43; 1242.53. ν44; 1270.29. ν45; 1287.03. ν46; 1288.95. ν47; 1300.35. ν48; 1322.94. ν49; 1328.06. ν50; 1330.62. ν51; 1338.17. ν52; 1340.07. ν53; 1359.76. ν54; 1361.92. ν55; 1394.97. ν56; 1397.68. ν57; 1516.74. ν58; 1520.74. ν59; 1525.99. ν60; 1529.52. ν61; 1542.75. ν62; 1553.73. ν63; 3063.31. ν64; 3063.37. ν65; 3067.62. ν66; 3069.95. ν67; 3077.27. ν68; 3079.84. ν69; 3097.51. ν70; 3103.36. ν71; 3111.86. ν72; 3112.71. ν73; 3127.68. ν74; 3129.03. ν75; 3136.03. ν76; 3143.02. ν77; 3153.09. ν78; 3166.08. | 38.9297. 27.8923. 0.041. 10.2654. 33.5366. 0.0085. 3.0835. 0.0428. 0.0316. 33.427. 110.8308. 46.0165. 0.2413. 9303.529. 526.3659. 0.6812. 0.2219. 5.8968. 0.0653. 6.2705. 2.9536. 0.6856. 0.0055. 0.5528. 0.1871. 1.1771. 1.9217. 4.138. 0.4794. 2.2591. 2.0966. 0.2361. 2.2548. 0.0542. 0.1006. 0.6018. 0.1518. 0.0213. 27.0206. 0.0018. 0.2744. 11.4189. 8.0718. 0.0004. 0.4431. 0.7887. 0.479. 0.0307. 3.0928. 0.8392. 2.6104. 41.0957. 0.3751. 15.6515. 3.2885. 2.4414. 0.0155. 8.33. 2.7749. 10.3174. 19.3734. 45.4829. 36.366. 30.0372. 20.0712. 48.7322. 49.742. 69.4691. 103.6163. 149.4729. 1.4538. 74.9856. 6.0018. 73.3502. 121.7255. 104.1185. 18.1559. 104.5249. | 13.05. 16.49. 32.34. 46.63. 68.05. 128.95. 187.74. 260.68. 318.52. 331.21. 402.78. 491.51. 532.43. 550.50. 638.60. 667.04. 750.11. 767.86. 812.23. 844.69. 881.33. 886.07. 915.13. 918.12. 940.29. 941.84. 952.73. 980.72. 984.10. 1018.45. 1033.29. 1063.61. 1073.19. 1074.11. 1079.26. 1094.83. 1149.57. 1166.92. 1183.86. 1213.92. 1220.64. 1222.99. 1244.95. 1270.66. 1282.61. 1288.85. 1300.59. 1322.94. 1325.88. 1327.89. 1338.38. 1342.81. 1361.71. 1379.92. 1386.85. 1394.53. 1516.80. 1522.56. 1524.52. 1528.25. 1543.74. 1555.35. 3058.13. 3058.38. 3070.84. 3077.74. 3079.80. 3081.53. 3102.49. 3107.58. 3110.68. 3115.24. 3121.68. 3128.76. 3133.07. 3142.69. 3147.66. 3153.78. | 25.6421. 22.7448. 9.3207. 11.857. 6.2506. 0.0589. 14.9395. 0.0245. 0.0486. 12.709. 2.5148. 5.491. 0.2685. 346.0482. 6249.947. 1.2896. 0.3906. 1.5668. 1.2026. 0.877. 3.0285. 0.6862. 0.1211. 0.674. 0.3208. 1.3336. 2.0928. 2.7818. 0.5033. 3.768. 4.0835. 0.047. 2.1406. 2.9419. 0.1166. 0.5983. 0.0365. 0.1203. 5.4355. 0.006. 0.078. 16.7433. 4.1751. 0.1602. 2.1474. 0.5635. 0.239. 0.0271. 0.2164. 1.4072. 1.7581. 3.5069. 10.8286. 3.5039. 17.5979. 0.3925. 48.4038. 1.9854. 0.2317. 18.0932. 40.5805. 13.3299. 34.325. 56.1495. 22.4837. 68.6684. 53.9451. 62.6216. 83.2044. 80.5284. 6.5876. 53.4766. 2.3256. 85.9346. 53.095. 124.8937. 40.6011. 186.3386. |

|  | TS1 JP-10/AlO |  | TS2 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -993.18. ν2; 15.07. ν3; 37.91. ν4; 68.90. ν5; 94.27. ν6; 141.69. ν7; 180.78. ν8; 260.90. ν9; 315.90. ν10; 332.00. ν11; 389.81. ν12; 495.85. ν13; 537.64. ν14; 557.48. ν15; 667.08. ν16; 734.33. ν17; 752.02. ν18; 768.47. ν19; 809.94. ν20; 842.54. ν21; 880.79. ν22; 882.56. ν23; 912.87. ν24; 920.62. ν25; 934.72. ν26; 941.74. ν27; 951.71. ν28; 976.70. ν29; 986.48. ν30; 1018.09. ν31; 1034.54. ν32; 1043.31. ν33; 1067.46. ν34; 1069.52. ν35; 1076.25. ν36; 1095.15. ν37; 1115.83. ν38; 1159.23. ν39; 1167.65. ν40; 1185.71. ν41; 1213.93. ν42; 1216.48. ν43; 1236.12. ν44; 1248.98. ν45; 1267.63. ν46; 1283.06. ν47; 1290.68. ν48; 1306.98. ν49; 1315.01. ν50; 1322.52. ν51; 1331.50. ν52; 1337.38. ν53; 1353.80. ν54; 1361.44. ν55; 1363.28. ν56; 1380.52. ν57; 1387.71. ν58; 1405.49. ν59; 1522.55. ν60; 1527.27. ν61; 1529.11. ν62; 1539.75. ν63; 1554.97. ν64; 3071.97. ν65; 3075.29. ν66; 3076.26. ν67; 3076.47. ν68; 3086.36. ν69; 3087.78. ν70; 3099.11. ν71; 3107.87. ν72; 3119.80. ν73; 3125.77. ν74; 3131.92. ν75; 3136.69. ν76; 3145.57. ν77; 3146.67. ν78; 3164.93. | 3271.0801. 0.6036. 1.3788. 1.9381. 1.5553. 1.8133. 1.6986. 7.1931. 4.5934. 0.3452. 6.4701. 0.5424. 0.6849. 2.8863. 2.3878. 215.7418. 0.4921. 4.2508. 15.2431. 48.3448. 3.8704. 0.6114. 3.1449. 9.0941. 5.702. 0.9562. 2.1183. 57.0062. 9.5641. 5.002. 1.8888. 173.9589. 9.9572. 3.8903. 6.9806. 335.7539. 306.2841. 54.201. 3.5998. 65.1352. 18.7186. 3.488. 51.9013. 1.2905. 350.9143. 1.4906. 47.9646. 63.6984. 112.9603. 0.5279. 9.9816. 19.2741. 242.3153. 12.7241. 27.5868. 7.8964. 36.7655. 88.9104. 2.2965. 4.6915. 7.2459. 7.4257. 12.9158. 11.5525. 14.0227. 27.7301. 22.6662. 10.6618. 49.102. 13.4361. 43.1271. 35.7314. 8.2309. 31.3563. 28.2931. 4.1161. 70.8167. 23.1997. | -868.58. 31.73. 37.91. 133.74. 177.30. 259.29. 312.03. 327.23. 401.99. 454.51. 480.71. 497.70. 537.57. 548.80. 568.20. 668.08. 748.01. 764.82. 817.49. 843.58. 875.91. 879.48. 906.64. 914.69. 937.09. 939.45. 953.05. 977.54. 1002.14. 1020.42. 1027.08. 1049.87. 1063.05. 1072.76. 1080.74. 1091.84. 1127.60. 1146.34. 1168.83. 1202.68. 1213.82. 1217.38. 1233.93. 1250.61. 1265.50. 1280.44. 1288.33. 1303.73. 1308.87. 1320.04. 1325.09. 1332.27. 1347.50. 1360.21. 1363.69. 1382.08. 1390.27. 1522.28. 1522.80. 1527.11. 1532.43. 1546.16. 1559.27. 3072.42. 3072.56. 3074.06. 3079.45. 3085.48. 3088.45. 3091.45. 3094.45. 3110.04. 3127.94. 3131.41. 3136.60. 3146.72. 3152.27. 3160.96. | 19417.4124. 0.2087. 0.5568. 0.041. 0.5322. 0.0381. 18.2947. 9.5249. 9.111. 360.8925. 1157.0138. 98.4125. 1038.8907. 68.351. 19.153. 11.068. 12.8386. 3.0538. 18.4656. 0.8002. 8.954. 0.8683. 4.5759. 25.4844. 9.5041. 2.303. 43.5399. 2.5348. 6.134. 27.0318. 6.9098. 297.9475. 13.122. 2.8982. 12.7665. 54.0248. 321.1419. 50.1873. 1.2847. 483.4916. 0.3349. 1.1. 37.4861. 474.2419. 255.1189. 36.6831. 684.0329. 1305.6723. 144.4434. 1.4243. 68.164. 13.162. 500.8126. 181.3874. 995.156. 143.2575. 1922.4873. 11.3465. 2.2441. 11.0037. 8.3384. 54.4113. 97.4121. 7.1476. 36.6055. 20.0482. 29.6881. 13.9053. 27.1617. 88.6767. 9.3349. 92.4328. 38.4383. 2.8344. 27.8708. 39.6767. 65.8554. 30.905. |

|  | TS3 |  | TS4 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -1325.81. ν2; 58.12. ν3; 61.39. ν4; 142.33. ν5; 177.69. ν6; 260.77. ν7; 314.03. ν8; 319.86. ν9; 332.10. ν10; 371.01. ν11; 390.28. ν12; 464.01. ν13; 535.35. ν14; 552.10. ν15; 619.19. ν16; 671.96. ν17; 745.33. ν18; 778.26. ν19; 810.55. ν20; 841.49. ν21; 882.58. ν22; 883.44. ν23; 908.65. ν24; 927.29. ν25; 930.50. ν26; 943.54. ν27; 945.96. ν28; 966.58. ν29; 978.52. ν30; 1019.48. ν31; 1029.38. ν32; 1059.41. ν33; 1061.90. ν34; 1071.01. ν35; 1076.45. ν36; 1095.94. ν37; 1108.91. ν38; 1117.51. ν39; 1171.46. ν40; 1186.92. ν41; 1213.09. ν42; 1223.95. ν43; 1224.59. ν44; 1229.33. ν45; 1263.33. ν46; 1267.52. ν47; 1289.24. ν48; 1295.07. ν49; 1313.98. ν50; 1320.17. ν51; 1326.31. ν52; 1341.82. ν53; 1353.67. ν54; 1364.21. ν55; 1365.94. ν56; 1389.90. ν57; 1390.45. ν58; 1510.95. ν59; 1523.24. ν60; 1528.10. ν61; 1530.97. ν62; 1545.45. ν63; 1552.39. ν64; 3066.91. ν65; 3067.45. ν66; 3077.66. ν67; 3081.73. ν68; 3087.42. ν69; 3090.65. ν70; 3092.87. ν71; 3104.51. ν72; 3120.35. ν73; 3123.41. ν74; 3124.54. ν75; 3128.90. ν76; 3148.05. ν77; 3153.90. ν78; 3158.81. | 28345.1992. 0.4065. 0.0571. 0.035. 1.3517. 0.0079. 0.035. 79.8031. 64.3034. 210.3668. 1.2096. 365.815. 0.9729. 39.291. 30.318. 0.0436. 0.267. 19.2688. 2.8624. 1.9319. 0.0161. 0.9171. 6.8158. 137.7507. 0.1477. 17.9595. 0.0018. 18.4975. 0.1233. 1.8017. 1.6633. 46.0838. 0.1181. 48.6169. 0.0508. 36.4342. 0.0179. 1251.742. 0.0845. 193.2214. 0.0099. 0.2758. 8.0293. 32.6305. 5.0074. 0.5716. 0.6485. 0.1574. 0.6872. 0.4244. 1.1007. 5.1984. 24.3743. 3.1226. 0.0549. 10.0203. 0.2554. 1494.6697. 2.4372. 2.0157. 361.8546. 1.8476. 405.8417. 2.8737. 37.3536. 26.2161. 33.3565. 117.1475. 58.8987. 24.4094. 47.56. 67.126. 20.9848. 31.8643. 3.928. 54.4735. 9.1335. 41.3255. | -506.92. 34.97. 38.78. 127.23. 173.26. 258.67. 313.37. 326.16. 401.84. 488.58. 525.22. 552.02. 611.22. 686.53. 743.56. 765.90. 804.92. 834.89. 861.42. 875.21. 904.45. 917.89. 923.76. 937.05. 941.93. 952.86. 977.12. 981.78. 1016.95. 1031.01. 1056.85. 1067.63. 1074.80. 1092.43. 1133.45. 1159.03. 1174.91. 1196.76. 1202.03. 1213.40. 1229.39. 1254.46. 1269.86. 1272.80. 1282.69. 1289.33. 1303.18. 1321.43. 1324.52. 1327.40. 1331.81. 1345.92. 1360.32. 1383.78. 1384.72. 1416.71. 1516.89. 1522.43. 1528.22. 1532.79. 1545.77. 1557.89. 1652.19. 3056.45. 3069.70. 3076.86. 3077.93. 3082.03. 3082.44. 3089.83. 3109.58. 3118.97. 3127.31. 3130.74. 3134.39. 3141.98. 3147.84. 3167.72. | 6870.1904. 0.4676. 0.3244. 0.1551. 17.1732. 3.0391. 1.6464. 23.4841. 0.4423. 141.9445. 8.6434. 28.4791. 2719.5648. 705.7731. 213.5919. 116.3752. 89.2432. 146.2567. 116.6038. 136.7934. 145.5968. 8.2154. 194.2148. 155.6536. 97.292. 370.8626. 78.0726. 9.2994. 268.8318. 143.5648. 77.6382. 25.842. 6.3745. 44.6204. 186.6093. 47.637. 269.8673. 334.0389. 462.5264. 243.8459. 455.6074. 765.7997. 50.4677. 271.2435. 191.0414. 50.8383. 1451.1853. 209.7029. 235.7564. 370.3159. 356.4206. 321.2419. 8.1924. 994.652. 1190.3273. 3487.3534. 21.0592. 10.2418. 209.784. 137.8874. 584.9517. 531.1511. 15293.0443. 42.7945. 30.2766. 65.7653. 44.8423. 55.2483. 5.0722. 118.7236. 101.34. 101.964. 28.5861. 37.9382. 62.2284. 107.5308. 39.9404. 164.6999. |

|  | TS5 |  | TS6 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -1158.72. ν2; 17.75. ν3; 45.37. ν4; 67.38. ν5; 97.74. ν6; 140.30. ν7; 179.42. ν8; 257.15. ν9; 321.59. ν10; 326.20. ν11; 401.94. ν12; 490.26. ν13; 526.47. ν14; 550.95. ν15; 660.26. ν16; 735.92. ν17; 751.56. ν18; 768.00. ν19; 811.36. ν20; 832.17. ν21; 847.06. ν22; 878.59. ν23; 883.44. ν24; 918.41. ν25; 919.92. ν26; 940.15. ν27; 952.95. ν28; 968.12. ν29; 985.67. ν30; 992.31. ν31; 1021.84. ν32; 1035.98. ν33; 1063.30. ν34; 1071.03. ν35; 1075.45. ν36; 1094.82. ν37; 1129.45. ν38; 1151.19. ν39; 1163.34. ν40; 1184.57. ν41; 1217.07. ν42; 1217.99. ν43; 1233.35. ν44; 1245.15. ν45; 1269.51. ν46; 1282.23. ν47; 1291.12. ν48; 1299.12. ν49; 1312.12. ν50; 1323.35. ν51; 1332.99. ν52; 1339.45. ν53; 1341.81. ν54; 1356.44. ν55; 1359.17. ν56; 1381.46. ν57; 1389.95. ν58; 1421.58. ν59; 1523.57. ν60; 1525.84. ν61; 1532.88. ν62; 1541.35. ν63; 1556.09. ν64; 3077.01. ν65; 3080.35. ν66; 3081.87. ν67; 3087.42. ν68; 3088.19. ν69; 3090.47. ν70; 3093.93. ν71; 3102.29. ν72; 3107.65. ν73; 3117.76. ν74; 3132.38. ν75; 3137.45. ν76; 3149.91. ν77; 3152.17. ν78; 3156.09. | 3759.1881. 0.9297. 1.0388. 1.9308. 1.4812. 1.8842. 0.2945. 3.5586. 4.6389. 2.5158. 0.6938. 5.8516. 5.7613. 13.3442. 35.5498. 211.9555. 0.2469. 0.3473. 4.7742. 322.8392. 82.6983. 0.6895. 2.9533. 0.2124. 8.5765. 0.1357. 1.4584. 26.2915. 3.6016. 46.4635. 3.174. 24.3536. 0.1935. 6.953. 0.2809. 1.3242. 101.804. 0.0461. 0.6913. 3.5788. 13.4337. 24.7971. 115.0117. 29.3118. 1.6024. 118.0556. 2.1482. 18.8512. 3.3056. 1.3616. 5.1105. 3.8294. 13.0719. 29.6278. 3.9005. 18.7961. 33.3653. 232.3392. 1.2818. 1.6271. 10.0424. 15.2491. 3.4104. 20.9239. 2.2236. 14.051. 38.9896. 10.7391. 64.2169. 11.9225. 60.8173. 22.1968. 29.3077. 0.1737. 34.1107. 8.2963. 56.63. 40.3093. | -946.56. 33.83. 35.14. 41.11. 160.11. 251.06. 258.11. 320.24. 382.37. 477.83. 490.96. 573.23. 589.75. 603.77. 741.03. 742.19. 761.29. 790.15. 816.97. 823.60. 855.76. 881.92. 912.19. 919.06. 943.78. 945.61. 955.82. 982.59. 985.20. 1013.11. 1043.75. 1053.64. 1061.95. 1086.36. 1100.78. 1121.16. 1135.16. 1156.62. 1165.20. 1179.99. 1218.11. 1227.11. 1239.78. 1267.91. 1291.99. 1293.15. 1303.38. 1305.58. 1309.69. 1325.97. 1334.26. 1335.36. 1352.02. 1360.78. 1369.12. 1387.20. 1402.36. 1426.48. 1515.59. 1525.58. 1530.59. 1534.69. 1555.94. 3070.22. 3073.96. 3077.92. 3081.33. 3087.06. 3087.71. 3093.33. 3111.24. 3113.71. 3117.16. 3128.24. 3130.82. 3139.01. 3147.99. 3172.80. | 18912.2857. 0.497. 0.5439. 0.0512. 20.6319. 0.0274. 3.6134. 0.5154. 107.5092. 47.0846. 2.7515. 665.8624. 152.6882. 744.5175. 26.4033. 472.618. 36.3075. 0.5968. 7.1642. 11.9444. 1.5017. 25.407. 13.8276. 1.6695. 18.9403. 3.1107. 3.5664. 22.8298. 0.007. 24.8285. 11.5583. 3.7777. 32.5282. 37.6049. 39.3276. 7.4585. 5.1841. 0.0105. 4.6154. 0.0629. 23.0516. 0.2106. 40.6947. 0.3671. 0.4979. 839.8128. 8.6148. 0.7029. 0.1947. 0.3836. 2.895. 934.7217. 7.4466. 3073.7504. 642.2788. 2.7069. 3829.5869. 304.7077. 8.1047. 2.1125. 68.5448. 50.0592. 5.8715. 9.4759. 5.8631. 8.5322. 62.4011. 25.0069. 62.9136. 49.8249. 84.109. 35.0188. 13.3744. 0.6156. 17.222. 62.7915. 71.3039. 35.7949. |

|  | vdW2 Site 1 JP-10/AlO |  | vdW2 Site 2 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 14.50. ν2; 28.71. ν3; 49.16. ν4; 83.98. ν5; 85.82. ν6; 154.52. ν7; 184.93. ν8; 290.84. ν9; 322.30. ν10; 330.75. ν11; 396.64. ν12; 424.80. ν13; 496.67. ν14; 528.13. ν15; 554.88. ν16; 569.01. ν17; 622.78. ν18; 668.61. ν19; 758.30. ν20; 781.20. ν21; 815.48. ν22; 868.05. ν23; 880.24. ν24; 884.61. ν25; 915.25. ν26; 924.00. ν27; 930.17. ν28; 941.10. ν29; 956.53. ν30; 961.14. ν31; 987.50. ν32; 1009.52. ν33; 1024.89. ν34; 1037.24. ν35; 1057.01. ν36; 1064.25. ν37; 1075.33. ν38; 1100.11. ν39; 1151.06. ν40; 1166.71. ν41; 1173.91. ν42; 1201.97. ν43; 1215.99. ν44; 1231.72. ν45; 1254.69. ν46; 1271.92. ν47; 1286.45. ν48; 1297.24. ν49; 1306.27. ν50; 1319.37. ν51; 1333.04. ν52; 1342.42. ν53; 1350.73. ν54; 1357.90. ν55; 1362.69. ν56; 1376.50. ν57; 1385.56. ν58; 1512.03. ν59; 1526.18. ν60; 1527.78. ν61; 1539.68. ν62; 1558.13. ν63; 3046.46. ν64; 3075.35. ν65; 3076.08. ν66; 3076.69. ν67; 3077.81. ν68; 3092.47. ν69; 3101.12. ν70; 3107.42. ν71; 3121.45. ν72; 3126.28. ν73; 3131.48. ν74; 3137.17. ν75; 3146.43. ν76; 3171.04. ν77; 3211.00. ν78; 3829.35. | 0.4438. 0.8293. 3.3197. 1.9209. 1.0702. 1.3146. 1.2473. 2.282. 2.3938. 2.7654. 6.5069. 124.8752. 16.3606. 8.077. 9.1029. 253.0468. 96.6667. 0.6924. 2.1696. 0.8691. 2.1641. 119.8005. 0.3171. 2.1525. 0.326. 0.8407. 1.5938. 1.0605. 0.0937. 0.1039. 4.7214. 0.8099. 1.5222. 4.6087. 0.5526. 0.187. 0.1719. 0.8551. 1.1643. 0.0904. 0.7617. 0.9991. 0.2165. 0.5295. 2.7897. 0.6198. 1.1441. 1.8561. 0.773. 0.3827. 1.3297. 1.6305. 3.4632. 0.9821. 0.7806. 2.1353. 0.649. 6.6184. 5.6075. 3.854. 3.5376. 10.7005. 22.4845. 24.7163. 35.0363. 7.8626. 14.683. 26.5145. 26.7645. 13.62. 50.8805. 7.2878. 30.7653. 27.5649. 58.3402. 16.2888. 19.8519. 517.3454. | 15.38. 30.35. 57.26. 70.31. 84.81. 137.52. 177.97. 263.57. 316.96. 328.94. 401.78. 412.58. 495.54. 519.82. 555.03. 561.28. 661.10. 731.21. 763.79. 801.70. 838.84. 857.77. 871.12. 878.19. 898.92. 914.57. 934.53. 940.05. 957.74. 974.92. 996.88. 1023.12. 1026.67. 1062.49. 1071.01. 1081.09. 1107.81. 1129.71. 1159.70. 1183.79. 1212.72. 1215.97. 1226.14. 1238.31. 1252.58. 1275.87. 1283.84. 1301.97. 1316.49. 1323.40. 1328.25. 1334.95. 1349.90. 1363.93. 1376.49. 1392.87. 1520.62. 1522.90. 1530.26. 1532.74. 1545.70. 1557.71. 3075.83. 3077.02. 3080.06. 3085.35. 3094.95. 3096.36. 3099.06. 3106.29. 3115.21. 3132.83. 3140.55. 3141.23. 3154.67. 3161.17. 3182.03. 3832.03. | 0.5811. 0.8934. 2.8778. 1.9007. 0.2598. 0.3932. 0.3268. 0.6714. 0.1404. 0.511. 7.1358. 130.1957. 3.2553. 7.1771. 3.8743. 304.9999. 1.1614. 0.2935. 0.5796. 1.2223. 0.5841. 25.1437. 98.9828. 0.3358. 0.2642. 0.4327. 0.0898. 1.6672. 1.1416. 1.34. 0.4599. 0.873. 2.5587. 0.2051. 0.0475. 0.3044. 0.2303. 0.1352. 1.3217. 1.1865. 0.388. 0.6502. 6.017. 2.0005. 3.5195. 0.674. 0.8316. 3.7351. 2.1636. 2.5604. 1.8784. 2.9426. 0.9687. 0.3006. 0.4667. 0.485. 2.4956. 0.4724. 5.6419. 11.4116. 11.3645. 13.9771. 34.0972. 20.7292. 4.5443. 26.8912. 17.2787. 29.7478. 48.5599. 24.7099. 29.8274. 25.8844. 6.485. 28.2929. 28.8077. 45.1915. 16.8376. 497.0561. |

|  | vdW2 Site 3 JP-10/AlO |  | vdW2 Site 4 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 22.85. ν2; 33.25. ν3; 46.46. ν4; 69.91. ν5; 102.74. ν6; 125.39. ν7; 187.28. ν8; 247.52. ν9; 315.56. ν10; 328.22. ν11; 379.10. ν12; 380.25. ν13; 456.06. ν14; 531.35. ν15; 542.38. ν16; 557.50. ν17; 667.49. ν18; 743.84. ν19; 766.56. ν20; 798.42. ν21; 808.77. ν22; 852.01. ν23; 863.64. ν24; 876.69. ν25; 887.46. ν26; 904.89. ν27; 931.95. ν28; 944.01. ν29; 947.14. ν30; 971.67. ν31; 976.20. ν32; 1018.72. ν33; 1024.01. ν34; 1040.51. ν35; 1066.45. ν36; 1071.32. ν37; 1076.39. ν38; 1096.56. ν39; 1173.41. ν40; 1182.74. ν41; 1209.69. ν42; 1214.39. ν43; 1223.91. ν44; 1224.67. ν45; 1248.19. ν46; 1263.42. ν47; 1286.20. ν48; 1286.27. ν49; 1311.62. ν50; 1319.62. ν51; 1325.03. ν52; 1344.46. ν53; 1348.80. ν54; 1363.58. ν55; 1363.71. ν56; 1381.53. ν57; 1383.07. ν58; 1523.06. ν59; 1526.38. ν60; 1527.50. ν61; 1543.66. ν62; 1545.74. ν63; 3073.80. ν64; 3076.71. ν65; 3081.95. ν66; 3086.41. ν67; 3087.25. ν68; 3090.17. ν69; 3092.91. ν70; 3129.99. ν71; 3131.90. ν72; 3135.50. ν73; 3136.40. ν74; 3144.15. ν75; 3150.64. ν76; 3153.14. ν77; 3190.45. ν78; 3861.54. | 1.8074. 0.0127. 3.9092. 0.8148. 1.8402. 0.8564. 0.814. 0.1899. 2.7301. 2.1775. 10.2494. 119.7963. 32.0656. 1.635. 55.5414. 98.4691. 0.0016. 1.2305. 14.2776. 7.9257. 3.3219. 0.5198. 145.0037. 0.7453. 0.1637. 0.2699. 0.1096. 2.3859. 0.3047. 0.9748. 2.6045. 1.6824. 1.3765. 0.1201. 0.1816. 0.091. 0.1953. 0.8159. 1.6252. 1.8898. 0.5277. 0.1922. 0.2955. 1.5325. 1.4233. 0.2341. 4.2162. 0.1945. 0.0067. 0.0397. 0.5484. 3.2325. 0.3153. 0.5017. 0.3836. 4.4837. 0.1273. 3.1338. 2.0034. 10.3457. 2.0939. 4.5482. 31.4969. 1.4939. 27.2288. 36.4234. 8.228. 19.6697. 71.3293. 22.0899. 23.2237. 0.1993. 27.1875. 19.6173. 36.6547. 60.144. 18.3199. 448.7079. | 16.04. 22.06. 45.13. 72.23. 88.61. 117.39. 174.33. 244.51. 301.12. 317.06. 392.56. 469.83. 487.09. 540.73. 555.07. 558.18. 635.65. 730.36. 754.47. 812.02. 839.79. 865.76. 869.70. 896.49. 902.36. 916.33. 921.16. 933.76. 947.07. 981.38. 983.65. 1021.22. 1037.30. 1062.02. 1070.71. 1080.00. 1113.06. 1145.48. 1148.18. 1174.32. 1179.61. 1208.67. 1231.02. 1246.74. 1250.11. 1268.40. 1277.97. 1289.96. 1322.42. 1323.50. 1331.22. 1334.70. 1356.47. 1359.16. 1370.10. 1384.60. 1505.93. 1521.49. 1526.15. 1531.38. 1541.15. 1555.98. 3026.47. 3057.94. 3075.76. 3082.39. 3083.37. 3085.98. 3096.50. 3100.11. 3120.90. 3131.79. 3137.84. 3143.55. 3145.92. 3151.02. 3166.33. 3769.73. | 0.2555. 1.6762. 3.1994. 0.8824. 0.4484. 0.4828. 1.6412. 3.1036. 0.3371. 1.6639. 0.3735. 130.4129. 1.2211. 4.3416. 58.2908. 172.239. 12.5175. 0.3412. 0.648. 1.99. 6.8955. 0.2884. 120.5194. 1.9442. 0.2877. 0.7775. 0.4257. 0.3464. 1.2835. 2.3953. 2.0246. 1.7741. 1.8759. 0.6446. 0.1404. 0.0795. 1.9771. 0.4244. 0.3583. 0.2448. 0.7034. 1.5663. 1.1657. 2.7825. 0.0977. 0.0664. 0.7467. 0.9533. 0.0945. 0.3995. 3.8402. 4.2951. 1.2905. 0.2039. 0.7192. 0.9923. 7.1635. 1.447. 2.907. 6.653. 12.3028. 6.0946. 25.0339. 9.8296. 12.5853. 42.2395. 16.7104. 19.6542. 46.1853. 27.3039. 48.5908. 26.0739. 34.3841. 9.1872. 11.305. 46.3075. 29.4946. 596.8993. |

|  | vdW2 Site 5 JP-10/AlO |  | vdW2 Site 6 JP-10/AlO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 7.05. ν2; 12.61. ν3; 40.89. ν4; 62.69. ν5; 91.22. ν6; 124.63. ν7; 138.93. ν8; 256.01. ν9; 281.12. ν10; 313.28. ν11; 352.42. ν12; 380.08. ν13; 403.87. ν14; 473.62. ν15; 499.38. ν16; 535.94. ν17; 632.14. ν18; 745.68. ν19; 761.27. ν20; 770.52. ν21; 814.37. ν22; 847.23. ν23; 852.93. ν24; 862.90. ν25; 887.86. ν26; 918.55. ν27; 936.22. ν28; 950.26. ν29; 954.36. ν30; 976.92. ν31; 985.95. ν32; 1003.82. ν33; 1033.40. ν34; 1043.02. ν35; 1065.10. ν36; 1073.54. ν37; 1097.50. ν38; 1103.43. ν39; 1138.74. ν40; 1156.37. ν41; 1178.40. ν42; 1207.46. ν43; 1228.57. ν44; 1239.91. ν45; 1257.03. ν46; 1265.21. ν47; 1291.15. ν48; 1297.77. ν49; 1316.07. ν50; 1321.02. ν51; 1329.95. ν52; 1333.38. ν53; 1339.26. ν54; 1348.33. ν55; 1370.14. ν56; 1378.01. ν57; 1389.45. ν58; 1515.07. ν59; 1524.86. ν60; 1527.77. ν61; 1544.22. ν62; 1555.19. ν63; 3030.04. ν64; 3033.47. ν65; 3080.00. ν66; 3084.28. ν67; 3088.74. ν68; 3089.61. ν69; 3096.84. ν70; 3103.82. ν71; 3115.15. ν72; 3122.76. ν73; 3130.20. ν74; 3144.36. ν75; 3149.58. ν76; 3151.52. ν77; 3221.03. ν78; 3914.16. | 0.1182. 0.7093. 1.009. 3.9369. 2.3488. 1.1393. 8.6535. 1.9826. 3.9451. 3.3422. 32.5757. 267.2557. 22.5437. 187.9611. 1.0409. 0.2863. 3.6395. 0.5377. 3.7474. 0.0051. 0.7192. 2.1336. 2.5354. 126.4786. 2.0407. 0.5427. 0.216. 0.1624. 1.6827. 2.3123. 0.4987. 1.8962. 0.7936. 0.6496. 0.434. 0.0109. 0.4465. 1.3938. 0.1942. 0.1821. 0.755. 0.2862. 5.1441. 1.5266. 0.1804. 0.2436. 2.0579. 0.3451. 0.7717. 0.3035. 0.0949. 2.9746. 1.8571. 5.2465. 2.8716. 2.6491. 1.3475. 3.0322. 2.3341. 4.161. 18.26. 4.6603. 23.2447. 23.8624. 21.2361. 15.3115. 24.6959. 50.3149. 28.1373. 21.7177. 66.3084. 15.4141. 0.8461. 24.4747. 64.4202. 23.5965. 16.5974. 288.6037. | 14.12. 29.20. 45.26. 71.45. 87.38. 120.09. 160.36. 253.09. 284.85. 323.98. 402.37. 434.58. 461.85. 500.46. 532.69. 552.99. 697.28. 700.59. 745.98. 789.42. 811.09. 841.62. 862.77. 868.93. 913.56. 920.64. 935.57. 949.61. 952.36. 971.79. 986.96. 991.87. 1037.56. 1055.06. 1066.84. 1075.82. 1087.08. 1097.67. 1149.63. 1161.60. 1170.80. 1206.34. 1218.74. 1232.37. 1255.38. 1267.33. 1286.12. 1295.75. 1311.84. 1325.38. 1329.58. 1334.84. 1336.09. 1363.45. 1368.27. 1381.68. 1393.33. 1506.54. 1509.58. 1525.17. 1534.94. 1554.91. 3004.88. 3005.98. 3080.04. 3082.58. 3089.58. 3090.11. 3090.59. 3109.37. 3112.93. 3115.61. 3123.94. 3131.04. 3142.61. 3150.57. 3213.20. 3834.67. | 0.758. 0.2424. 3.5525. 0.1727. 1.577. 0.2363. 5.7919. 0.5596. 1.9617. 2.7344. 1.9801. 119.7852. 20.7013. 20.1988. 0.0356. 316.9114. 0.9507. 4.4179. 0.431. 0.3052. 0.8662. 2.0316. 1.0313. 120.7525. 1.8624. 0.3778. 0.9232. 0.3984. 1.6662. 1.3146. 0.548. 2.2688. 3.0623. 0.2724. 0.5769. 0.1256. 0.0537. 0.0329. 0.7467. 0.0346. 0.7427. 0.1685. 0.029. 3.6319. 2.7196. 0.1171. 1.1349. 0.3102. 0.117. 0.0274. 0.464. 5.9386. 0.3018. 0.3423. 7.5949. 0.6564. 0.655. 10.5987. 4.2552. 1.6738. 18.8879. 5.6066. 21.4429. 22.6578. 19.5436. 23.397. 58.3059. 11.5354. 8.3503. 2.6276. 82.4087. 29.4235. 14.701. 0.0045. 27.2062. 60.97. 25.9556. 430.6408. |

|  | vdW1 Site 1 JP-10/BO |  | vdW1 Site2 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 25.22. ν2; 28.20. ν3; 41.87. ν4; 47.01. ν5; 64.05. ν6; 135.43. ν7; 179.85. ν8; 261.57. ν9; 318.68. ν10; 332.36. ν11; 404.33. ν12; 496.04. ν13; 533.01. ν14; 556.37. ν15; 668.85. ν16; 752.97. ν17; 766.82. ν18; 811.44. ν19; 843.38. ν20; 881.79. ν21; 883.10. ν22; 916.33. ν23; 918.54. ν24; 941.19. ν25; 942.64. ν26; 952.36. ν27; 985.14. ν28; 985.59. ν29; 1020.62. ν30; 1028.53. ν31; 1066.23. ν32; 1069.03. ν33; 1075.24. ν34; 1076.52. ν35; 1095.19. ν36; 1155.16. ν37; 1170.51. ν38; 1183.65. ν39; 1215.19. ν40; 1221.52. ν41; 1227.43. ν42; 1245.21. ν43; 1270.57. ν44; 1287.39. ν45; 1294.04. ν46; 1307.14. ν47; 1319.85. ν48; 1326.67. ν49; 1334.36. ν50; 1342.10. ν51; 1345.50. ν52; 1363.09. ν53; 1364.93. ν54; 1384.20. ν55; 1387.91. ν56; 1522.93. ν57; 1524.98. ν58; 1529.17. ν59; 1533.93. ν60; 1547.80. ν61; 1561.58. ν62; 1912.39. ν63; 3067.19. ν64; 3070.54. ν65; 3076.32. ν66; 3081.66. ν67; 3083.60. ν68; 3083.90. ν69; 3086.32. ν70; 3087.53. ν71; 3109.53. ν72; 3115.32. ν73; 3126.21. ν74; 3129.36. ν75; 3139.90. ν76; 3145.71. ν77; 3147.62. ν78; 3165.12. | 10.2391. 11.4026. 8.1567. 6.1212. 0.3342. 0.0037. 0.0551. 0.0464. 0.0704. 0.4163. 0.0015. 0.4426. 0.2006. 1.5602. 0.83. 0.3057. 0.7247. 0.9058. 0.8878. 1.0874. 2.134. 0.0836. 0.9404. 0.082. 1.5478. 1.4747. 2.321. 0.3338. 2.0434. 1.4684. 0.0209. 0.2564. 0.0453. 0.0612. 0.8207. 0.1692. 0.2051. 1.6119. 0.1902. 0.0875. 2.3231. 1.3384. 0.022. 3.0543. 0.772. 0.0025. 0.0501. 0.3669. 0.2285. 5.7713. 0.0122. 0.283. 2.1026. 3.3768. 0.1504. 1.3486. 2.6419. 2.8968. 8.6982. 9.8715. 5.5372. 143.8264. 3.1441. 37.068. 23.1088. 31.672. 45.5786. 28.7317. 69.1679. 3.5902. 87.9166. 10.3538. 0.2346. 28.9422. 20.663. 15.8866. 99.8338. 11.9748. | 24.97. 27.95. 41.75. 46.93. 64.06. 135.44. 179.85. 261.57. 318.68. 332.36. 404.34. 496.04. 533.01. 556.37. 668.85. 752.97. 766.82. 811.43. 843.38. 881.79. 883.11. 916.33. 918.54. 941.19. 942.64. 952.34. 985.15. 985.58. 1020.62. 1028.53. 1066.24. 1069.03. 1075.24. 1076.53. 1095.19. 1155.16. 1170.51. 1183.65. 1215.19. 1221.52. 1227.43. 1245.21. 1270.57. 1287.39. 1294.04. 1307.14. 1319.85. 1326.67. 1334.36. 1342.10. 1345.50. 1363.09. 1364.93. 1384.20. 1387.91. 1522.93. 1524.98. 1529.17. 1533.93. 1547.80. 1561.58. 1912.43. 3067.19. 3070.54. 3076.32. 3081.66. 3083.60. 3083.90. 3086.32. 3087.53. 3109.53. 3115.31. 3126.21. 3129.35. 3139.90. 3145.71. 3147.62. 3165.12. | 10.4206. 11.5301. 7.9755. 5.9934. 0.3339. 0.0037. 0.0551. 0.0464. 0.0704. 0.4164. 0.0015. 0.4426. 0.2006. 1.5603. 0.8301. 0.3057. 0.7247. 0.906. 0.8877. 1.0875. 2.134. 0.0836. 0.9408. 0.082. 1.5473. 1.4751. 2.3208. 0.3341. 2.043. 1.4685. 0.0209. 0.2564. 0.0453. 0.0612. 0.8207. 0.1692. 0.205. 1.6117. 0.1901. 0.0876. 2.3231. 1.3386. 0.0219. 3.055. 0.7725. 0.0024. 0.0501. 0.3669. 0.2295. 5.7694. 0.0122. 0.283. 2.1027. 3.3774. 0.1504. 1.3468. 2.6413. 2.8972. 8.7018. 9.8705. 5.5366. 143.8168. 3.1412. 37.0687. 23.1088. 31.6419. 45.5826. 28.7855. 69.1636. 3.5741. 87.9197. 10.3542. 0.2332. 28.9439. 20.6566. 15.8678. 99.8489. 11.9752. |

|  | vdW1 Site3 JP-10/BO |  | vdW1 Site4 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 25.01. ν2; 28.00. ν3; 41.77. ν4; 46.94. ν5; 64.05. ν6; 135.45. ν7; 179.86. ν8; 261.58. ν9; 318.68. ν10; 332.37. ν11; 404.34. ν12; 496.04. ν13; 533.01. ν14; 556.38. ν15; 668.86. ν16; 752.97. ν17; 766.82. ν18; 811.44. ν19; 843.38. ν20; 881.78. ν21; 883.10. ν22; 916.33. ν23; 918.53. ν24; 941.18. ν25; 942.64. ν26; 952.35. ν27; 985.14. ν28; 985.58. ν29; 1020.62. ν30; 1028.52. ν31; 1066.24. ν32; 1069.03. ν33; 1075.24. ν34; 1076.52. ν35; 1095.19. ν36; 1155.16. ν37; 1170.51. ν38; 1183.65. ν39; 1215.19. ν40; 1221.53. ν41; 1227.43. ν42; 1245.21. ν43; 1270.57. ν44; 1287.39. ν45; 1294.04. ν46; 1307.14. ν47; 1319.85. ν48; 1326.67. ν49; 1334.37. ν50; 1342.10. ν51; 1345.50. ν52; 1363.09. ν53; 1364.93. ν54; 1384.20. ν55; 1387.91. ν56; 1522.93. ν57; 1524.98. ν58; 1529.17. ν59; 1533.93. ν60; 1547.80. ν61; 1561.58. ν62; 1912.43. ν63; 3067.19. ν64; 3070.53. ν65; 3076.30. ν66; 3081.66. ν67; 3083.58. ν68; 3083.90. ν69; 3086.31. ν70; 3087.54. ν71; 3109.52. ν72; 3115.30. ν73; 3126.19. ν74; 3129.34. ν75; 3139.88. ν76; 3145.70. ν77; 3147.60. ν78; 3165.10. | 10.4022. 11.5204. 7.9948. 6.0032. 0.3331. 0.0037. 0.055. 0.0464. 0.0704. 0.4163. 0.0015. 0.4425. 0.2006. 1.5601. 0.8299. 0.3057. 0.7244. 0.9059. 0.8877. 1.0873. 2.134. 0.0837. 0.9403. 0.0819. 1.5474. 1.4747. 2.3203. 0.3339. 2.0433. 1.4683. 0.0209. 0.2565. 0.0453. 0.0612. 0.8208. 0.1692. 0.2051. 1.6119. 0.1903. 0.0875. 2.3233. 1.3383. 0.022. 3.0537. 0.7719. 0.0025. 0.0501. 0.3669. 0.2287. 5.7711. 0.0122. 0.283. 2.1027. 3.3765. 0.1504. 1.3474. 2.642. 2.8966. 8.6984. 9.8724. 5.5376. 143.8152. 3.1403. 37.0701. 23.1113. 31.5678. 45.566. 28.7217. 69.2393. 3.6115. 87.9164. 10.3601. 0.2336. 28.9391. 20.677. 15.8691. 99.8642. 11.9742. | 27.76. 29.79. 33.53. 42.94. 55.95. 128.21. 187.85. 262.06. 318.97. 330.55. 403.79. 492.75. 532.80. 557.69. 669.81. 753.19. 765.81. 810.27. 841.09. 881.85. 882.77. 913.96. 918.06. 941.04. 941.19. 952.17. 980.35. 986.15. 1021.61. 1025.25. 1063.95. 1068.00. 1074.37. 1078.78. 1095.78. 1150.17. 1168.50. 1183.11. 1217.11. 1221.45. 1226.57. 1244.32. 1270.01. 1282.57. 1291.74. 1305.02. 1317.35. 1324.64. 1331.12. 1341.09. 1341.80. 1364.87. 1373.41. 1377.23. 1380.13. 1523.98. 1525.14. 1526.82. 1536.87. 1547.60. 1557.81. 1914.12. 3054.60. 3070.51. 3072.68. 3073.16. 3077.45. 3087.39. 3088.58. 3090.13. 3113.51. 3119.03. 3126.51. 3132.06. 3134.51. 3146.25. 3151.14. 3155.33. | 8.8529. 7.5264. 0.7163. 42.7611. 1.9084. 0.0162. 0.2858. 0.1114. 0.0705. 0.0201. 0.0599. 0.4325. 0.228. 1.0373. 0.8783. 0.3022. 0.6634. 1.5409. 0.9672. 1.9589. 0.6132. 0.2055. 0.5606. 0.0333. 1.0092. 1.2621. 3.2247. 0.3965. 2.0061. 1.1128. 0.0056. 0.1429. 0.0326. 0.1377. 0.7191. 0.2554. 0.0679. 1.1836. 0.3799. 0.0594. 3.7636. 1.3509. 0.0383. 0.8493. 1.4175. 0.0011. 0.1921. 0.3111. 0.9038. 5.5236. 0.353. 1.0352. 0.3437. 2.9754. 0.3432. 0.107. 4.6663. 1.9742. 9.136. 16.9774. 6.0959. 72.1057. 6.0678. 57.631. 28.1118. 38.3365. 24.1082. 64.9358. 25.933. 26.3741. 71.4722. 7.8932. 1.4997. 34.4639. 25.672. 55.5298. 28.813. 43.8505. |

|  | vdW1 Site5 JP-10/BO |  | vdW1 Site6 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 16.32. ν2; 31.83. ν3; 46.61. ν4; 55.42. ν5; 60.91. ν6; 131.47. ν7; 180.22. ν8; 261.98. ν9; 319.24. ν10; 332.25. ν11; 403.18. ν12; 492.59. ν13; 532.41. ν14; 556.82. ν15; 668.73. ν16; 751.91. ν17; 766.29. ν18; 811.31. ν19; 844.97. ν20; 881.58. ν21; 882.66. ν22; 913.85. ν23; 918.38. ν24; 939.25. ν25; 941.89. ν26; 955.36. ν27; 980.72. ν28; 986.92. ν29; 1019.90. ν30; 1028.42. ν31; 1063.41. ν32; 1069.73. ν33; 1075.96. ν34; 1079.10. ν35; 1094.24. ν36; 1149.74. ν37; 1166.88. ν38; 1185.99. ν39; 1217.66. ν40; 1219.59. ν41; 1227.93. ν42; 1244.58. ν43; 1269.96. ν44; 1285.21. ν45; 1291.27. ν46; 1307.71. ν47; 1320.69. ν48; 1326.41. ν49; 1330.24. ν50; 1340.55. ν51; 1342.21. ν52; 1361.93. ν53; 1363.41. ν54; 1384.43. ν55; 1389.02. ν56; 1523.41. ν57; 1523.82. ν58; 1528.72. ν59; 1533.32. ν60; 1547.08. ν61; 1557.54. ν62; 1913.15. ν63; 3071.47. ν64; 3072.62. ν65; 3073.58. ν66; 3075.95. ν67; 3076.74. ν68; 3085.69. ν69; 3087.27. ν70; 3096.53. ν71; 3101.79. ν72; 3115.71. ν73; 3124.94. ν74; 3130.40. ν75; 3138.37. ν76; 3145.73. ν77; 3147.38. ν78; 3154.53. | 4.7766. 8.8446. 2.4556. 40.045. 4.9459. 0.021. 0.0019. 0.0167. 0.0857. 0.0609. 0.059. 0.351. 0.2932. 0.5982. 0.9191. 0.4196. 0.5512. 0.8836. 0.8828. 2.0695. 1.0606. 0.142. 0.5651. 0.0405. 1.541. 1.6284. 3.0369. 0.9147. 2.1362. 1.1878. 0.0737. 0.2694. 0.077. 0.0545. 0.6561. 0.14. 0.0555. 2.2576. 0.05. 0.0091. 3.2541. 2.428. 0.0072. 1.5747. 0.9021. 0.0672. 0.0825. 0.5504. 0.9209. 4.2151. 1.899. 0.884. 2.2728. 1.8569. 0.5162. 0.1357. 2.1706. 2.7789. 10.4657. 13.6939. 5.9277. 73.6334. 17.8843. 10.6228. 25.164. 37.6267. 6.2658. 39.5679. 48.5005. 55.3004. 62.7507. 26.9262. 3.1015. 31.0599. 29.4067. 2.197. 90.2866. 32.6233. | 25.22. 28.20. 41.87. 47.00. 64.04. 135.43. 179.85. 261.57. 318.68. 332.36. 404.33. 496.04. 533.01. 556.37. 668.85. 752.97. 766.82. 811.44. 843.38. 881.78. 883.10. 916.33. 918.53. 941.18. 942.64. 952.36. 985.13. 985.58. 1020.61. 1028.52. 1066.23. 1069.03. 1075.24. 1076.52. 1095.19. 1155.15. 1170.51. 1183.65. 1215.19. 1221.52. 1227.43. 1245.21. 1270.57. 1287.39. 1294.04. 1307.14. 1319.85. 1326.67. 1334.36. 1342.10. 1345.50. 1363.09. 1364.93. 1384.20. 1387.91. 1522.93. 1524.98. 1529.17. 1533.93. 1547.80. 1561.58. 1912.40. 3067.20. 3070.54. 3076.31. 3081.67. 3083.60. 3083.91. 3086.32. 3087.54. 3109.53. 3115.32. 3126.20. 3129.36. 3139.89. 3145.71. 3147.62. 3165.13. | 10.239. 11.3984. 8.1581. 6.1256. 0.3345. 0.0037. 0.0551. 0.0464. 0.0704. 0.4163. 0.0015. 0.4427. 0.2006. 1.5598. 0.83. 0.3058. 0.7243. 0.9059. 0.8877. 1.0872. 2.1341. 0.0836. 0.9404. 0.0819. 1.5476. 1.4742. 2.3208. 0.3339. 2.0433. 1.4681. 0.0209. 0.2565. 0.0453. 0.0612. 0.8205. 0.1692. 0.2051. 1.6121. 0.1902. 0.0874. 2.3233. 1.3382. 0.022. 3.0534. 0.7717. 0.0024. 0.0501. 0.3669. 0.2283. 5.7714. 0.0121. 0.2831. 2.1023. 3.3757. 0.1506. 1.3483. 2.6418. 2.8966. 8.6978. 9.8723. 5.5387. 143.8216. 3.1392. 37.0656. 23.112. 31.6052. 45.5824. 28.745. 69.2064. 3.5952. 87.9156. 10.3572. 0.2337. 28.9492. 20.6622. 15.9342. 99.7907. 11.9697. |

|  | TS1 JP-10/BO |  | TS2 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -1403.20. ν2; 30.82. ν3; 31.71. ν4; 114.58. ν5; 151.14. ν6; 162.42. ν7; 186.72. ν8; 244.15. ν9; 305.22. ν10; 335.62. ν11; 378.85. ν12; 494.34. ν13; 502.54. ν14; 547.68. ν15; 566.99. ν16; 670.14. ν17; 755.57. ν18; 777.29. ν19; 815.53. ν20; 871.53. ν21; 882.88. ν22; 899.00. ν23; 915.67. ν24; 928.88. ν25; 937.41. ν26; 941.71. ν27; 953.21. ν28; 981.37. ν29; 988.23. ν30; 1017.70. ν31; 1035.44. ν32; 1056.25. ν33; 1064.96. ν34; 1069.48. ν35; 1077.05. ν36; 1110.18. ν37; 1149.58. ν38; 1169.32. ν39; 1184.25. ν40; 1206.50. ν41; 1216.86. ν42; 1222.50. ν43; 1242.35. ν44; 1249.38. ν45; 1282.08. ν46; 1287.79. ν47; 1298.88. ν48; 1309.08. ν49; 1322.19. ν50; 1333.13. ν51; 1337.94. ν52; 1340.80. ν53; 1358.38. ν54; 1362.52. ν55; 1364.60. ν56; 1380.46. ν57; 1387.11. ν58; 1520.97. ν59; 1527.21. ν60; 1528.18. ν61; 1539.01. ν62; 1555.52. ν63; 1908.50. ν64; 3066.21. ν65; 3075.46. ν66; 3076.89. ν67; 3077.67. ν68; 3078.00. ν69; 3090.71. ν70; 3093.38. ν71; 3118.12. ν72; 3122.63. ν73; 3126.67. ν74; 3133.45. ν75; 3138.44. ν76; 3143.04. ν77; 3147.22. ν78; 3159.61. | 168.5055. 4.2171. 4.1266. 2.0527. 1.7476. 0.616. 0.5447. 0.3902. 0.2981. 0.0522. 0.1128. 0.6457. 5.1846. 0.1101. 0.5367. 1.742. 0.9736. 0.4746. 1.2946. 0.4167. 0.2821. 2.1405. 0.7131. 1.5409. 0.4008. 0.959. 0.5996. 2.8485. 5.4582. 2.3007. 2.3098. 2.7429. 1.2842. 0.271. 0.1609. 3.2893. 0.3025. 0.628. 0.981. 4.0002. 0.1832. 1.5948. 0.4329. 2.3393. 3.3128. 1.9528. 1.4666. 1.4284. 0.5659. 0.5739. 4.9806. 1.5645. 1.912. 0.5659. 2.0331. 2.4836. 0.8399. 4.5357. 7.4976. 3.2984. 7.5204. 15.9563. 142.6126. 24.6438. 24.4323. 10.1929. 18.9904. 20.9078. 41.3083. 8.4537. 33.4145. 18.409. 11.471. 34.2565. 26.3505. 17.7946. 52.2843. 28.4779. | -1519.46. 33.27. 41.88. 130.83. 165.00. 184.36. 187.12. 267.66. 273.96. 326.27. 339.31. 403.81. 495.37. 529.41. 556.32. 663.96. 742.45. 767.72. 816.95. 841.70. 877.99. 881.39. 905.78. 925.48. 938.06. 940.59. 969.50. 978.73. 1005.16. 1022.19. 1027.35. 1063.65. 1072.13. 1082.18. 1092.12. 1106.66. 1152.67. 1166.20. 1174.95. 1208.27. 1215.09. 1218.80. 1237.72. 1254.35. 1267.28. 1284.79. 1290.86. 1311.48. 1319.42. 1326.43. 1333.85. 1335.98. 1351.57. 1363.99. 1377.46. 1387.78. 1522.26. 1522.72. 1527.68. 1532.94. 1545.50. 1556.92. 1914.96. 3076.56. 3078.59. 3080.19. 3081.42. 3085.06. 3093.60. 3097.66. 3100.63. 3115.79. 3134.80. 3139.37. 3140.02. 3149.06. 3158.13. 3168.90. | 2.9098. 2.9417. 3.041. 0.8193. 2.9825. 1.0285. 2.9685. 0.1221. 0.5572. 0.2026. 0.0794. 0.1039. 0.6331. 0.446. 0.6983. 1.1427. 2.4972. 6.2292. 5.1316. 1.4082. 1.8481. 2.6286. 1.0488. 1.12. 0.5402. 1.6842. 6.3433. 1.973. 8.0328. 1.0068. 2.1113. 0.2253. 0.3864. 0.2487. 4.3581. 0.3755. 2.8121. 3.5013. 1.1628. 8.3286. 0.1445. 1.9036. 8.0875. 3.056. 0.7909. 1.375. 0.8809. 7.4323. 3.5538. 1.9677. 3.3962. 3.1496. 2.221. 0.172. 0.8924. 0.4789. 2.4123. 0.3228. 3.3689. 11.4094. 12.7036. 9.4423. 100.7352. 19.768. 27.845. 18.1342. 1.6148. 19.5862. 35.0389. 40.9224. 8.5607. 41.9722. 27.2253. 6.3554. 16.0135. 38.7967. 42.4141. 20.7908. |

|  | TS3 JP-10/BO |  | TS4 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -1633.90. ν2; 40.25. ν3; 43.92. ν4; 138.19. ν5; 158.07. ν6; 185.94. ν7; 206.77. ν8; 262.74. ν9; 285.00. ν10; 320.34. ν11; 327.63. ν12; 435.59. ν13; 534.78. ν14; 545.19. ν15; 599.55. ν16; 669.03. ν17; 739.03. ν18; 776.40. ν19; 811.30. ν20; 840.26. ν21; 880.94. ν22; 881.23. ν23; 906.53. ν24; 926.21. ν25; 942.13. ν26; 950.37. ν27; 963.71. ν28; 976.84. ν29; 1019.53. ν30; 1023.46. ν31; 1024.79. ν32; 1065.87. ν33; 1072.43. ν34; 1075.99. ν35; 1083.83. ν36; 1095.57. ν37; 1146.78. ν38; 1166.97. ν39; 1185.34. ν40; 1217.17. ν41; 1220.19. ν42; 1221.04. ν43; 1224.96. ν44; 1261.91. ν45; 1266.90. ν46; 1282.70. ν47; 1293.50. ν48; 1316.10. ν49; 1322.52. ν50; 1327.41. ν51; 1337.01. ν52; 1341.70. ν53; 1358.53. ν54; 1363.15. ν55; 1365.64. ν56; 1384.50. ν57; 1387.08. ν58; 1524.25. ν59; 1528.10. ν60; 1528.12. ν61; 1544.28. ν62; 1545.85. ν63; 1910.67. ν64; 3076.47. ν65; 3077.39. ν66; 3082.78. ν67; 3083.38. ν68; 3084.00. ν69; 3090.72. ν70; 3093.49. ν71; 3118.39. ν72; 3127.16. ν73; 3132.74. ν74; 3134.86. ν75; 3136.18. ν76; 3139.08. ν77; 3149.30. ν78; 3154.66. | 3.6622. 2.9962. 3.4046. 0.0004. 2.1508. 3.5711. 2.6338. 0.1365. 1.13. 0.0744. 0.018. 0.7685. 0.6381. 0.3383. 5.4477. 0.3644. 1.5049. 0.6683. 1.6339. 2.354. 0.8076. 1.0592. 0.3934. 0. 1.8831. 0.109. 0.4176. 0.4274. 0.1025. 2.6242. 2.6189. 4.3579. 0.0726. 0.4392. 0.4878. 0.8567. 1.8672. 1.1748. 12.7316. 0.0437. 0.7401. 4.5668. 1.5079. 0.4713. 0.1451. 1.6829. 0.0324. 0.1664. 0.0697. 2.2152. 0.4909. 2.833. 2.3769. 0.9666. 0.045. 2.838. 0.3327. 3.6314. 5.0402. 5.3741. 0.1761. 11.5092. 101.1099. 3.993. 28.7076. 23.6819. 13.6448. 27.2025. 10.4046. 75.1234. 11.6096. 45.176. 15.5608. 15.612. 4.2834. 22.1071. 46.0715. 53.6723. | -1260.83. 27.22. 32.44. 109.89. 147.59. 167.70. 194.12. 262.24. 291.47. 321.49. 340.83. 401.58. 499.06. 536.27. 556.20. 684.14. 753.40. 767.42. 816.16. 848.05. 878.19. 890.29. 911.21. 916.97. 933.69. 938.84. 950.05. 980.88. 985.90. 1022.87. 1044.79. 1061.90. 1074.48. 1081.65. 1102.86. 1113.30. 1151.23. 1165.93. 1186.98. 1205.56. 1213.15. 1233.55. 1242.37. 1264.89. 1271.58. 1279.82. 1290.26. 1292.21. 1322.34. 1328.55. 1332.04. 1339.48. 1360.16. 1362.33. 1367.80. 1379.67. 1513.14. 1523.12. 1527.76. 1532.84. 1543.58. 1556.48. 1905.36. 3058.74. 3059.40. 3077.52. 3080.76. 3085.99. 3087.42. 3095.58. 3116.33. 3120.94. 3129.14. 3136.30. 3138.13. 3147.82. 3152.42. 3155.07. | 83.202. 3.5843. 3.3641. 0.9275. 1.056. 0.4069. 1.5312. 0.1205. 1.5511. 0.039. 0.4303. 0.1506. 0.2289. 0.2371. 0.6342. 0.8315. 0.6877. 5.9237. 0.3454. 0.0678. 1.5768. 3.2153. 0.8917. 0.2967. 3.0381. 0.2882. 2.1595. 3.3916. 1.3306. 3.6213. 1.0582. 0.3201. 0.6189. 0.9545. 1.5222. 0.8139. 1.821. 0.7194. 1.6718. 9.8409. 1.3744. 3.8621. 0.0291. 1.1298. 0.9668. 0.2142. 1.8233. 0.3492. 0.2395. 0.4962. 2.8922. 5.9452. 1.4573. 1.0827. 1.3406. 0.7483. 6.4575. 2.4008. 2.2827. 12.4447. 15.6225. 4.8101. 132.7458. 16.0321. 13.4112. 16.419. 21.3382. 20.7994. 29.5822. 36.1959. 21.084. 46.6219. 16.0643. 1.1119. 28.5914. 15.3983. 35.297. 46.3146. |

|  | TS5 JP-10/BO |  | TS6 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -1471.12. ν2; 32.49. ν3; 38.74. ν4; 106.50. ν5; 143.67. ν6; 169.14. ν7; 190.54. ν8; 234.19. ν9; 292.03. ν10; 327.89. ν11; 398.72. ν12; 437.19. ν13; 504.33. ν14; 535.60. ν15; 598.72. ν16; 701.45. ν17; 755.66. ν18; 770.07. ν19; 814.91. ν20; 848.60. ν21; 874.80. ν22; 888.07. ν23; 918.98. ν24; 931.30. ν25; 942.00. ν26; 951.90. ν27; 966.27. ν28; 982.17. ν29; 986.92. ν30; 1025.61. ν31; 1028.19. ν32; 1064.53. ν33; 1072.10. ν34; 1075.45. ν35; 1094.87. ν36; 1115.15. ν37; 1150.50. ν38; 1160.80. ν39; 1181.71. ν40; 1202.69. ν41; 1218.55. ν42; 1221.02. ν43; 1242.76. ν44; 1257.00. ν45; 1270.73. ν46; 1292.46. ν47; 1297.81. ν48; 1312.62. ν49; 1322.85. ν50; 1329.80. ν51; 1333.59. ν52; 1338.87. ν53; 1341.93. ν54; 1350.67. ν55; 1362.81. ν56; 1381.13. ν57; 1389.39. ν58; 1522.58. ν59; 1526.57. ν60; 1530.39. ν61; 1541.60. ν62; 1556.43. ν63; 1911.02. ν64; 3061.03. ν65; 3069.99. ν66; 3080.34. ν67; 3082.92. ν68; 3088.54. ν69; 3089.59. ν70; 3092.34. ν71; 3115.20. ν72; 3120.50. ν73; 3127.85. ν74; 3133.10. ν75; 3138.57. ν76; 3147.74. ν77; 3152.17. ν78; 3152.70. | 100.942. 3.8424. 3.5258. 2.5144. 0.7238. 2.3885. 0.8349. 0.1508. 0.0402. 0.0902. 0.1502. 0.6801. 0.2605. 1.0319. 3.7465. 6.5642. 0.2918. 0.8768. 0.4749. 1.1562. 2.8571. 0.7659. 0.3918. 1.3306. 0.6435. 1.3903. 2.1792. 3.8294. 0.2321. 1.5665. 1.5894. 0.1258. 0.4753. 1.1218. 1.3885. 0.9585. 0.0802. 1.1004. 3.4361. 2.1681. 1.822. 1.2089. 0.7786. 1.3414. 0.0837. 1.3845. 0.5649. 1.2752. 1.4772. 1.4602. 1.1551. 3.2494. 2.5423. 2.3897. 1.8574. 1.9849. 0.5153. 2.0515. 2.0657. 10.8322. 15.2547. 4.9296. 137.2431. 8.6494. 18.6669. 17.143. 19.4697. 39.2683. 3.793. 54.7429. 61.7967. 5.3483. 19.3165. 0.3997. 21.5642. 4.88. 57.4395. 45.884. | -1384.87. 22.84. 35.65. 115.16. 115.92. 172.52. 181.13. 263.79. 320.20. 325.44. 408.37. 450.34. 497.04. 535.52. 618.52. 676.83. 750.05. 775.95. 810.25. 841.65. 876.62. 899.31. 916.90. 919.30. 940.83. 944.72. 952.38. 979.82. 986.45. 1026.56. 1027.46. 1066.16. 1069.13. 1075.78. 1094.14. 1095.56. 1151.35. 1164.57. 1183.50. 1219.10. 1230.32. 1232.51. 1242.03. 1268.93. 1270.57. 1291.64. 1301.20. 1310.49. 1323.65. 1326.57. 1333.55. 1334.87. 1349.62. 1352.24. 1368.45. 1385.13. 1386.92. 1511.40. 1517.44. 1526.48. 1539.00. 1556.82. 1909.21. 3053.11. 3054.64. 3078.80. 3082.69. 3087.80. 3091.51. 3092.49. 3114.71. 3120.20. 3122.04. 3122.85. 3132.90. 3143.18. 3147.31. 3152.34. | 105.4313. 3.4005. 3.7634. 3.407. 1.0033. 0.971. 0.8875. 0.0088. 0.4977. 0.153. 0.314. 2.0056. 1.2432. 0.2106. 3.1422. 0.4392. 0.2892. 0.833. 1.7571. 2.1557. 1.0643. 1.8768. 1.6066. 0.551. 0.7043. 0.5111. 1.5034. 2.1033. 0.369. 2.8935. 1.9148. 0.1377. 2.2543. 0.004. 1.043. 0.0089. 0.5364. 0.0057. 0.4492. 0.0134. 6.0972. 0.0049. 7.8002. 0.2836. 19.7531. 2.2444. 0.3653. 0.0513. 0.0722. 4.2874. 3.2241. 0.487. 2.9386. 1.9151. 6.1217. 1.1584. 0.5232. 11.0875. 1.1378. 1.7271. 20.9748. 5.4228. 128.45. 15.8746. 10.1655. 0.0865. 20.8039. 27.5572. 21.2279. 45.9977. 65.2964. 11.9794. 25.8958. 14.0512. 0.0257. 31.1123. 23.4208. 55.2308. |

|  | vdW2 Site 1 JP-10/BO |  | vdW2 Site 2 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 10.90. ν2; 19.15. ν3; 51.99. ν4; 78.71. ν5; 87.76. ν6; 153.12. ν7; 180.43. ν8; 284.39. ν9; 313.29. ν10; 330.22. ν11; 391.09. ν12; 491.75. ν13; 509.53. ν14; 551.78. ν15; 590.31. ν16; 668.39. ν17; 758.09. ν18; 780.41. ν19; 804.02. ν20; 811.65. ν21; 815.44. ν22; 880.13. ν23; 883.81. ν24; 914.68. ν25; 923.43. ν26; 930.49. ν27; 941.19. ν28; 955.75. ν29; 960.19. ν30; 982.75. ν31; 1008.82. ν32; 1023.73. ν33; 1037.42. ν34; 1057.37. ν35; 1064.76. ν36; 1075.71. ν37; 1096.46. ν38; 1142.85. ν39; 1164.64. ν40; 1170.69. ν41; 1202.04. ν42; 1216.16. ν43; 1230.38. ν44; 1254.85. ν45; 1272.34. ν46; 1286.46. ν47; 1293.04. ν48; 1306.59. ν49; 1318.21. ν50; 1332.03. ν51; 1342.00. ν52; 1351.87. ν53; 1358.10. ν54; 1362.85. ν55; 1376.92. ν56; 1385.27. ν57; 1511.27. ν58; 1525.37. ν59; 1528.11. ν60; 1537.25. ν61; 1553.99. ν62; 1811.96. ν63; 2892.37. ν64; 3034.60. ν65; 3074.96. ν66; 3076.53. ν67; 3077.08. ν68; 3078.04. ν69; 3093.02. ν70; 3095.80. ν71; 3097.15. ν72; 3118.55. ν73; 3122.87. ν74; 3131.74. ν75; 3137.07. ν76; 3145.93. ν77; 3160.52. ν78; 3219.66. | 1.7423. 1.9005. 0.6205. 13.2506. 15.0544. 0.1635. 0.2086. 1.0903. 2.7867. 0.0851. 1.8314. 2.3945. 19.2379. 0.3829. 13.492. 0.8488. 0.7355. 0.5943. 6.6028. 7.3764. 1.4534. 0.2778. 2.1453. 0.3006. 0.7171. 1.5998. 1.2304. 0.3167. 0.1889. 3.5599. 0.6915. 1.5915. 3.3402. 0.1764. 0.1442. 0.1466. 1.1931. 0.8794. 0.2243. 0.5909. 1.1471. 0.2419. 0.6329. 1.718. 1.6815. 1.519. 2.207. 0.6186. 0.4994. 1.464. 1.5703. 2.7494. 1.0579. 0.6981. 1.9478. 0.5716. 5.6874. 3.3013. 4.0104. 7.5938. 12.6563. 45.2736. 3.1071. 35.0407. 23.067. 33.3633. 20.0801. 1.0983. 6.9715. 41.8828. 28.8342. 56.3976. 13.1932. 32.0241. 27.6638. 54.7583. 27.7594. 21.0165. | 8.04. 14.96. 50.43. 74.23. 90.02. 136.43. 179.27. 263.80. 317.34. 331.39. 402.37. 494.73. 521.59. 555.72. 661.28. 730.91. 764.03. 801.64. 808.67. 817.57. 838.61. 856.15. 879.04. 899.89. 913.97. 935.57. 940.23. 957.42. 976.11. 995.82. 1022.63. 1026.67. 1062.74. 1072.34. 1079.50. 1107.24. 1126.73. 1158.92. 1181.44. 1212.56. 1214.37. 1226.06. 1236.38. 1251.97. 1275.65. 1283.91. 1302.20. 1317.32. 1321.80. 1327.30. 1333.72. 1348.05. 1363.91. 1376.41. 1389.48. 1521.05. 1523.07. 1528.17. 1532.81. 1545.03. 1556.62. 1810.69. 2889.92. 3076.07. 3077.65. 3080.36. 3081.34. 3084.74. 3095.16. 3097.71. 3102.53. 3113.67. 3133.24. 3138.54. 3139.58. 3148.27. 3159.39. 3171.33. | 0.5259. 1.9442. 0.2882. 14.3083. 15.7316. 0.1699. 0.0492. 0.1989. 0.4557. 0.0694. 0.0858. 0.7179. 0.6503. 0.5677. 1.4542. 0.171. 0.3294. 0.6994. 7.0748. 7.4708. 0.7136. 4.6048. 0.5096. 0.168. 0.4276. 0.1019. 1.9179. 2.0693. 1.5435. 0.4202. 0.79. 2.8781. 0.1963. 0.0481. 0.2286. 0.3734. 0.3864. 1.384. 0.7918. 0.2473. 0.7338. 5.2179. 1.9939. 3.5809. 0.6021. 1.4332. 2.7443. 1.6662. 1.2459. 2.1155. 2.438. 1.2017. 0.1464. 0.575. 0.7402. 2.3159. 0.4551. 4.5486. 11.4186. 12.0487. 9.0366. 46.8834. 3.5118. 21.2937. 31.1702. 10.7315. 15.4824. 26.3672. 28.2804. 48.8118. 20.2208. 36.6237. 25.8959. 22.7906. 6.2804. 43.6475. 44.4864. 24.1231. |

|  | vdW2 Site 3 JP-10/BO |  | vdW2 Site 4 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 12.46. ν2; 18.96. ν3; 44.03. ν4; 76.72. ν5; 82.09. ν6; 110.12. ν7; 184.13. ν8; 243.06. ν9; 316.94. ν10; 317.27. ν11; 369.47. ν12; 456.64. ν13; 531.40. ν14; 545.03. ν15; 666.72. ν16; 743.30. ν17; 745.80. ν18; 786.79. ν19; 796.51. ν20; 804.19. ν21; 809.16. ν22; 848.33. ν23; 875.77. ν24; 886.09. ν25; 905.47. ν26; 930.28. ν27; 943.94. ν28; 946.84. ν29; 973.71. ν30; 975.40. ν31; 1018.64. ν32; 1022.79. ν33; 1039.57. ν34; 1065.35. ν35; 1072.03. ν36; 1076.00. ν37; 1096.29. ν38; 1170.96. ν39; 1182.37. ν40; 1208.70. ν41; 1215.94. ν42; 1222.78. ν43; 1225.19. ν44; 1248.73. ν45; 1263.22. ν46; 1283.07. ν47; 1286.67. ν48; 1310.78. ν49; 1320.00. ν50; 1324.59. ν51; 1343.97. ν52; 1344.37. ν53; 1363.38. ν54; 1363.52. ν55; 1378.88. ν56; 1381.19. ν57; 1519.47. ν58; 1523.37. ν59; 1525.98. ν60; 1540.91. ν61; 1544.77. ν62; 1813.21. ν63; 2902.73. ν64; 3074.48. ν65; 3075.53. ν66; 3076.10. ν67; 3076.41. ν68; 3080.77. ν69; 3089.10. ν70; 3091.99. ν71; 3129.33. ν72; 3131.13. ν73; 3132.67. ν74; 3134.12. ν75; 3136.46. ν76; 3145.64. ν77; 3151.63. ν78; 3200.49. | 2.3083. 1.7465. 0.1734. 12.7347. 14.675. 0.4675. 0.4444. 0.0605. 0.0777. 0.4832. 4.138. 6.6157. 0.6856. 1.1894. 0.25. 17.5152. 1.1748. 2.9739. 7.197. 7.457. 0.8666. 2.2939. 0.9018. 1.3137. 0.6366. 0.0056. 2.3332. 0.2228. 0.4926. 2.4049. 2.2824. 1.4667. 0.127. 0.0561. 0.0343. 0.5087. 1.0037. 0.8238. 1.8269. 1.2738. 0.3039. 0.7326. 1.4818. 1.0625. 0.655. 2.2761. 0.0322. 0.0013. 0.0246. 0.4074. 2.2717. 0.012. 0.4937. 0.8201. 2.9471. 0.383. 4.6966. 1.3611. 7.6344. 2.1132. 7.7065. 40.7126. 0.3053. 30.0001. 25.1619. 22.7287. 0.9433. 30.1418. 17.7803. 69.4078. 34.8252. 22.0736. 0.8343. 24.2827. 24.514. 53.8831. 52.7262. 23.8061. | 13.16. 18.96. 55.11. 80.88. 86.79. 121.77. 167.67. 238.59. 299.65. 316.21. 390.17. 486.20. 540.56. 557.08. 630.57. 730.58. 752.91. 811.24. 812.26. 817.22. 838.03. 864.68. 895.48. 902.01. 914.90. 919.59. 933.89. 946.56. 981.54. 982.75. 1020.92. 1034.94. 1059.19. 1069.14. 1077.37. 1113.83. 1143.18. 1147.49. 1171.11. 1177.28. 1207.52. 1230.18. 1244.14. 1249.96. 1266.92. 1276.15. 1289.45. 1320.63. 1323.13. 1329.75. 1334.56. 1356.50. 1357.69. 1368.25. 1384.03. 1509.16. 1521.98. 1525.30. 1532.10. 1541.60. 1554.60. 1810.16. 2878.38. 3025.78. 3033.51. 3076.21. 3080.36. 3082.32. 3083.39. 3093.46. 3095.09. 3120.62. 3132.04. 3135.55. 3136.65. 3145.42. 3149.46. 3155.75. | 1.212. 1.4963. 1.2326. 12.6277. 11.6648. 1.2487. 0.3609. 0.3783. 0.5982. 0.1449. 0.032. 0.767. 0.236. 0.8934. 3.5491. 0.2398. 0.4215. 5.4244. 3.3856. 6.846. 1.7176. 0.7982. 1.9243. 0.8024. 0.6505. 0.4807. 0.25. 1.3287. 1.5038. 3.3917. 1.5263. 1.5789. 0.2001. 0.0621. 0.0947. 2.1617. 0.4684. 0.1157. 0.0653. 0.6736. 2.0357. 1.3928. 2.283. 0.6586. 0.13. 1.157. 1.1039. 0.3296. 0.2706. 2.0512. 4.7091. 1.4581. 0.4577. 0.8157. 0.7363. 6.9806. 0.9165. 2.1274. 9.5236. 14.1701. 4.4979. 51.4216. 5.7793. 24.5265. 26.3864. 12.5743. 17.4293. 34.7996. 22.4228. 53.7379. 37.116. 46.7307. 24.7458. 2.2268. 33.6631. 8.3852. 49.9838. 48.1098. |

|  | vdW5 Site 5 JP-10/BO |  | vdW2 Site 6 JP-10/BO |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 12.06. ν2; 16.32. ν3; 44.92. ν4; 61.45. ν5; 86.38. ν6; 122.36. ν7; 139.81. ν8; 257.10. ν9; 292.19. ν10; 316.52. ν11; 368.74. ν12; 402.28. ν13; 499.67. ν14; 535.15. ν15; 620.57. ν16; 745.07. ν17; 763.32. ν18; 769.57. ν19; 794.28. ν20; 799.48. ν21; 813.70. ν22; 846.48. ν23; 861.27. ν24; 888.43. ν25; 918.59. ν26; 935.75. ν27; 951.98. ν28; 954.61. ν29; 977.31. ν30; 986.30. ν31; 1004.63. ν32; 1029.56. ν33; 1045.30. ν34; 1064.91. ν35; 1072.10. ν36; 1091.15. ν37; 1098.21. ν38; 1136.85. ν39; 1154.38. ν40; 1177.44. ν41; 1204.93. ν42; 1226.89. ν43; 1236.53. ν44; 1252.41. ν45; 1264.27. ν46; 1291.76. ν47; 1297.70. ν48; 1310.96. ν49; 1317.00. ν50; 1330.89. ν51; 1332.83. ν52; 1338.53. ν53; 1345.83. ν54; 1365.11. ν55; 1377.85. ν56; 1388.29. ν57; 1511.12. ν58; 1525.37. ν59; 1527.13. ν60; 1543.39. ν61; 1555.13. ν62; 1814.64. ν63; 2906.44. ν64; 3001.15. ν65; 3009.54. ν66; 3080.47. ν67; 3084.89. ν68; 3086.99. ν69; 3089.52. ν70; 3090.17. ν71; 3108.50. ν72; 3115.43. ν73; 3123.42. ν74; 3130.27. ν75; 3143.40. ν76; 3149.57. ν77; 3152.37. ν78; 3223.87. | 2.8851. 2.9613. 5.3304. 8.4374. 12.052. 0.3061. 0.7437. 0.3972. 2.9512. 1.8189. 32.5124. 0.4808. 0.541. 0.1299. 0.7962. 0.3963. 2.6066. 0.2419. 7.8351. 7.3839. 0.7819. 0.6128. 0.7291. 1.7767. 0.5754. 0.237. 0.083. 1.538. 2.372. 0.5351. 2.3979. 1.7672. 0.2019. 0.1669. 0.0979. 0.1097. 0.8214. 0.0402. 0.2962. 1.0312. 0.3439. 4.4629. 0.4794. 0.5829. 0.12. 1.6305. 0.4752. 0.5947. 0.5844. 0.0795. 1.5882. 1.6737. 5.6809. 1.2468. 2.3669. 0.7429. 2.4593. 2.566. 5.3044. 16.0419. 4.1319. 40.6824. 0.8494. 42.4352. 40.5198. 21.2368. 10.9704. 33.5865. 19.6049. 52.4023. 26.706. 64.1346. 14.9669. 0.9723. 26.8063. 56.7951. 26.2656. 19.4333. | 20.48. 43.97. 65.21. 78.25. 132.79. 142.47. 155.27. 256.59. 290.63. 328.18. 403.33. 469.24. 504.94. 532.91. 696.55. 700.22. 746.77. 770.45. 777.48. 789.48. 810.75. 841.19. 862.72. 914.30. 920.66. 935.40. 951.15. 952.65. 973.26. 987.23. 991.72. 1038.87. 1054.19. 1066.69. 1075.14. 1086.50. 1099.97. 1150.02. 1162.60. 1169.10. 1206.94. 1219.51. 1233.07. 1255.49. 1267.84. 1288.13. 1297.47. 1313.36. 1323.70. 1328.95. 1334.74. 1335.45. 1364.31. 1369.90. 1379.71. 1390.95. 1505.67. 1512.39. 1525.20. 1535.33. 1555.00. 1803.89. 2912.17. 3002.83. 3004.89. 3073.93. 3079.64. 3083.14. 3089.23. 3090.96. 3101.89. 3111.69. 3116.32. 3122.29. 3130.35. 3143.48. 3150.03. 3210.44. | 11.9246. 0.6539. 5.2745. 0.4795. 0.5041. 7.5732. 33.2842. 0.0117. 0.4948. 0.019. 0.0396. 28.4758. 5.8117. 0.0527. 2.0634. 2.0929. 0.3362. 29.0286. 10.3227. 0.3215. 0.8614. 1.3818. 0.5729. 2.3861. 0.3921. 1.0768. 0.5175. 1.3993. 1.3255. 0.4643. 2.3896. 2.0464. 0.0856. 0.4797. 0.2623. 0.0085. 0.0886. 0.882. 0.0054. 1.2031. 0.4009. 0.1697. 2.8481. 2.9619. 0.1865. 1.3028. 0.2047. 0.1162. 0.1616. 0.092. 2.7386. 3.6333. 0.8069. 5.2374. 0.5773. 0.6731. 11.2548. 4.2738. 1.58. 17.7862. 5.0743. 22.2762. 3.2033. 23.1778. 22.9136. 10.4859. 17.2548. 21.9568. 52.4256. 44.4523. 9.9801. 71.4728. 20.9991. 11.8443. 0.137. 26.0725. 58.7599. 29.9922. |

|  | vdW1 Site 1 JP-10/BO2 |  | vdW1 Site 2 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 20.34. ν2; 25.81. ν3; 34.54. ν4; 40.03. ν5; 53.31. ν6; 135.16. ν7; 181.90. ν8; 265.84. ν9; 321.48. ν10; 333.14. ν11; 405.53. ν12; 445.13. ν13; 489.49. ν14; 495.33. ν15; 533.64. ν16; 556.15. ν17; 668.11. ν18; 751.80. ν19; 766.05. ν20; 811.05. ν21; 841.34. ν22; 881.71. ν23; 882.12. ν24; 913.00. ν25; 918.21. ν26; 939.30. ν27; 941.80. ν28; 952.12. ν29; 964.61. ν30; 982.50. ν31; 989.63. ν32; 1019.76. ν33; 1026.56. ν34; 1063.17. ν35; 1069.03. ν36; 1075.21. ν37; 1077.00. ν38; 1094.13. ν39; 1155.02. ν40; 1167.26. ν41; 1183.64. ν42; 1215.86. ν43; 1219.79. ν44; 1226.69. ν45; 1244.08. ν46; 1271.67. ν47; 1284.60. ν48; 1293.80. ν49; 1306.39. ν50; 1320.80. ν51; 1327.15. ν52; 1331.16. ν53; 1341.80. ν54; 1343.98. ν55; 1362.27. ν56; 1364.92. ν57; 1383.54. ν58; 1388.02. ν59; 1523.17. ν60; 1524.23. ν61; 1527.47. ν62; 1533.95. ν63; 1546.52. ν64; 1558.22. ν65; 2196.34. ν66; 3070.20. ν67; 3074.08. ν68; 3074.28. ν69; 3074.40. ν70; 3079.80. ν71; 3085.30. ν72; 3090.01. ν73; 3096.98. ν74; 3110.84. ν75; 3119.08. ν76; 3128.97. ν77; 3129.43. ν78; 3134.23. ν79; 3143.56. ν80; 3149.82. ν81; 3158.71. | 0.9436. 0.2536. 0.1153. 2.1405. 0.9517. 0.0658. 0.0045. 0.196. 0.1562. 0.0447. 0.095. 63.2813. 85.475. 0.703. 0.4134. 0.4819. 0.852. 0.3454. 0.605. 1.0631. 1.0934. 1.089. 1.3627. 0.0973. 0.6032. 0.0398. 1.2317. 1.4909. 0.0319. 3.5683. 0.4577. 2.1287. 1.6946. 0.0578. 0.2889. 0.1913. 0.0884. 0.6224. 0.3245. 0.0251. 1.3244. 0.2398. 0.0453. 1.8197. 2.6267. 0.0503. 1.3151. 0.9986. 0.0051. 0.2284. 0.6269. 1.299. 2.3669. 2.3484. 0.6019. 1.7016. 1.7043. 0.4773. 1.8977. 2.084. 2.9108. 9.4502. 12.8554. 4.9139. 562.7852. 9.5855. 22.4667. 17.5108. 28.958. 30.2366. 31.2378. 62.667. 20.1872. 72.7232. 11.7421. 3.5331. 35.132. 29.871. 44.4937. 68.6737. 27.4565. | 15.97. 30.02. 50.28. 61.26. 64.72. 132.15. 179.79. 261.80. 319.39. 331.76. 402.93. 431.83. 486.15. 492.38. 532.22. 556.73. 668.43. 751.66. 765.95. 810.35. 843.69. 881.24. 882.74. 913.67. 918.58. 939.46. 942.62. 957.93. 964.74. 980.72. 989.08. 1020.17. 1029.21. 1064.92. 1069.60. 1076.41. 1079.53. 1093.64. 1149.25. 1166.16. 1189.78. 1218.02. 1218.88. 1227.92. 1244.95. 1270.22. 1286.13. 1292.60. 1309.67. 1320.78. 1326.34. 1331.04. 1340.59. 1343.24. 1362.68. 1363.65. 1383.65. 1388.36. 1522.96. 1523.76. 1528.34. 1533.26. 1546.76. 1557.35. 2065.91. 3070.81. 3072.01. 3073.47. 3076.52. 3076.91. 3081.87. 3089.08. 3091.90. 3096.57. 3116.24. 3128.91. 3131.28. 3137.88. 3145.58. 3149.02. 3155.51. | 0.7548. 0.3814. 0.0495. 3.458. 0.4665. 0.024. 0.0001. 0.0083. 0.1815. 0.0622. 0.4082. 127.7401. 33.1337. 0.58. 0.2073. 0.5651. 1.108. 0.4325. 0.5976. 0.9188. 0.824. 1.7024. 1.1809. 0.1785. 0.4137. 0.0592. 1.4846. 1.5389. 0.3038. 2.8328. 1.0767. 2.6677. 1.2117. 0.0042. 0.1714. 0.0389. 0.0832. 0.4283. 0.3761. 0.0608. 2.221. 0.0396. 0.0333. 2.9171. 2.9157. 0.1194. 1.7269. 0.9689. 0.0534. 0.0524. 0.4692. 0.6854. 2.629. 3.4067. 0.8232. 2.3338. 1.9874. 0.2657. 0.6025. 2.2274. 2.6657. 10.9987. 14.206. 5.4252. 182.342. 0.7691. 32.7965. 17.4838. 19.1837. 20.2004. 75.2233. 47.1133. 42.4844. 52.6157. 30.579. 0.5242. 29.9857. 26.0005. 21.3804. 71.1596. 31.5835. |

|  | vdW1 Site 3 JP-10/BO2 |  | vdW1 Site 4 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 20.75. ν2; 32.04. ν3; 47.01. ν4; 59.87. ν5; 65.88. ν6; 134.27. ν7; 179.73. ν8; 262.52. ν9; 318.45. ν10; 332.85. ν11; 403.75. ν12; 427.00. ν13; 484.41. ν14; 496.25. ν15; 533.68. ν16; 557.21. ν17; 668.88. ν18; 751.16. ν19; 766.89. ν20; 812.09. ν21; 843.23. ν22; 881.41. ν23; 883.08. ν24; 914.74. ν25; 919.61. ν26; 939.53. ν27; 942.34. ν28; 949.76. ν29; 964.02. ν30; 984.38. ν31; 988.44. ν32; 1021.19. ν33; 1028.53. ν34; 1067.82. ν35; 1069.93. ν36; 1076.54. ν37; 1078.35. ν38; 1094.60. ν39; 1154.91. ν40; 1169.12. ν41; 1186.24. ν42; 1216.32. ν43; 1219.99. ν44; 1227.41. ν45; 1244.59. ν46; 1268.44. ν47; 1285.76. ν48; 1291.65. ν49; 1307.55. ν50; 1320.45. ν51; 1326.66. ν52; 1332.30. ν53; 1339.66. ν54; 1346.33. ν55; 1362.86. ν56; 1364.65. ν57; 1384.20. ν58; 1387.61. ν59; 1523.81. ν60; 1525.47. ν61; 1529.94. ν62; 1533.96. ν63; 1548.12. ν64; 1559.89. ν65; 2041.91. ν66; 3070.95. ν67; 3072.76. ν68; 3075.01. ν69; 3075.37. ν70; 3079.76. ν71; 3080.88. ν72; 3087.34. ν73; 3088.86. ν74; 3102.45. ν75; 3117.25. ν76; 3130.58. ν77; 3131.35. ν78; 3135.89. ν79; 3144.13. ν80; 3150.11. ν81; 3150.37. | 0.9219. 0.3783. 0.4521. 2.7667. 0.491. 0.014. 0.0352. 0.079. 0.1115. 0.2036. 0.2404. 131.9233. 34.0021. 0.951. 0.3977. 0.5167. 0.9533. 0.2907. 0.8621. 1.3837. 0.8264. 1.0391. 1.6915. 0.1387. 0.4796. 0.2061. 1.0807. 2.6601. 0.5064. 2.2775. 1.5579. 2.4364. 1.3895. 0.017. 0.1903. 0.1044. 0.0997. 0.4939. 0.6665. 0.044. 1.5116. 0.2817. 0.5929. 2.6813. 1.86. 0.051. 1.3419. 1.7949. 0.0383. 0.2725. 0.621. 1.6759. 4.2663. 1.3667. 0.6915. 1.1055. 1.0007. 0.2709. 0.864. 2.7656. 3.2396. 8.6776. 14.8715. 7.1918. 139.756. 9.6552. 7.671. 19.1269. 40.3906. 24.7243. 5.0037. 35.3116. 68.4693. 82.0789. 25.6752. 0.2555. 31.6708. 29.0988. 20.2967. 73.0009. 22.3482. | 9.61. 31.62. 43.81. 52.00. 62.73. 127.55. 186.99. 263.35. 319.87. 331.21. 404.23. 429.06. 482.47. 492.61. 533.05. 557.12. 669.63. 754.07. 765.06. 809.07. 840.44. 882.11. 882.76. 913.39. 918.69. 940.72. 941.99. 952.20. 963.32. 980.11. 986.37. 1021.86. 1023.06. 1064.29. 1067.23. 1075.71. 1078.36. 1095.17. 1149.99. 1168.42. 1184.56. 1216.58. 1221.00. 1228.01. 1244.05. 1269.67. 1282.17. 1292.31. 1306.89. 1316.42. 1323.32. 1331.67. 1341.28. 1341.73. 1365.29. 1369.37. 1373.25. 1377.75. 1523.90. 1525.45. 1526.72. 1536.47. 1547.37. 1557.89. 2069.23. 3034.34. 3073.75. 3074.34. 3079.71. 3080.75. 3085.66. 3089.34. 3089.64. 3114.40. 3119.83. 3130.39. 3131.80. 3136.00. 3147.95. 3149.89. 3154.08. | 1.1432. 0.0745. 0.01. 1.3046. 2.1252. 0.0073. 0.4162. 0.1054. 0.0639. 0.0048. 0.2542. 124.0241. 35.1324. 0.4981. 0.3263. 0.513. 0.7824. 0.2707. 0.837. 1.1988. 0.887. 1.835. 0.9389. 0.17. 0.5518. 1.1034. 0.0721. 1.0666. 0.353. 3.0123. 0.4545. 2.1949. 1.5685. 0.0153. 0.1364. 0.4149. 0.148. 0.7105. 0.3521. 0.0639. 1.6216. 0.404. 0.0733. 3.0626. 1.2218. 0.1423. 1.0875. 1.4734. 0.0887. 0.1326. 0.3379. 0.7194. 4.1862. 1.7961. 0.6058. 0.3915. 2.0629. 1.406. 0.244. 5.7573. 1.0896. 9.6943. 17.9668. 6.4064. 193.6789. 71.4523. 21.8116. 11.6274. 34.1822. 46.5685. 27.1662. 36.3946. 42.7428. 71.6393. 8.5764. 0.6074. 32.7056. 25.4265. 2.8309. 87.2264. 39.1543. |

|  | vdW1 Site 5 JP-10/BO2 |  | vdW1 Site 6 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 28.53. ν2; 33.30. ν3; 45.43. ν4; 51.26. ν5; 63.05. ν6; 68.07. ν7; 225.10. ν8; 260.17. ν9; 265.39. ν10; 326.59. ν11; 408.17. ν12; 433.03. ν13; 484.65. ν14; 488.11. ν15; 493.96. ν16; 630.31. ν17; 722.74. ν18; 752.76. ν19; 793.66. ν20; 815.55. ν21; 817.40. ν22; 853.01. ν23; 858.05. ν24; 908.37. ν25; 915.43. ν26; 930.87. ν27; 946.03. ν28; 955.10. ν29; 964.39. ν30; 973.15. ν31; 985.22. ν32; 1012.62. ν33; 1016.89. ν34; 1051.25. ν35; 1064.63. ν36; 1093.11. ν37; 1107.69. ν38; 1121.12. ν39; 1134.09. ν40; 1155.57. ν41; 1168.44. ν42; 1216.22. ν43; 1221.25. ν44; 1228.54. ν45; 1242.23. ν46; 1270.20. ν47; 1293.20. ν48; 1303.61. ν49; 1310.27. ν50; 1312.73. ν51; 1327.95. ν52; 1331.89. ν53; 1342.38. ν54; 1350.20. ν55; 1354.93. ν56; 1371.25. ν57; 1382.84. ν58; 1392.39. ν59; 1519.20. ν60; 1524.27. ν61; 1529.14. ν62; 1533.71. ν63; 1552.56. ν64; 1566.65. ν65; 2078.03. ν66; 3033.27. ν67; 3073.51. ν68; 3074.28. ν69; 3078.77. ν70; 3089.88. ν71; 3090.47. ν72; 3098.22. ν73; 3103.54. ν74; 3113.79. ν75; 3119.57. ν76; 3123.08. ν77; 3127.87. ν78; 3129.03. ν79; 3150.51. ν80; 3153.64. ν81; 3183.04. | 1.0958. 0.4644. 0.208. 0.936. 1.407. 1.0311. 0.052. 0.1567. 0.1535. 0.1457. 0.2338. 127.2996. 1.335. 37.1899. 0.1551. 0.7425. 0.0601. 0.2587. 1.1491. 0.3097. 0.6498. 1.4504. 1.5324. 2.3451. 0.6345. 0.2049. 0.6611. 1.0999. 0.1458. 3.5959. 0.3729. 0.8548. 1.986. 0.4794. 0.22. 0.8416. 0.6968. 0.15. 0.2608. 0.2553. 0.7361. 1.8523. 2.2181. 0.7912. 0.4178. 0.4428. 0.6644. 0.0728. 0.4857. 0.708. 1.6773. 1.2402. 0.0233. 3.7335. 0.4854. 5.4997. 0.0802. 0.1539. 7.6039. 0.3686. 3.4855. 6.5998. 14.5963. 9.1657. 198.9796. 81.8614. 26.7473. 27.2619. 56.0982. 24.2537. 44.6014. 41.6082. 9.0607. 67.2654. 8.8337. 16.2387. 18.8486. 14.6061. 19.488. 88.903. 21.8969. | 20.83. 34.81. 42.08. 45.05. 69.76. 135.21. 191.92. 261.35. 319.34. 334.50. 405.10. 443.53. 487.66. 496.42. 532.96. 555.32. 669.04. 752.82. 766.75. 811.58. 843.39. 881.96. 883.19. 915.48. 918.53. 938.36. 940.65. 951.90. 965.52. 983.52. 985.88. 1016.96. 1028.92. 1066.13. 1068.83. 1075.04. 1076.19. 1096.51. 1155.59. 1170.15. 1184.11. 1212.97. 1221.92. 1227.54. 1245.27. 1270.73. 1287.05. 1294.86. 1307.83. 1319.38. 1327.19. 1335.14. 1342.88. 1346.58. 1363.35. 1365.69. 1384.88. 1388.87. 1524.80. 1525.26. 1527.61. 1536.06. 1547.60. 1561.56. 2164.86. 3069.73. 3071.10. 3077.88. 3081.27. 3081.62. 3084.65. 3087.76. 3089.50. 3110.84. 3116.59. 3123.01. 3127.62. 3138.43. 3144.31. 3147.61. 3162.23. | 0.8052. 1.555. 0.5998. 0.1373. 1.3065. 0.0014. 0.1202. 0.0627. 0.085. 0.3934. 0.0066. 60.0162. 78.3564. 0.8031. 0.1993. 0.4621. 0.854. 0.3453. 0.4933. 0.8921. 0.9864. 0.7472. 2.3177. 0.1763. 0.908. 0.0062. 1.5308. 1.2808. 0.0175. 2.1468. 0.5098. 2.7075. 1.3904. 0.0293. 0.2018. 0.0263. 0.0614. 0.8308. 0.2016. 0.0436. 1.3152. 0.3971. 0.0697. 2.5199. 1.0985. 0.0969. 2.4318. 0.8647. 0.0042. 0.1818. 0.3867. 0.256. 6.2826. 0.0783. 0.5669. 2.2094. 3.1248. 0.2703. 0.9225. 3.2556. 1.6554. 10.2764. 10.4087. 6.8159. 517.1047. 3.2967. 37.9625. 22.8263. 40.5674. 11.4192. 33.6558. 71.5806. 10.2259. 82.5749. 10.8463. 31.4826. 0.3539. 23.0962. 32.824. 84.4018. 13.3377. |

|  | TS1 JP-10/BO2 |  | TS2 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -353.57. ν2; 13.52. ν3; 37.21. ν4; 57.56. ν5; 101.49. ν6; 141.47. ν7; 177.86. ν8; 265.60. ν9; 323.07. ν10; 335.92. ν11; 395.28. ν12; 487.80. ν13; 494.64. ν14; 499.41. ν15; 535.55. ν16; 556.27. ν17; 668.26. ν18; 751.39. ν19; 760.19. ν20; 804.47. ν21; 826.23. ν22; 881.52. ν23; 882.84. ν24; 913.99. ν25; 922.82. ν26; 934.28. ν27; 941.66. ν28; 952.47. ν29; 977.64. ν30; 984.09. ν31; 988.96. ν32; 1016.90. ν33; 1027.45. ν34; 1051.76. ν35; 1064.48. ν36; 1066.93. ν37; 1077.36. ν38; 1091.87. ν39; 1147.44. ν40; 1169.38. ν41; 1170.44. ν42; 1203.59. ν43; 1215.89. ν44; 1216.91. ν45; 1239.72. ν46; 1252.77. ν47; 1282.70. ν48; 1288.15. ν49; 1299.20. ν50; 1310.22. ν51; 1324.91. ν52; 1330.61. ν53; 1337.94. ν54; 1340.30. ν55; 1361.62. ν56; 1362.94. ν57; 1380.80. ν58; 1384.76. ν59; 1418.79. ν60; 1524.08. ν61; 1527.75. ν62; 1532.05. ν63; 1540.92. ν64; 1555.42. ν65; 1911.37. ν66; 2140.48. ν67; 3074.57. ν68; 3076.56. ν69; 3076.96. ν70; 3077.43. ν71; 3083.61. ν72; 3089.63. ν73; 3095.07. ν74; 3121.74. ν75; 3122.90. ν76; 3129.19. ν77; 3133.10. ν78; 3138.03. ν79; 3140.95. ν80; 3146.87. ν81; 3159.50. | 714.269. 1.0207. 0. 0.8058. 3.0469. 0.5212. 0.75. 10.4215. 7.6397. 0.2924. 7.4443. 20.9243. 22.6648. 28.8995. 2.2899. 1.8574. 2.2303. 0.6726. 14.2664. 24.5623. 27.5526. 0.8154. 2.5587. 0.2618. 4.666. 0.4549. 0.4547. 3.6548. 4.4193. 20.6829. 11.0702. 1.9514. 3.3068. 23.1099. 0.8541. 9.2612. 0.2073. 17.2044. 4.9641. 0.0376. 5.2325. 6.6443. 28.5209. 8.8248. 1.2848. 8.0154. 13.7213. 2.1518. 13.9827. 9.2674. 0.5909. 11.2958. 8.6617. 45.318. 0.7148. 2.4903. 18.5303. 17.3225. 149.2531. 0.6195. 5.1645. 13.1338. 4.9099. 14.4521. 2734.1216. 3502.3698. 19.5082. 11.8509. 15.0436. 29.0116. 10.5153. 42.2216. 14.0073. 20.4028. 35.7665. 9.5282. 31.921. 27.3972. 19.5693. 55.5337. 30.0649. | -431.02. 20.52. 45.02. 60.90. 114.35. 139.18. 180.09. 264.12. 319.95. 331.80. 402.58. 459.76. 491.38. 498.69. 527.87. 557.25. 665.98. 743.54. 761.74. 805.93. 840.64. 872.64. 880.85. 906.47. 912.93. 921.88. 939.69. 943.72. 967.61. 975.70. 992.82. 1008.33. 1022.92. 1037.63. 1061.72. 1071.53. 1074.15. 1088.11. 1125.53. 1131.12. 1173.02. 1208.78. 1214.31. 1217.71. 1235.78. 1259.16. 1271.10. 1284.94. 1297.56. 1313.22. 1321.44. 1327.45. 1330.84. 1336.59. 1352.69. 1364.25. 1380.07. 1388.39. 1522.50. 1524.55. 1528.69. 1533.01. 1546.57. 1555.41. 1825.19. 2036.45. 3075.66. 3076.34. 3079.87. 3083.92. 3087.74. 3097.55. 3102.75. 3104.33. 3119.24. 3134.71. 3140.78. 3141.55. 3150.23. 3160.18. 3171.91. | 1140.5985. 1.0231. 0.0167. 0.4577. 2.7941. 0.7622. 0.2268. 0.3117. 2.1071. 0.0653. 0.0366. 1.2351. 0.9338. 34.9528. 1.5856. 0.6991. 1.1949. 16.8205. 48.2176. 78.4909. 42.7678. 135.4473. 12.7064. 189.1266. 34.4594. 384.0394. 13.1949. 24.6921. 24.5471. 9.4493. 0.7745. 58.3312. 6.9488. 15.1515. 14.4307. 8.1175. 4.0294. 0.5302. 2.7254. 42.4255. 11.1223. 5.2765. 5.9926. 0.5286. 5.9751. 4.945. 25.5491. 2.2464. 14.1615. 0.3465. 10.3123. 0.7616. 3.5531. 4.3799. 12.6513. 0.1106. 2.1113. 2.3199. 7.6343. 6.6636. 1.1822. 12.9986. 25.6779. 44.7476. 4518.8553. 1070.0888. 23.9627. 10.0893. 32.1671. 5.6226. 25.2329. 33.378. 26.8312. 9.4098. 40.0308. 27.8202. 3.3096. 20.0422. 34.15. 36.2589. 21.8838. |

|  | TS3 JP-10/BO2 |  | TS4 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -598.46. ν2; 4.01. ν3; 52.96. ν4; 68.94. ν5; 98.45. ν6; 138.10. ν7; 191.05. ν8; 262.25. ν9; 318.14. ν10; 333.97. ν11; 404.89. ν12; 440.47. ν13; 501.87. ν14; 532.02. ν15; 548.69. ν16; 575.59. ν17; 666.40. ν18; 741.35. ν19; 761.59. ν20; 808.09. ν21; 839.88. ν22; 868.79. ν23; 874.08. ν24; 894.98. ν25; 911.52. ν26; 922.47. ν27; 939.62. ν28; 943.93. ν29; 969.72. ν30; 977.80. ν31; 998.52. ν32; 1006.33. ν33; 1028.24. ν34; 1034.68. ν35; 1069.81. ν36; 1073.48. ν37; 1076.76. ν38; 1095.77. ν39; 1098.61. ν40; 1156.66. ν41; 1167.01. ν42; 1190.08. ν43; 1215.72. ν44; 1218.72. ν45; 1226.88. ν46; 1236.48. ν47; 1252.44. ν48; 1268.99. ν49; 1287.02. ν50; 1297.72. ν51; 1315.10. ν52; 1321.78. ν53; 1328.57. ν54; 1341.00. ν55; 1349.92. ν56; 1364.53. ν57; 1365.83. ν58; 1386.79. ν59; 1388.18. ν60; 1524.53. ν61; 1528.44. ν62; 1531.70. ν63; 1546.28. ν64; 1547.85. ν65; 1823.62. ν66; 2018.89. ν67; 3076.18. ν68; 3077.78. ν69; 3086.06. ν70; 3088.72. ν71; 3089.28. ν72; 3092.56. ν73; 3095.39. ν74; 3120.46. ν75; 3128.69. ν76; 3133.17. ν77; 3136.48. ν78; 3138.49. ν79; 3144.82. ν80; 3153.08. ν81; 3157.07. | 2613.3736. 1.2498. 0.7753. 0.0217. 2.3663. 0.0243. 1.9696. 0.2443. 0.0022. 1.4222. 21.3434. 9.975. 32.6751. 0.3529. 2.5257. 1.3343. 1.223. 0.9027. 237.1344. 18.2843. 44.9816. 516.3801. 3.849. 292.656. 0.7225. 244.1108. 0.4702. 17.1511. 106.8948. 0.5366. 19.2268. 3.1212. 0.9917. 0.7055. 38.0198. 39.6218. 0.0539. 1.7459. 0.4759. 1071.0841. 0.1975. 140.5386. 0.0202. 0.2615. 17.4865. 4.1513. 3.9375. 1.0826. 3.6561. 0.1574. 0.7452. 0.232. 0.1488. 3.8714. 12.3793. 0.4329. 1.4309. 11.971. 0.3474. 3.061. 2.3005. 4.1626. 7.5393. 5.4064. 3726.754. 269.7729. 33.1783. 2.8305. 19.9062. 38.6451. 14.6822. 14.9971. 63.465. 5.2163. 48.4081. 7.6666. 19.7368. 1.4014. 17.7647. 37.8228. 48.3825. | -1193.49. 48.67. 90.94. 115.25. 139.35. 164.13. 185.94. 273.70. 300.23. 319.31. 330.97. 399.66. 485.01. 537.73. 544.70. 552.79. 635.46. 659.91. 728.81. 756.08. 806.91. 842.27. 867.92. 895.29. 899.99. 911.88. 919.42. 935.15. 950.18. 976.79. 987.83. 1022.56. 1032.87. 1053.47. 1061.16. 1077.34. 1079.71. 1101.72. 1123.29. 1149.31. 1152.27. 1164.40. 1180.30. 1208.67. 1223.32. 1235.49. 1245.58. 1266.92. 1273.24. 1286.70. 1296.67. 1324.29. 1327.09. 1330.25. 1341.93. 1361.02. 1364.33. 1367.29. 1373.41. 1493.64. 1523.01. 1533.06. 1534.29. 1542.65. 1559.52. 1905.65. 3049.70. 3064.83. 3081.29. 3093.70. 3096.15. 3096.82. 3107.40. 3133.35. 3141.79. 3145.98. 3152.97. 3156.77. 3159.07. 3163.25. 3177.76. | 7068.8658. 1.9946. 0.8584. 0.747. 0.7877. 0.7787. 0.1585. 3.638. 172.7633. 0.2176. 0.7069. 3.4039. 13.8318. 0.8758. 21.217. 7.5925. 46.8972. 473.203. 18.1062. 6.6702. 4.8924. 4.4096. 22.8953. 19.1843. 9.4882. 7.8363. 1.7442. 0.8504. 4.9465. 6.5681. 2.6951. 16.6795. 34.4613. 8.1773. 14.9356. 4.5156. 11.4647. 3.2329. 50.2939. 34.1829. 49.2051. 18.9625. 117.3081. 0.9236. 80.2033. 40.8791. 3.2944. 4.1175. 0.9694. 5.2659. 3.1309. 6.942. 0.1646. 24.2915. 7.7687. 6.3394. 3.0567. 2.3826. 1.4958. 11.5595. 2.1074. 10.9166. 6.7091. 11.9074. 6.443. 1013.4951. 5.2. 4.0082. 16.3308. 30.8617. 18.9003. 14.478. 31.0499. 29.2331. 7.0105. 25.0211. 23.9547. 6.2124. 3.3032. 16.746. 11.0528. |

|  | TS5 JP-10/BO2 |  | TS6 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; -466.92. ν2; 19.95. ν3; 46.34. ν4; 63.44. ν5; 74.32. ν6; 122.41. ν7; 216.83. ν8; 249.79. ν9; 261.40. ν10; 313.76. ν11; 403.29. ν12; 467.26. ν13; 493.44. ν14; 497.09. ν15; 513.69. ν16; 624.93. ν17; 721.62. ν18; 753.43. ν19; 776.82. ν20; 807.97. ν21; 819.91. ν22; 844.43. ν23; 855.77. ν24; 899.47. ν25; 917.51. ν26; 930.68. ν27; 936.92. ν28; 955.77. ν29; 972.01. ν30; 984.02. ν31; 988.22. ν32; 1010.27. ν33; 1018.26. ν34; 1049.86. ν35; 1065.13. ν36; 1086.77. ν37; 1092.25. ν38; 1113.28. ν39; 1129.17. ν40; 1151.28. ν41; 1167.08. ν42; 1210.45. ν43; 1214.47. ν44; 1222.64. ν45; 1235.15. ν46; 1254.51. ν47; 1268.28. ν48; 1292.10. ν49; 1304.70. ν50; 1307.50. ν51; 1327.15. ν52; 1329.40. ν53; 1332.43. ν54; 1342.46. ν55; 1344.37. ν56; 1370.03. ν57; 1388.54. ν58; 1392.49. ν59; 1431.96. ν60; 1521.26. ν61; 1526.71. ν62; 1530.14. ν63; 1546.71. ν64; 1561.55. ν65; 1915.76. ν66; 2137.98. ν67; 3079.67. ν68; 3082.56. ν69; 3088.61. ν70; 3091.15. ν71; 3091.88. ν72; 3098.07. ν73; 3107.30. ν74; 3112.57. ν75; 3115.72. ν76; 3121.11. ν77; 3130.84. ν78; 3134.53. ν79; 3150.78. ν80; 3153.49. ν81; 3176.90. | 929.7386. 0.6479. 0.2416. 1.1027. 0.3607. 1.1518. 4.7075. 0.1696. 4.7222. 3.0366. 0.9551. 12.0459. 9.2232. 37.1421. 44.7684. 14.0362. 15.6516. 0.3004. 48.0554. 8.2922. 4.0948. 9.2077. 1.4974. 26.7708. 0.6384. 6.9754. 10.236. 1.3781. 3.5037. 3.3598. 6.8578. 3.4649. 3.8354. 4.482. 12.9456. 46.0536. 3.6014. 0.4101. 0.0504. 3.4359. 11.2787. 71.951. 6.6378. 4.2143. 10.3687. 6.5392. 9.0582. 3.7722. 3.6122. 4.0491. 5.1019. 1.893. 3.2515. 0.433. 40.3078. 2.8216. 1.3038. 0.4309. 9.1013. 3.6064. 2.3065. 18.4365. 25.325. 6.8702. 1683.2422. 2740.6255. 22.4465. 13.7615. 14.0221. 12.3689. 50.7095. 22.485. 10.7894. 5.9518. 91.5297. 9.4178. 13.6385. 0.1945. 18.928. 65.1627. 19.9361. | -2114.01. 49.41. 67.38. 103.87. 126.60. 187.41. 224.29. 254.75. 295.66. 326.42. 346.57. 409.52. 491.85. 504.68. 535.81. 595.37. 704.92. 718.20. 737.11. 774.38. 813.94. 824.50. 846.51. 863.85. 907.94. 919.39. 923.40. 949.93. 955.90. 969.27. 988.25. 1004.89. 1014.58. 1041.68. 1064.74. 1067.76. 1077.21. 1093.46. 1110.57. 1142.35. 1160.31. 1172.27. 1214.85. 1226.67. 1237.70. 1242.96. 1263.57. 1272.92. 1288.36. 1298.52. 1310.19. 1318.80. 1326.92. 1328.90. 1338.98. 1344.10. 1354.01. 1373.36. 1384.39. 1394.83. 1486.53. 1497.01. 1527.36. 1541.14. 1562.60. 1919.70. 3037.01. 3055.15. 3083.31. 3090.15. 3092.71. 3101.47. 3103.45. 3110.69. 3117.06. 3118.53. 3133.85. 3140.59. 3150.09. 3152.94. 3187.62. | 15943.5411. 2.393. 0.7971. 1.9112. 0.6714. 3.6182. 5.8467. 2.3392. 5.8954. 0.2172. 66.6118. 0.8072. 0.5514. 0.4628. 40.2445. 181.2974. 8.2044. 5.2556. 5.4287. 0.2441. 0.2624. 2.9318. 7.974. 4.9861. 1.1967. 2.0103. 41.4041. 0.5785. 0.4046. 4.2155. 0.712. 16.9006. 6.7097. 28.0866. 14.1209. 2.2345. 15.2452. 0.5111. 0.5047. 2.6469. 5.5145. 1.7413. 72.7411. 1.4417. 27.8998. 21.7862. 75.269. 10.7697. 13.7352. 6.0486. 4.3417. 6.2081. 0.3671. 12.801. 4.0004. 1.8739. 7.6422. 6.7937. 1.7097. 0.2975. 31.3514. 6.8118. 2.483. 12.1193. 2.9288. 569.444. 10.1661. 14.1249. 19.8876. 8.6556. 46.1508. 18.6811. 25.9844. 6.4079. 34.1603. 9.7158. 1.5096. 5.2697. 16.3727. 41.8261. 14.0649. |

|  | vdW2 Site 1 JP-10/BO2 |  | vdW2 Site 2 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 20.50. ν2; 26.79. ν3; 62.53. ν4; 64.30. ν5; 128.71. ν6; 160.09. ν7; 188.05. ν8; 293.91. ν9; 326.48. ν10; 332.29. ν11; 399.24. ν12; 489.66. ν13; 492.79. ν14; 510.17. ν15; 521.43. ν16; 552.90. ν17; 568.22. ν18; 668.56. ν19; 686.36. ν20; 758.95. ν21; 782.39. ν22; 816.86. ν23; 880.12. ν24; 882.01. ν25; 914.76. ν26; 922.32. ν27; 930.86. ν28; 940.96. ν29; 955.25. ν30; 961.71. ν31; 982.71. ν32; 1010.26. ν33; 1023.27. ν34; 1026.41. ν35; 1035.60. ν36; 1053.98. ν37; 1065.03. ν38; 1073.72. ν39; 1079.25. ν40; 1102.99. ν41; 1150.04. ν42; 1167.80. ν43; 1174.16. ν44; 1203.29. ν45; 1217.16. ν46; 1231.05. ν47; 1254.60. ν48; 1276.54. ν49; 1289.57. ν50; 1295.90. ν51; 1306.83. ν52; 1319.05. ν53; 1333.27. ν54; 1343.28. ν55; 1348.99. ν56; 1359.27. ν57; 1363.48. ν58; 1377.43. ν59; 1386.00. ν60; 1509.03. ν61; 1526.34. ν62; 1528.38. ν63; 1539.14. ν64; 1557.19. ν65; 2062.07. ν66; 3038.20. ν67; 3076.77. ν68; 3078.35. ν69; 3079.32. ν70; 3081.21. ν71; 3095.36. ν72; 3103.91. ν73; 3104.99. ν74; 3123.06. ν75; 3127.57. ν76; 3134.54. ν77; 3140.37. ν78; 3149.16. ν79; 3168.35. ν80; 3198.84. ν81; 3522.17. | 2.3706. 1.4865. 0.2913. 1.848. 4.3932. 2.8505. 2.2894. 2.442. 3.6955. 0.8125. 0.3028. 27.9685. 17.8878. 81.2635. 3.2436. 7.4453. 41.6398. 1.2331. 72.7748. 3.5682. 1.8365. 1.7802. 0.2213. 4.6889. 0.6505. 0.9635. 1.3691. 0.9506. 0.204. 0.2359. 4.6985. 0.4433. 22.8335. 1.8728. 0.7364. 7.1745. 1.1539. 46.435. 32.7842. 8.6332. 3.0302. 0.3431. 0.8513. 0.9288. 0.2388. 0.5322. 2.3723. 2.3164. 1.1751. 2.8415. 0.9057. 0.5421. 1.5956. 1.3732. 3.9895. 0.8176. 0.6481. 2.302. 0.8747. 7.8306. 4.0125. 4.3549. 6.8561. 14.2639. 333.1714. 22.1868. 22.2034. 31.7121. 8.7818. 12.287. 25.6074. 1.9017. 32.0258. 29.5525. 14.5785. 29.6036. 25.0509. 48.6414. 19.783. 18.0309. 939.8796. | 7.74. 21.55. 53.37. 63.36. 133.04. 139.54. 178.87. 263.65. 317.11. 331.72. 401.57. 478.59. 486.27. 499.09. 516.56. 521.08. 557.16. 660.84. 725.87. 765.21. 800.88. 839.57. 859.24. 879.23. 900.44. 914.27. 936.33. 942.21. 961.23. 976.14. 997.50. 1022.91. 1024.86. 1028.12. 1063.30. 1072.48. 1077.92. 1082.68. 1108.96. 1126.93. 1159.16. 1183.56. 1214.21. 1216.39. 1226.96. 1237.46. 1252.87. 1276.41. 1285.81. 1303.58. 1317.26. 1322.18. 1328.52. 1335.78. 1350.10. 1365.56. 1376.46. 1390.03. 1520.56. 1523.12. 1530.70. 1532.85. 1545.65. 1557.28. 2058.76. 3076.74. 3080.17. 3082.27. 3086.06. 3089.17. 3099.05. 3104.84. 3107.52. 3117.94. 3135.80. 3144.92. 3145.65. 3155.61. 3165.14. 3179.00. 3487.35. | 1.0856. 1.2096. 0.9811. 4.1443. 6.1822. 5.0262. 0.1801. 0.3976. 0.5325. 0.057. 0.0604. 76.4358. 29.2379. 27.3207. 17.3574. 3.9195. 0.6097. 1.6425. 0.2849. 0.3382. 1.0136. 1.3396. 3.5759. 0.7243. 0.4342. 0.844. 0.2399. 2.325. 2.0639. 1.5785. 0.4824. 1.1234. 17.4262. 2.5941. 0.0504. 0.7405. 89.1786. 43.1928. 0.4846. 0.9603. 2.782. 1.4677. 1.5716. 0.2982. 6.0983. 2.1883. 3.3616. 0.4685. 2.2081. 3.4981. 2.1279. 0.7077. 2.0981. 2.845. 1.8164. 0.4439. 0.614. 1.0674. 2.7043. 0.5812. 6.2592. 11.1794. 10.5044. 9.2041. 298.2644. 19.9313. 15.7278. 27.1933. 2.1487. 23.6542. 30.7729. 25.9469. 14.7123. 36.7172. 25.4349. 20.277. 8.1374. 22.7291. 32.2116. 18.6567. 928.0309. |

|  | vdW2 Site 3 JP-10/BO2 |  | vdW1 Site 4 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 12.1168. ν2; 49.6797. ν3; 59.289. ν4; 74.7655. ν5; 115.244. ν6; 125.2828. ν7; 193.7937. ν8; 245.3831. ν9; 316.1639. ν10; 318.4052. ν11; 394.2835. ν12; 452.3282. ν13; 475.5891. ν14; 509.461. ν15; 515.8287. ν16; 532.8848. ν17; 549.0566. ν18; 666.957. ν19; 738.6039. ν20; 774.1267. ν21; 807.1504. ν22; 818.7799. ν23; 863.1253. ν24; 872.8306. ν25; 884.5734. ν26; 903.9749. ν27; 927.178. ν28; 943.5852. ν29; 949.1392. ν30; 968.4874. ν31; 975.6283. ν32; 1020.213. ν33; 1022.797. ν34; 1023.24. ν35; 1041.697. ν36; 1057.218. ν37; 1067.001. ν38; 1072.108. ν39; 1080.11. ν40; 1096.973. ν41; 1167.701. ν42; 1183.156. ν43; 1208.8. ν44; 1219.588. ν45; 1222.979. ν46; 1225.47. ν47; 1247.918. ν48; 1262.791. ν49; 1278.604. ν50; 1287.105. ν51; 1312.581. ν52; 1323.327. ν53; 1325.89. ν54; 1340.032. ν55; 1345.056. ν56; 1363.668. ν57; 1364.432. ν58; 1377.423. ν59; 1380.473. ν60; 1523.474. ν61; 1526.141. ν62; 1528.758. ν63; 1543.467. ν64; 1545.071. ν65; 2063.051. ν66; 3076.225. ν67; 3080.695. ν68; 3081.82. ν69; 3084.158. ν70; 3085.221. ν71; 3093.467. ν72; 3096.666. ν73; 3134.469. ν74; 3136.564. ν75; 3137.628. ν76; 3139.047. ν77; 3139.851. ν78; 3156.055. ν79; 3156.724. ν80; 3173.306. ν81; 3605.203. | 0.4315. 0.8641. 3.3385. 0.0328. 6.587. 0.9894. 0.4441. 0.0104. 0.4274. 0.1103. 2.2733. 90.2324. 53.4671. 20.6341. 10.5285. 2.6377. 1.4981. 0.018. 1.5339. 3.7796. 0.2074. 11.9918. 10.1696. 0.6075. 4.8868. 0.1917. 0.0358. 1.8465. 0.3332. 1.1937. 3.9225. 0.7266. 43.8685. 4.7183. 3.4352. 96.7339. 0.0597. 0.3235. 0.6462. 2.8208. 0.9671. 2.1185. 0.5052. 0.272. 0.8852. 1.5527. 1.7171. 0.3915. 2.777. 0.0081. 0.0028. 0.1132. 0.7342. 0.0947. 2.8246. 1.2661. 0.2928. 2.2829. 0.257. 3.4713. 4.0334. 13.771. 0.3833. 7.3029. 298.9734. 20.5125. 16.185. 3.4178. 30.9515. 26.6547. 25.3843. 52.8194. 29.2062. 1.628. 34.2155. 12.1862. 29.0367. 27.1853. 37.5725. 20.87. 840.4576. | 30.41. 50.56. 57.17. 71.76. 123.52. 138.89. 183.79. 254.86. 306.34. 319.89. 394.26. 487.21. 488.91. 517.11. 536.71. 554.82. 568.75. 645.24. 731.20. 755.27. 810.93. 840.70. 866.17. 897.06. 901.86. 914.08. 920.15. 934.00. 947.42. 979.67. 985.07. 1022.38. 1024.36. 1036.56. 1059.58. 1071.99. 1077.99. 1090.98. 1111.27. 1146.54. 1150.35. 1174.46. 1182.47. 1206.35. 1230.86. 1247.09. 1253.90. 1269.55. 1278.52. 1291.87. 1321.94. 1324.12. 1330.97. 1339.16. 1358.49. 1359.77. 1369.01. 1378.52. 1505.73. 1522.26. 1532.79. 1533.50. 1542.63. 1560.09. 2055.32. 3031.28. 3051.85. 3079.16. 3084.77. 3086.51. 3089.71. 3099.12. 3101.38. 3126.07. 3134.91. 3142.66. 3143.32. 3149.33. 3154.18. 3161.13. 3412.31. | 1.5073. 1.8945. 2.5573. 1.765. 1.0062. 5.76. 3.0695. 0.6036. 1.5376. 0.1568. 0.0361. 35.5508. 0.5968. 48.165. 4.4233. 1.4027. 67.2147. 5.3149. 0.269. 0.8696. 2.494. 2.9125. 0.2896. 2.4924. 1.0059. 0.8858. 0.5292. 0.2371. 1.7036. 3.9548. 2.2087. 0.7131. 18.0678. 5.9431. 1.0741. 0.8556. 5.1316. 86.7918. 4.8182. 3.4955. 1.3787. 0.5519. 0.5706. 3.9115. 1.2784. 1.634. 0.3748. 0.0308. 1.7188. 1.7618. 0.3022. 0.2453. 3.2922. 4.3833. 1.342. 0.2758. 0.9709. 1.6303. 8.6751. 1.3351. 9.5566. 4.8621. 14.3953. 5.3042. 286.2429. 18.697. 6.3082. 11.0008. 15.927. 34.6799. 15.7452. 39.4447. 21.065. 39.1885. 21.1375. 29.1259. 3.5653. 7.008. 36.9329. 33.0417. 856.9246. |

|  | vdW2 Site 5 JP-10/BO2 |  | vdW2 Site 6 JP-10/BO2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequencies(cm-1) | IR Inten | Frequencies(cm-1) | IR Inten |
| ν1; 27.40. ν2; 45.09. ν3; 51.58. ν4; 68.84. ν5; 104.21. ν6; 141.22. ν7; 175.29. ν8; 248.17. ν9; 280.97. ν10; 334.43. ν11; 401.33. ν12; 481.18. ν13; 492.57. ν14; 511.08. ν15; 515.39. ν16; 535.40. ν17; 587.15. ν18; 707.74. ν19; 740.38. ν20; 756.58. ν21; 791.40. ν22; 816.46. ν23; 827.09. ν24; 853.10. ν25; 887.54. ν26; 919.45. ν27; 931.50. ν28; 939.22. ν29; 955.82. ν30; 970.15. ν31; 986.01. ν32; 1003.77. ν33; 1020.24. ν34; 1024.51. ν35; 1044.35. ν36; 1064.89. ν37; 1070.34. ν38; 1072.74. ν39; 1093.20. ν40; 1111.23. ν41; 1139.29. ν42; 1160.23. ν43; 1170.52. ν44; 1201.97. ν45; 1226.17. ν46; 1238.61. ν47; 1258.91. ν48; 1271.52. ν49; 1292.68. ν50; 1306.45. ν51; 1312.32. ν52; 1321.21. ν53; 1327.63. ν54; 1333.27. ν55; 1341.83. ν56; 1349.67. ν57; 1368.32. ν58; 1378.60. ν59; 1395.34. ν60; 1512.88. ν61; 1525.86. ν62; 1534.19. ν63; 1544.59. ν64; 1555.69. ν65; 2058.66. ν66; 3031.52. ν67; 3050.84. ν68; 3082.62. ν69; 3083.13. ν70; 3089.98. ν71; 3092.47. ν72; 3094.24. ν73; 3109.09. ν74; 3119.67. ν75; 3124.75. ν76; 3133.92. ν77; 3149.71. ν78; 3152.82. ν79; 3155.65. ν80; 3192.13. ν81; 3541.12. | 1.0546. 0.8708. 0.3489. 6.7314. 0.4027. 5.7408. 5.2943. 0.1633. 0.9841. 0.664. 1.3043. 38.6487. 6.6547. 44.4692. 40.1264. 38.3458. 24.1459. 2.0404. 0.3705. 0.5993. 2.1718. 0.9598. 0.7141. 2.9196. 2.5107. 0.4369. 0.5963. 0.5357. 1.6401. 1.3644. 0.1588. 2.4258. 2.1783. 22.0734. 2.0014. 33.3195. 5.2737. 112.2041. 3.1353. 0.3612. 0.3054. 1.3404. 0.6394. 0.4935. 5.3337. 1.2298. 0.2411. 0.4298. 1.5302. 2.3412. 0.0613. 1.2255. 1.4725. 3.5467. 0.198. 4.734. 1.5112. 4.2658. 0.8608. 5.3279. 2.5165. 12.6938. 19.7558. 4.245. 255.2814. 18.0839. 14.8272. 13.2513. 21.2073. 26.7757. 38.6218. 25.6923. 7.6225. 66.9521. 7.7386. 0.4968. 9.632. 46.7784. 29.5014. 15.9397. 712.0001. | 28.35. 44.57. 53.95. 83.08. 93.65. 125.31. 198.11. 250.89. 269.57. 328.17. 403.75. 472.27. 480.19. 504.25. 509.13. 520.77. 610.44. 723.29. 743.27. 773.29. 779.92. 814.68. 827.11. 850.26. 910.39. 916.91. 931.60. 949.38. 952.20. 957.11. 987.77. 994.51. 1021.22. 1024.19. 1056.33. 1061.03. 1064.37. 1070.35. 1092.70. 1109.47. 1137.56. 1159.94. 1169.90. 1207.56. 1223.43. 1234.44. 1259.01. 1269.42. 1283.06. 1294.68. 1312.92. 1317.21. 1324.82. 1336.00. 1343.52. 1359.04. 1371.34. 1383.80. 1395.15. 1500.17. 1507.88. 1526.49. 1531.17. 1554.94. 2059.75. 3013.63. 3031.21. 3075.95. 3082.11. 3088.17. 3091.43. 3092.49. 3097.52. 3105.04. 3116.28. 3130.74. 3132.44. 3151.44. 3170.02. 3179.16. 3609.41. | 1.5453. 1.2241. 5.8144. 0.5329. 1.6806. 3.9177. 5.7278. 0.0104. 0.0978. 0.0892. 0.4322. 44.1407. 41.5306. 42.1724. 58.6732. 3.9243. 30.3889. 0.4437. 1.1704. 1.9214. 2.2165. 0.9549. 0.8195. 1.0435. 1.7039. 0.7932. 1.0522. 0.0796. 0.3439. 4.1573. 1.8083. 1.5029. 22.9115. 4.8425. 4.3807. 114.0015. 4.0765. 0.4138. 0.2109. 4.1366. 1.1965. 0.3378. 2.3742. 1.2055. 0.6613. 2.2658. 0.0785. 0.4317. 0.202. 1.2759. 0.1761. 0.3763. 0.6806. 5.2306. 0.756. 0.4358. 7.1499. 0.2417. 0.3342. 14.6164. 4.3073. 2.1516. 11.711. 4.4804. 256.1781. 20.0173. 22.9476. 7.9398. 19.4837. 13.9358. 39.7169. 11.9807. 19.2275. 48.7384. 45.7013. 7.5596. 2.2648. 47.2067. 33.8499. 22.0342. 589.4182. |

Table S7: B3LYP/cc-pVTZ cartesian coordinates and vibrational frequencies of  van-der-Waals complexes (vdW), transition states (TS), and products of the reactions of atomic and molecular oxygen with JP-10;  the vdW R2-O2H, vdW R4-O2H, and tsR4-O2H are obtained at the MP2/cc-pVDZ level.

| Atom | X | Y | Z | Atom | X | Y | Z |
| --- | --- | --- | --- | --- | --- | --- | --- |
| JP-10 |  |  |  |  |  |  |  |
| C | 0.221599 | -0.586778 | 0.787828 |  |  |  |  |
| C | 0.221599 | -0.586778 | -0.787828 |  |  |  |  |
| C | 0.221599 | 0.917698 | 1.132164 |  |  |  |  |
| C | 0.221599 | 0.917698 | -1.132164 |  |  |  |  |
| C | -0.640430 | 1.510860 | 0.000000 |  |  |  |  |
| C | 1.610944 | 1.491910 | 0.780878 |  |  |  |  |
| C | 1.610944 | 1.491910 | -0.780878 |  |  |  |  |
| C | -1.025973 | -1.391810 | 1.205692 |  |  |  |  |
| C | -1.025973 | -1.391810 | -1.205692 |  |  |  |  |
| C | -1.332464 | -2.291529 | 0.000000 |  |  |  |  |
| H | 1.116767 | -1.067916 | 1.185227 |  |  |  |  |
| H | 1.116767 | -1.067916 | -1.185227 |  |  |  |  |
| H | -0.101929 | 1.137231 | 2.149267 |  |  |  |  |
| H | -0.101929 | 1.137231 | -2.149267 |  |  |  |  |
| H | -1.670972 | 1.157614 | 0.000000 |  |  |  |  |
| H | -0.652613 | 2.601951 | 0.000000 |  |  |  |  |
| H | 2.418876 | 0.892255 | 1.201430 |  |  |  |  |
| H | 1.721563 | 2.504095 | 1.171744 |  |  |  |  |
| H | 1.721563 | 2.504095 | -1.171744 |  |  |  |  |
| H | 2.418876 | 0.892255 | -1.201430 |  |  |  |  |
| H | -1.869551 | -0.719955 | 1.384894 |  |  |  |  |
| H | -0.867295 | -1.953863 | 2.126671 |  |  |  |  |
| H | -0.867295 | -1.953863 | -2.126671 |  |  |  |  |
| H | -1.869551 | -0.719955 | -1.384894 |  |  |  |  |
| H | -0.660917 | -3.154606 | 0.000000 |  |  |  |  |
| H | -2.353016 | -2.676881 | 0 |  |  |  |  |

| R1 |  |  |  | R2 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.356808 | 0.791831 | -0.530988 | C | -0.367857 | -0.853431 | -0.460482 |
| C | 0.306839 | -0.781831 | -0.511081 | C | -0.341184 | 0.739732 | -0.549712 |
| C | -0.909247 | 1.179987 | 0.296881 | C | 0.873855 | -1.094842 | 0.366479 |
| C | -0.950367 | -1.087387 | 0.336458 | C | 0.915189 | 1.110978 | 0.277478 |
| C | -0.928521 | 0.060642 | 1.365959 | C | 0.898150 | 0.026865 | 1.392021 |
| C | -2.099939 | 0.789000 | -0.524269 | C | 2.140895 | -0.885474 | -0.434481 |
| C | -2.198711 | -0.711808 | -0.499849 | C | 2.174627 | 0.690305 | -0.520471 |
| C | 1.723928 | 1.179859 | 0.070428 | C | -1.735623 | -1.205494 | 0.158285 |
| C | 1.657420 | -1.233391 | 0.082264 | C | -1.699702 | 1.204189 | 0.010152 |
| C | 2.609570 | -0.053165 | -0.161268 | C | -2.633182 | -0.002263 | -0.164079 |
| H | 0.277473 | 1.180997 | -1.545990 | H | -0.276890 | -1.304312 | -1.448923 |
| H | 0.194274 | -1.187244 | -1.517718 | H | -0.231081 | 1.070387 | -1.583457 |
| H | -0.975840 | -2.097827 | 0.742262 | H | 0.931206 | 2.149093 | 0.610262 |
| H | -0.050345 | 0.054299 | 2.010286 | H | 0.023426 | 0.075124 | 2.037162 |
| H | -1.820111 | 0.091397 | 1.992398 | H | 1.795616 | 0.039603 | 2.010162 |
| H | -2.609640 | 1.433385 | -1.225666 | H | 2.103959 | -1.357978 | -1.415330 |
| H | -3.117591 | -1.057909 | -0.008343 | H | 3.021517 | -1.262225 | 0.086782 |
| H | -2.192756 | -1.167349 | -1.495715 | H | 3.078576 | 1.085558 | -0.056182 |
| H | 1.630318 | 1.369333 | 1.142746 | H | 2.148392 | 1.049337 | -1.549613 |
| H | 2.130629 | 2.086527 | -0.378501 | H | -1.643581 | -1.320204 | 1.240408 |
| H | 2.014041 | -2.164103 | -0.360161 | H | -2.128945 | -2.145937 | -0.227922 |
| H | 1.560276 | -1.409704 | 1.156724 | H | -2.066351 | 2.100800 | -0.491105 |
| H | 2.961562 | -0.067230 | -1.196427 | H | -1.609675 | 1.447883 | 1.071824 |
| H | 3.492062 | -0.074574 | 0.479762 | H | -2.975105 | -0.060414 | -1.201185 |
| H | -0.901028 | 2.207591 | 0.657136 | H | -3.522067 | 0.049889 | 0.465979 |

| R3 |  |  |  | R4 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.357220 | 0.789040 | -0.493336 | C | 0.386982 | 0.745511 | -0.346332 |
| C | 0.357220 | -0.789040 | -0.493336 | C | 0.373830 | -0.771908 | -0.459568 |
| C | -0.884615 | 1.136071 | 0.364225 | C | -0.882722 | 1.142475 | 0.353113 |
| C | -0.884615 | -1.136071 | 0.364225 | C | -0.932601 | -1.131885 | 0.291198 |
| C | -0.889656 | 0.000000 | 1.351703 | C | -1.004469 | -0.029734 | 1.370591 |
| C | -2.149542 | 0.781904 | -0.472582 | C | -2.081289 | 0.833922 | -0.582121 |
| C | -2.149542 | -0.781904 | -0.472582 | C | -2.113919 | -0.726898 | -0.619452 |
| C | 1.718837 | 1.202758 | 0.098313 | C | 1.771233 | 1.247046 | -0.055594 |
| C | 1.718837 | -1.202758 | 0.098313 | C | 1.734374 | -1.182593 | 0.141857 |
| C | 2.637239 | 0.000000 | -0.155561 | C | 2.661917 | -0.006477 | -0.217693 |
| H | 0.250809 | 1.189074 | -1.502976 | H | 0.323691 | -1.125168 | -1.496125 |
| H | 0.250809 | -1.189074 | -1.502976 | H | -0.889255 | 2.147470 | 0.770822 |
| H | -0.886695 | 2.148385 | 0.763180 | H | -0.980092 | -2.160334 | 0.646722 |
| H | -0.886694 | -2.148385 | 0.763181 | H | -0.185759 | -0.060090 | 2.089497 |
| H | -1.356771 | 0.000000 | 2.326702 | H | -1.949387 | -0.027044 | 1.917823 |
| H | -2.101546 | 1.204921 | -1.477358 | H | -1.947358 | 1.275129 | -1.568627 |
| H | -3.048160 | 1.172421 | 0.004885 | H | -3.004351 | 1.236430 | -0.162412 |
| H | -3.048160 | -1.172421 | 0.004885 | H | -3.055338 | -1.107766 | -0.221885 |
| H | -2.101546 | -1.204922 | -1.477358 | H | -2.004011 | -1.123002 | -1.629252 |
| H | 1.620652 | 1.362626 | 1.175268 | H | 1.831302 | 1.635067 | 0.971050 |
| H | 2.097249 | 2.129779 | -0.334168 | H | 2.086103 | 2.070038 | -0.704088 |
| H | 2.097249 | -2.129779 | -0.334168 | H | 2.095703 | -2.139750 | -0.236205 |
| H | 1.620652 | -1.362626 | 1.175268 | H | 1.653818 | -1.271026 | 1.228535 |
| H | 2.976297 | 0.000000 | -1.195430 | H | 2.982869 | -0.097348 | -1.257985 |
| H | 3.527560 | 0.000000 | 0.474775 | H | 3.562062 | 0.030623 | 0.396137 |

| R5 |  |  |  | R6 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.354822 | 0.825549 | -0.527558 | C | 0.378264 | 0.788215 | -0.592492 |
| C | 0.398518 | -0.747160 | -0.568349 | C | 0.378264 | -0.788214 | -0.592493 |
| C | -0.875036 | 1.119032 | 0.379462 | C | -0.814966 | 1.129964 | 0.326439 |
| C | -0.826934 | -1.141531 | 0.283694 | C | -0.814967 | -1.129965 | 0.326436 |
| C | -0.822960 | -0.052455 | 1.375750 | C | -0.746245 | -0.000002 | 1.372604 |
| C | -2.145412 | 0.778215 | -0.425799 | C | -2.120891 | 0.780262 | -0.416516 |
| C | -2.107161 | -0.780851 | -0.500026 | C | -2.120892 | -0.780260 | -0.416518 |
| C | 1.692891 | 1.232101 | -0.018594 | C | 1.763975 | 1.241534 | -0.071369 |
| C | 1.768750 | -1.159745 | 0.021685 | C | 1.763974 | -1.241534 | -0.071369 |
| C | 2.661012 | 0.099699 | -0.024271 | C | 2.569660 | 0.000000 | 0.088275 |
| H | 0.171613 | 1.258958 | -1.519951 | H | 0.211684 | 1.187054 | -1.593210 |
| H | 0.298379 | -1.124448 | -1.586799 | H | 0.211685 | -1.187052 | -1.593212 |
| H | -0.871702 | 2.120148 | 0.807533 | H | -0.788334 | 2.148027 | 0.713501 |
| H | -0.801317 | -2.173347 | 0.633018 | H | -0.788336 | -2.148030 | 0.713494 |
| H | 0.073615 | -0.050865 | 1.994937 | H | 0.174143 | -0.000004 | 1.956924 |
| H | -1.696761 | -0.099638 | 2.027529 | H | -1.592580 | -0.000003 | 2.061282 |
| H | -2.144533 | 1.246699 | -1.410624 | H | -2.143788 | 1.201565 | -1.422132 |
| H | -3.038112 | 1.123638 | 0.096950 | H | -2.986955 | 1.172048 | 0.118245 |
| H | -2.986862 | -1.216972 | -0.025396 | H | -2.986957 | -1.172046 | 0.118240 |
| H | -2.075452 | -1.151923 | -1.525102 | H | -2.143788 | -1.201559 | -1.422136 |
| H | 1.979056 | 2.263338 | 0.140529 | H | 1.664983 | 1.785478 | 0.880045 |
| H | 2.207755 | -1.998306 | -0.519133 | H | 2.237746 | 1.955603 | -0.755016 |
| H | 1.647388 | -1.481567 | 1.057547 | H | 2.237744 | -1.955605 | -0.755014 |
| H | 3.265714 | 0.106438 | -0.945315 | H | 1.664980 | -1.785477 | 0.880046 |
| H | 3.380277 | 0.140731 | 0.798313 | H | 3.610716 | 0.000001 | 0.380962 |

| vdW R1-OH |  |  |  | vdW R2-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.772810 | -0.657213 | -0.692403 | C | 0.273851 | 0.423926 | -0.757221 |
| C | -1.019410 | 0.859983 | -0.354834 | C | 1.043481 | -0.895272 | -0.292165 |
| C | 0.648642 | -0.912862 | -0.094862 | C | -1.056529 | 0.195484 | -0.076934 |
| C | 0.272106 | 1.270509 | 0.388679 | C | -0.001553 | -1.614043 | 0.598023 |
| C | 0.621563 | -0.015376 | 1.164488 | C | -0.725898 | -0.417084 | 1.275696 |
| C | 1.608738 | -0.148799 | -0.958924 | C | -1.887978 | -0.861903 | -0.771596 |
| C | 1.424137 | 1.315865 | -0.645727 | C | -1.130254 | -2.166033 | -0.308156 |
| C | -1.936338 | -1.432605 | -0.039277 | C | 1.149336 | 1.600354 | -0.280725 |
| C | -2.324308 | 0.896014 | 0.466896 | C | 2.321732 | -0.395011 | 0.407607 |
| C | -3.062600 | -0.396545 | 0.089088 | C | 2.561466 | 1.010267 | -0.161615 |
| H | -0.770848 | -0.833952 | -1.768052 | H | 0.160592 | 0.453004 | -1.840705 |
| H | -1.141337 | 1.452805 | -1.262561 | H | 1.304806 | -1.513630 | -1.151724 |
| H | 0.175723 | 2.178962 | 0.980969 | H | -2.010427 | 1.915653 | 0.153441 |
| H | -0.135557 | -0.307968 | 1.889868 | H | 0.428925 | -2.357868 | 1.268121 |
| H | 1.586704 | 0.033014 | 1.667746 | H | -0.078905 | 0.189382 | 1.905051 |
| H | 1.974006 | -0.514306 | -1.910731 | H | -1.601854 | -0.718344 | 1.848857 |
| H | 2.324605 | 1.761112 | -0.205062 | H | -1.900634 | -0.744536 | -1.854034 |
| H | 1.185059 | 1.915315 | -1.529002 | H | -2.919725 | -0.867514 | -0.420465 |
| H | -1.648901 | -1.788689 | 0.952964 | H | -1.796232 | -2.820077 | 0.254608 |
| H | -2.226343 | -2.308201 | -0.620409 | H | -0.739735 | -2.736708 | -1.150619 |
| H | -2.912037 | 1.793057 | 0.270530 | H | 0.811268 | 1.957100 | 0.694086 |
| H | -2.100411 | 0.891002 | 1.536662 | H | 1.096323 | 2.449626 | -0.961174 |
| H | -3.562805 | -0.270976 | -0.874963 | H | 3.165061 | -1.067970 | 0.248903 |
| H | -3.825960 | -0.682015 | 0.813950 | H | 2.164100 | -0.331839 | 1.487216 |
| H | 0.878226 | -1.967343 | 0.049546 | H | 3.019226 | 0.937044 | -1.151907 |
| O | 4.250659 | -0.681646 | 0.513332 | H | 3.225736 | 1.614584 | 0.456925 |
| H | 3.436283 | -0.572466 | -0.036847 | O | -2.451806 | 2.794748 | 0.301992 |

| vdW R3-OH |  |  |  | vdW R4-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.923025 | 0.789747 | 0.528084 | C | 0.389887 | 0.318598 | 0.458269 |
| C | -0.923016 | -0.789583 | 0.528334 | C | 0.286425 | -0.491632 | -0.832623 |
| C | 0.529605 | 1.137831 | 0.088002 | C | -0.920893 | 0.153746 | 1.181134 |
| C | 0.529620 | -1.137790 | 0.088369 | C | -1.108701 | -1.146934 | -0.678421 |
| C | 0.808682 | -0.000132 | -0.860509 | C | -1.209594 | -1.340425 | 0.850235 |
| C | 1.472666 | 0.781470 | 1.264380 | C | -2.043210 | 0.847851 | 0.365997 |
| C | 1.472676 | -0.781033 | 1.264633 | C | -2.168784 | -0.046656 | -0.907322 |
| C | -2.048635 | 1.204540 | -0.439484 | C | 1.757830 | 0.164010 | 1.067663 |
| C | -2.048623 | -1.204694 | -0.439103 | C | 1.547684 | -1.381273 | -0.798337 |
| C | -2.999478 | -0.000086 | -0.469911 | C | 2.581000 | -0.530378 | -0.037756 |
| H | -1.118872 | 1.191483 | 1.523482 | H | 0.576047 | 2.230282 | -0.216202 |
| H | -1.118863 | -1.191005 | 1.523858 | H | 0.315381 | 0.129843 | -1.734202 |
| H | 0.645418 | 2.149171 | -0.295539 | H | -0.902743 | 0.420444 | 2.235852 |
| H | 0.645451 | -2.149253 | -0.294843 | H | -1.253925 | -2.036979 | -1.288689 |
| H | 0.592296 | -0.000306 | -1.921180 | H | -0.467066 | -2.024374 | 1.260772 |
| H | 2.858315 | -0.000202 | -1.287534 | H | -2.199305 | -1.662413 | 1.178729 |
| H | 1.119327 | 1.203949 | 2.205086 | H | -1.799293 | 1.882150 | 0.130641 |
| H | 2.475971 | 1.165849 | 1.084947 | H | -2.971938 | 0.850405 | 0.937375 |
| H | 2.475987 | -1.165457 | 1.085328 | H | -3.165499 | -0.482119 | -0.982652 |
| H | 1.119338 | -1.203209 | 2.205475 | H | -1.987609 | 0.509647 | -1.827049 |
| H | -1.643359 | 1.374232 | -1.440607 | H | 1.695920 | -0.469823 | 1.962842 |
| H | -2.539061 | 2.128795 | -0.133213 | H | 2.203529 | 1.105846 | 1.397959 |
| H | -2.539040 | -2.128855 | -0.132535 | H | 1.885102 | -1.671384 | -1.793491 |
| H | -1.643348 | -1.374702 | -1.440172 | H | 1.343749 | -2.300287 | -0.242827 |
| H | -3.630759 | 0.000053 | 0.422829 | H | 3.003794 | 0.222381 | -0.706647 |
| H | -3.663345 | -0.000226 | -1.335189 | H | 3.410329 | -1.116740 | 0.357268 |
| O | 3.842715 | -0.000242 | -1.385870 | O | 0.705457 | 3.141460 | -0.585339 |

| vdW R5-OH |  |  |  | vdW R6-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.000263 | -0.204620 | 1.048616 | C | 0.124857 | 0.241986 | 0.782553 |
| C | 0.302265 | -1.241672 | -0.095180 | C | 0.124164 | 0.207567 | -0.793329 |
| C | 0.777390 | 1.062675 | 0.586286 | C | -1.319409 | -0.172185 | 1.135305 |
| C | 1.247730 | -0.454323 | -1.026855 | C | -1.320431 | -0.220775 | -1.126335 |
| C | 0.665407 | 0.970953 | -0.946793 | C | -1.641121 | -1.193511 | 0.026150 |
| C | 2.280484 | 0.786618 | 0.795788 | C | -2.261901 | 0.990436 | 0.760073 |
| C | 2.601843 | -0.270060 | -0.308035 | C | -2.262410 | 0.957058 | -0.800475 |
| C | -1.487970 | -0.130462 | 1.122979 | C | 1.234000 | -0.731744 | 1.246385 |
| C | -1.068034 | -1.618958 | -0.705775 | C | 1.231868 | -0.786562 | -1.215284 |
| C | -2.125839 | -1.237982 | 0.349812 | C | 2.023799 | -1.051580 | 0.021402 |
| H | 0.399903 | -0.526444 | 2.018616 | H | 0.340317 | 1.242605 | 1.155671 |
| H | 0.795906 | -2.132248 | 0.295655 | H | 0.340169 | 1.190797 | -1.209865 |
| H | 0.425644 | 1.984819 | 1.046306 | H | -1.436564 | -0.520699 | 2.160880 |
| H | 1.333422 | -0.882952 | -2.024630 | H | -1.438952 | -0.612978 | -2.135847 |
| H | -0.354296 | 1.056434 | -1.319637 | H | -1.003992 | -2.078218 | 0.044829 |
| H | 1.281311 | 1.710695 | -1.460041 | H | -2.681619 | -1.521099 | 0.033641 |
| H | 2.496291 | 0.425204 | 1.801685 | H | -1.914496 | 1.943054 | 1.160709 |
| H | 2.861166 | 1.697399 | 0.646862 | H | -3.263385 | 0.818250 | 1.155670 |
| H | 3.358204 | 0.103647 | -0.998701 | H | -3.264214 | 0.768616 | -1.187756 |
| H | 2.975811 | -1.207679 | 0.104701 | H | -1.914988 | 1.891621 | -1.241580 |
| H | -2.337894 | 1.488424 | -0.044277 | H | 0.796973 | -1.649635 | 1.668517 |
| H | -2.000446 | 0.394610 | 1.921212 | H | 1.845496 | -0.312482 | 2.050522 |
| H | -1.117171 | -2.672898 | -0.978152 | H | 1.842209 | -0.403957 | -2.038469 |
| H | -1.244034 | -1.046793 | -1.617973 | H | 0.793328 | -1.722141 | -1.595189 |
| H | -2.328828 | -2.090347 | 1.016819 | H | 3.227865 | 0.678377 | -0.013078 |
| H | -3.091907 | -0.972347 | -0.087232 | H | 2.888687 | -1.703653 | 0.035098 |
| O | -2.826790 | 2.087183 | -0.655784 | O | 3.655333 | 1.568425 | -0.032803 |

| tsR1-OH |  |  |  | tsR2-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.684089 | -0.703386 | -0.616337 | C | 0.331526 | 0.442619 | -0.731374 |
| C | -0.958984 | 0.834603 | -0.427124 | C | 0.872733 | -0.993399 | -0.322555 |
| C | 0.674291 | -0.904512 | 0.109609 | C | -1.023046 | 0.440877 | -0.032312 |
| C | 0.280553 | 1.312267 | 0.359347 | C | -0.264922 | -1.559740 | 0.560298 |
| C | 0.576788 | 0.104798 | 1.271023 | C | -0.773575 | -0.290671 | 1.288043 |
| C | 1.734756 | -0.241588 | -0.760640 | C | -2.012059 | -0.469710 | -0.754693 |
| C | 1.494421 | 1.269002 | -0.598647 | C | -1.474870 | -1.887625 | -0.346104 |
| C | -1.895102 | -1.429452 | 0.006931 | C | 1.393846 | 1.444216 | -0.237735 |
| C | -2.316600 | 0.928363 | 0.298526 | C | 2.224745 | -0.738143 | 0.372356 |
| C | -3.027030 | -0.392582 | -0.030110 | C | 2.689769 | 0.625422 | -0.157438 |
| H | -0.600127 | -0.969084 | -1.670830 | H | 0.207601 | 0.528806 | -1.810748 |
| H | -1.022134 | 1.347562 | -1.388008 | H | 1.019965 | -1.618808 | -1.203989 |
| H | 0.150530 | 2.271937 | 0.857315 | H | -1.500812 | 1.649109 | 0.129038 |
| H | -0.221593 | -0.118071 | 1.976706 | H | 0.044059 | -2.385892 | 1.199869 |
| H | 1.512602 | 0.198809 | 1.821171 | H | -0.030397 | 0.180877 | 1.926989 |
| H | 1.841097 | -0.620935 | -1.775786 | H | -1.681139 | -0.461384 | 1.865917 |
| H | 2.360352 | 1.761845 | -0.151373 | H | -2.010655 | -0.310434 | -1.832023 |
| H | 1.301723 | 1.763272 | -1.552241 | H | -3.028525 | -0.314460 | -0.395047 |
| H | -1.682270 | -1.703861 | 1.043006 | H | -2.233549 | -2.443653 | 0.204633 |
| H | -2.141573 | -2.350190 | -0.522147 | H | -1.189748 | -2.487236 | -1.210515 |
| H | -2.888188 | 1.805521 | -0.005688 | H | 1.129629 | 1.822417 | 0.751804 |
| H | -2.166822 | 1.005358 | 1.378408 | H | 1.473880 | 2.311013 | -0.892756 |
| H | -3.454741 | -0.344888 | -1.035195 | H | 2.941383 | -1.537303 | 0.180200 |
| H | -3.841741 | -0.624597 | 0.656857 | H | 2.090974 | -0.684718 | 1.455776 |
| H | 0.885155 | -1.939751 | 0.371519 | H | 3.119969 | 0.509260 | -1.155936 |
| O | 3.981481 | -0.705651 | 0.322641 | H | 3.450856 | 1.090995 | 0.469530 |
| H | 2.841851 | -0.502800 | -0.260298 | O | -1.948547 | 2.758541 | 0.310792 |

| tsR3-OH |  |  |  | tsR4-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.840475 | -0.791620 | -0.551145 | C | 0.380817 | 0.519905 | 0.332603 |
| C | -0.840477 | 0.786740 | -0.558175 | C | 0.316396 | -0.508174 | -0.834191 |
| C | 0.600522 | -1.138254 | -0.091165 | C | -0.909509 | 0.298551 | 1.120995 |
| C | 0.600598 | 1.137423 | -0.101506 | C | -1.007210 | -1.250104 | -0.538720 |
| C | 0.860385 | 0.004029 | 0.884249 | C | -1.045494 | -1.241107 | 1.003570 |
| C | 1.568017 | -0.786425 | -1.243172 | C | -2.110092 | 0.766186 | 0.267261 |
| C | 1.567986 | 0.775023 | -1.250327 | C | -2.175973 | -0.298297 | -0.872695 |
| C | -1.988422 | -1.204466 | 0.391344 | C | 1.737820 | 0.364724 | 1.016465 |
| C | -1.988310 | 1.207901 | 0.380781 | C | 1.631061 | -1.308695 | -0.723658 |
| C | -2.938282 | 0.001820 | 0.398753 | C | 2.609889 | -0.350500 | -0.026606 |
| H | -1.016333 | -1.195830 | -1.549058 | H | 0.374165 | 1.651203 | -0.148962 |
| H | -1.016508 | 1.182059 | -1.559615 | H | 0.270959 | -0.015255 | -1.807238 |
| H | 0.709887 | -2.148360 | 0.298416 | H | -0.891416 | 0.707425 | 2.129539 |
| H | 0.710095 | 2.151020 | 0.278864 | H | -1.079329 | -2.225971 | -1.017053 |
| H | 0.339117 | 0.008374 | 1.838602 | H | -0.228535 | -1.790385 | 1.470248 |
| H | 2.102962 | 0.005699 | 1.259828 | H | -1.987619 | -1.608299 | 1.413025 |
| H | 1.236889 | -1.213201 | -2.189825 | H | -1.968109 | 1.777240 | -0.108544 |
| H | 2.566394 | -1.169047 | -1.036929 | H | -3.021613 | 0.756987 | 0.865152 |
| H | 2.566369 | 1.159566 | -1.047724 | H | -3.125518 | -0.834018 | -0.854735 |
| H | 1.236741 | 1.193078 | -2.200825 | H | -2.071622 | 0.144304 | -1.863363 |
| H | -1.608991 | -1.378390 | 1.401592 | H | 1.625411 | -0.258723 | 1.909963 |
| H | -2.473732 | -2.126995 | 0.072181 | H | 2.153234 | 1.317226 | 1.345959 |
| H | -2.473539 | 2.127677 | 0.053650 | H | 1.989039 | -1.650862 | -1.694636 |
| H | -1.608765 | 1.390528 | 1.389444 | H | 1.480552 | -2.196940 | -0.104588 |
| H | -3.551738 | -0.002116 | -0.506276 | H | 2.992968 | 0.377922 | -0.744801 |
| H | -3.619416 | 0.005579 | 1.250385 | H | 3.468281 | -0.859308 | 0.412444 |
| O | 3.286415 | 0.007166 | 1.586185 | O | 0.431614 | 2.844065 | -0.709070 |

| tsR5-OH |  |  |  | tsR6-OH |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.141546 | -0.013232 | 0.995418 | C | 0.116043 | 0.787808 | -0.261506 |
| C | 0.110400 | -1.220595 | 0.017834 | C | 0.116052 | -0.787840 | -0.261303 |
| C | 0.820266 | 1.076382 | 0.460971 | C | -1.305058 | 1.131923 | 0.232088 |
| C | 1.197700 | -0.671969 | -0.929761 | C | -1.305032 | -1.131855 | 0.232404 |
| C | 0.799108 | 0.811585 | -1.057003 | C | -1.581426 | 0.000170 | 1.241958 |
| C | 2.258747 | 0.646981 | 0.818970 | C | -2.302098 | 0.780538 | -0.892590 |
| C | 2.518070 | -0.560736 | -0.136779 | C | -2.302082 | -0.780822 | -0.892377 |
| C | -1.639728 | 0.255379 | 0.932400 | C | 1.278020 | 1.215526 | 0.659048 |
| C | -1.258769 | -1.537743 | -0.620749 | C | 1.278005 | -1.215318 | 0.659368 |
| C | -2.298006 | -0.990719 | 0.369509 | C | 2.180872 | 0.000111 | 0.749377 |
| H | 0.118175 | -0.258148 | 2.029336 | H | 0.283494 | 1.182594 | -1.263143 |
| H | 0.475648 | -2.095413 | 0.558098 | H | 0.283495 | -1.182884 | -1.262839 |
| H | 0.561564 | 2.084798 | 0.777465 | H | -1.406126 | 2.149369 | 0.608513 |
| H | 1.288076 | -1.228403 | -1.861829 | H | -1.406063 | -2.149199 | 0.609114 |
| H | -0.174039 | 0.972983 | -1.520611 | H | -0.908732 | 0.000293 | 2.099800 |
| H | 1.536367 | 1.406518 | -1.597882 | H | -2.607029 | 0.000209 | 1.613708 |
| H | 2.359449 | 0.380782 | 1.871624 | H | -1.999926 | 1.201117 | -1.851968 |
| H | 2.959455 | 1.458787 | 0.622319 | H | -3.294196 | 1.171739 | -0.665025 |
| H | 3.354525 | -0.357193 | -0.805912 | H | -3.294172 | -1.171984 | -0.664713 |
| H | 2.750446 | -1.480491 | 0.401158 | H | -1.999890 | -1.201657 | -1.851637 |
| H | -1.846134 | 1.160738 | 0.102932 | H | 0.911778 | 1.456412 | 1.664230 |
| H | -2.088391 | 0.686968 | 1.826443 | H | 1.795915 | 2.105412 | 0.299605 |
| H | -1.386261 | -2.602028 | -0.817567 | H | 1.795892 | -2.105317 | 0.300197 |
| H | -1.363171 | -1.019348 | -1.575788 | H | 0.911727 | -1.455897 | 1.664612 |
| H | -2.459976 | -1.705134 | 1.185774 | H | 2.867379 | -0.000034 | -0.288136 |
| H | -3.271696 | -0.797377 | -0.081143 | H | 2.941121 | 0.000206 | 1.529326 |
| O | -2.126435 | 2.077495 | -0.777411 | O | 3.510695 | -0.000229 | -1.417556 |

| vdW R1-O2H |  |  |  | vdW R2-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.507452 | -0.708164 | 0.321538 | C | -0.043276 | 0.434461 | -0.505791 |
| C | -1.057497 | 0.138299 | -0.886946 | C | 1.524169 | 0.152366 | -0.527007 |
| C | 0.173582 | 0.370962 | 1.215553 | C | -0.506924 | -0.764630 | 0.301938 |
| C | -0.661835 | 1.585133 | -0.513900 | C | 1.663893 | -1.151591 | 0.298297 |
| C | -0.793229 | 1.572269 | 1.022573 | C | 0.556036 | -0.970806 | 1.375816 |
| C | 1.377584 | 0.877793 | 0.470581 | C | -0.471955 | -2.047167 | -0.513372 |
| C | 0.870275 | 1.730960 | -0.669368 | C | 1.080190 | -2.322193 | -0.534678 |
| C | -1.730262 | -1.427786 | 0.925665 | C | -0.199768 | 1.829624 | 0.135655 |
| C | -2.570047 | -0.160204 | -0.949303 | C | 2.167090 | 1.415425 | 0.085417 |
| C | -2.735631 | -1.507922 | -0.232117 | C | 1.135881 | 2.526741 | -0.166945 |
| H | 0.220882 | -1.449330 | -0.006086 | H | -0.480677 | 0.423418 | -1.517080 |
| H | -0.585253 | -0.156492 | -1.825026 | H | 1.883981 | 0.001416 | -1.560441 |
| H | -1.231453 | 2.349139 | -1.040204 | H | -2.229504 | -0.219789 | 0.652761 |
| H | -1.802794 | 1.374668 | 1.379937 | H | 2.685201 | -1.332722 | 0.673759 |
| H | -0.432158 | 2.487665 | 1.491678 | H | 0.716442 | -0.105221 | 2.036456 |
| H | 1.183543 | 2.773638 | -0.543350 | H | 0.399384 | -1.877273 | 1.983914 |
| H | 1.231311 | 1.419018 | -1.654161 | H | -0.902078 | -1.914620 | -1.518351 |
| H | -2.156406 | -0.841845 | 1.743635 | H | -1.009560 | -2.867527 | -0.009296 |
| H | -1.471917 | -2.404634 | 1.334577 | H | 1.310815 | -3.291663 | -0.061602 |
| H | -2.947036 | -0.174414 | -1.972125 | H | 1.487342 | -2.339907 | -1.559497 |
| H | -3.131009 | 0.610980 | -0.414892 | H | -0.327955 | 1.736766 | 1.229960 |
| H | -2.460977 | -2.324037 | -0.905559 | H | -1.080513 | 2.363245 | -0.254820 |
| H | -3.757526 | -1.693638 | 0.100446 | H | 3.158655 | 1.629448 | -0.347699 |
| H | 0.362450 | 0.048288 | 2.236959 | H | 2.304465 | 1.282051 | 1.174682 |
| H | 2.348749 | 1.022533 | 0.930683 | H | 1.165233 | 2.827377 | -1.230920 |
| O | 4.182935 | -0.957603 | 0.035916 | H | 1.306740 | 3.430271 | 0.442432 |
| O | 3.071306 | -1.208722 | -0.634159 | O | -3.318509 | 0.545029 | -0.609785 |
| H | 2.402742 | -0.538975 | -0.296214 | O | -3.158989 | 0.160140 | 0.631006 |

| vdW R3-O2H |  |  |  | vdW R4-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.708905 | 1.027648 | 0.788596 | C | 0.369232 | -0.123234 | 0.648194 |
| C | 0.708905 | 1.027648 | -0.788596 | C | 0.301841 | -0.427834 | -0.857101 |
| C | -0.757361 | 0.684935 | 1.138550 | C | -0.959654 | -0.540218 | 1.238432 |
| C | -0.757361 | 0.684935 | -1.138550 | C | -1.094994 | -1.081618 | -0.975105 |
| C | -1.155265 | -0.223373 | 0.000000 | C | -1.229387 | -1.811717 | 0.381154 |
| C | -1.632611 | 1.923427 | 0.782384 | C | -2.062176 | 0.407999 | 0.701205 |
| C | -1.632611 | 1.923427 | -0.782384 | C | -2.141727 | 0.047145 | -0.817046 |
| C | 1.772024 | -0.008460 | 1.204902 | C | 1.723133 | -0.527584 | 1.195050 |
| C | 1.772024 | -0.008460 | -1.204902 | C | 1.557369 | -1.296980 | -1.089974 |
| C | 2.718018 | -0.101909 | 0.000000 | C | 2.571450 | -0.731165 | -0.077649 |
| H | 0.972233 | 2.008243 | 1.186685 | H | 0.498062 | 1.717812 | 0.565156 |
| H | 0.972233 | 2.008243 | -1.186685 | H | 0.362109 | 0.484020 | -1.480358 |
| H | -0.909171 | 0.313321 | 2.149423 | H | -0.959989 | -0.674011 | 2.331619 |
| H | -0.909171 | 0.313321 | -2.149423 | H | -1.228696 | -1.698523 | -1.878723 |
| H | -0.472640 | -1.906370 | 0.000000 | H | -0.480515 | -2.607002 | 0.536819 |
| H | -2.076459 | -0.801631 | 0.000000 | H | -2.238133 | -2.228924 | 0.551291 |
| H | -1.218187 | 2.838379 | 1.207084 | H | -1.818786 | 1.467810 | 0.875398 |
| H | -2.642910 | 1.807588 | 1.173362 | H | -3.017105 | 0.195412 | 1.211288 |
| H | -2.642910 | 1.807588 | -1.173362 | H | -3.148602 | -0.316270 | -1.083522 |
| H | -1.218187 | 2.838379 | -1.207084 | H | -1.909935 | 0.909624 | -1.462874 |
| H | 1.307147 | -0.981881 | 1.381246 | H | 1.619847 | -1.483835 | 1.749693 |
| H | 2.282055 | 0.269309 | 2.127640 | H | 2.154326 | 0.203070 | 1.902806 |
| H | 2.282055 | 0.269309 | -2.127640 | H | 1.913667 | -1.259419 | -2.132774 |
| H | 1.307147 | -0.981881 | -1.381246 | H | 1.339097 | -2.353033 | -0.843752 |
| H | 3.407688 | 0.746600 | 0.000000 | H | 2.938792 | 0.248464 | -0.434674 |
| H | 3.321456 | -1.009919 | 0.000000 | H | 3.446225 | -1.382881 | 0.082533 |
| O | -0.296075 | -2.909153 | 0.000000 | O | 0.583738 | 2.713608 | 0.455240 |
| O | -1.482722 | -3.480537 | 0.000000 | O | 0.206151 | 2.947507 | -0.776852 |

| vdW R5-O2H |  |  |  | vdW R6-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.265931 | 0.180784 | 0.982522 | C | 0.102029 | -0.542138 | 0.411286 |
| C | -1.104927 | 1.184990 | 0.109529 | C | 0.309471 | 0.487352 | -0.764462 |
| C | -0.605528 | -1.201198 | 0.351366 | C | 1.526335 | -0.698270 | 0.984972 |
| C | -1.848639 | 0.248632 | -0.866123 | C | 1.824216 | 0.777248 | -0.703880 |
| C | -0.792096 | -0.841466 | -1.134071 | C | 2.101805 | 0.721369 | 0.811617 |
| C | -2.051133 | -1.553800 | 0.757963 | C | 2.372120 | -1.494315 | -0.030818 |
| C | -2.907630 | -0.545005 | -0.070830 | C | 2.576737 | -0.476575 | -1.196570 |
| C | 1.143234 | 0.669213 | 0.896101 | C | -0.942047 | 0.080163 | 1.366855 |
| C | -0.081942 | 2.146112 | -0.540054 | C | -0.613965 | 1.691076 | -0.465058 |
| C | 1.197109 | 2.045147 | 0.314343 | C | -1.533070 | 1.233419 | 0.621867 |
| H | -0.581883 | 0.174348 | 2.032879 | H | -0.271224 | -1.496908 | 0.042797 |
| H | -1.811179 | 1.748516 | 0.720262 | H | 0.041044 | 0.051692 | -1.726666 |
| H | 0.122962 | -1.977952 | 0.576416 | H | 1.548669 | -1.108368 | 1.993950 |
| H | -2.246458 | 0.758553 | -1.742618 | H | 2.115175 | 1.694612 | -1.214595 |
| H | 0.112215 | -0.471340 | -1.616298 | H | 1.573160 | 1.483617 | 1.384812 |
| H | -1.177244 | -1.672883 | -1.725466 | H | 3.163174 | 0.786270 | 1.054876 |
| H | -2.210510 | -1.460203 | 1.832432 | H | 1.871088 | -2.407670 | -0.352092 |
| H | -2.284330 | -2.583008 | 0.484166 | H | 3.327550 | -1.785382 | 0.406700 |
| H | -3.585004 | -1.068983 | -0.745522 | H | 3.634691 | -0.257926 | -1.344552 |
| H | -3.516565 | 0.104993 | 0.558277 | H | 2.185410 | -0.840624 | -2.146876 |
| H | 2.224761 | -0.404771 | -0.295186 | H | -0.467650 | 0.437393 | 2.293436 |
| H | 1.921138 | 0.290967 | 1.552895 | H | -1.693545 | -0.647111 | 1.684819 |
| H | -0.460019 | 3.166229 | -0.599357 | H | -1.143453 | 2.044186 | -1.354197 |
| H | 0.136016 | 1.830361 | -1.561869 | H | -0.029113 | 2.556024 | -0.117443 |
| H | 1.175848 | 2.787626 | 1.126884 | H | -2.869887 | 0.305674 | -0.283227 |
| H | 2.111928 | 2.251365 | -0.246447 | H | -2.252550 | 1.903429 | 1.080916 |
| O | 2.925179 | -0.932384 | -0.781539 | O | -3.576674 | -0.240775 | -0.758740 |
| O | 3.821474 | -1.251899 | 0.137049 | O | -3.557618 | -1.433585 | -0.193449 |

| tsR1-O2H |  |  |  | tsR2-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | -0.495616 | -0.721972 | 0.281931 | C | -0.033601 | -0.457722 | -0.577851 |
| C | -1.050496 | 0.182051 | -0.881492 | C | -1.548604 | 0.018249 | -0.475686 |
| C | 0.235132 | 0.300902 | 1.197450 | C | 0.642594 | 0.658162 | 0.201858 |
| C | -0.600814 | 1.601054 | -0.468777 | C | -1.460242 | 1.314773 | 0.367472 |
| C | -0.695605 | 1.539558 | 1.069280 | C | -0.306707 | 0.979534 | 1.354403 |
| C | 1.448394 | 0.807421 | 0.454666 | C | 0.700697 | 1.950431 | -0.601831 |
| C | 0.930320 | 1.705855 | -0.656832 | C | -0.799653 | 2.416804 | -0.499795 |
| C | -1.723725 | -1.428222 | 0.890681 | C | -0.004059 | -1.871197 | 0.040796 |
| C | -2.572515 | -0.068935 | -0.914223 | C | -2.297082 | -1.164603 | 0.176234 |
| C | -2.759882 | -1.436883 | -0.242466 | C | -1.435565 | -2.391804 | -0.161264 |
| H | 0.202670 | -1.470198 | -0.090442 | H | 0.323843 | -0.484011 | -1.620163 |
| H | -0.611268 | -0.093384 | -1.841171 | H | -1.964904 | 0.230724 | -1.476594 |
| H | -1.157865 | 2.400414 | -0.954728 | H | 2.022283 | 0.132363 | 0.537187 |
| H | -1.701305 | 1.360388 | 1.446882 | H | -2.418865 | 1.615394 | 0.822939 |
| H | -0.294474 | 2.426675 | 1.559906 | H | -0.522603 | 0.129512 | 2.019525 |
| H | 1.278851 | 2.733233 | -0.512092 | H | 0.009483 | 1.848655 | 1.955191 |
| H | 1.257647 | 1.404729 | -1.655742 | H | 1.032916 | 1.780371 | -1.637938 |
| H | -2.112476 | -0.861387 | 1.740257 | H | 1.376052 | 2.687946 | -0.136952 |
| H | -1.484230 | -2.426528 | 1.257053 | H | -0.869122 | 3.399300 | -0.003097 |
| H | -2.975917 | -0.033778 | -1.926419 | H | -1.279181 | 2.502891 | -1.489214 |
| H | -3.095946 | 0.697841 | -0.337034 | H | 0.219144 | -1.810994 | 1.121941 |
| H | -2.526383 | -2.234983 | -0.952031 | H | 0.772581 | -2.502171 | -0.418744 |
| H | -3.778102 | -1.605474 | 0.109862 | H | -3.337505 | -1.245873 | -0.180873 |
| H | 0.432815 | -0.062976 | 2.203247 | H | -2.334183 | -1.032296 | 1.273629 |
| H | 2.362047 | 1.060083 | 0.986568 | H | -1.583734 | -2.670667 | -1.221273 |
| O | 4.059961 | -1.049384 | -0.037079 | H | -1.671622 | -3.275911 | 0.454796 |
| O | 2.895433 | -1.171758 | -0.614016 | O | 3.190166 | -0.931244 | -0.495426 |
| H | 2.269621 | -0.410494 | -0.206676 | O | 2.994677 | -0.321381 | 0.627129 |

| tsR3-O2H |  |  |  | tsR4-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.752162 | 0.978413 | 0.788471 | C | 0.359874 | -0.027627 | 0.619729 |
| C | 0.752162 | 0.978413 | -0.788471 | C | 0.276664 | -0.440477 | -0.864324 |
| C | -0.728701 | 0.708246 | 1.138575 | C | -0.983137 | -0.379265 | 1.236379 |
| C | -0.728701 | 0.708246 | -1.138575 | C | -1.135100 | -1.066756 | -0.933677 |
| C | -1.175437 | -0.179715 | 0.000000 | C | -1.277344 | -1.700476 | 0.469204 |
| C | -1.542086 | 1.987998 | 0.782436 | C | -2.070070 | 0.548782 | 0.639713 |
| C | -1.542086 | 1.987998 | -0.782436 | C | -2.157655 | 0.091258 | -0.851442 |
| C | 1.765533 | -0.106447 | 1.205086 | C | 1.683493 | -0.508327 | 1.195575 |
| C | 1.765533 | -0.106447 | -1.205086 | C | 1.503649 | -1.359690 | -1.052092 |
| C | 2.706073 | -0.243658 | 0.000000 | C | 2.532966 | -0.790663 | -0.058381 |
| H | 1.062252 | 1.945438 | 1.186081 | H | 0.509983 | 1.428784 | 0.552775 |
| H | 1.062252 | 1.945438 | -1.186081 | H | 0.356776 | 0.432550 | -1.538805 |
| H | -0.898791 | 0.344851 | 2.149556 | H | -0.981402 | -0.437824 | 2.336372 |
| H | -0.898791 | 0.344851 | -2.149556 | H | -1.284100 | -1.741095 | -1.792896 |
| H | -0.586732 | -1.793564 | 0.000000 | H | -0.542904 | -2.497568 | 0.675314 |
| H | -2.143664 | -0.677107 | 0.000000 | H | -2.292465 | -2.085995 | 0.672740 |
| H | -1.083026 | 2.881350 | 1.207158 | H | -1.810286 | 1.613437 | 0.745078 |
| H | -2.556847 | 1.922115 | 1.173472 | H | -3.026981 | 0.382705 | 1.162871 |
| H | -2.556847 | 1.922115 | -1.173472 | H | -3.172024 | -0.267051 | -1.095553 |
| H | -1.083026 | 2.881350 | -1.207158 | H | -1.907020 | 0.904108 | -1.552443 |
| H | 1.256571 | -1.057251 | 1.381720 | H | 1.509585 | -1.445931 | 1.762807 |
| H | 2.288164 | 0.147996 | 2.127507 | H | 2.144757 | 0.210202 | 1.895891 |
| H | 2.288164 | 0.147996 | -2.127507 | H | 1.864052 | -1.375858 | -2.093939 |
| H | 1.256571 | -1.057251 | -1.381720 | H | 1.248627 | -2.397373 | -0.766030 |
| H | 3.434435 | 0.571888 | 0.000000 | H | 2.936337 | 0.161136 | -0.449986 |
| H | 3.266444 | -1.178833 | 0.000000 | H | 3.382523 | -1.466718 | 0.133969 |
| O | -0.422969 | -2.817981 | 0.000000 | O | 0.652874 | 2.518676 | 0.429818 |
| O | -1.608760 | -3.378228 | 0.000000 | O | 0.430188 | 2.779065 | -0.811350 |

| tsR5-O2H |  |  |  | tsR6-O2H |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | 0.237001 | -0.165886 | 0.984433 | C | 0.098941 | -0.585726 | 0.358764 |
| C | 0.969975 | -1.220224 | 0.075475 | C | 0.302567 | 0.527286 | -0.738603 |
| C | 0.694150 | 1.192704 | 0.381485 | C | 1.517324 | -0.754457 | 0.943354 |
| C | 1.783905 | -0.333088 | -0.889514 | C | 1.810240 | 0.841123 | -0.633807 |
| C | 0.829756 | 0.856133 | -1.115513 | C | 2.067074 | 0.684239 | 0.878301 |
| C | 2.171206 | 1.399905 | 0.775661 | C | 2.393694 | -1.461265 | -0.111810 |
| C | 2.921516 | 0.339256 | -0.090720 | C | 2.594684 | -0.360841 | -1.200641 |
| C | -1.220301 | -0.527853 | 0.919366 | C | -0.972117 | -0.051434 | 1.336303 |
| C | -0.146177 | -2.070928 | -0.571204 | C | -0.649199 | 1.687262 | -0.368551 |
| C | -1.373116 | -1.907047 | 0.343658 | C | -1.599032 | 1.122391 | 0.646093 |
| H | 0.564294 | -0.217023 | 2.029175 | H | -0.248954 | -1.519519 | -0.081510 |
| H | 1.629372 | -1.859500 | 0.664017 | H | 0.056310 | 0.155625 | -1.733065 |
| H | 0.043711 | 2.027790 | 0.634382 | H | 1.533235 | -1.233538 | 1.921596 |
| H | 2.121870 | -0.855482 | -1.783590 | H | 2.090380 | 1.797365 | -1.074471 |
| H | -0.109695 | 0.587432 | -1.596200 | H | 1.515634 | 1.394393 | 1.495135 |
| H | 1.285362 | 1.664539 | -1.688616 | H | 3.123389 | 0.751659 | 1.142014 |
| H | 2.334879 | 1.264121 | 1.845017 | H | 1.916054 | -2.359422 | -0.503783 |
| H | 2.494650 | 2.410236 | 0.524242 | H | 3.348359 | -1.763750 | 0.319594 |
| H | 3.635131 | 0.817063 | -0.762330 | H | 3.650078 | -0.112489 | -1.316459 |
| H | 3.476834 | -0.379505 | 0.512726 | H | 2.224228 | -0.664932 | -2.179933 |
| H | -2.002689 | 0.416096 | -0.089305 | H | -0.518659 | 0.275782 | 2.283325 |
| H | -1.901004 | -0.184747 | 1.695956 | H | -1.702280 | -0.818381 | 1.606907 |
| H | 0.147864 | -3.113433 | -0.689001 | H | -1.153854 | 2.110896 | -1.240409 |
| H | -0.381410 | -1.693227 | -1.568028 | H | -0.091699 | 2.522696 | 0.079180 |
| H | -1.341793 | -2.642375 | 1.160833 | H | -2.741548 | 0.354887 | -0.227435 |
| H | -2.324931 | -2.067218 | -0.166864 | H | -2.290318 | 1.771699 | 1.176007 |
| O | -2.648219 | 1.022840 | -0.702810 | O | -3.472964 | -0.185555 | -0.778342 |
| O | -3.711774 | 1.283086 | 0.002664 | O | -3.538963 | -1.383750 | -0.262046 |

|  | JP-10 |  |  |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 132.37 | 0.0112 |  |  |
| ν2 | 175.83 | 0.0024 |  |  |
| ν3 | 264.43 | 0.0613 |  |  |
| ν4 | 314.4 | 0.0388 |  |  |
| ν5 | 316.61 | 0.0535 |  |  |
| ν6 | 394.96 | 0.0293 |  |  |
| ν7 | 489.18 | 0.2313 |  |  |
| ν8 | 532.92 | 0.1785 |  |  |
| ν9 | 554.31 | 0.6264 |  |  |
| ν10 | 671.91 | 0.6036 |  |  |
| ν11 | 738.15 | 0.2999 |  |  |
| ν12 | 752.67 | 0.3414 |  |  |
| ν13 | 791.27 | 1.3181 |  |  |
| ν14 | 829.07 | 0.5855 |  |  |
| ν15 | 864.53 | 1.0142 |  |  |
| ν16 | 865.08 | 0.0232 |  |  |
| ν17 | 887.77 | 0.5934 |  |  |
| ν18 | 891.04 | 0.0758 |  |  |
| ν19 | 912.58 | 0.8196 |  |  |
| ν20 | 917.25 | 0.0674 |  |  |
| ν21 | 923.99 | 0.9959 |  |  |
| ν22 | 955.67 | 1.8485 |  |  |
| ν23 | 961.26 | 0.0214 |  |  |
| ν24 | 990.79 | 1.6513 |  |  |
| ν25 | 998.36 | 0.5391 |  |  |
| ν26 | 1042.02 | 0.2663 |  |  |
| ν27 | 1048.92 | 0.4814 |  |  |
| ν28 | 1052.57 | 0.0513 |  |  |
| ν29 | 1053.46 | 0.025 |  |  |
| ν30 | 1073.39 | 0.6124 |  |  |
| ν31 | 1137.02 | 0.1158 |  |  |
| ν32 | 1151.23 | 0.0064 |  |  |
| ν33 | 1169.34 | 1.0532 |  |  |
| ν34 | 1194.09 | 0.198 |  |  |
| ν35 | 1203.91 | 0.0851 |  |  |
| ν36 | 1207.67 | 1.4543 |  |  |
| ν37 | 1226.44 | 1.2542 |  |  |
| ν38 | 1253.48 | 0.0104 |  |  |
| ν39 | 1262.65 | 0.7486 |  |  |
| ν40 | 1292.21 | 1.2505 |  |  |
| ν41 | 1305.31 | 0.0002 |  |  |
| ν42 | 1307.75 | 0.2664 |  |  |
| ν43 | 1314.54 | 0.4983 |  |  |
| ν44 | 1320.92 | 0.0042 |  |  |
| ν45 | 1326.65 | 0.0641 |  |  |
| ν46 | 1333.18 | 1.0454 |  |  |
| ν47 | 1344.57 | 0.7653 |  |  |
| ν48 | 1352.54 | 0.9778 |  |  |
| ν49 | 1367.11 | 0.8201 |  |  |
| ν50 | 1371.99 | 0.4778 |  |  |
| ν51 | 1493.72 | 0.1473 |  |  |
| ν52 | 1495.36 | 2.3993 |  |  |
| ν53 | 1496.43 | 1.1264 |  |  |
| ν54 | 1502.51 | 6.5608 |  |  |
| ν55 | 1513.53 | 8.926 |  |  |
| ν56 | 1524.14 | 3.8204 |  |  |
| ν57 | 3016.21 | 16.8227 |  |  |
| ν58 | 3021.07 | 29.0278 |  |  |
| ν59 | 3024.72 | 24.1971 |  |  |
| ν60 | 3029.55 | 1.3904 |  |  |
| ν61 | 3034.93 | 24.4597 |  |  |
| ν62 | 3042.89 | 17.3718 |  |  |
| ν63 | 3044.74 | 82.9402 |  |  |
| ν64 | 3046.88 | 34.4594 |  |  |
| ν65 | 3063 | 5.8434 |  |  |
| ν66 | 3067.74 | 45.6645 |  |  |
| ν67 | 3070.4 | 31.8506 |  |  |
| ν68 | 3072.12 | 109.9999 |  |  |
| ν69 | 3076.4 | 45.4314 |  |  |
| ν70 | 3079.32 | 11.4533 |  |  |
| ν71 | 3085.88 | 99.6687 |  |  |
| ν72 | 3090.62 | 39.6989 |  |  |

|  | R1 |  | R2 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 144.14 | 0.0916 | 137.73 | 0.0767 |
| ν2 | 172.45 | 0.1305 | 173.99 | 0.0496 |
| ν3 | 267.5 | 7.2001 | 266.86 | 0.2483 |
| ν4 | 298 | 2.165 | 313.65 | 0.2096 |
| ν5 | 315.87 | 0.3488 | 316.41 | 0.2939 |
| ν6 | 366.1 | 5.5818 | 394.46 | 0.0744 |
| ν7 | 435.92 | 13.0759 | 492.3 | 0.599 |
| ν8 | 491.93 | 0.4299 | 522.52 | 0.7427 |
| ν9 | 547.4 | 0.0591 | 552.08 | 0.618 |
| ν10 | 566.54 | 3.3887 | 664.62 | 1.1613 |
| ν11 | 671.19 | 0.5024 | 713.45 | 0.1548 |
| ν12 | 743.93 | 0.6185 | 749.37 | 0.269 |
| ν13 | 763.34 | 0.2909 | 769.77 | 0.6977 |
| ν14 | 791.79 | 1.5729 | 824.04 | 0.4542 |
| ν15 | 861.88 | 0.2907 | 834.7 | 3.756 |
| ν16 | 863.91 | 0.3945 | 853.7 | 0.4236 |
| ν17 | 886.39 | 0.5003 | 871.01 | 0.181 |
| ν18 | 900.77 | 1.2501 | 882.7 | 0.3417 |
| ν19 | 907.54 | 0.486 | 908.99 | 1.6557 |
| ν20 | 912.59 | 0.8491 | 915.2 | 0.2637 |
| ν21 | 932.46 | 0.1256 | 928.22 | 1.3881 |
| ν22 | 935.22 | 0.2481 | 947.59 | 1.3123 |
| ν23 | 955.54 | 2.0572 | 966.65 | 0.5089 |
| ν24 | 978.33 | 0.7943 | 991.39 | 0.7622 |
| ν25 | 994.17 | 1.0163 | 1002.8 | 1.6883 |
| ν26 | 1008.42 | 1.4141 | 1037.72 | 0.4684 |
| ν27 | 1032.36 | 0.0319 | 1048.55 | 0.1456 |
| ν28 | 1040.72 | 0.7618 | 1059.42 | 0.1583 |
| ν29 | 1049.02 | 0.026 | 1083.87 | 0.1635 |
| ν30 | 1069.1 | 0.6036 | 1093.98 | 0.1091 |
| ν31 | 1119.32 | 0.4389 | 1140.49 | 1.0979 |
| ν32 | 1142.62 | 0.2572 | 1163.29 | 0.1783 |
| ν33 | 1154.7 | 0.6472 | 1190.06 | 0.1626 |
| ν34 | 1184.65 | 0.7262 | 1196.93 | 0.6595 |
| ν35 | 1193.68 | 0.3631 | 1207.64 | 4.6767 |
| ν36 | 1207.11 | 0.1274 | 1217.27 | 1.3779 |
| ν37 | 1231.32 | 1.2258 | 1233.13 | 1.5708 |
| ν38 | 1251.86 | 0.8086 | 1255.58 | 0.9227 |
| ν39 | 1272.11 | 0.402 | 1262.96 | 0.6151 |
| ν40 | 1283.04 | 1.9516 | 1292 | 1.6531 |
| ν41 | 1302.23 | 0.1749 | 1301.77 | 0.6656 |
| ν42 | 1306.89 | 0.1404 | 1308.57 | 0.2938 |
| ν43 | 1319.51 | 0.3661 | 1315.41 | 0.7123 |
| ν44 | 1324.17 | 0.3823 | 1321.25 | 1.0947 |
| ν45 | 1336.03 | 1.3279 | 1335.26 | 0.4959 |
| ν46 | 1343.25 | 0.9062 | 1343.39 | 0.3136 |
| ν47 | 1345.69 | 0.5726 | 1358.6 | 0.4468 |
| ν48 | 1359.53 | 1.1246 | 1372.6 | 0.762 |
| ν49 | 1366.83 | 0.4175 | 1490.52 | 1.0101 |
| ν50 | 1473.74 | 3.8526 | 1492.99 | 0.0972 |
| ν51 | 1494.17 | 1.621 | 1496.24 | 2.5589 |
| ν52 | 1495.91 | 2.5165 | 1500.85 | 7.364 |
| ν53 | 1505.73 | 5.1738 | 1511.11 | 6.8655 |
| ν54 | 1518.41 | 7.6693 | 1522.39 | 5.5066 |
| ν55 | 2962.7 | 47.8864 | 3017.6 | 23.3304 |
| ν56 | 3005.25 | 27.6022 | 3024.99 | 27.5936 |
| ν57 | 3017.44 | 18.3495 | 3034.22 | 16.5652 |
| ν58 | 3023.01 | 31.5333 | 3036.72 | 13.5793 |
| ν59 | 3026.27 | 24.7536 | 3038.81 | 18.3207 |
| ν60 | 3036.08 | 8.3388 | 3047.68 | 47.047 |
| ν61 | 3051.88 | 48.6339 | 3052.82 | 49.4094 |
| ν62 | 3053.71 | 10.7873 | 3057.79 | 27.5609 |
| ν63 | 3067.94 | 38.65 | 3067.8 | 42.5488 |
| ν64 | 3072.11 | 42.4071 | 3071.04 | 33.7399 |
| ν65 | 3078.2 | 81.4318 | 3073.07 | 56.3947 |
| ν66 | 3079.83 | 96.0844 | 3074.57 | 13.1348 |
| ν67 | 3083.68 | 6.6638 | 3083.2 | 53.6511 |
| ν68 | 3096.52 | 33.3638 | 3094.52 | 74.4557 |
| ν69 | 3192.55 | 22.4166 | 3108.19 | 32.335 |

|  | R3 |  | R4 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 112.75 | 0.0013 | 118.71 | 0.0982 |
| ν2 | 178.4 | 0.1225 | 156.58 | 0.1601 |
| ν3 | 251.42 | 0.037 | 234.82 | 0.4595 |
| ν4 | 300.12 | 1.3246 | 281.27 | 0.2846 |
| ν5 | 314.22 | 0.0548 | 314.04 | 0.0844 |
| ν6 | 333.29 | 8.0965 | 383.13 | 0.0241 |
| ν7 | 423.63 | 5.0365 | 482.08 | 0.6028 |
| ν8 | 532.05 | 0.5301 | 538.75 | 0.2116 |
| ν9 | 544.12 | 0.9831 | 560.16 | 1.0979 |
| ν10 | 665.9 | 13.1529 | 620.83 | 3.3064 |
| ν11 | 671.51 | 0.2193 | 719.6 | 0.077 |
| ν12 | 737.38 | 1.3347 | 737.1 | 0.2361 |
| ν13 | 762.63 | 0.6053 | 795.28 | 1.9847 |
| ν14 | 791.98 | 0.8512 | 825.7 | 0.7923 |
| ν15 | 831.42 | 1.563 | 843.08 | 0.17 |
| ν16 | 850.8 | 0.3443 | 872.27 | 0.7838 |
| ν17 | 867.47 | 0.0807 | 878.75 | 0.5798 |
| ν18 | 872.88 | 1.1343 | 886.89 | 0.3659 |
| ν19 | 909 | 0.0569 | 891.39 | 0.6118 |
| ν20 | 915.01 | 1.9186 | 903.4 | 0.2422 |
| ν21 | 921.14 | 0.0378 | 915.97 | 0.8334 |
| ν22 | 947.82 | 1.3689 | 954.23 | 0.079 |
| ν23 | 947.98 | 0.134 | 957.47 | 2.9678 |
| ν24 | 987.98 | 1.5697 | 987.35 | 1.1165 |
| ν25 | 990.03 | 0.0979 | 1014.5 | 0.2568 |
| ν26 | 992.66 | 0.997 | 1036.96 | 0.0286 |
| ν27 | 1036.21 | 0.1587 | 1043.09 | 1.0385 |
| ν28 | 1048.32 | 0.092 | 1058.67 | 0.1445 |
| ν29 | 1055.38 | 0.1271 | 1090.39 | 1.1632 |
| ν30 | 1072.28 | 0.6894 | 1122.98 | 0.4735 |
| ν31 | 1152.62 | 0.3515 | 1131.23 | 0.137 |
| ν32 | 1163.64 | 1.0785 | 1148.93 | 0.1773 |
| ν33 | 1187.04 | 0.9747 | 1165.15 | 0.6424 |
| ν34 | 1191.49 | 0.2726 | 1189.63 | 1.8604 |
| ν35 | 1203.2 | 0.3981 | 1205.61 | 1.3702 |
| ν36 | 1205.53 | 0.3846 | 1221.96 | 1.0038 |
| ν37 | 1237.15 | 1.1689 | 1230.18 | 0.3143 |
| ν38 | 1246.11 | 0.0073 | 1249.07 | 0.3255 |
| ν39 | 1260.48 | 1.5996 | 1252.11 | 0.5066 |
| ν40 | 1277.88 | 0.0043 | 1285.64 | 1.1026 |
| ν41 | 1301.24 | 0.0147 | 1303.8 | 0.6094 |
| ν42 | 1308.16 | 0.3664 | 1309.86 | 0.2144 |
| ν43 | 1316.38 | 0.007 | 1312.03 | 0.1984 |
| ν44 | 1328.09 | 0.1424 | 1324.56 | 1.122 |
| ν45 | 1332.26 | 0.4739 | 1337.28 | 0.5783 |
| ν46 | 1345.31 | 0.5263 | 1341.01 | 1.2093 |
| ν47 | 1346.75 | 0.3768 | 1350.3 | 0.0196 |
| ν48 | 1363.3 | 2.1732 | 1363.06 | 0.3218 |
| ν49 | 1366.74 | 0.4244 | 1474.48 | 3.1552 |
| ν50 | 1489.61 | 3.0274 | 1491.73 | 0.3539 |
| ν51 | 1492.68 | 0.6336 | 1493.77 | 1.4779 |
| ν52 | 1494.24 | 5.2637 | 1499.83 | 5.8859 |
| ν53 | 1508.07 | 0.7402 | 1507.59 | 7.0511 |
| ν54 | 1509.95 | 6.5107 | 1520.41 | 2.1935 |
| ν55 | 3014.87 | 20.9594 | 2955.29 | 36.2429 |
| ν56 | 3020.93 | 32.1861 | 2976.34 | 27.4842 |
| ν57 | 3024.68 | 22.8561 | 3011.5 | 21.9143 |
| ν58 | 3029.64 | 7.1275 | 3023.08 | 14.2887 |
| ν59 | 3033.54 | 28.0222 | 3033.31 | 52.8643 |
| ν60 | 3041.28 | 15.2047 | 3036.15 | 26.4074 |
| ν61 | 3046.42 | 88.4567 | 3036.66 | 41.546 |
| ν62 | 3065.25 | 0.0936 | 3047.21 | 64.4467 |
| ν63 | 3067.92 | 38.5508 | 3069.7 | 13.186 |
| ν64 | 3070.38 | 50.0545 | 3070.4 | 54.6294 |
| ν65 | 3077.91 | 61.4707 | 3079.35 | 61.0943 |
| ν66 | 3086.04 | 65.1896 | 3079.7 | 37.7455 |
| ν67 | 3090.49 | 74.4246 | 3084.8 | 44.56 |
| ν68 | 3093.56 | 14.3785 | 3090.44 | 22.6704 |
| ν69 | 3185.75 | 18.6547 | 3093.15 | 61.0325 |

|  | R5 |  | R6 |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 117.54 | 0.078 | 44.39 | 0.9717 |
| ν2 | 130.03 | 0.2488 | 105.48 | 0.001 |
| ν3 | 260.81 | 0.2589 | 256.3 | 0.017 |
| ν4 | 278.81 | 0.4121 | 257.55 | 0.7199 |
| ν5 | 314.66 | 0.4143 | 323.58 | 0 |
| ν6 | 393.11 | 0.5897 | 389.9 | 17.5186 |
| ν7 | 423.72 | 19.2794 | 395.34 | 6.8536 |
| ν8 | 497.02 | 1.0396 | 494.33 | 0.1102 |
| ν9 | 534 | 0.1252 | 527.9 | 0.0025 |
| ν10 | 627.67 | 0.5817 | 693.96 | 0.3037 |
| ν11 | 737.25 | 0.0973 | 718.94 | 0.4832 |
| ν12 | 749.56 | 1.4282 | 729.5 | 0.1642 |
| ν13 | 765.25 | 0.9295 | 764.56 | 0.0285 |
| ν14 | 795.78 | 0.7469 | 796.61 | 1.0192 |
| ν15 | 830.66 | 0.3578 | 829.04 | 0.7482 |
| ν16 | 845.15 | 0.4212 | 835.9 | 0.4135 |
| ν17 | 869.45 | 0.9338 | 887.43 | 0.4564 |
| ν18 | 886.7 | 0.658 | 889.07 | 0.812 |
| ν19 | 904.13 | 0.2894 | 908.77 | 0.7099 |
| ν20 | 921.91 | 0.0814 | 924.6 | 1.0064 |
| ν21 | 924.93 | 1.3023 | 936.59 | 0.4479 |
| ν22 | 947.98 | 1.3356 | 941.94 | 0.9111 |
| ν23 | 960.55 | 0.1525 | 962.31 | 0.0613 |
| ν24 | 977.33 | 1.585 | 964.3 | 1.2647 |
| ν25 | 1000.35 | 0.8711 | 1012.62 | 1.6014 |
| ν26 | 1018.04 | 0.38 | 1019.76 | 0.0168 |
| ν27 | 1046.88 | 0.4199 | 1043.6 | 0.5475 |
| ν28 | 1050.01 | 0.1124 | 1055.13 | 0.7413 |
| ν29 | 1063.81 | 0.3506 | 1059.14 | 0.3877 |
| ν30 | 1073.9 | 1.1094 | 1082.78 | 0.0481 |
| ν31 | 1118.89 | 0.0402 | 1127.43 | 0.478 |
| ν32 | 1141.4 | 0.2253 | 1139.44 | 0.6212 |
| ν33 | 1159.52 | 0.7048 | 1146.52 | 0.1233 |
| ν34 | 1183.37 | 0.2825 | 1174.32 | 0.6634 |
| ν35 | 1206.14 | 2.6552 | 1199.12 | 0.0617 |
| ν36 | 1217 | 0.8212 | 1210.9 | 1.252 |
| ν37 | 1229.67 | 0.5063 | 1230.86 | 1.4038 |
| ν38 | 1246.93 | 0.0596 | 1251.82 | 0.0033 |
| ν39 | 1278.47 | 0.3802 | 1267.67 | 0.0054 |
| ν40 | 1286.32 | 1.0909 | 1293.03 | 1.0358 |
| ν41 | 1295.15 | 0.122 | 1301.71 | 0.1589 |
| ν42 | 1299.97 | 0.3742 | 1305.94 | 0.1114 |
| ν43 | 1311.11 | 0.3983 | 1309.85 | 0.4764 |
| ν44 | 1319.79 | 0.968 | 1322.05 | 0.3622 |
| ν45 | 1322.92 | 1.3454 | 1328.56 | 2.0577 |
| ν46 | 1334.76 | 2.2571 | 1347.86 | 0.085 |
| ν47 | 1348.15 | 0.7248 | 1354.3 | 2.4838 |
| ν48 | 1361.49 | 1.0143 | 1364.48 | 0.0572 |
| ν49 | 1370.92 | 1.212 | 1377.57 | 1.3146 |
| ν50 | 1472.81 | 1.8999 | 1471.5 | 5.5625 |
| ν51 | 1494.92 | 1.0556 | 1474.42 | 1.8097 |
| ν52 | 1496.09 | 3.1172 | 1494.93 | 1.0178 |
| ν53 | 1507.38 | 10.2599 | 1503.57 | 8.3837 |
| ν54 | 1520.71 | 2.8065 | 1522.32 | 3.4532 |
| ν55 | 2915.82 | 48.3636 | 2932.28 | 37.7165 |
| ν56 | 2948.9 | 37.5495 | 2934.23 | 29.0825 |
| ν57 | 3022.4 | 28.5809 | 2983.45 | 37.9977 |
| ν58 | 3034.74 | 26.2904 | 2983.63 | 26.3922 |
| ν59 | 3040.46 | 24.6668 | 3034.46 | 20.1696 |
| ν60 | 3043.34 | 20.5903 | 3043.05 | 46.2238 |
| ν61 | 3044.25 | 74.3395 | 3044.88 | 17.4481 |
| ν62 | 3046.6 | 30.0892 | 3045.28 | 45.6163 |
| ν63 | 3062.85 | 4.5672 | 3060.42 | 53.313 |
| ν64 | 3074.43 | 62.3167 | 3063.07 | 9.496 |
| ν65 | 3077.52 | 56.994 | 3073.14 | 86.2422 |
| ν66 | 3083.26 | 25.8908 | 3079.75 | 4.2022 |
| ν67 | 3086.63 | 73.6727 | 3084.8 | 46.3141 |
| ν68 | 3090.17 | 31.1567 | 3086.94 | 69.297 |
| ν69 | 3173.89 | 24.6839 | 3179.57 | 31.2055 |

|  | vdW R1-OH |  | vdW R2-OH |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 34.67 | 2.2341 | 29.5 | 1.6018 |
| ν2 | 49.18 | 2.7602 | 33.41 | 1.9271 |
| ν3 | 110.54 | 0.3226 | 117.35 | 0.0673 |
| ν4 | 147.99 | 0.7535 | 136.44 | 0.0516 |
| ν5 | 178.8 | 0.5656 | 174.92 | 0.0433 |
| ν6 | 292.87 | 1.1954 | 265.13 | 0.3102 |
| ν7 | 314.18 | 0.9586 | 312.68 | 0.1121 |
| ν8 | 320.57 | 2.5221 | 315.88 | 0.1015 |
| ν9 | 388.71 | 0.4457 | 394.28 | 0.0995 |
| ν10 | 476.03 | 60.2942 | 489.65 | 3.2687 |
| ν11 | 489.42 | 36.4313 | 513.19 | 25.0076 |
| ν12 | 499.34 | 29.1939 | 537.77 | 40.8873 |
| ν13 | 542.39 | 35.179 | 549.79 | 29.0164 |
| ν14 | 552.08 | 4.7228 | 556 | 29.8317 |
| ν15 | 618.08 | 31.9418 | 662.57 | 1.2422 |
| ν16 | 671.79 | 0.5105 | 710.26 | 0.3886 |
| ν17 | 743.73 | 1.5346 | 749.83 | 0.2754 |
| ν18 | 766.09 | 0.3978 | 770.46 | 0.9756 |
| ν19 | 793.9 | 1.7245 | 825.14 | 0.7536 |
| ν20 | 861 | 1.6552 | 837.86 | 1.5367 |
| ν21 | 863.48 | 0.3244 | 855.16 | 0.5558 |
| ν22 | 887.56 | 0.591 | 870.69 | 0.3188 |
| ν23 | 901.62 | 1.2749 | 884.07 | 0.3658 |
| ν24 | 907.25 | 0.4466 | 909.19 | 1.7766 |
| ν25 | 912.21 | 0.4658 | 914.52 | 0.1815 |
| ν26 | 931.41 | 0.3592 | 930 | 1.448 |
| ν27 | 933.55 | 0.3333 | 949.06 | 0.7645 |
| ν28 | 954.94 | 3.9593 | 968.1 | 0.2518 |
| ν29 | 980.61 | 0.7543 | 991.2 | 0.7287 |
| ν30 | 998.21 | 1.6943 | 1003.84 | 1.7231 |
| ν31 | 1009.34 | 1.6054 | 1037.64 | 0.5651 |
| ν32 | 1032.76 | 0.0488 | 1048.3 | 0.1524 |
| ν33 | 1041.18 | 1.0015 | 1061.28 | 0.1915 |
| ν34 | 1049.8 | 0.0157 | 1084.85 | 0.2919 |
| ν35 | 1073.16 | 1.7395 | 1094.16 | 0.1141 |
| ν36 | 1126.29 | 0.8699 | 1142.1 | 1.8982 |
| ν37 | 1147.79 | 0.1996 | 1165.49 | 1.0857 |
| ν38 | 1156.86 | 0.777 | 1191.36 | 0.3022 |
| ν39 | 1185.42 | 0.5803 | 1198.09 | 0.9587 |
| ν40 | 1194.79 | 0.3792 | 1207.56 | 6.0398 |
| ν41 | 1207.92 | 0.2427 | 1219.36 | 1.4835 |
| ν42 | 1232.08 | 1.5779 | 1236.19 | 1.8953 |
| ν43 | 1253.23 | 1.0518 | 1256.96 | 0.9031 |
| ν44 | 1272.75 | 0.3841 | 1263.91 | 0.424 |
| ν45 | 1285.66 | 2.3056 | 1293.21 | 2.069 |
| ν46 | 1302.57 | 0.2267 | 1302.32 | 1.0444 |
| ν47 | 1308.45 | 0.4104 | 1310.44 | 0.3604 |
| ν48 | 1320.84 | 0.6729 | 1317.12 | 0.5485 |
| ν49 | 1325.59 | 0.6556 | 1323.45 | 0.9846 |
| ν50 | 1334.04 | 1.8021 | 1336.73 | 0.5393 |
| ν51 | 1343.37 | 0.7713 | 1344.22 | 0.314 |
| ν52 | 1346.71 | 0.4965 | 1359.45 | 0.632 |
| ν53 | 1360.97 | 1.2283 | 1374.18 | 0.3956 |
| ν54 | 1368.12 | 0.6324 | 1491.14 | 1.3246 |
| ν55 | 1469 | 5.1656 | 1493.64 | 0.23 |
| ν56 | 1495.34 | 1.9362 | 1495.39 | 2.7309 |
| ν57 | 1496.68 | 2.804 | 1501.61 | 7.6312 |
| ν58 | 1507.89 | 3.3919 | 1511.24 | 6.4151 |
| ν59 | 1522.33 | 9.5702 | 1523.31 | 6.9196 |
| ν60 | 2977.92 | 30.7494 | 3019.74 | 21.4966 |
| ν61 | 3019.46 | 19.1784 | 3027.02 | 27.6727 |
| ν62 | 3023.32 | 14.6018 | 3039.54 | 13.3643 |
| ν63 | 3025.67 | 31.3902 | 3041.82 | 7.3922 |
| ν64 | 3029.54 | 24.3785 | 3044.53 | 22.649 |
| ν65 | 3037.12 | 8.4382 | 3054.15 | 32.5557 |
| ν66 | 3052.33 | 37.4339 | 3058.96 | 42.6635 |
| ν67 | 3062.04 | 11.9571 | 3064.53 | 17.7147 |
| ν68 | 3071.04 | 38.6185 | 3072.64 | 30.0775 |
| ν69 | 3075.12 | 41.8223 | 3076.27 | 48.2444 |
| ν70 | 3082.76 | 75.6567 | 3077.27 | 48.0084 |
| ν71 | 3082.98 | 69.6326 | 3081.03 | 11.4474 |
| ν72 | 3087.83 | 10.1442 | 3089.09 | 47.5226 |
| ν73 | 3106.56 | 24.638 | 3101.57 | 57.0882 |
| ν74 | 3162.29 | 20.1079 | 3116.67 | 26.0955 |
| ν75 | 3386.25 | 299.2574 | 3243.95 | 297.4061 |
|  | vdW R3-OH |  | vdW R4-OH |  |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 31.96 | 1.9521 | 33.58 | 1.6595 |
| ν2 | 51.24 | 2.627 | 49.67 | 2.363 |
| ν3 | 102.34 | 0.1827 | 116.68 | 0.0735 |
| ν4 | 117.05 | 0.2951 | 124.83 | 0.1713 |
| ν5 | 184.08 | 0.7473 | 167.07 | 0.6637 |
| ν6 | 257.78 | 0.0129 | 249.65 | 1.196 |
| ν7 | 309.33 | 0.8064 | 284.58 | 0.3864 |
| ν8 | 314.58 | 0.1619 | 314.04 | 0.5603 |
| ν9 | 391.74 | 2.6605 | 385.75 | 0.0127 |
| ν10 | 426.24 | 9.925 | 484.43 | 0.7529 |
| ν11 | 452.62 | 54.6468 | 515.3 | 58.2087 |
| ν12 | 506.86 | 86.4264 | 531.36 | 29.4202 |
| ν13 | 531.47 | 0.2534 | 548.53 | 41.024 |
| ν14 | 553.1 | 2.0794 | 558.26 | 1.9571 |
| ν15 | 664.35 | 1.8755 | 636.23 | 5.0957 |
| ν16 | 717.92 | 12.7592 | 719.4 | 0.1844 |
| ν17 | 740.53 | 0.5144 | 738.18 | 0.5997 |
| ν18 | 766.2 | 12.6196 | 793.6 | 2.3261 |
| ν19 | 789.45 | 0.8442 | 827.39 | 1.0255 |
| ν20 | 840.48 | 2.5554 | 847.23 | 0.1073 |
| ν21 | 846.05 | 0.6727 | 872.92 | 0.8435 |
| ν22 | 867.19 | 0.5757 | 877.67 | 0.9114 |
| ν23 | 883.39 | 0.9571 | 887.11 | 0.5044 |
| ν24 | 893.08 | 0.804 | 893.91 | 0.4327 |
| ν25 | 914.53 | 0.0446 | 903.92 | 0.08 |
| ν26 | 914.65 | 2.2032 | 916.92 | 0.8357 |
| ν27 | 943.14 | 1.4322 | 955.09 | 0.9419 |
| ν28 | 980.9 | 0.4579 | 958.24 | 2.4491 |
| ν29 | 982.74 | 1.4369 | 988.9 | 1.1862 |
| ν30 | 985.12 | 0.0233 | 1014.62 | 0.4707 |
| ν31 | 1010.62 | 0.9248 | 1038.58 | 0.0252 |
| ν32 | 1035.86 | 0.4501 | 1045.09 | 1.2739 |
| ν33 | 1045.36 | 0.1284 | 1059.48 | 0.0296 |
| ν34 | 1056.27 | 0.1295 | 1087.59 | 1.1826 |
| ν35 | 1072.79 | 0.7356 | 1122.81 | 0.2192 |
| ν36 | 1151.31 | 1.0893 | 1134.46 | 0.2442 |
| ν37 | 1171.35 | 1.8807 | 1154.85 | 0.6179 |
| ν38 | 1180.95 | 0.6504 | 1163.01 | 1.027 |
| ν39 | 1192.01 | 0.4109 | 1187.1 | 2.6156 |
| ν40 | 1201.91 | 0.3459 | 1205.6 | 1.6855 |
| ν41 | 1217.08 | 0.2159 | 1223.6 | 1.4885 |
| ν42 | 1234.72 | 0.1017 | 1231.16 | 0.2773 |
| ν43 | 1253.37 | 2.2294 | 1250.68 | 0.2709 |
| ν44 | 1260.49 | 0.9991 | 1254.25 | 1.1011 |
| ν45 | 1275.92 | 0.1441 | 1286.71 | 1.1869 |
| ν46 | 1301.5 | 0.0205 | 1303.46 | 0.2171 |
| ν47 | 1305.51 | 0.4978 | 1310.4 | 0.2546 |
| ν48 | 1317.15 | 0.1382 | 1313.08 | 0.0976 |
| ν49 | 1327.21 | 0.241 | 1326.43 | 1.3336 |
| ν50 | 1334.73 | 0.5237 | 1340.01 | 0.6236 |
| ν51 | 1344.52 | 0.6845 | 1341.49 | 0.5137 |
| ν52 | 1344.88 | 0.4008 | 1350.04 | 0.4063 |
| ν53 | 1360.96 | 0.2253 | 1358.03 | 0.3873 |
| ν54 | 1365.76 | 2.5 | 1470.22 | 6.5338 |
| ν55 | 1475.63 | 0.0938 | 1492.38 | 0.8626 |
| ν56 | 1493.92 | 2.8922 | 1497.97 | 1.7781 |
| ν57 | 1496.33 | 5.1057 | 1501.44 | 5.4227 |
| ν58 | 1510.91 | 2.7605 | 1508.57 | 8.0771 |
| ν59 | 1514.85 | 7.0096 | 1522.89 | 2.4138 |
| ν60 | 3017.49 | 13.9449 | 2964.96 | 26.208 |
| ν61 | 3020.97 | 28.8017 | 2987.99 | 17.0751 |
| ν62 | 3026.64 | 31.4963 | 3024.59 | 21.394 |
| ν63 | 3032.42 | 0.0662 | 3027.62 | 3.4462 |
| ν64 | 3043.82 | 31.5081 | 3040.08 | 40.4197 |
| ν65 | 3045.44 | 22.3587 | 3041.84 | 27.6185 |
| ν66 | 3054.7 | 64.9224 | 3042.55 | 35.6 |
| ν67 | 3071.91 | 38.2749 | 3052.44 | 51.1791 |
| ν68 | 3074.3 | 30.9074 | 3075.86 | 3.4809 |
| ν69 | 3075.53 | 15.3445 | 3077.12 | 58.084 |
| ν70 | 3081.37 | 60.0786 | 3083.84 | 59.7234 |
| ν71 | 3095.09 | 62.2718 | 3085.3 | 25.8482 |
| ν72 | 3095.56 | 18.4366 | 3089.08 | 39.1889 |
| ν73 | 3099.19 | 33.1865 | 3094.7 | 24.5872 |
| ν74 | 3169.4 | 13.605 | 3100.58 | 36.8133 |
| ν75 | 3372.37 | 275.5598 | 3324.28 | 281.8576 |
|  | vdW R5-OH |  | vdW R6-OH |  |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 31.84 | 1.7789 | 29.17 | 2.2935 |
| ν2 | 48.34 | 1.8513 | 31.16 | 2.3311 |
| ν3 | 95.14 | 0.2494 | 98.34 | 0.2037 |
| ν4 | 132.81 | 0.2407 | 119.72 | 0.1593 |
| ν5 | 159.09 | 2.5202 | 172.36 | 5.4222 |
| ν6 | 264.03 | 0.2642 | 258 | 0.2089 |
| ν7 | 296.12 | 1.736 | 274.79 | 1.2496 |
| ν8 | 315.19 | 1.4068 | 320.35 | 1.0875 |
| ν9 | 394.75 | 1.1806 | 393.65 | 4.338 |
| ν10 | 431.82 | 85.1826 | 441.63 | 56.5173 |
| ν11 | 438.28 | 59.2958 | 452.62 | 47.1751 |
| ν12 | 495.22 | 11.1572 | 489.47 | 10.2232 |
| ν13 | 533.15 | 6.5314 | 533.41 | 0.0637 |
| ν14 | 541.69 | 21.7777 | 534.42 | 62.0755 |
| ν15 | 636.4 | 3.8224 | 691.22 | 1.6782 |
| ν16 | 737.16 | 0.2874 | 691.5 | 1.3417 |
| ν17 | 746.34 | 0.96 | 731.46 | 0.2608 |
| ν18 | 775.61 | 2.856 | 775.96 | 0.4837 |
| ν19 | 797.64 | 0.4546 | 796.32 | 0.6349 |
| ν20 | 829.98 | 0.3954 | 828.32 | 0.7722 |
| ν21 | 848.68 | 0.3419 | 844.53 | 0.6844 |
| ν22 | 869.84 | 1.7206 | 886.48 | 0.5198 |
| ν23 | 887.03 | 0.6403 | 888.23 | 0.4033 |
| ν24 | 903.65 | 0.2831 | 912.2 | 0.6834 |
| ν25 | 920.65 | 0.4237 | 923.44 | 1.1716 |
| ν26 | 924.38 | 1.4443 | 927.01 | 0.7851 |
| ν27 | 947.71 | 1.0358 | 950.21 | 1.2157 |
| ν28 | 960.99 | 0.1207 | 961.99 | 0.0178 |
| ν29 | 980.49 | 1.177 | 965.07 | 1.1607 |
| ν30 | 998.75 | 1.0993 | 1007.23 | 3.8437 |
| ν31 | 1016.82 | 1.0084 | 1023.74 | 0.0027 |
| ν32 | 1046 | 0.1423 | 1043.88 | 0.6649 |
| ν33 | 1050.24 | 0.1047 | 1052.74 | 0.5806 |
| ν34 | 1060.42 | 0.8123 | 1058.12 | 0.3018 |
| ν35 | 1071.54 | 1.821 | 1068.42 | 0.4481 |
| ν36 | 1122.22 | 0.203 | 1129.98 | 0.7868 |
| ν37 | 1143.88 | 0.4023 | 1145.37 | 0.0085 |
| ν38 | 1161.3 | 0.5363 | 1150.8 | 1.0968 |
| ν39 | 1184.8 | 1.1546 | 1182.97 | 0.4464 |
| ν40 | 1204.93 | 2.8879 | 1196.81 | 0.1123 |
| ν41 | 1217.82 | 0.4363 | 1211.93 | 1.3274 |
| ν42 | 1227.86 | 0.3336 | 1232.95 | 1.6353 |
| ν43 | 1247.74 | 0.1595 | 1249.9 | 0.1381 |
| ν44 | 1277.56 | 0.8224 | 1263.47 | 0.5344 |
| ν45 | 1288.37 | 1.4109 | 1292.83 | 0.8666 |
| ν46 | 1295.44 | 1.4265 | 1307.18 | 0.0641 |
| ν47 | 1300.99 | 0.3541 | 1307.58 | 0.1685 |
| ν48 | 1313.69 | 0.6619 | 1307.69 | 0.1179 |
| ν49 | 1318.98 | 1.3908 | 1322.19 | 0.7117 |
| ν50 | 1323.81 | 0.1712 | 1326.87 | 2.7391 |
| ν51 | 1335.53 | 2.5229 | 1343.71 | 0.0073 |
| ν52 | 1348.64 | 1.7499 | 1353.14 | 3.22 |
| ν53 | 1362.39 | 0.5999 | 1366.28 | 0.0893 |
| ν54 | 1368.95 | 0.9293 | 1373.46 | 0.6594 |
| ν55 | 1468.43 | 5.5208 | 1463.06 | 5.0912 |
| ν56 | 1495.16 | 1.2143 | 1471.13 | 2.7258 |
| ν57 | 1498.47 | 2.1661 | 1495.65 | 1.0964 |
| ν58 | 1508.6 | 12.202 | 1504.23 | 9.7094 |
| ν59 | 1523.49 | 2.7833 | 1523.12 | 3.7739 |
| ν60 | 2929.3 | 32.48 | 2932.18 | 16.6271 |
| ν61 | 2963.89 | 28.3246 | 2934.89 | 27.634 |
| ν62 | 3029.3 | 16.1912 | 3018.03 | 28.1619 |
| ν63 | 3037.41 | 24.8631 | 3019.06 | 16.7718 |
| ν64 | 3045.16 | 21.156 | 3037.45 | 19.9857 |
| ν65 | 3045.5 | 6.9261 | 3044.5 | 39.0211 |
| ν66 | 3047.78 | 94.6336 | 3047.81 | 49.3061 |
| ν67 | 3050.2 | 12.5271 | 3053.62 | 16.5938 |
| ν68 | 3065.7 | 4.1386 | 3066.9 | 15.2941 |
| ν69 | 3078.25 | 69.9068 | 3069.02 | 33.317 |
| ν70 | 3082.63 | 24.9538 | 3074.01 | 80.3611 |
| ν71 | 3085.14 | 18.7127 | 3081.54 | 2.2359 |
| ν72 | 3088.8 | 80.0611 | 3084.64 | 33.2568 |
| ν73 | 3093.58 | 32.2448 | 3089.31 | 81.8036 |
| ν74 | 3149.72 | 21.6937 | 3160.63 | 27.4172 |
| ν75 | 3456.42 | 189.3358 | 3411.42 | 236.6912 |
|  | tsR1-OH |  | tsR2-OH |  |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -932.5 | 891.971 | -1274.16 | 562.6168 |
| ν2 | 70.7 | 2.332 | 72.87 | 2.411 |
| ν3 | 78.81 | 2.6707 | 84.1 | 1.767 |
| ν4 | 146.04 | 0.7486 | 144.95 | 0.2605 |
| ν5 | 178.37 | 0.6195 | 175.14 | 0.0211 |
| ν6 | 269.32 | 4.9218 | 268.37 | 0.2518 |
| ν7 | 306.58 | 1.2243 | 309.06 | 0.5869 |
| ν8 | 322.16 | 0.7114 | 316.56 | 0.1363 |
| ν9 | 375.06 | 1.143 | 377.68 | 2.2338 |
| ν10 | 493.41 | 0.3357 | 398.88 | 0.6269 |
| ν11 | 539.95 | 3.519 | 490.43 | 0.1806 |
| ν12 | 558.36 | 1.3247 | 530.84 | 1.2352 |
| ν13 | 631.8 | 82.1758 | 553.38 | 0.9572 |
| ν14 | 681.26 | 24.3216 | 666.82 | 0.9409 |
| ν15 | 746.63 | 11.746 | 722.66 | 1.147 |
| ν16 | 757.58 | 2.9913 | 753.34 | 1.8528 |
| ν17 | 794.22 | 1.5093 | 790.7 | 3.2541 |
| ν18 | 842.54 | 8.9397 | 827.47 | 1.5875 |
| ν19 | 864.64 | 0.2246 | 858.99 | 0.138 |
| ν20 | 868.74 | 1.5064 | 867.8 | 1.2016 |
| ν21 | 889.83 | 1.0304 | 878.87 | 0.6124 |
| ν22 | 898.86 | 4.2587 | 894.99 | 2.4254 |
| ν23 | 911.81 | 0.0576 | 910.18 | 2.2615 |
| ν24 | 913.79 | 1.3419 | 915.62 | 0.2206 |
| ν25 | 926.56 | 0.9301 | 936.8 | 3.4974 |
| ν26 | 953.35 | 7.569 | 954.16 | 0.6611 |
| ν27 | 956.2 | 1.4766 | 971.33 | 11.1644 |
| ν28 | 987.35 | 2.9066 | 991.28 | 4.8185 |
| ν29 | 1006.42 | 4.7284 | 995.74 | 8.0401 |
| ν30 | 1032.25 | 2.7951 | 1004.28 | 7.3196 |
| ν31 | 1035.93 | 2.4614 | 1039.9 | 0.4124 |
| ν32 | 1041.62 | 1.4192 | 1048.14 | 3.5134 |
| ν33 | 1051.29 | 0.006 | 1050.55 | 2.079 |
| ν34 | 1079.33 | 0.6731 | 1062.7 | 0.2715 |
| ν35 | 1136.12 | 6.1294 | 1091.93 | 2.416 |
| ν36 | 1137.11 | 3.347 | 1118.88 | 3.3018 |
| ν37 | 1154.01 | 0.5803 | 1148.21 | 3.9525 |
| ν38 | 1174.46 | 6.7857 | 1178.95 | 7.1977 |
| ν39 | 1192.74 | 1.1719 | 1193.09 | 0.5238 |
| ν40 | 1196.21 | 1.2977 | 1201.14 | 0.6267 |
| ν41 | 1213.99 | 0.6269 | 1212.24 | 4.8875 |
| ν42 | 1225.96 | 4.2398 | 1230.02 | 3.2782 |
| ν43 | 1249.36 | 8.5277 | 1251.3 | 3.0854 |
| ν44 | 1261.03 | 2.0505 | 1260.76 | 0.5367 |
| ν45 | 1288.42 | 1.2536 | 1271.8 | 1.2113 |
| ν46 | 1291.83 | 1.2551 | 1298.9 | 1.9059 |
| ν47 | 1304.31 | 0.3851 | 1306.61 | 3.5262 |
| ν48 | 1312.48 | 0.2264 | 1314.11 | 0.6568 |
| ν49 | 1320.93 | 0.3974 | 1320.16 | 0.2144 |
| ν50 | 1325.16 | 1.3528 | 1326.91 | 1.7673 |
| ν51 | 1328.86 | 1.7959 | 1338.23 | 1.36 |
| ν52 | 1343.12 | 0.747 | 1344.08 | 0.456 |
| ν53 | 1349.14 | 0.5234 | 1360.65 | 1.1517 |
| ν54 | 1363.19 | 1.814 | 1371.09 | 0.2161 |
| ν55 | 1370.15 | 0.4695 | 1493.23 | 0.6478 |
| ν56 | 1482.32 | 6.0591 | 1493.93 | 1.1189 |
| ν57 | 1495.35 | 2.1346 | 1496.47 | 2.0157 |
| ν58 | 1496.83 | 2.726 | 1502.15 | 7.1454 |
| ν59 | 1507.49 | 3.9428 | 1512.43 | 7.269 |
| ν60 | 1521.1 | 9.8328 | 1524.61 | 6.2709 |
| ν61 | 3019.55 | 21.3664 | 3019.65 | 21.5207 |
| ν62 | 3025.86 | 28.2259 | 3026.81 | 28.3738 |
| ν63 | 3029.44 | 19.9982 | 3038.97 | 12.1392 |
| ν64 | 3030.67 | 26.5356 | 3041.02 | 5.8513 |
| ν65 | 3034.45 | 3.069 | 3045.17 | 29.4561 |
| ν66 | 3048.11 | 34.6066 | 3056.6 | 5.0664 |
| ν67 | 3062.45 | 12.6764 | 3059.38 | 67.8769 |
| ν68 | 3062.97 | 14.7917 | 3065.19 | 14.1679 |
| ν69 | 3071.6 | 43.053 | 3072.89 | 29.6595 |
| ν70 | 3075.27 | 42.8529 | 3077.22 | 25.7547 |
| ν71 | 3082.4 | 66.29 | 3077.87 | 54.9347 |
| ν72 | 3083.28 | 55.2831 | 3080.85 | 27.1755 |
| ν73 | 3087.05 | 43.0799 | 3089.7 | 46.8997 |
| ν74 | 3094.29 | 17.7348 | 3102.22 | 53.1647 |
| ν75 | 3106.81 | 24.8145 | 3115.32 | 26.9397 |
|  | tsR3-OH |  | tsR4-OH |  |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -1301.13 | 599.9046 | -655.93 | 619.5207 |
| ν2 | 85.89 | 2.0128 | 79.03 | 1.7397 |
| ν3 | 88.77 | 2.2444 | 87.44 | 2.3239 |
| ν4 | 131.11 | 0.4323 | 146.12 | 0.5478 |
| ν5 | 174.21 | 0.569 | 172.36 | 1.1252 |
| ν6 | 263.5 | 0.282 | 268.07 | 0.584 |
| ν7 | 282.06 | 0.7367 | 307.71 | 2.3507 |
| ν8 | 315.04 | 0.0084 | 317.58 | 0.1673 |
| ν9 | 372 | 0.798 | 393.96 | 0.0327 |
| ν10 | 432.37 | 0.1411 | 479.17 | 22.4097 |
| ν11 | 535.37 | 0.087 | 532.7 | 4.2869 |
| ν12 | 553.85 | 3.2082 | 552.67 | 10.9825 |
| ν13 | 607.89 | 11.8973 | 568.08 | 138.4318 |
| ν14 | 665.43 | 1.4587 | 695.62 | 23.6959 |
| ν15 | 737.06 | 1.6311 | 741.94 | 3.3278 |
| ν16 | 752.01 | 1.574 | 767.67 | 46.6427 |
| ν17 | 789.15 | 2.0476 | 796.21 | 1.9947 |
| ν18 | 835.58 | 6.2237 | 832.73 | 0.5416 |
| ν19 | 854.29 | 0.5683 | 860.27 | 1.8152 |
| ν20 | 863.9 | 0.0815 | 868.53 | 3.7245 |
| ν21 | 885.23 | 0.2812 | 885.97 | 2.6278 |
| ν22 | 888.25 | 0.7461 | 889.93 | 0.6212 |
| ν23 | 911.11 | 0.5375 | 908.74 | 0.0651 |
| ν24 | 915.67 | 0.0063 | 913.49 | 1.237 |
| ν25 | 927.78 | 3.0971 | 924.57 | 9.8232 |
| ν26 | 947.56 | 5.7733 | 955.38 | 3.4549 |
| ν27 | 973.69 | 1.8093 | 960.19 | 1.1229 |
| ν28 | 987.44 | 2.1968 | 991.33 | 6.0706 |
| ν29 | 992.23 | 1.411 | 1010.22 | 1.3798 |
| ν30 | 1031.37 | 3.772 | 1046.18 | 0.9294 |
| ν31 | 1036.07 | 2.7023 | 1048.29 | 1.4758 |
| ν32 | 1039.33 | 0.1646 | 1052.78 | 1.9537 |
| ν33 | 1050.4 | 0.0408 | 1061.74 | 17.4861 |
| ν34 | 1074.32 | 0.6791 | 1076.51 | 2.0801 |
| ν35 | 1078.07 | 3.7279 | 1123.39 | 2.243 |
| ν36 | 1147.57 | 1.0357 | 1145.26 | 2.9123 |
| ν37 | 1163.56 | 17.3184 | 1152.18 | 4.6217 |
| ν38 | 1186.57 | 5.2459 | 1178.61 | 4.8426 |
| ν39 | 1193.51 | 0.4463 | 1190.77 | 1.6092 |
| ν40 | 1194.63 | 0.022 | 1198.35 | 5.8007 |
| ν41 | 1215.92 | 2.2093 | 1204.89 | 3.2327 |
| ν42 | 1232.14 | 2.2533 | 1224.46 | 0.2688 |
| ν43 | 1237.04 | 0.1604 | 1248.36 | 1.809 |
| ν44 | 1260.01 | 4.1101 | 1256.16 | 0.484 |
| ν45 | 1267.2 | 2.1424 | 1268.98 | 1.9735 |
| ν46 | 1287.15 | 0.0491 | 1291.31 | 1.123 |
| ν47 | 1303.31 | 0.0395 | 1307.92 | 0.2445 |
| ν48 | 1311.28 | 0.2544 | 1314.38 | 1.4222 |
| ν49 | 1318.15 | 0.16 | 1318.18 | 0.3237 |
| ν50 | 1327.63 | 0.3534 | 1331.21 | 1.2302 |
| ν51 | 1332.97 | 0.8895 | 1339.05 | 1.2264 |
| ν52 | 1342.95 | 0.5805 | 1345.22 | 1.2967 |
| ν53 | 1347.76 | 0.8957 | 1349.84 | 0.1563 |
| ν54 | 1361.98 | 0.1699 | 1358.61 | 0.4546 |
| ν55 | 1366.28 | 3.6244 | 1475.81 | 6.4612 |
| ν56 | 1469.2 | 0.0384 | 1493.72 | 1.3551 |
| ν57 | 1496.88 | 3.0291 | 1497.26 | 1.4702 |
| ν58 | 1497.29 | 4.7292 | 1501.8 | 6.0628 |
| ν59 | 1512.25 | 0.026 | 1509.71 | 9.4151 |
| ν60 | 1513.08 | 11.6834 | 1522 | 2.202 |
| ν61 | 3018.69 | 14.9679 | 3003.82 | 14.7823 |
| ν62 | 3023.46 | 28.0796 | 3022.95 | 14.3514 |
| ν63 | 3028.11 | 28.706 | 3034.12 | 21.4468 |
| ν64 | 3034.36 | 0.0053 | 3035.32 | 20.5331 |
| ν65 | 3046.29 | 29.4899 | 3042.26 | 28.2646 |
| ν66 | 3047.49 | 20.351 | 3047.98 | 29.1859 |
| ν67 | 3057.66 | 64.4634 | 3054.4 | 47.9652 |
| ν68 | 3072.86 | 37.2639 | 3072.78 | 23.5533 |
| ν69 | 3075 | 35.1829 | 3076.21 | 6.8386 |
| ν70 | 3077.3 | 10.6038 | 3077.66 | 55.7308 |
| ν71 | 3082 | 56.8219 | 3081.25 | 59.5346 |
| ν72 | 3091.96 | 62.5993 | 3084.35 | 38.2624 |
| ν73 | 3092.07 | 8.1117 | 3090.46 | 28.7693 |
| ν74 | 3102.08 | 37.0362 | 3093.52 | 33.7737 |
| ν75 | 3110.61 | 24.1379 | 3106.95 | 22.5549 |
|  | tsR5-OH |  | tsR6-OH |  |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -946.34 | 595.9346 | -922.56 | 745.9918 |
| ν2 | 64.73 | 1.3763 | 57.13 | 2.3371 |
| ν3 | 87.97 | 1.7397 | 75.08 | 2.0341 |
| ν4 | 142.37 | 0.6667 | 142.86 | 0.427 |
| ν5 | 195.92 | 0.8493 | 182.95 | 3.0993 |
| ν6 | 269.92 | 0.3515 | 263.26 | 0.1131 |
| ν7 | 310.69 | 2.2719 | 311.37 | 2.5877 |
| ν8 | 319.9 | 1.0452 | 320.25 | 0.4483 |
| ν9 | 396.96 | 0.3426 | 398.16 | 0.6244 |
| ν10 | 497.55 | 0.1428 | 490.21 | 0.0497 |
| ν11 | 529.65 | 3.6858 | 534.96 | 0.4385 |
| ν12 | 577.73 | 0.7433 | 579.94 | 10.924 |
| ν13 | 602.56 | 72.2332 | 639.19 | 96.7388 |
| ν14 | 697.35 | 2.973 | 672.68 | 0.9517 |
| ν15 | 738.3 | 0.7882 | 735.54 | 0.3537 |
| ν16 | 748.37 | 0.3382 | 758.78 | 5.7572 |
| ν17 | 792.12 | 3.3737 | 791.39 | 3.9104 |
| ν18 | 828.17 | 0.9957 | 828.64 | 1.5033 |
| ν19 | 857.73 | 2.7682 | 859.18 | 0.5428 |
| ν20 | 864.43 | 1.968 | 864.83 | 9.2874 |
| ν21 | 886.93 | 0.868 | 887.7 | 1.1158 |
| ν22 | 893.01 | 0.7778 | 887.92 | 0.1672 |
| ν23 | 910.35 | 1.1396 | 914.47 | 1.2901 |
| ν24 | 921.21 | 1.8638 | 915.25 | 0.5261 |
| ν25 | 925.13 | 0.9294 | 924.07 | 2.2371 |
| ν26 | 956.22 | 1.1111 | 954.56 | 0.9523 |
| ν27 | 960.94 | 0.0923 | 961.39 | 0.0034 |
| ν28 | 991.27 | 1.4005 | 992.87 | 2.7903 |
| ν29 | 997.89 | 2.4938 | 996.83 | 4.1753 |
| ν30 | 1034.85 | 0.3321 | 1037.81 | 2.6596 |
| ν31 | 1047.26 | 0.1999 | 1048.44 | 0.322 |
| ν32 | 1049.53 | 0.2236 | 1050.11 | 0.0393 |
| ν33 | 1053.55 | 0.0471 | 1062.01 | 0.8249 |
| ν34 | 1074.97 | 5.2227 | 1065.79 | 2.0044 |
| ν35 | 1112.13 | 8.8797 | 1133.9 | 0.254 |
| ν36 | 1140.3 | 0.8144 | 1141.18 | 2.0317 |
| ν37 | 1154.74 | 6.7027 | 1163.84 | 2.8746 |
| ν38 | 1167.81 | 1.4875 | 1169.41 | 3.2939 |
| ν39 | 1197.87 | 4.2131 | 1193.72 | 27.1512 |
| ν40 | 1204.49 | 2.1962 | 1200.93 | 0.2146 |
| ν41 | 1213.34 | 0.4806 | 1214.24 | 0.7013 |
| ν42 | 1225.02 | 2.6486 | 1233.29 | 2.0042 |
| ν43 | 1250.77 | 2.487 | 1239.77 | 0 |
| ν44 | 1276.39 | 1.8655 | 1258.38 | 0.0027 |
| ν45 | 1287.83 | 10.5341 | 1278.79 | 3.1371 |
| ν46 | 1293.49 | 0.728 | 1292.69 | 1.0688 |
| ν47 | 1301.58 | 3.8055 | 1306.67 | 0.0615 |
| ν48 | 1312.25 | 1.2006 | 1308 | 0.0007 |
| ν49 | 1316.34 | 0.5527 | 1312.59 | 2.3296 |
| ν50 | 1322.99 | 0.7779 | 1319.78 | 0.1982 |
| ν51 | 1331.88 | 0.9414 | 1326.37 | 0.4812 |
| ν52 | 1337.04 | 2.4507 | 1337.41 | 1.3539 |
| ν53 | 1348 | 4.9518 | 1353.01 | 3.2163 |
| ν54 | 1355.57 | 0.5492 | 1368.36 | 0.6661 |
| ν55 | 1368.35 | 0.4025 | 1371.22 | 0.1674 |
| ν56 | 1476.96 | 5.9225 | 1472.3 | 7.4279 |
| ν57 | 1495.71 | 1.2403 | 1482.17 | 2.0569 |
| ν58 | 1497.4 | 2.7705 | 1495.89 | 1.0462 |
| ν59 | 1508.23 | 10.8641 | 1505.5 | 11.3301 |
| ν60 | 1522.13 | 3.9041 | 1523.62 | 4.0251 |
| ν61 | 2988.67 | 18.0315 | 2988.62 | 7.3786 |
| ν62 | 3008.85 | 13.668 | 2992.57 | 15.2631 |
| ν63 | 3037.29 | 18.5197 | 3037.65 | 21.4573 |
| ν64 | 3039 | 33.0755 | 3046.02 | 44.9002 |
| ν65 | 3042.01 | 7.8687 | 3048.1 | 42.3535 |
| ν66 | 3043.91 | 42.5605 | 3049.96 | 0.4423 |
| ν67 | 3048.5 | 54.7978 | 3058.76 | 14.7804 |
| ν68 | 3065.7 | 2.2712 | 3066.62 | 0.5391 |
| ν69 | 3073.51 | 17.1549 | 3069.31 | 39.381 |
| ν70 | 3079.45 | 51.2641 | 3073.86 | 89.2775 |
| ν71 | 3081.36 | 40.5813 | 3073.86 | 28.7372 |
| ν72 | 3084.75 | 42.5557 | 3081.69 | 6.1464 |
| ν73 | 3087.01 | 13.9289 | 3086.31 | 39.2842 |
| ν74 | 3088.03 | 79.5672 | 3089.69 | 73.8952 |
| ν75 | 3094.96 | 28.825 | 3090.89 | 34.5264 |

|  | vdW R1-O2H |  | vdW R2-O2H |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 24.68 | 1.5639 | 24.01 | 1.3122 |
| ν2 | 32.33 | 1.3439 | 53.57 | 0.829 |
| ν3 | 57.27 | 0.0517 | 57.03 | 0.8597 |
| ν4 | 93.05 | 0.3479 | 99.18 | 0.9423 |
| ν5 | 130.73 | 4.3947 | 138.32 | 0.0056 |
| ν6 | 164.63 | 1.9729 | 179.49 | 0.9171 |
| ν7 | 186.66 | 2.1611 | 200.47 | 11.0995 |
| ν8 | 301 | 0.4818 | 261.96 | 0.4994 |
| ν9 | 316.55 | 0.1732 | 316.31 | 0.233 |
| ν10 | 353.05 | 0.5826 | 330.45 | 0.1032 |
| ν11 | 407.51 | 0.1103 | 397.38 | 0.0254 |
| ν12 | 490.84 | 1.2629 | 484.96 | 0.4098 |
| ν13 | 539.48 | 0.266 | 515.96 | 2.331 |
| ν14 | 549.57 | 1.0159 | 544.14 | 0.6776 |
| ν15 | 607.84 | 19.9738 | 622.3 | 75.2357 |
| ν16 | 627.88 | 53.744 | 652.71 | 0.6565 |
| ν17 | 674.58 | 0.4392 | 724.63 | 0.217 |
| ν18 | 746.62 | 0.38 | 758.23 | 0.184 |
| ν19 | 765.84 | 0.2468 | 800.71 | 0.7757 |
| ν20 | 791.83 | 1.9541 | 829.64 | 0.7453 |
| ν21 | 856.22 | 0.9074 | 855.68 | 1.9692 |
| ν22 | 863.48 | 0.0347 | 875.32 | 0.4134 |
| ν23 | 884.46 | 0.3421 | 891.23 | 0.1546 |
| ν24 | 897.56 | 0.3446 | 912.05 | 0.5392 |
| ν25 | 910.06 | 0.1087 | 923.8 | 0.253 |
| ν26 | 913.09 | 0.8231 | 938.38 | 1.3756 |
| ν27 | 930.07 | 0.1834 | 955.6 | 1.4649 |
| ν28 | 950.45 | 1.8406 | 967.46 | 0.8419 |
| ν29 | 958.01 | 3.6533 | 990.06 | 0.2337 |
| ν30 | 982.42 | 1.3846 | 1013.23 | 0.3991 |
| ν31 | 990.25 | 1.7006 | 1018.3 | 1.4902 |
| ν32 | 998.53 | 0.9648 | 1052.48 | 0.0654 |
| ν33 | 1039.53 | 0.371 | 1057.69 | 0.0664 |
| ν34 | 1049.15 | 0.1252 | 1068.18 | 0.5291 |
| ν35 | 1054.5 | 0.6244 | 1097.16 | 0.4192 |
| ν36 | 1067.31 | 1.1524 | 1119.43 | 0.3362 |
| ν37 | 1118.26 | 0.2743 | 1147.61 | 1.4395 |
| ν38 | 1141.06 | 0.2546 | 1167.94 | 1.9407 |
| ν39 | 1162.18 | 1.2372 | 1196.41 | 0.0724 |
| ν40 | 1178.33 | 15.0418 | 1198.6 | 1.4412 |
| ν41 | 1187.13 | 0.6067 | 1208.63 | 3.829 |
| ν42 | 1195.28 | 0.3186 | 1219.75 | 2.1416 |
| ν43 | 1209.01 | 0.3813 | 1233.04 | 3.0346 |
| ν44 | 1229.46 | 0.4533 | 1256.84 | 0.1331 |
| ν45 | 1254.95 | 1.3583 | 1262.08 | 23.56 |
| ν46 | 1279.95 | 1.5245 | 1267.51 | 36.5368 |
| ν47 | 1286.32 | 0.6502 | 1279.57 | 2.058 |
| ν48 | 1304.15 | 0.4802 | 1292.52 | 1.1092 |
| ν49 | 1309.09 | 0.1748 | 1308.86 | 0.3041 |
| ν50 | 1320.81 | 0.33 | 1312.03 | 1.0826 |
| ν51 | 1324.8 | 0.3647 | 1315.52 | 0.729 |
| ν52 | 1335.15 | 1.0473 | 1327.84 | 0.4506 |
| ν53 | 1344.71 | 0.746 | 1344.48 | 0.0141 |
| ν54 | 1348.12 | 0.7632 | 1353.83 | 0.4681 |
| ν55 | 1364.63 | 0.4836 | 1372.29 | 0.8754 |
| ν56 | 1370.76 | 0.4613 | 1470.95 | 1.2164 |
| ν57 | 1470.79 | 6.1704 | 1472.78 | 0.227 |
| ν58 | 1495.14 | 1.7565 | 1478.47 | 2.1214 |
| ν59 | 1497.25 | 3.0625 | 1483.76 | 10.4259 |
| ν60 | 1502.55 | 10.2434 | 1496.92 | 6.7809 |
| ν61 | 1507.33 | 9.6349 | 1506.17 | 6.9355 |
| ν62 | 1520.76 | 8.3029 | 1521.02 | 18.3033 |
| ν63 | 2951.94 | 304.6055 | 3071.88 | 406.3918 |
| ν64 | 2993.29 | 35.409 | 3080.52 | 24.5839 |
| ν65 | 3020.25 | 13.0456 | 3083.11 | 28.8543 |
| ν66 | 3020.64 | 19.4068 | 3087.07 | 25.162 |
| ν67 | 3024.91 | 29.7649 | 3092.82 | 20.2697 |
| ν68 | 3029.93 | 27.1104 | 3094.96 | 18.0435 |
| ν69 | 3040.49 | 8.862 | 3106.52 | 38.5109 |
| ν70 | 3055.2 | 42.5611 | 3112.72 | 20.2411 |
| ν71 | 3057.53 | 20.7549 | 3128.82 | 32.9195 |
| ν72 | 3072.99 | 34.3008 | 3131.84 | 6.6612 |
| ν73 | 3076.45 | 43.2845 | 3147.89 | 23.8241 |
| ν74 | 3084.23 | 81.8866 | 3154.98 | 11.1563 |
| ν75 | 3086.67 | 42.1779 | 3155.47 | 27.5404 |
| ν76 | 3098.68 | 18.9452 | 3169.85 | 19.6185 |
| ν77 | 3099.77 | 29.6955 | 3177.02 | 25.7186 |
| ν78 | 3150.07 | 7.9329 | 3186.6 | 18.3915 |

|  | vdW R3-O2H |  | vdW R4-O2H |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 32.31 | 1.2021 | 34.06 | 1.1821 |
| ν2 | 41.95 | 1.611 | 60.23 | 0.4826 |
| ν3 | 61.8 | 0.0183 | 68.18 | 0.7221 |
| ν4 | 74.33 | 0.2362 | 112.76 | 0.4758 |
| ν5 | 123.86 | 0.034 | 124.5 | 0.2239 |
| ν6 | 147.75 | 3.8694 | 179.81 | 0.2528 |
| ν7 | 199.68 | 1.9581 | 208.07 | 9.91 |
| ν8 | 256.19 | 0.2385 | 250.42 | 0.5524 |
| ν9 | 310.98 | 0.0396 | 305.02 | 1.2092 |
| ν10 | 314.8 | 0.0062 | 320.52 | 0.1278 |
| ν11 | 402.15 | 0.1989 | 389.11 | 0.0359 |
| ν12 | 532.38 | 0.1071 | 479.04 | 0.8115 |
| ν13 | 536.13 | 3.3212 | 533.7 | 0.5474 |
| ν14 | 551.36 | 2.2442 | 545.67 | 0.8747 |
| ν15 | 666.13 | 14.1625 | 633.46 | 3.8686 |
| ν16 | 691.41 | 30.5727 | 663.36 | 72.4388 |
| ν17 | 727.4 | 0.0473 | 726.92 | 0.6222 |
| ν18 | 757.82 | 0.597 | 751.21 | 1.1399 |
| ν19 | 787.31 | 0.1788 | 807.09 | 1.6468 |
| ν20 | 807.19 | 3.3968 | 829.83 | 2.4436 |
| ν21 | 840.54 | 2.348 | 862.54 | 0.2414 |
| ν22 | 851.93 | 0.0467 | 892.31 | 0.3084 |
| ν23 | 868.27 | 0.0652 | 894.82 | 1.78 |
| ν24 | 874.63 | 1.4551 | 912.66 | 0.6329 |
| ν25 | 912.25 | 0.0027 | 916.9 | 0.1949 |
| ν26 | 916.05 | 1.78 | 931.75 | 0.0157 |
| ν27 | 921.6 | 0.0187 | 944.26 | 0.9742 |
| ν28 | 942.86 | 0.1425 | 969.61 | 2.9124 |
| ν29 | 946.59 | 0.3523 | 976.09 | 0.8631 |
| ν30 | 990.82 | 1.7113 | 1015.06 | 0.5472 |
| ν31 | 992.97 | 1.7709 | 1024.1 | 2.2832 |
| ν32 | 1002.24 | 0.2645 | 1047.8 | 0.4499 |
| ν33 | 1040.77 | 0.1772 | 1061.61 | 0.2833 |
| ν34 | 1052.26 | 0.0001 | 1067.04 | 0.1104 |
| ν35 | 1057.62 | 0.1849 | 1102.54 | 1.4185 |
| ν36 | 1071.59 | 0.7993 | 1131.52 | 0.0405 |
| ν37 | 1151.43 | 0.535 | 1136.84 | 0.0774 |
| ν38 | 1159.41 | 12.0202 | 1162.3 | 0.3228 |
| ν39 | 1179 | 14.585 | 1165.8 | 1.4778 |
| ν40 | 1192.83 | 2.2258 | 1195.98 | 2.5647 |
| ν41 | 1193.87 | 0.1747 | 1217.44 | 0.2749 |
| ν42 | 1204.02 | 0.8886 | 1229.4 | 4.6784 |
| ν43 | 1205.31 | 0.6793 | 1237.26 | 0.8397 |
| ν44 | 1235.35 | 1.8726 | 1247.51 | 0.3911 |
| ν45 | 1246.92 | 0.0005 | 1260.15 | 12.1313 |
| ν46 | 1261.05 | 1.0162 | 1265.25 | 46.4701 |
| ν47 | 1282.39 | 0.005 | 1271.05 | 0.2201 |
| ν48 | 1304.51 | 0.003 | 1298.97 | 0.513 |
| ν49 | 1311.96 | 0.3051 | 1305.23 | 0.1953 |
| ν50 | 1317.51 | 0.0001 | 1315.15 | 1.3696 |
| ν51 | 1327.7 | 0.029 | 1323.15 | 1.3132 |
| ν52 | 1332.76 | 0.7873 | 1338.62 | 0.5028 |
| ν53 | 1346.48 | 0.7266 | 1341.03 | 0.0272 |
| ν54 | 1350.04 | 0.0272 | 1350.44 | 0.4724 |
| ν55 | 1364.49 | 0.6901 | 1368.67 | 0.6883 |
| ν56 | 1369.68 | 0.3149 | 1454.45 | 7.0352 |
| ν57 | 1492.96 | 1.5202 | 1472.05 | 1.0282 |
| ν58 | 1493.35 | 3.3813 | 1477.47 | 1.741 |
| ν59 | 1497.78 | 2.8542 | 1482.72 | 8.3521 |
| ν60 | 1503.21 | 14.5985 | 1492.6 | 6.9192 |
| ν61 | 1509.46 | 4.5426 | 1506.37 | 4.7108 |
| ν62 | 1519.96 | 6.0171 | 1525.89 | 8.2544 |
| ν63 | 2626.18 | 88.7933 | 3037.75 | 36.1291 |
| ν64 | 3018.71 | 15.6357 | 3069.86 | 407.6858 |
| ν65 | 3025.1 | 24.97 | 3078.88 | 19.4352 |
| ν66 | 3029.89 | 28.6808 | 3083.13 | 2.9793 |
| ν67 | 3037.61 | 4.3652 | 3088.61 | 23.5368 |
| ν68 | 3041.36 | 24.866 | 3090.15 | 16.2005 |
| ν69 | 3048.77 | 14.6564 | 3094.76 | 16.4375 |
| ν70 | 3053.32 | 76.5299 | 3105.67 | 44.6255 |
| ν71 | 3073.76 | 7.9575 | 3116.48 | 27.5166 |
| ν72 | 3074.96 | 38.4207 | 3138.03 | 38.2969 |
| ν73 | 3075.6 | 31.2517 | 3148.81 | 19.9863 |
| ν74 | 3082.98 | 65.9086 | 3153.27 | 33.2007 |
| ν75 | 3093.92 | 47.8054 | 3157.67 | 1.4761 |
| ν76 | 3097.28 | 55.5116 | 3157.88 | 7.0162 |
| ν77 | 3097.98 | 9.341 | 3162.8 | 34.743 |
| ν78 | 3117.4 | 12.9118 | 3175.07 | 26.5958 |

|  | vdW R5-O2H |  | vdW R6-O2H |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | 18.45 | 1.524 | 19.36 | 1.3998 |
| ν2 | 36.34 | 1.2313 | 39.75 | 0.4617 |
| ν3 | 51.55 | 0.1552 | 52.97 | 1.0484 |
| ν4 | 90.82 | 0.2422 | 94.07 | 0.3113 |
| ν5 | 120.14 | 2.0982 | 126.86 | 0.3467 |
| ν6 | 144.51 | 0.3787 | 186.78 | 0.8231 |
| ν7 | 195.39 | 4.9313 | 201.96 | 8.7813 |
| ν8 | 269.86 | 0.2479 | 260.94 | 0.0168 |
| ν9 | 308.59 | 0.3787 | 281.01 | 1.0672 |
| ν10 | 333.41 | 1.2126 | 325.52 | 0.0796 |
| ν11 | 395.14 | 0.2343 | 395.98 | 0.5889 |
| ν12 | 491.83 | 0.4441 | 490.39 | 0.9203 |
| ν13 | 534.78 | 0.3398 | 533.32 | 0.4724 |
| ν14 | 581.91 | 11.2958 | 547.95 | 14.2294 |
| ν15 | 613.15 | 60.049 | 687.6 | 1.5465 |
| ν16 | 658.51 | 8.5592 | 692.59 | 40.7838 |
| ν17 | 736.94 | 0.3744 | 712.55 | 20.0851 |
| ν18 | 746.55 | 1.2586 | 732.12 | 0.4649 |
| ν19 | 781.84 | 4.004 | 778.3 | 0.938 |
| ν20 | 800.37 | 0.69 | 798.29 | 0.6912 |
| ν21 | 829.94 | 0.3486 | 828.37 | 1.0606 |
| ν22 | 850.08 | 0.5871 | 845.7 | 0.301 |
| ν23 | 870.39 | 1.5243 | 886.57 | 1.0281 |
| ν24 | 887.26 | 0.603 | 888.17 | 0.4948 |
| ν25 | 903.17 | 0.366 | 913.7 | 0.7071 |
| ν26 | 920.98 | 0.3723 | 923.75 | 1.0176 |
| ν27 | 924.63 | 1.2577 | 924.23 | 1.8734 |
| ν28 | 947.54 | 1.5656 | 948.65 | 0.5762 |
| ν29 | 961.36 | 0.2855 | 962.26 | 0.026 |
| ν30 | 981.28 | 1.1212 | 966.83 | 1.8278 |
| ν31 | 998.39 | 0.6324 | 1004.55 | 2.7674 |
| ν32 | 1017.42 | 0.9503 | 1024.47 | 0.5262 |
| ν33 | 1046.14 | 0.1196 | 1044.67 | 0.8787 |
| ν34 | 1049.67 | 0.1287 | 1051.82 | 0.8008 |
| ν35 | 1059.67 | 0.697 | 1058.67 | 0.4567 |
| ν36 | 1071.59 | 2.0018 | 1074.22 | 0.003 |
| ν37 | 1123.81 | 0.5861 | 1130.19 | 0.8499 |
| ν38 | 1143.55 | 0.1805 | 1145.54 | 0.101 |
| ν39 | 1161.82 | 0.7129 | 1153.01 | 0.4992 |
| ν40 | 1176.09 | 13.5192 | 1175.83 | 15.8454 |
| ν41 | 1186.53 | 2.2944 | 1192.01 | 3.7222 |
| ν42 | 1205.33 | 3.5316 | 1198.53 | 0.0185 |
| ν43 | 1218.65 | 0.3903 | 1213.09 | 1.2984 |
| ν44 | 1227.7 | 0.3719 | 1233.81 | 2.0236 |
| ν45 | 1248.21 | 0.2519 | 1249.71 | 0.4037 |
| ν46 | 1277.69 | 1.3171 | 1262.84 | 0.7614 |
| ν47 | 1288.05 | 1.3784 | 1292.65 | 1.0791 |
| ν48 | 1294.92 | 0.7951 | 1307.22 | 0.0509 |
| ν49 | 1301.66 | 0.4167 | 1308.93 | 0.6173 |
| ν50 | 1314.78 | 0.2572 | 1311.3 | 0.3579 |
| ν51 | 1319.8 | 1.6941 | 1321.91 | 1.201 |
| ν52 | 1324.06 | 0.4398 | 1327.06 | 1.6529 |
| ν53 | 1335.84 | 1.8757 | 1346.17 | 0.3133 |
| ν54 | 1349.17 | 1.6194 | 1354.71 | 4.0234 |
| ν55 | 1362.48 | 0.6573 | 1365.62 | 0.1477 |
| ν56 | 1368.91 | 1.0759 | 1370.71 | 0.8852 |
| ν57 | 1469.02 | 4.0518 | 1458.81 | 19.8817 |
| ν58 | 1492.55 | 14.3168 | 1468.63 | 4.2905 |
| ν59 | 1495.91 | 0.8417 | 1496.31 | 1.0858 |
| ν60 | 1497.7 | 3.8445 | 1504.17 | 9.2433 |
| ν61 | 1509.92 | 11.3912 | 1507.2 | 9.2372 |
| ν62 | 1522.78 | 1.6135 | 1523.21 | 3.9234 |
| ν63 | 2935.27 | 29.6311 | 2785.53 | 199.0387 |
| ν64 | 2971.51 | 30.7998 | 2938.86 | 13.6759 |
| ν65 | 2999.53 | 247.1953 | 2941.98 | 20.9887 |
| ν66 | 3034.28 | 26.2647 | 3024.6 | 16.6952 |
| ν67 | 3039.18 | 25.6884 | 3033.3 | 5.8841 |
| ν68 | 3046.41 | 12.3807 | 3038.25 | 19.7717 |
| ν69 | 3046.99 | 9.1826 | 3044.82 | 37.4833 |
| ν70 | 3049.21 | 107.1955 | 3048.46 | 48.8684 |
| ν71 | 3051.8 | 12.6307 | 3054.24 | 13.8542 |
| ν72 | 3067.75 | 3.5407 | 3067.56 | 14.5735 |
| ν73 | 3079.77 | 51.9366 | 3069 | 28.6668 |
| ν74 | 3084.27 | 43.1111 | 3074.65 | 75.1828 |
| ν75 | 3088.44 | 35.7434 | 3081.99 | 2.9094 |
| ν76 | 3091.98 | 47.0152 | 3084.57 | 33.5859 |
| ν77 | 3092.43 | 44.1936 | 3089.95 | 79.4418 |
| ν78 | 3132.18 | 7.9185 | 3140.56 | 28.4242 |

|  | tsR1-O2H |  |  |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -507.33 | 87.3089 |  |  |
| ν2 | 25.69 | 1.1685 |  |  |
| ν3 | 41.71 | 1.2673 |  |  |
| ν4 | 74.86 | 0.2723 |  |  |
| ν5 | 138.03 | 1.246 |  |  |
| ν6 | 164.3 | 0.4884 |  |  |
| ν7 | 176.1 | 0.0733 |  |  |
| ν8 | 299.18 | 0.7187 |  |  |
| ν9 | 315.47 | 0.1615 |  |  |
| ν10 | 328.88 | 3.536 |  |  |
| ν11 | 400.28 | 2.7662 |  |  |
| ν12 | 489.81 | 1.3566 |  |  |
| ν13 | 533.85 | 0.4938 |  |  |
| ν14 | 555.8 | 0.4071 |  |  |
| ν15 | 623.93 | 8.2114 |  |  |
| ν16 | 675.09 | 1.0007 |  |  |
| ν17 | 744.11 | 1.557 |  |  |
| ν18 | 760.35 | 6.8655 |  |  |
| ν19 | 792.37 | 1.4527 |  |  |
| ν20 | 844.45 | 8.0192 |  |  |
| ν21 | 861.85 | 1.9815 |  |  |
| ν22 | 871.58 | 22.3855 |  |  |
| ν23 | 875.9 | 7.5775 |  |  |
| ν24 | 895.48 | 5.334 |  |  |
| ν25 | 909.97 | 1.5336 |  |  |
| ν26 | 911.25 | 0.47 |  |  |
| ν27 | 927.3 | 1.962 |  |  |
| ν28 | 952.01 | 4.9997 |  |  |
| ν29 | 957.91 | 5.0076 |  |  |
| ν30 | 978.78 | 3.8228 |  |  |
| ν31 | 991.49 | 1.7425 |  |  |
| ν32 | 995.66 | 3.7744 |  |  |
| ν33 | 1041.12 | 0.7253 |  |  |
| ν34 | 1050.45 | 1.2523 |  |  |
| ν35 | 1058.9 | 1.0805 |  |  |
| ν36 | 1063.29 | 7.3434 |  |  |
| ν37 | 1105.33 | 14.6627 |  |  |
| ν38 | 1135.1 | 3.8423 |  |  |
| ν39 | 1156.54 | 8.1609 |  |  |
| ν40 | 1173.32 | 17.618 |  |  |
| ν41 | 1189.68 | 0.3909 |  |  |
| ν42 | 1195.71 | 0.3819 |  |  |
| ν43 | 1210.53 | 1.0375 |  |  |
| ν44 | 1227.82 | 0.3158 |  |  |
| ν45 | 1256.21 | 0.9646 |  |  |
| ν46 | 1279.23 | 1.0453 |  |  |
| ν47 | 1290.32 | 0.4718 |  |  |
| ν48 | 1305.17 | 0.4328 |  |  |
| ν49 | 1310.3 | 0.3509 |  |  |
| ν50 | 1320.58 | 0.2665 |  |  |
| ν51 | 1323.84 | 0.1224 |  |  |
| ν52 | 1330.83 | 1.6671 |  |  |
| ν53 | 1344.55 | 0.6303 |  |  |
| ν54 | 1349.15 | 1.2455 |  |  |
| ν55 | 1366.12 | 0.307 |  |  |
| ν56 | 1373.41 | 0.5273 |  |  |
| ν57 | 1469.78 | 3.2453 |  |  |
| ν58 | 1473.74 | 6.6858 |  |  |
| ν59 | 1495.2 | 1.815 |  |  |
| ν60 | 1497.07 | 2.9768 |  |  |
| ν61 | 1506.79 | 5.4828 |  |  |
| ν62 | 1520.53 | 8.3178 |  |  |
| ν63 | 1674.77 | 11.6324 |  |  |
| ν64 | 3007.99 | 26.5795 |  |  |
| ν65 | 3020.31 | 12.8411 |  |  |
| ν66 | 3024.51 | 27.7991 |  |  |
| ν67 | 3029.35 | 26.9983 |  |  |
| ν68 | 3033.56 | 7.9443 |  |  |
| ν69 | 3042.94 | 16.028 |  |  |
| ν70 | 3054.55 | 32.5081 |  |  |
| ν71 | 3062.5 | 20.4839 |  |  |
| ν72 | 3073.34 | 33.6736 |  |  |
| ν73 | 3076.72 | 42.6568 |  |  |
| ν74 | 3084.78 | 89.2472 |  |  |
| ν75 | 3085.77 | 31.5698 |  |  |
| ν76 | 3097.07 | 11.6038 |  |  |
| ν77 | 3098.87 | 36.0451 |  |  |
| ν78 | 3117.51 | 19.1249 |  |  |

|  | tsR3-O2H |  | tsR4-O2H |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -114.09 | 3.999 | -1429.39 | 350.373 |
| ν2 | 33.74 | 1.1147 | 36.26 | 1.5682 |
| ν3 | 51.04 | 1.3224 | 78.18 | 0.7212 |
| ν4 | 68.36 | 0.0567 | 96.27 | 0.9742 |
| ν5 | 125.15 | 0.0339 | 142.44 | 0.3441 |
| ν6 | 149.41 | 2.0056 | 161.25 | 0.6585 |
| ν7 | 197.94 | 0.8471 | 227.96 | 1.4425 |
| ν8 | 256.68 | 0.242 | 270.96 | 0.267 |
| ν9 | 311.91 | 0.0665 | 305.55 | 0.0754 |
| ν10 | 314.31 | 0.0049 | 328.99 | 0.0271 |
| ν11 | 399.23 | 1.2796 | 389.81 | 0.7861 |
| ν12 | 532.28 | 0.2078 | 421.1 | 3.1698 |
| ν13 | 548.11 | 0.4209 | 506.41 | 1.275 |
| ν14 | 556.9 | 7.5824 | 533.55 | 0.2969 |
| ν15 | 670.95 | 1.3091 | 546.07 | 1.3554 |
| ν16 | 722.8 | 7.4411 | 691.92 | 2.3131 |
| ν17 | 754.07 | 0.3711 | 750.7 | 0.9209 |
| ν18 | 767.5 | 29.9022 | 784.13 | 2.3903 |
| ν19 | 779.23 | 1.3504 | 813.64 | 1.198 |
| ν20 | 811.64 | 0.5118 | 848.6 | 4.1051 |
| ν21 | 834.69 | 4.5461 | 874.72 | 2.0878 |
| ν22 | 852.79 | 0.0008 | 893.56 | 2.3892 |
| ν23 | 868.77 | 0.1146 | 909.47 | 1.4507 |
| ν24 | 874.74 | 0.471 | 915.37 | 0.3906 |
| ν25 | 912.78 | 0.0022 | 930.05 | 1.181 |
| ν26 | 915.54 | 1.3656 | 934.52 | 0.5078 |
| ν27 | 922.87 | 0.1733 | 947.83 | 2.2671 |
| ν28 | 937.52 | 1.171 | 969.21 | 3.1675 |
| ν29 | 946.42 | 0.3309 | 977.09 | 1.712 |
| ν30 | 990.77 | 2.6082 | 1000.86 | 23.1104 |
| ν31 | 993.6 | 1.7226 | 1022.3 | 7.0845 |
| ν32 | 1003.78 | 0.4361 | 1031.23 | 3.536 |
| ν33 | 1041.17 | 0.2572 | 1051.62 | 2.0948 |
| ν34 | 1052.2 | 0.0016 | 1065.6 | 0.6757 |
| ν35 | 1058.57 | 0.1974 | 1070.76 | 0.1631 |
| ν36 | 1071.35 | 1.7521 | 1100.12 | 1.102 |
| ν37 | 1149.6 | 33.3973 | 1134.88 | 0.9068 |
| ν38 | 1151.2 | 0.4968 | 1144.52 | 2.208 |
| ν39 | 1179.08 | 11.7515 | 1160.9 | 1.2194 |
| ν40 | 1193.79 | 0.1579 | 1194.38 | 4.9277 |
| ν41 | 1195.81 | 4.2723 | 1197.31 | 2.5264 |
| ν42 | 1204.11 | 0.6797 | 1216.91 | 1.5411 |
| ν43 | 1205.51 | 0.6213 | 1232.74 | 2.3179 |
| ν44 | 1234.94 | 2.1293 | 1236.2 | 0.0935 |
| ν45 | 1246.76 | 0.0001 | 1250.23 | 0.5285 |
| ν46 | 1261.48 | 0.8613 | 1264.9 | 0.3631 |
| ν47 | 1283 | 0.005 | 1271.78 | 0.9724 |
| ν48 | 1304.76 | 0.0038 | 1300.55 | 0.2431 |
| ν49 | 1312.32 | 0.422 | 1305.81 | 0.9032 |
| ν50 | 1317.39 | 0.0017 | 1315.08 | 1.6782 |
| ν51 | 1327.89 | 0.0437 | 1323.92 | 1.3681 |
| ν52 | 1332.76 | 0.9229 | 1337.68 | 0.249 |
| ν53 | 1346.43 | 0.6953 | 1341.97 | 0.0574 |
| ν54 | 1350.35 | 0.0141 | 1349.68 | 1.0468 |
| ν55 | 1364.37 | 0.5752 | 1362.79 | 0.4603 |
| ν56 | 1369.75 | 0.3088 | 1417.39 | 19.2351 |
| ν57 | 1492.9 | 1.5094 | 1455.83 | 5.5837 |
| ν58 | 1494.68 | 2.0905 | 1472.41 | 1.2312 |
| ν59 | 1498.04 | 2.9327 | 1477.59 | 2.3304 |
| ν60 | 1505.09 | 11.7862 | 1483.52 | 8.2622 |
| ν61 | 1509.49 | 5.1595 | 1493.28 | 6.5137 |
| ν62 | 1522.64 | 5.8166 | 1507.92 | 3.4634 |
| ν63 | 2182.23 | 7.4846 | 1542.04 | 13.4645 |
| ν64 | 3019.37 | 19.5244 | 3046.74 | 16.6449 |
| ν65 | 3027.85 | 26.286 | 3078.08 | 10.0615 |
| ν66 | 3032 | 21.9442 | 3082.32 | 5.3467 |
| ν67 | 3037.46 | 4.6228 | 3089.24 | 21.936 |
| ν68 | 3041.36 | 24.9056 | 3090.79 | 28.1157 |
| ν69 | 3048.72 | 13.6604 | 3094.82 | 17.2205 |
| ν70 | 3053.19 | 79.6952 | 3106.59 | 38.6715 |
| ν71 | 3073.86 | 4.2216 | 3125.62 | 16.492 |
| ν72 | 3075.33 | 40.6523 | 3136.79 | 39.7446 |
| ν73 | 3075.75 | 31.606 | 3146.69 | 20.5253 |
| ν74 | 3083.6 | 64.7872 | 3153.3 | 32.0551 |
| ν75 | 3093.65 | 39.555 | 3157.65 | 3.3491 |
| ν76 | 3095.58 | 15.3675 | 3158.46 | 8.5779 |
| ν77 | 3097 | 55.4044 | 3162.79 | 30.7729 |
| ν78 | 3109.25 | 17.2621 | 3177.11 | 20.9041 |

|  | tsR5-O2H |  | tsR6-O2H |  |
| --- | --- | --- | --- | --- |
| Normal modes | Frequency(cm-1) | IR Inten | Frequency(cm-1) | IR Inten |
| ν1 | -716.37 | 174.5419 | -419.76 | 30.6858 |
| ν2 | 11.53 | 1.1077 | 26.74 | 1.4338 |
| ν3 | 54.52 | 1.0525 | 50.59 | 0.4635 |
| ν4 | 70.97 | 0.4327 | 63.98 | 1.0036 |
| ν5 | 132.2 | 0.168 | 134.53 | 0.9436 |
| ν6 | 159.78 | 1.2114 | 136.92 | 0.0253 |
| ν7 | 175.38 | 0.0948 | 238.93 | 1.6433 |
| ν8 | 269.25 | 0.3882 | 264.39 | 0.0773 |
| ν9 | 291.78 | 1.3957 | 288.89 | 0.3795 |
| ν10 | 319.78 | 0.5222 | 331.14 | 0.1138 |
| ν11 | 395.77 | 0.1272 | 397.07 | 0.8335 |
| ν12 | 495.8 | 0.648 | 492.42 | 0.7711 |
| ν13 | 532.64 | 1.0127 | 534.6 | 0.1062 |
| ν14 | 600.15 | 1.3879 | 568.23 | 3.059 |
| ν15 | 644.25 | 11.0005 | 685.44 | 0.3926 |
| ν16 | 735.78 | 0.9598 | 702.02 | 5.8043 |
| ν17 | 745.99 | 0.1226 | 733.22 | 0.3734 |
| ν18 | 770.6 | 10.2864 | 781.08 | 0.276 |
| ν19 | 793.19 | 6.3382 | 795.96 | 6.1231 |
| ν20 | 827.96 | 1.8492 | 827.94 | 2.6429 |
| ν21 | 847.04 | 7.4273 | 848.93 | 0.2959 |
| ν22 | 860.38 | 4.4339 | 886.86 | 1.8852 |
| ν23 | 887.38 | 0.811 | 887.61 | 1.1277 |
| ν24 | 889.28 | 11.8902 | 894.37 | 26.7081 |
| ν25 | 908.74 | 18.3546 | 910.9 | 8.6293 |
| ν26 | 912.38 | 5.1111 | 922.67 | 3.4347 |
| ν27 | 923.88 | 0.8485 | 924.52 | 3.2344 |
| ν28 | 951.15 | 5.6343 | 929.28 | 19.7909 |
| ν29 | 961.14 | 0.6407 | 962.17 | 0.0795 |
| ν30 | 983.75 | 12.2083 | 963.48 | 9.9241 |
| ν31 | 987.64 | 2.0908 | 1003.02 | 2.832 |
| ν32 | 1011.17 | 6.8354 | 1016.13 | 9.9875 |
| ν33 | 1035.33 | 10.7554 | 1046.22 | 0.6794 |
| ν34 | 1049.25 | 3.0756 | 1051.99 | 0.6426 |
| ν35 | 1050.28 | 0.1808 | 1057.75 | 3.2557 |
| ν36 | 1058.69 | 2.0102 | 1075.56 | 0.0114 |
| ν37 | 1095.98 | 13.981 | 1108.46 | 37.4992 |
| ν38 | 1140.41 | 2.2916 | 1132.2 | 0.8842 |
| ν39 | 1157.86 | 6.6953 | 1146.84 | 0.05 |
| ν40 | 1163.42 | 0.7126 | 1167.1 | 10.3544 |
| ν41 | 1197.51 | 4.4788 | 1199.3 | 0.024 |
| ν42 | 1203.94 | 4.7689 | 1209.76 | 3.9474 |
| ν43 | 1219.07 | 0.2409 | 1214.41 | 1.9075 |
| ν44 | 1225.14 | 0.8788 | 1236.6 | 2.7532 |
| ν45 | 1249.51 | 0.5167 | 1247.17 | 0.69 |
| ν46 | 1276.46 | 1.5214 | 1259.83 | 0.5131 |
| ν47 | 1289.32 | 1.0117 | 1293.14 | 1.1107 |
| ν48 | 1294.97 | 1.6672 | 1307.63 | 0.0561 |
| ν49 | 1302.33 | 1.0462 | 1310.32 | 1.8178 |
| ν50 | 1315.76 | 0.4763 | 1311.29 | 0.3221 |
| ν51 | 1318.19 | 1.6682 | 1321.3 | 1.7202 |
| ν52 | 1324.53 | 0.5539 | 1326.16 | 1.3754 |
| ν53 | 1335.71 | 1.5413 | 1344.4 | 0.5109 |
| ν54 | 1348.22 | 3.2167 | 1354.18 | 4.9442 |
| ν55 | 1359.04 | 0.3854 | 1365.48 | 0.29 |
| ν56 | 1367.98 | 0.6056 | 1369.65 | 0.7588 |
| ν57 | 1422.88 | 1.6119 | 1458.37 | 17.9869 |
| ν58 | 1471.12 | 4.5909 | 1469.87 | 4.773 |
| ν59 | 1496.04 | 1.2596 | 1492.36 | 1.3606 |
| ν60 | 1498.76 | 2.0571 | 1496 | 1.2026 |
| ν61 | 1508.58 | 12.2207 | 1504.88 | 10.6079 |
| ν62 | 1523.48 | 4.0006 | 1523.67 | 4.1736 |
| ν63 | 1589.71 | 13.4338 | 1716.93 | 10.1756 |
| ν64 | 2951.66 | 21.4571 | 2949.84 | 11.4299 |
| ν65 | 2982.48 | 20.1287 | 2953.21 | 21.9928 |
| ν66 | 3037.35 | 7.6821 | 3032.47 | 14.3828 |
| ν67 | 3038.76 | 31.3387 | 3035.93 | 5.4257 |
| ν68 | 3045.07 | 13.6183 | 3038.34 | 18.5954 |
| ν69 | 3048.98 | 73.904 | 3045.66 | 38.5631 |
| ν70 | 3052.95 | 28.8134 | 3048.57 | 47.5375 |
| ν71 | 3054.13 | 15.7368 | 3054.61 | 14.4922 |
| ν72 | 3067.21 | 2.9892 | 3067.65 | 15.3314 |
| ν73 | 3079.93 | 48.0367 | 3068.67 | 25.0619 |
| ν74 | 3084.78 | 44.781 | 3074.77 | 75.8192 |
| ν75 | 3088.51 | 51.2097 | 3082.04 | 4.4966 |
| ν76 | 3092.82 | 36.9823 | 3085.5 | 32.7305 |
| ν77 | 3098.74 | 29.4799 | 3090.07 | 79.3461 |
| ν78 | 3105.54 | 15.2297 | 3123.43 | 30.057 |